A Study on the Characteristics of Toluene Adsorption in Activated Biochar of Waste Wood Synthesis by Hydrothermal Carbonization

Jin Man Chang, Ph.D. student, University of Seoul, ROK Jai-Young Lee, Professor, University of Seoul, ROK

Abstract

About 62% of the total emissions of volatile organic compounds in Korea are emitted from painting facilities. Automobile painting facilities emit few volatile organic compounds, but they are adjacent to residential areas and significantly impact the human body. The main component of volatile organic compounds in automobile painting facilities is toluene gas, which occupies a high concentration and specific gravity, which harms the human body. Therefore, this study examines the adsorption characteristics of air pollutants of activated biochar synthesized through the hydrothermal carbonization and activation process using waste wood. Activated biochar had synthesized by HTC and chemical activation with various conditions and selected the optimum condition. The study analyzed the surface area, pore volume, size, and distribution of activated biochar. The optimal condition for carbonization is 4 hours at 300°C, grain size is over 4.75mm, and the optimal condition for activating is 800°C using a KOH. The carbon contents have increased a maximum of two times to raw materials. The surface area of activated biochar is from 872.2 ~ 1387.7 m2/g. As for the activated biochar synthesized under optimal conditions, it took less than 5 minutes to remove Toluene below 50 ppm, which is the appropriate VOC emission standard, and it is similar to that of commercial activated carbon. Activated biochar manufactured using HTC is believed to be available in painting facilities.

Image

Figure 1. Flow chart of this study

Recent Publications

- YoungJin Lee (2017) A Study on Assessment of Biochar Adsorption Applicability by Physical and Chemical Characterization with Livestock Manure, Journal of Soil and Groundwater Environment 22(2):52-57.

- Minhee Won (2021) A Feasibility Study of Wood Waste to Solid Bio-Coal using Hydrothermal Carbonization(HTC), J. Korea Soc. Waste Manag 38(6):561-568

Acknowledgement

This work was supported by the Korea Ministry of Environment as Waste to Energy-Recycling Human Resource Development Project.(YL-WE-22-001)

Biography

Jin Man Chang is studying for a Ph.D. program at the University of Seoul. Research on waste treatment and thermal treatment is being conducted.

Email: ricky54@naver.com

Notes/Comments:

Presenting author details 
Full name: Jin Man Chang
Contact number: +82-10-3773-6337
Twitter account: -
Linked In account: -

Session name/ number: 
Category: Poster presentation