A Study on the effectiveness of Chitosan Phosphate as a stabilizer for soil contaminated with heavy metals.

Jeong-Hyun LEE, MS, University of Seoul, Republic of Korea

Tai-Ran Yu, MS, University of Seoul, Republic of Korea

Abstract (300 word limit)

Statement of the Problem: The study intends to create an environmentally-friendly stabilizer using chitosan sourced from the chitin found in discarded shells of crabs and shrimps. Chitin contains active components like hydroxyl and amino groups that are useful in eliminating heavy metal ions and bioabsorption. The goal is to assess the effectiveness and performance of the stabilizer and confirm how it affects the stabilization process. Methodology & Theoretical Orientation: To create chitosan phosphorylated, chitosan from Aladdin was bought. Samples were then placed in numerous containers with CTS and P-CTS at ratios of 1%, 3%, 5%, 7%, and 9%. Upon stirring, the soil was sprayed with distilled water to achieve 20% moisture content and left to cure for periods of 1, 5, 10, 20, and 30 days. A subsequent experiment was conducted to measure elution of heavy metals to assess the stabilizer's effectiveness. Findings: Cu and Pb from the control group, as well as the experimental groups injected with CTS and P-CTS, were extracted in an SM&T experiment. The comparison of the control group to the soil that received P-CTS injection revealed that the Cu ion exchange form had a significant share, while the residual form increased from 9% to 14%. The control group showed a considerable presence of the Fe-Mn oxide binding form in the ion exchange form, but the injected soil exhibited an evident rise in the residual form from 2% to 7%. Ultimately, P-CTS decreased the mobility and biological impact of Cu and Pb in heavy metal-contaminated soil, thus stabilizing it. Conclusion & Significance: Using P-CTS as a stabilizer is anticipated to be advantageous due to its cost-effectiveness through the utilization of waste resources and enhanced efficiency compared to CTS. Consequently, P-CTS is deemed a fitting stabilizing agent.

Image

Recent Publications (minimum 5)

- Kim (2021) “Simultaneous Stabilization of Arsenic and Lead using Iron Phosphate”, Korean Society of Soil Science and Fertilizer, 46-46

- Park (2020) “Risk Assessment for Co-contaminated Soil Including As and Hg in the Vicinity of Abandoned Metal Mine” Journal of Korean Society of Environmental Engineeers 42(2): 75-87.

- P. Kumararaja (2018) “Chitosan-g-poly(acrylic acid)-bentonite composite: a potential immobilizing agent of heavy metals in soil” Spinger/Cellulose volume 25: 3985-3999

- Song et al..(2018) “Stabilization of heavy metals in soil by chitosan and its derivatives” doi: 10.16085/j.issn.1000-6613

- Lei Zhang (2016) “Removal of heavy metal ions using chitosan and modified chitosan: A review” Journal of Molecular Liquids 175-191

This work was supported by the Korea Ministry of Environment as Waste to Energy-Recycling Human Resource Development Project.(YL-WE-22-001)

Paste your Logo here

Biography (150 word limit)

Deanna Mulvihill has her expertise in evaluation and passion in improving the health and wellbeing. Her open and contextual evaluation model based on responsive constructivists creates new pathways for improving healthcare. She has built this model after years of experience in research, evaluation, teaching and administration both in hospital and education institutions. The foundation is based on fourth generation evaluation (Guba& Lincoln, 1989) which is a methodology that utilizes the previous generations of evaluation: measurement, description and judgment. It allows for value-pluralism. This approach is responsive to all stakeholders and has a different way of focusing.

Email:

Notes/Comments:

Presenting author details 
Full name: 
Contact number:
Twitter account:
Linked In account:

Session name/ number: 
Category: (Oral presentation/ Poster presentation)