# Synthesis and experimental investigation of effects of iron-titanium oxide nanoparticles on rheology and filtration of water-based drilling fluids

Samad Sabbaghi*, Milad Jafari and Rahmatallah Saboori

Shiraz University, Iran

Abstract

Drilling operations are one of the most important processes in the oil industry and the most important and widely used part in drilling operations is the drilling mud system. Drilling mud according to the assigned and very diverse tasks must be a suitable combination and compatible with operating conditions such as the type of manufacturer and the type and quality of oil in the reservoir. Also, drilling fluid alone contains about 15 to 20% due to drilling process. According to the above, it is necessary to improve the properties of drilling fluid such as rheological and filtration of drilling fluid and other properties to increase efficiency and reduce costs drilling process. In this research, the rheology and filtration properties of water-based drilling mud have been evaluated to which iron titanium oxide nanoparticles have been added. For this purpose, iron titanium oxide nanoparticles were synthesized by sol-gel method. To analyses the appearance, size and morphology of nanoparticles, various analyses were performed, including field emission scanning electron microscopy analysis, X-Ray Diffraction (XRD) and Fourier Transform Infrared Spectroscopy (FTIR). These analyses show spherical nanoparticles with an approximate size distribution of 20 nm that have accumulated. Nanoparticles were added to the base drilling fluid in different weight percentages and the properties of viscosity, plastic viscosity and yield stress of Nano fluids were compared with the base drilling mud and a concentration of 0.5 wt.% was considered as the optimal concentration. At this concentration, the apparent viscosity was about 262% and the plastic viscosity was more than 233% and the yield stress was about 442% compared to the base fluid. The amount of fluid loss was improved by 57% and the thickness of the mud cake was reduced by 32%.

# Biography

# Samad Sabbaghi is a PhD holder, Professor in Nano Chem. Eng. Dep., Faculty of Advanced Technologies, Nanotechnology Research Institute. His Scientific & Executive Records are Responsible for Oil, Gas and Petrochemical Projects in Shiraz University, Vice Chancellor of Faculty of Advanced Technologies, Head of Nano Chem. Eng. Dep., Head of Incubators Center of Oil, Gas and Petrochemical (Fars Science and Tech. Park), Top Researcher of Shiraz University in 2010, Top Researcher of Fars Science and Tech. Park 2012, Top Researcher of Shiraz University in 2013, Top Teacher of Shiraz University in 2017, Top Researcher of Shiraz University in 2018, Receiving the bronze statue of Iranian Nanotechnology Community, Appreciation Letter of Iranian Nanotechnology Community, Executive Secretary of the International Conference on Nano, Executive Secretary of the Research Week 2009, Executive Secretary of ASPA 2014 Asia-Pacific Conference, Head of Nano Chem. Eng. Dep. 2007-2017, Head of Drilling Nano Fluid Laboratory, Head of Nanotechnology Research Institute.