## Slide 1: About OMICS Group
OMICS Group International is an amalgamation of Open Access publications and worldwide international science conferences and events. Established in the year 2007 with the sole aim of making the information on Sciences and technology ‘Open Access’, OMICS Group publishes 400 online open access scholarly journals in all aspects of Science, Engineering, Management and Technology journals. OMICS Group has been instrumental in taking the knowledge on Science & technology to the doorsteps of ordinary men and women. Research Scholars, Students, Libraries, Educational Institutions, Research centers and the industry are main stakeholders that benefitted greatly from this knowledge dissemination. OMICS Group also organizes 300 International conferences annually across the globe, where knowledge transfer takes place through debates, round table discussions, poster presentations, workshops, symposia and exhibitions.

## Slide 2: About OMICS Group Conferences
OMICS Group International is a pioneer and leading science event organizer, which publishes around 400 open access journals and conducts over 300 Medical, Clinical, Engineering, Life Sciences, Phrama scientific conferences all over the globe annually with the support of more than 1000 scientific associations and 30,000 editorial board members and 3.5 million followers to its credit.
OMICS Group has organized 500 conferences, workshops and national symposiums across the major cities including San Francisco, Las Vegas, San Antonio, Omaha, Orlando, Raleigh, Santa Clara, Chicago, Philadelphia, Baltimore, United Kingdom, Valencia, Dubai, Beijing, Hyderabad, Bengaluru and Mumbai.

## Slide 3
Shdai-140727
Green Chemistry
NPR to MDI,DDI,HDI:DPC
NIR to P-Urea:DPC
NIR to PU through Cyclic Carbonate
Other Carbonate Routes to PU and PA
Summary
Prof. Shenghong A. Dai
National Chung-Hsin University
Taichung, Taiwan
1
Green Processes to Diisocyanates and PU Elastomers
via Carbonate Raw Materials: New NPR and NIR Processes
Green Chem-2014 Philadelphia

## Slide 4
Winterton: 12 Green Engineeing Principles
( Green Chem., 2001, 3 G73.)
1. Identify and quantify by-products. (副產物鑑定及量化)
2. Report conversions, selectivity's, and productivities. (明示程序之轉化率/產率/選擇率)
3. Establish full mass-balance for the process. (建立完整質量平衡)
4. Measure catalyst and solvent loses in air and aqueous effulent.
5. Investigate basic thermochemistry.
6. Anticipate heat and mass transfer limitations.
7. Consult a chemical or process engineer. (與化工人咨詢要點)
8. Consider the effect of overall process on choice of chemistry. (作完整化學選項之考量)
9. Help develop and apply sustainability measures.(發展永續發展之要項)
10. Quantify and minimize the use of utilities.
11. Recognize where safety and waste minimization are incompatible. (安全及減廢之考量)
12 Monitor, report, and minimize the laboratory waste emitted.
3
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 5
Shdai-131227
Green chemistry is a way to minimize chemical threat to human being and environment.
Anastas and Wnerer: (12 principles) chemical reliability, safety, high selectivity, energy efficiency, re-usability.
NPR / NIR- Our Green Research Goals:
- Non-phosgene process of producing isocyanates
- Minimize chlorine-containing reagents and products
- Ambient synthesis condition
- Use low-toxic chemicals – avoid isocyanates in PU making
- Employ sustainable low-cost raw materials
NPR: Non-phosgene Route (非光氣製程- Isocyanates)
NIR: Non-isocyanate Route (非異氰酸鹽製程- PU)
Green Chemistry– NPR, NIR Processes
4
Green Chem-2014 Philadelphia

## Slide 6
Phosgene Process-MDI from Benzene
( Polyurethane Handbook by Huntsman)
Con. H2SO4/HNO3
Formaldehyde
Phosgene
5
Shdai-140727
Green Chem-2014 Philadelphia
Toxic chemicals

## Slide 7
Phosgene Process- p-MDI from p-MDA
(MDI)
(p-MDI) x= 1 to 6
MDI Isomers Mp (C) Bp(C)
2,2’-MDI 46 140 / 0.5
2,4’-MDI 35 152 / 0.5
4,4’-MDI 41 161 / 0.5
60:40/2,4’:4,4’ 14
Ternary <0
MCB
Dist..
PhNCO &
low Boilers
4,4’-MDI
(>98.5%)
2,2-;2,4’-;4,4’-
MDI
Bottoms
Ref: H. Ulrich in “Chemistry and Technology of Isocyanates, John Wiley, p385 (1996)
PU
Rigid Foams
Crude MDA
P-MDA
6
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 8
The Problems Associated with Phosgene Process
Safety problem: Phosgene is a highly toxic chemical with low Lethal threshold.
Phosgene process generates large amount of HClg .
HClg is a highly corrosive agent, and hence requires high-cost of maintenance.
HClg needs to be managed into PVC or oxidized to recover as chlorine.
MDI will contain hydrolyzable and non-hydrolyzable chlorides impurities.
MDI process requires highly safety facilities to prevent accidents/fatality.
Require large sum of initial cost for a large integration site and safety facilities.
7
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 9
Non-phosgene Routes to MDI
Over 40 plus years of research but with no practical process in use
R= Me, Et, Ph
DPC (1)
(2)
(3)
8
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 10
Carbonylation Reagents
Phosgene still is the most efficient/cheap raw materials.
15
Shdai-140727
Green Chem-2014 Philadelphia
Olin
ARCO
Asahi
Bayer, BASF
Dow, Eni Chem,
Asahi
Monsanto
(current)

## Slide 11
NPR to MDI – Prior Arts
ARCO : Three-Step Process from Nitrobenzene (1974)
(1) Reductive Cabonylation:
(2) Condensation:
(3) Thermolysis:
Toxic catalyst and hart to recover [Step (1)]
High temperature to crack carbamate [Step(3)]
9
Shdai-140727
Green Chem-2014 Philadelphia
Se

## Slide 12
Asahi : Three Step Process from Aniline (1978)
1. Oxidative Carbonylation:
2. Condensation:
3. Decomposition:
NH2 + CO + EtOH + 1/2 O2
NHCOOEt + H2O
(EPC)
NHCOOEt + CH2O
- H2O
N-CH2-- NHCOOET
(N-benzyl compound)
N-CH2-- NHCOOET
(EPC)
COOEt
COOEt
EtOCONH
CH2-- NHCOOET
EtOCONH
CH2-- NHCOOET
(MDU)
-2 EtOH
O=C=N
CH2-- N=C=O
H+
“Pd”
(MDI)
Similar problems to ARCO’s; Being Scaled-up in pilot
240℃
10
Shdai-140727
NPR to MDI – Prior Arts
Green Chem-2014 Philadelphia

## Slide 13
Lynodell’ DPC Route to MDI
[ R. W. Mason, US Patent 6,781,010 (2004) ]
MDA Condensation with Formic Acid:
Carbonylation of Formamaide with DPC and Thermolysis:
Trans-esterification of MDA with Phenyl Formate:
HCOOPh + MDA
180℃~200℃
180℃~200℃
+ HCOOPh
13
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 14
Lynodell’ DPC Process to MDI
[ R. W. Mason, US Patent 6,781,010 (2004) ]
Advantages:
- Themolysis temperature of biscarbamate into MDI seems milder (<200 ℃)
- The yields to MDA-formamaide and MDI are high.
- Phenyl formate, the by-product, could be re-used.
Disadvantages:
- MDI needs to be re-distilled to separate from solvent/by-product.
- Highly corrosive formic acid was used as the carbonylation agent.
14
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 15
Shdai-131227
Monsanto: CO2 Carbonylation-Dehydration Process
BASE PRESSURE CO2 DEHYD. AGENT % YIELD
NEt3 1 ATM POCl3 98%
NEt3 1 ATM PCl3 96%
NEt3 1 ATM SO3 99%
CyTEG 80 PSI (CF3CO)2O 91%
CyTEP 80 PSI SOCl2 70%
( 5mm) (10 mm) 25 ml
NPR to Aliphatic Diisocyanates
Applicable only to aliphatic diamines
Require strong tertiary amine to stabilize the initial carbamic acid
C8H17NH2 + 2 base
1) CO2, CH3CN
2) 0 C; Dehydration
agent/ CH2Cl2
C8H17N=C=O
12
Green Chem-2014 Philadelphia

## Slide 16
NPR to IPDI : Urea Route
Applicable only to aliphatic diamine. (Bayer, Huls, BASF)
11
Shdai-140727
Green Chem-2014 Philadelphia
Franz M, USP 4,596,678(1986)

## Slide 17
Shdai-131227
Shdai-131227
Japan Asahi ( phenol system )
＋
Diphenyl carbonate
(DPC)
1,6-Hexanediamine
(HDA)
Hexane-1,6-bis(phenyl carbamate)
2
Phenol
Thin film
Distillation
Column
(D=5cm 、L=2m)
Excess
Phenol
Vacuum
Distillation
Thermolysis
( 150~230℃ )
( 1.3~15KPa )
50℃
Continuous
Process
Hexamethylene-1,6-diisocyanate
＋
● Total operation time= 10 day
● Hexane-1,6-bis(phenyl carbamate) Yield= 99.5%
● DPC recycling rates= 99.9% ( 232℃、15KPa、119g/hr )
● Phenol recycling rates= 99.9% ( 230℃、1atm、200g/hr )
● HDI Yield= 95.3% ( 150℃、1.5KPa、140g/hr )
● HDI Purity= 99.8% ( L.C )
MW=116.21
【244g/116.21=2.1mol】
MW=214.22
【1350g/214.22=6.3mol】
MW=94.11
【987g/94.11=10.5mol】
[24] M. Shinohata, N. Miyake, EP 2275405(2011) to Asahi
5L storage tank
200g/hr
Phenol as solvent and DPC as carbonylation agent
Most similar to our approach for aliphatic iso
Slow processing speed
NPR to Aliphatic Diisocyanates : Review of Prior Arts
(4) Carbonylation
(5) Thermolysis
32
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 18
16
Principal Carbonylation Agents
>>
>>
>
>
>
>
>
(Phosgene) (di-t-butylcarbonyl carbonate) (DPC, diphenyl carbonate)
(di-alkyl carbonate) (DMC, dimethyl carbonate) (urea) (carbon monoxide) (carbon dioxide)
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 19
Dai’s Group - 4,4’-MDI and P-urea Processes
Polyurea
(1) Carbonylation
(2) Thermolysis
(3) Trans-esterification
MDA
MDA-DPC
MDI
Aniline
(1) DPC carbonylation of MDA (2) Thermolysis to make MDI (3) NIR to Polyurea
17
Benzoic acid
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 20
Potential Sources of DPG for NPR to MDI
(1) DPC/Benzoic acid /cat.
(2)
(3) Transesterification
18
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 21
NPR- Our Optimization of 4,4’-DP-MDC Synthesis
Fig 1. Effect of carboxylic acids
of different pKas on
4,4’-DP-MDC yields.
Fig 2. Effect of different benzoic acid
amounts on 4,4’-DP-MDC yields.
Fig 3. Effect of diphenyl carbonate
concentrations on
4,4’-DP-MDC yields.
Compositiona | Biscarbamate Yield (%) | Urea Yield(%)b
4,4’-MDA/DPC/Benzoic acid(1/6/0.2/0) | 65 | 1.06
4,4’-MDA/DPC/Benzoic acid/Pyridine(1/6/0.2/0.009) | 97 | 0.15
4,4’-MDA/DPC/Benzoic acid/TEDA(1/6/0.2/0.009) | 99 | 0.15
aMolar ratio. At 40 C ~60 C bCalculated by 1H-NMR analysis. |  | 
Benzoic acid
identified
5m% >
DPC/MDA = 6.0
19
Catalyzed by pyridine or TEDA.
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 22
NPR-Mechanism of Carbonylation:
Co-catalyzed by benzoic acid/tertiary amine
Key active intermediate anhydride A in carbonylation of amine
20
(carbamate)
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 23
NPR- MDA Carbonylation with DPC
( IR and 1H-NMR of the MDA-DPC; mp 194 ℃)
IR 1H-NMR
MDA-DPC/dodecane: No detection of diphenyl urea formation
21
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 24
NPR-Thermolysis of MDI-DPC into MDI (a)
(Monitoring Thermolysis of MDA-DPC 200℃in Dodecane )
22
Green Chem-2014 Philadelphia
Shdai-140727

## Slide 25
NPR- Thermolysis of MDA-DPC into MDI
Isolated MDI (76%) after fractionation
23
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 26
Summary of Lab-scale MDI Synthesis
Carried out in dodecane (bp:216℃) at boiling temperature
MDA-DPC conversion rate at 100%
MDI crude yield >95%; Purified after distillation >76 %
Recovered solvent and phenol >95%
Little (CDI) by-product formation in the heating
No chlorine content in the product
The use of polar solvent resulted in complicated products.
24
Shdai-140727
Green Chem-2014 Philadelphia
NPR- Thermolysis of MDA-DPC into MDI (b)

## Slide 27
Solvent | DMSO | DMF | THF | MeCN | Dioxane | DME | CHCl3 | MeOH | Pyr | TMS
結構式 |  |  |  |  |  |  |  |  |  | 
Bp(℃) | 189 | 153 | 65 | 81 | 100 | 64 | 60 | 65 | 115 | 285
Relative Polarity (water=1) | 0.444 | 0.404 | 0.207 | 0.46 | 0.164 | - | 0.259 | 0.762 | 0.3 | 0.41
Condition | rt | rt | reflux | rt | reflux | rt | rt | rt | rt | 70
Time | 15min | 15min | 5h | 1h | 5h | 24h | 24h | 24h | 2.5h | 2h
Yield(%) | 96 | 74 | 92 | 79 | 65 | 92 | 90 | 74 | 85 | 89
( B. Thavonekham, Synthesis, 1997, 1189-1194 )
Trans-amination of Ph-carbamate in Different Solvents
25
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 28
NIR-MDA-DPC and Diamines into Polyurea
NIR to P-urea
MDA-DPC Short Chain Extender Long Chain Diamine
Polyurea Elastomers
26
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 29
Solvent Diamines Extender Hard Segment% Mol. Wt
DMSO Jeffamine-2000 1,6-HAD 57 54,400
DMSO Jeffamine-2000 PPG-230 61 71,000
DMSO Jeffamine-2000 1,8-diamino-3,6-dioxetane 58 131,000
TMS Jeffamine-2000 1,6-HAD 46 79,000a
(59,676)b
TMS Jeffamine-2000 H12-MDA 40 84,269a
(68,000)b
TMS Jeffamine-2000 IPDA 40 61,338a
(57,170)b
Run at 60~100℃ in DMSO as the solvent. (Hard to separate with PhOH )
Run at 60~140℃ in TMS with recovering of phenol/TMS
a. Distilled phenol+ TMS b. just distill phenol after the reaction
NIR: Polyurea from MDA-DPC and Diamines
27
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 30
Run No. | Polyurea | Tda (℃) | Tg (℃) | Yield (%) | Tensile Strength (MPa) | Elongation (%) | ηinh | TMS Recovery (%) | Phenol Recovery (%)
9 | H12MDA-90-DBa | 290 | -56.9 | 97 | 25.5 | 425.4 | 0.71 | 95 | 88
12 | HDA-90-DB | 287 | -59.3 | 86 | 10.4 | 547.8 | 0.42 | 92 | 79
14 | m-XDA-90-DB | 280 | -58.4 | 98 | 3.6 | 186.1 | 0.35 | 94 | 87
15 | IPDA-90-DB | 282 | -57.3 | 100 | 16.9 | 1003.4 | 0.46 | 95 | 91
a 5% weight loss. B Distillation (140℃, 7×10-3 mmHg, 1h). |  |  |  |  |  |  |  |  | 
NIR- Polyurea Prepared in TMS
28
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 31
29
Shdai-140727
Green Chem-2014 Philadelphia
NIR-MDA-DPC Polyurea Prepared in TMS

## Slide 32
“Non-Phosgene Route (NPR) to Aliphatic Diisocyanates”
Wei-Hsing Lin (Lin, W-S; Ph. D Candidate; NCHU)
NPR to Aliphatic Diisocyanates
30
Shdai-140727

## Slide 33
25℃ for 2hr
60℃ for 9hr
Benzoic acid
Pyrolysis
Pyrolysis
Pyrolysis
DPC
DPC
EGDEE
EGDEE
DM-BPC
BM-BPC
ABA-DP-Biscarbmate
DDI
BDI
DDA
BDA
1-isocyanato-4-
(isocyanatomethyl)benzene; IBI
Pyrolysis
HM-BPC
HDI
HDA
Diphenyl ether
Our Overall 2-Step NPR Scheme: HDI, DDI, BDI, IBI (4) (5)
Aliphatic ISO:
Mixed ISO:
Advantages: a. Reactivity DPC>> DMC; b. Lower temperature for isocyanate generation
(4) Carbonylation (5) Pyrolysis
33
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 34
25℃、2hr
EGDEE; Recrystallization
75℃、20min
65℃、2hr
(Vacuum)
Overnight
(RT)
(4) NPR First Step: Carbonylation of 1,12-dodecane Diamine
Filtration
34
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 35
NPR- Monitoring of Carbonylation by IR: C12 Diamine
25℃、0hr
25℃、10min
25℃、1hr
25℃、2hr
1777cm-1(C=O)
【DPC】
1698cm-1(C=O)
【DMBPC】
3280cm-1(N-H)
【Stretching 】
35
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 36
 | C-12 –biscarbamate preparation
Molar ratio | DDA：DPC＝ 1：2.05
Weight ratio | DDA：DPC＝ 5 g：10.96 g
Catalyst | Catalyst-free
Nitrogen flux | N2 =0.3L/min
Reaction solvent | EGDEE＝ 48 g （S.C=25% ）
Reaction Temp. | 25℃
Reaction time | 2hr
DMBPC Yield | 98％
Urea yield | Non
Melting point | 121.5℃ ~ 122.4℃
NPR First Step: Carbonylation Data of 1,12-dodecane Diamine
36
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 37
NPR- NMR of 1,12-Dodecamethylene-Bis-phenyl carbamate
37
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 38
Thermo-Data of 1,12-Dodecamethylene-Bisphenyl carbamate
Td(5%)= 181.6℃
Td(50%)= 228℃
Mp =123 ℃
38
Green Chem-2014 Philadelphia

## Slide 39
NPR to 1,6-hexamethylene-bis(phenyl carbamate)
 | C-6-biscarbamate preparation
Molar ratio | HDA：DPC＝ 1：2.05
Weight ratio | HDA：DPC＝ 215 g：813 g
Catalyst | Catalyst-free
Nitrogen flux | N2 =0.3L/min
Agitation speed | 200rpm
Reaction solvent | EGDEE＝ 2500 ml
Reaction Temp. | 25℃
Reaction time | 2hr
HMBPC Yield | 95％
Urea yield | Non
Melting point | 127℃ ~ 128.2℃
39
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 40
Shdai-131227
[27] Luc Ubaghs, Isocyanate-free Synthesis of（Functional）Polyureas, Polyurethanes, and Urethane-
containing Copolymers , 2005, P.49
NPR- NMR of 1,6-Hexamethylene-Bis(phenyl carbamate)
40
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 41
Biscarbamates | DDI (C12) | HDI (C6) | BDI (C4)
Biscarbmate Yield | DMBPC 98% | HMBPC 98% | BMBPC 89%
Melting point (DSC) | 122.5 ℃ | 126.6 ℃ | 162℃
Td (TGA; 5%) | 181.6 ℃ | 147.4 ℃ | 167.7 ℃
1-isocyanato-4-(isocyanatomethyl)benzene
ABA-DP-Biscarbamate 85%
175.8 ℃
167.7 ℃
Aliphatic Bis-carbamates Mixed
(4) Summary : Bis-Carbamate Preparations
Excellent yield of biscarbamates could be prepared from C12, C6 and C4 diamine/+DPC.
C4-biscarbamate crystal was contaminated ~ 6% of phenol that could not be separated.
Preparation of ABA-biscarbamate is best done in two step.
41
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 42
Ice cool
Themal sensor
(inner)
Themal sensor
(outer)
Themal sensor
(distillation)
Heating belt
Fractionation
column
1,12-dodecamethylene-bis(phenyl carbamate)
Thermolysis
Dodecamethylene-1,12-diisocyanate
( bp = 168℃ at 3mmHg )
Benzoyl chloride as stabilizer
2
Diphenyl ether
( bp = 82℃ at 3mmHg or
250 ℃ at atm pressure )
Typical Set-up for Thermolysis of Biscarbamates
42
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 43
 |  | CG1020317
Weight |  | DMBPC＝ 5 g
Catalyst |  | Benzoyl chloride＝ 0.013 g
Nitrogen flux |  | Non
Solvent |  | Diphenyl ether＝ 45 g （S.C=10% ）
Pyrolysis | Initial NCO | 180℃
 | Maximum NCO | 254℃（ HMBPC disappeared after 0.5hr at 240 ℃ ）
 | Final | All NCO peaks disappear
Reactor byproduct |  | No yellow coking by-products
Flask (Ice cool) | Initial product | 240℃（ Phenol appeared for 0hr at 240 ℃ ）
 | Final product | 254℃（ Phenol appeared for 0.5hr at 240 ℃ ）
1,12-diisocyanatododecane Yield |  | 84％
Phenol recycling rate |  | 100％
NPR- (5) Data on Isolation C-12 -Diisocyanate
43
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 44
minutes
Quantitative Analyses of C12-(NCO)2 by Quenching
C12-(NCO)2 + MeOH
4.4
（Methanol）
9.3
（DDU）
(1) Mobile phase= 55%Methanol + 45%H2O
(2) Wave length= 205nm
(3) Flow rate= 0.5ml/min
(4) Const flow rate
50mg DDU + 1ml Methanol
15mg DDU + 1ml Methanol
Yield＝84%
(by HPLC)
44
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 45
28
240℃、0.5hr
Monitoring
DDI by IR
(1) Mobile phase= 55%Methanol+ 40%H2O
(2) Wave length= 205nm
(3) Flow rate= 0.5ml/min
Quantitative analyses of DDU by HPLC
Experiment (3) – One-pot two-stage NPR process
Pyrolysis
Capped by 10X MEOH
(90 ℃ 1hr)
Separated by DDI and
Diphenyl Ether (Vacuum)
Reactor
Flask (100%phenol)
SC = 18%
DMBPC → DDI
Pure DDI
(80%)
Pure Diphenyl Ether
(99%)
Reactor

## Slide 46
Experiment (3) – One-pot two-stage NPR process
DDI
(S.C= 18%)
Phenol appeared
(One-pot)
Figure 12. DMBPC biscarbamates decrease (%) and DDI diisocyanates formation (%) in the pyrolysis in one-pot two stage NPR process under 18% solid content in Diphenyl Ether at (a) 100℃, (b) 120℃, (c) 140℃, (d) 160℃, (e) 180℃, (f) 200℃, (g) 220℃ (phenol was collected in the flask), (h) 240℃, (i) 240℃-0.5 hr, (j) 240℃-1 hr.

## Slide 47
Experiment (3) – One-pot two-stage NPR process
22
DMBPC → DDI | CG1030203
Molar ratio | DDA：DPC＝ 1：2.05
Weight ratio | DDA：DPC＝ 10 g：21.9 g ( SC=25% )
Catalyst | Catalyst-free
Nitrogen flux | N2 =0.3L/min
Agitation speed | 200rpm
Carbonylation solvent | Diphenyl Ether ( DPE )＝ 96 g
Carbonylation Conditions | 60℃、2hr
DMBPC Yield ( HPLC ) | 100％
Pyrolysis solvent | Diphenyl Ether ( DPE ) as pyrolysis solvent ( SC=18% )
Stabilizer (Benzoyl chloride) | None
Pyrolysis Conditions | 240℃、0.5hr ( 220℃→NCO, 220℃→Phenol )
Recycling rate | Phenol =100％、Diphenyl Ether =99％
Isocyanate Yield (HPLC) | Pure DDI=80%、Trimer=20%

## Slide 48
Shdai-140727
Green Chem-2014 Philadelphia
Summary：One-pot two-stage NPR process
Summary：One-pot two-stage NPR process
Summary：One-pot two-stage NPR process
Summary：One-pot two-stage NPR process
 | DDI | HDI | 
Carbonylation solvent (Reaction S.C%) | EGDEE (25%) | EGDEE (25%) | 
Molar ratio | DDA : DPC =1 : 2.05 | HDA : DPC =1 : 2.05 | 
Catalyst | none | none | 
Reaction condition | 25℃、2hr | 25℃、2hr | 
Biscarbmate Yield | 98% (DMBPC) | 98% (HMBPC) | 
Pyrolysis solvent (Reaction S.C%) | DPE (10%) | DPE (2.5%) | DPE (10%)
Cracked time (carbamate disappeared) | 240℃、0.5hr (254℃) | 240℃、2hr (254℃) | 240℃、1.5hr (254℃)
Stabilizer (Benzoyl chloride) | Exist (1 / 145 ) | none | Exist (1 / 145 )
Isocyanate Yield | DDI=84% Trimer=16% | HDI=76% Trimer=12% Biuret=8% | HDI=47% Trimer=14% Biuret=4% Allophanate=35%
DDI | HDI
DPE (25%) | DPE (25%)
DDA : DPC =1 : 2.05 | HDA : DPC =1 : 2.05
none | none
60℃、2hr | 60℃、2hr
100% (DMBPC) | 100% (HMBPC)
DPE (18%) | DPE (16%)
240℃、0.5hr (260℃) | 240℃、1hr (258℃)
none | Benzoyl chloride / HMBPC = 1 / 145 (molar ratio)
DDI=80% Trimer=20% | HDI=42% Trimer=34% Biuret=16% Allophanate=3%
Two step (original process)
One-pot two-stage NPR process
Summary：One-pot two-stage NPR process

## Slide 49
Non isocyanate / Phosgene Route (NIR/NPR)
Chen, H.Y.; Pan, W. C.; Lin, C. H.; Huang, C.Y.; and Dai, S. A., Journal of Polymer Research, 19(2), 9754-9765,2012.
(DPC) (6) Trans-esterification
(DPC)
(4)
(5)
47
Shdai-140727
Green Chem-2014 Philadelphia
NPR
NIR

## Slide 50
NIR- Method 1: One Step-One Pot Process
48
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 51
NIR- Method 2: Two-step Process with Hard Segment Prepared First
49
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 52
NIR- Method 3: Two-step Process with Soft Segment Prepared First
50
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 53
NIR- Monitoring by FT-IR in Method 3
51
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 54
Properties of NIR-PUaE
Methoda | HSb (%) | Yield (%) | phenol recycle ratio (%) | ηinh | Tdc (℃) | Tg (℃) | Tc (℃) | Elongation (%) | Tensile strength (MPa)
1 | 30 | 100 | 88 | 0.25 | 268 | -62 | / | 174 | 3.84
2 |  | 97 | 82 | 0.49 | 262 | -64 | 187 | 469 | 18
3 |  | 94 | 89 | 0.26 | 231 | -65 | 170 | 92 | 3.28
1 | 40 | 94 | 78 | 0.29 | 250 | -60 | 181 | 315 | 17.6
2 |  | 96 | 85 | 0.42 | 251 | -60 | 192 | 160 | 15.2
3 |  | 89 | 84 | 0.28 | 243 | -64 | / | 208 | 11.79
a: Method of synthesis(1 :one pot ; 2: two steps-Hard first ; 3: two steps-Soft first) b: Hard segment ratio c: 5% weight lose temperature |  |  |  |  |  |  |  |  | 
52
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 55: NIR- Polyurea Analysis of GPC
Section 1
Section 2
Method | Area (%) |  |  | ηinh
 | A1 High Molecular Region | A2 Median Molecular Region | A3 Low Molecular Region | 
1 | 37% | 45% | 18% | 0.25
2 | 44% | 33% | 23% | 0.49
3 | 11% | 83% | 6% | 0.26
Section 3
53
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 56
NIR- Method 4: Three-steps Process
54
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 57
NIR- Monitoring by FT-IR in Method 4
55
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 58
Properties of NIR-Polyurea(Method 4)
short chain diamine (1) | short chain diamine (2) | long chain diamine | HSa (%) | Yield (%) | phenol recycle ratio (%) | ηinh | Tdb (℃) | Tg (℃) | Elongation (%) | Tensile Strength (MPa)
HDA | IPDA | D2000 | 30 | 94 | 96 | 0.56 | 264 | -56 | 664 | 15.6
HDA | IPDA | ED2003 |  | 89 | 100 | 0.64 | 298 | -60 | 1462 | 0.98
MDA | IPDA | D2000 |  | 68 | 65 | 0.23 | 283 | -55 | 64 | 0.43
HDA | IPDA | D2000 | 40 | 83 | 44 | 0.62 | 284 | -61 | 469 | 33.4
a: Hard Segment ratio b: 5% weight lose temperature |  |  |  |  |  |  |  |  |  | 
56
Green Chem-2014 Philadelphia
Shdai-140727

## Slide 59
Analysis of AFM
3D-display
pmPUaE(DPC-D2000-IPDA)
roughness:1.09nm
hSPUaE(DPC-IPDA-D2000)
roughness:11.06nm
Method 1
Method 2
57
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 60
Analysis of AFM
sSPUaE(DPC-D2000-IPDA)
roughness:18.85nm
SPUaE(HDA-DPC-D2000-IPDA)
roughness:12.7nm
Method 3
Method 4
58
Green Chem-2014 Philadelphia
Shdai-140727

## Slide 61
Shdai-131227
NIR -Conclusion
Method 1：One step → Random → no phase separation
Method 2：Hard segment first →gathered hard segment → clear phase separation and better properties
Method 3：Soft segment first → scattered hydrogen bond → small phase separation and poor properties
Method 4：Three steps → high MW and phase separation
59
Green Chem-2014 Philadelphia

## Slide 62
Shdai-131227
NIR Process with DPC
Advantages of our PUaE:
  Raw materials (DPC and diamines) are inexpensive.
  Low chlorine in PUaE
  Can synthesize segmented PU elastomers
  Mechanical and thermal properties of PUaE are better than traditional PU.
  In line with the principles of green chemistry
  Lower capital expenses for scaling-up
Disadvantages:
- phenol/TMS recovery and recycle
60
Green Chem-2014 Philadelphia

## Slide 63
Non-phosgene Route to PCs
59a
In essence, our NPR process to PU is comparable to that BPA to PC of Asahi’process both using DPC as the key reagent. (taken from Principle of Indstrial Organic Chemistry)
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 64
Non-Isocyanate Route to Polyurethane via Cyclic Carbonates
Oleg L.Figovsky,Features of Reaction Amino-cyclocarbonate for Production of New Type Nonisocyanate Polyurethane Coatings. Macromol.Symp, 2002,187(325~332)
Polyurethane
Cyclo bis(carbonate)s
Diamine
+
Ring-opening reaction with no by-product generation
63
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 65
b
a
+
(7) Products Found in CC-Amine Reactions
a
b
(ring-opening)
(trans-amination)
Ring-opening of Glycerin cyclic carbonate
formed un-desirable urea by-products in 0.3~8%
使用Model compound C (由epoxy合成之CC) 並無出現副產物的問題
所以在製備NIPU時,盡量使用Compound C types之CC進行non-isocyanate為佳.
65
Green Chem-2014 Philadelphia
Shdai-140727

## Slide 66
The system must be strickly free from water until used.
The hydrolytically unstable chemical bonds.
The use of toxic/reactive isocyanate.
Conventional PU (Iso/alc.)
NIPU using CC/ amines
Porous-free and moisture-insensitive.
Intermolecular hydrogen bond endow NIPU with good properties.
Without using isocyanate.
(7) Comparison of PU and NIPU
66
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 67
(7) Cyclic Carbonate Formation from CO2 and Oxiranes
V. Calo, A. Nacci, A. Monopoli,Org. Lett. 2002,4,2561-2563
67
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 68
N. Kihara, T. Endo, J. Polym, Sci, 1993,31,2765-2773
Crosslinking PU
HDI
Aluminium triisopropoxide
(7) Crosslinked PU from HAD/CC from BPA-DGE
CO2
BPA-DGE (Epoxy)
68
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 69
Chen Kan-Nan’s Crosslinking Approach
69
J. Polym. Res., 2012, 19, 9900
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 70
(7) : Synthesis of M1 Prepolymer
1H-NMR
IR
BCS
Diglyme
@ 100°C，16hr
M1
GPC
70
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 71
Shdai-131227
PU(MBI-79XX-XX)
BI-7950(50%,75%,100%) BI-7960(50%,75%,100%) BI-7982(50%,75%,100%)
Chain Extending by Adding Blocked
Isocyanate
其中(50%,75%,100%)
代表其末端胺的反應程度
(7): Chain Extending of M1 Prepolymer with Blocked Isocyanate
71
1.由Epoxy Resin(BE-188)合成出的Amine-terminated prepolymer 不會出現 urea by-product, 但其分子量約在1200左右,而加入了商業化的Blocked isocyanate作鏈長時,其分子量呈現多區塊的分布,無法避免仍存在小區塊分子產生.
2. 由添加的blocked isocyanate之不同,交聯程度增加,可看見大分子區塊面積些微增加,第一區塊比例由4%~10%,區塊由三個(MBI 7950)變為四個(MBI-7982)最佳.
3.但主區塊的分子量成長有限,此部份仍未完全作最佳化.
Green Chem-2014 Philadelphia

## Slide 72
FTIR Monitoring of Preparing BCS I+ 1,4-Bis(3-aminopropyl)-piperazine at eq ratio 1.25:1 in DMAc
產物命名: BCS type-amine-BCS過量比例-solvent-溫度-solid content
若沒特別註明溫度為100°C solid cotent 為 low
72
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 73
Reaction of BCS II with1,4-Bis(3-aminopropyl)-piperazine
@100°C
1,4-Bis(3-aminopropyl)-piperazine
+
 | Mn | MW | PD
20130903 | 56,192 | 846,578 | 15.0657
Tg = 78.1 C
Td (5%) = 274 C
Char Y = 1.64%
E% = 7%
TS = 20.84 Mpa
%wt increase in water = 0.23% (2wks)
73
In anisole
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 74
Reaction of BCS II with1,4-Bis(3-aminopropyl)-piperazine
74
Cyclic carbonate
Carbamate
No sign of urea
In Anisole Solution
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 75
Shdai-131227
75
Keys to High Molecular Weights PUs from Ring- Opening of CC
Selection of reactive diamines and bis-cyclic carbonates
Suitable solvent to maintain efficient mixing
High shear mixing of high viscosity products
Mild reaction without by-product formation (< 100 C)
Promoted by efficient catalyst: (Data obtained in different reaction time)
Green Chem-2014 Philadelphia

## Slide 76
76
Summary
Successful NPR Developed Using DPC as Carbonylating agent:
MDA MDI
HMDA + DPC Biscarbamates HDI
DDA DDI
Successful Polyurea Elastomers Development via NIR
200-240℃
Biscarbamates
DPC
Polyurea Elastomers
HMDA/Jeffamine2000/IPDI
(One-pot three step)
PU Plastics Synthesized through NIR:
CC from Epoxy(BPA DGE)+Diamine
PU (In Progress)
△
△
△
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 77
77
Other NIR Process under Study(Dai Group)
(PC recycle and re-use as PU)
(GMA to ODMA to PU-acrylate/ DSM)
(Biscarbamate as blocked isocyanate)
Poly-(IPP-cyclic carboanate)
A.
B.
C.
D.
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 78
78
Acknowledgements
大東公司(GRECO) 新力美(DSM)
National Science Concil of Taiwan
Chen, S. Y (MDI) ;
Pan, Elisa (Polyurea elastomers)
Lin, W-S (HDI,DDI)
Ku, K.T.(CC to PU) Li, 紫菁(CC to PU)
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 79
79
Dai’s Group - 2012
Dai’s Group - 2013
(1)
(2)
(3)
(4)
(3)
Chen, 陳學永
Ku, 顧冠增
Pan, 潘玫蓁
Li, 李紫菁
Lin, 林維興
Shdai-140727
Green Chem-2014 Philadelphia

## Slide 80: Let Us Meet Again
We welcome you all to our future conferences of OMICS Group International
Please Visit: www.omicsgroup.com
www.conferenceseries.com
www.pharmaceuticalconferences.com