## Slide 1
Professor Adam Lee
a.f.lee@aston.ac.uk
Biofuels & Bioenergy August 27th 2015
European Bioenergy Research Institute
Rational design of nanoengineered catalysts for biofuels production

## Slide 2
CO2
H2O
.OH + H+
CH4, CH3OH
H2
Semiconductor
e-
Solar fuels/chemicals
Reforming
Cracking
Biorefining
Switchgrass
Corn husks
Jatropha curcas
Chemical synthesis
Green
Chemistry
Fossil fuel refining
2
Aqueous phase
Low T
Organic phase
High T
Heterogeneous Catalysis: Chemicals & Energy
Unsustainable
Sustainable
Economic

## Slide 3: Biofuels: non-food crops
Renewable biofuels require waste/non-food feedstocks.
Non-edible components of crops
(stems, leaves and husks).
Agricultural or forestry waste,
or short rotation crops.
Algae
Switchgrass
Jatropha  minimal cultivation.
Aquatic biomass.
Lignocellulosic feedstocks
Oleo-feedstocks
Jatropha curcas
~ 2.2-2.7 ton oil/ha
(www.reuk.co.uk)
~180 x more oil/ha than Jatropha
Chem. Soc. Rev. 2014, 43, 7887
Catal. Today 2014, 242, 3

## Slide 4: Thermochemical routes to biofuels
  Pyrolytic routes to bio-oil not selective  unstable acidic mixtures.
  Transesterification offers a low energy route to fuel.

## Slide 5: Challenges for Lignocellulosic Bio-fuels
Cellulose
Lignin
Sensitive to poisoning.
require e.g. esterification or
ketonisation pretreatments
Hydrodeoxygenation used to upgrade oil to fuel
Pyrolysis
Bio-oil

## Slide 6: Biofuel Synthesis from Plant/Algal Oils
Biodiesel
+
Glycerol
n-Alkane
+
Propane
Transesterification
Hydrotreating
Oil Triglyceride
Bio-fuel
Synthesis
Methanol
+
catalyst
Hydrogen
+
catalyst
‘Drop in’ technology
Reformed fuel – e.g. Jet fuel
Need renewable H2
Higher temperature process
Energy efficient
Cheap technology
Localised fuel distribution
Fuel properties oil dependent

## Slide 7: Biodiesel synthesis
H2O
NaOMe
Oil
stable emulsions
aqueous quench
New Heterogeneous Catalysts
 Facile biodiesel separation

Process Intensification
 Improved energy efficiency
Glycerol
Biodiesel
(FAME)
3 +
Triglyceride
(TAG)
3 CH3OH
energy intensive separation
Cat. Sci. Tech. 2012, 1, 1
Second-generation biofuels from lignocellulose or sustainable bio-oils.
Renewable
bio-oils
Jatropha
Algae
Bio-oil transesterification
J. Biobased Mater. Bioenergy 2007, 1, 19
Low
carbon

## Slide 8: Process variables
Biodiesel synthesis
2. Catalyst type
Fatty acid content?
Unsaturation/chain length
Glyceryl trioleate
C18 unsaturated
Glyceryl tripalmitate
C16 saturated
1. Oil composition
Solid acid vs solid base
Compatibility with oil?
Acid/Base strength?
Effect of porosity?
H+ CH3OH
Fatty Acid (FFA)
FAME
Zeolites
Hydrotalcites
Process Intensification
3. Reactor Design
Batch vs Flow
Flow
in
Baffled
tube
Flow out
Oscillation
Uniform catalyst suspension
Ind Eng Chem Res 2001, 40, 5371

## Slide 9: Hierarchical porous nanostructures
Highly organized
macroporous-mesoporous Al2O3
Enhanced mass-transport for bulky feedstocks
Calcination under O2
at 600 °C
Hybrid macro-mesophase
formation
Precursor
infiltration
Sedimentation
of PS beads
Evaporation of
supernatant
Static conditions
at 60 °C
Pluronic P123
HNO3
Soft Template
Aluminum Isopropoxide/TEOS
Ethanol
Ageing (5 hours)
Hard Template
(polystyrene)
JACS 2009, 131, 12896
Green Chem. 2010, 12, 296
Chem. Soc. Rev. 2013
42, 3876

## Slide 10: Hierarchical Solid Acids
Chart: FFA esterification TOF / h-1
| SBA-15 | MM-SBA-1 | MM-SBA-2 | MM-SBA-4
C16 TOF | 23.5 | 27 | 32 | 36


C8 TOF | 3.294 | 5.616 | 7.05 | 7.794
Macroporous-mesoporous solid acid catalyst:
Hierarchical solids tune structure
and promote biofuels synthesis
Palmitic acid
Triglyceride
SiO2
SiO2
O2
Macro-Meso SiO2
Green Chem. 2010, 12, 296

## Slide 11: Hierarchical Macro-Mesoporous Supports
Si(OEt)4
Polystyrene
nanospheres
Calcine
Micellar array Templated SiO2 Mesoporous SiO2
Templated macro-mesoporous SiO2 Macro-mesoporous SiO2
1 m
128 nm
J. Am. Chem. Soc., 2009, 131,12896
Green Chem. 2010, 12, 296

## Slide 12: Hierarchical Solid Bases
2 m
300 nm
Macroporous HT
Chart: TOF enhancement
| C4 | C8 | C12 | C18
 | 1.0989 | 2.5 | 4.0667 | 9.3333
Bio-oil chain length
Hydrotalcite solid base catalysts:
1 m
Conventional HT
MgxAlyOx+1.5y
Macropores enhance bulky
bio-oil transformation
Energy Env. Sci. 2012, 5, 6145

## Slide 13: Thin Film Hydrotalcites
Can we generate high area HT thin films to further improve mass transport ?
Green Chem. 2015, 17, 2398
XRD confirms formation of Mg2Al HT phase.
Enhanced base site accessibility and TOF for TAG transesterification
Chart: TAG Chain Length
| C12 | C18
Conv HT | 2 | 1
HT MMSBA-15 | 9.5 | 4.5
Silica
Macropore
SBA-15
Mesopores
Hydrotalcite

## Slide 14: Process Intensification
Chart: Reaction time / min
| 30 | 45 | 60 | 75 | 90 | 105 | 135 | 165 | 195 | 225
TON Flow | 20.5734 | 33.3139 | 48.18 | 63.174 | 77.0333 | 90.8911 | 106.6724 | 125.5504 | 144.7854 | 163.614
% Acid Conversion Flow | 10.7393 | 13.3011 | 15.5202 | 15.6538 | 14.4691 | 14.4675 | 16.4757 | 19.7086 | 20.0813 | 19.6571
Net flow in
Baffled
tube
Net
flow out
Oscillation
No Oscillation
Sedimentation
Oscillation
Uniform suspension
First heterogeneously catalysed OBR reaction
 solid acid catalysed esterification.
Cumulative TON equivalent to stirred batch.
Catal Sci & Tech. 2013, 3, 2373
Conventional plug flow reactors long catalyst beds for slow reaxn.
Oscillatory Baffled Reactor (OBR) superimposes oscillatory on net slow flow.
 baffled cell acts as CSTR  catalyst particles entrained between baffles.

## Slide 15
Catalyst Development
Reduced
Pollution
Surface Chemistry
Materials Design
Chemical Engineering
Conclusions
Energy
efficient
Renewable
resources
Sustainable Chemistry

## Slide 16: Acknowledgements
Professor Karen Wilson
Dr Jean-Philippe Dacquin  Jean-Michele Caderon
Dr Cyril Pirez  Dr Amin Osatiashtiani
 Jeremy Dhainaut
 Dr James Bennett
Huddersfield:
Prof D. Robert Brown
Dr Marta Granollers
Bath:
Prof Tina Düren
Dr Jennifer Williams
Newcastle:
Prof Adam P Harvey
Dr Ahn Phan
Valentine Eze
University of Rey Juan Carlos (Madrid)
Prof Juan Melero
Prof Gabriel Morales Sanchez

## Slide 17
Huber – Upgrading of Aqueous Phase

## Slide 18
Bio-oils are complex unstable mixtures - require upgrading to improve:
  oil stability by eliminating reactive components
  hydrocarbon yield by condensing short chain components
  oil compatibility for refining
Improve fuel stability
C-C chain growth
Reduce acidity
Isomerise
https://engineering.purdue.edu/H2biomass/research.php
?
Cracking
Aromatization
- Decarboxylation
Esterification
Dehydration
- Decarboxylation
- Deoxygenation
- Condensation
- Ketonization
Solid Bases
Solid Acids
Mixed metal oxides
Metal (PGM) doped oxides
Enormous opportunities for catalyst and process design
Catalytic Bio-oil Upgrading

## Slide 19
Alkane Fuels – HMF platform
Science, 2006, 312, 1933.
Fructose 5-HMF
Aqueous
Organic
Continuous 5-HMF extraction into the organic phase reduces side reactions.
C12 alkane
+ HMF
H2
H2O
Metal doped solid acid for HDO
C9 alkane
H+/H2
H2O
Acid catalysed aldol condensation
C15 alkane
+ HMF
H2
H2O
H2

## Slide 20
Routes to Biodiesel from Algae or Jatropha
Salt water strains
Polyunsaturated
C20-C22 chains common
Phosphorus problem (10-20% phospholipid)
Biodiesel
C18 unsaturated chains
15% free fatty acid
Poisonous seed cake
Need right climate (developing countries)
Reactor
H2O/nutrients
Algae
CO2
Pump
Recirculating Tank
Filter
Dry
Extract
Cultivate
Harvest
Separate
Press
Green Fuel Technologies, Cambridge MA.
Bioreactor
Jatropha plantation
?

## Slide 21
Decentralised Fast Pyrolysis & Local Use
21
http://www.ars.usda.gov/

## Slide 22: Diffusion modelling framework
Wilke Chang correlation for infinite dilution diffusion coefficient
Physical properties of chemicals
Binary diffusion coefficient
Effective diffusivity
Diffusion flux
Power law based intrinsic kinetics
Reaction flux
Add and update product concentration profile
Reactant conversion profile
Catalyst design parameters
Goal to validate and predict catalyst design parameters:
RSC Advances 2013, 3, 6226

## Slide 23
Model substrates for esterification
x
Typical Reaction conditions
Reaction temperature 50-80 °C
Atmospheric pressure
Reaction under air
Identify solvent to use as model bio-oil so as to work as acid concentration representative of that in oil.

## Slide 24: Lignocellulose Conversion
Fuels or
Chemicals
Fractionation
Require catalytic methods to convert lignocellulose to fuels or platform chemicals
Biocatalysis:
 dilute, impure aqueous chemicals
 Energy intensive product isolation
H+
Cellulose
WASTE

## Slide 25: Petrochemical to Bio-refining
Biomass
source
Fuels
Solvent
Bulk chemicals
Plastics
Fibres
Fine chemicals
Oils


Fuel & chemical co-production improves process economics

## Slide 26: Carbohydrate Transformations
Large pore materials as solid supports
Solid catalysts to reduce waste
C-O-C, C-OH cleavage
Selective hydrogenation or oxidation
C-OH Dehydration

Bifunctional Catalysis
H+
OH
Pt
H2
Dehydration
+ Hydrogenation
Bifunctional catalysts improve process efficiency

## Slide 27: Bio-oil Pretreatment 2: Esterification
RSO3H
+ Octyl
MCM-41
Increased hydrophobicity promotes esterification activity
Green Chem. 2010, 12, 1383
Hydrophobic materials required to improve water tolerance