## Slide 1
Adolfo Iulianelli
Institute on Membrane Technology of the Italian National Research Council (ITM-CNR),
Via P. Bucci Cubo 17/C c/o University of Calabria, Rende (CS), 87036 – Italy; a.iulianelli@itm.cnr.it; +39 0984 492011
An overview about inorganic membrane technology application in the field of hydrogen generation and purification
SEPARATION TECHNIQUES 2016 – Valencia, September 26-28, 2016

## Slide 2
ITM-CNR
Institute on Membrane Technology
University of Calabria
ITM-CNR (Headquarter)
ITM-CNR Laboratories
ITM-CNR Laboratories

## Slide 3
Institute & Activity
Inorganic membrane reactor
ITM-CNR
Membrane contactors
Water desalination by membrane filtration
Gas separation: polymeric and inorganic membranes
PEM fuel cell
Membrane bioreactor

## Slide 5
FOSSIL FUELS
BIOMASS
Crude oil
Natural gas
Coal
Lignocellulosic
biomass
Sugar and
Starch crops
Oil crops
Wet
biomass
Refining
Blending
LPG
Petrol
Diesel
CNG,
LNG
FTL
DME
MeOH
Mixed
Alcohol
Bioethanol,
Butanol
Biodiesel,
Bioglycerol
Green
Diesel
Synthesis
Refining
Refining
Esterification
Gasification
Pyrolysis
Fermentation
Extraction
Hydro-
Thermal
Upgrade
Anaerobic
Digestion
(Biogas)
Hydrolysis

## Slide 6
Techniques for H2 separation
Membrane technology for H2 separation
ITM-CNR
Institute on Membrane Technology

## Slide 7
Membrane | Polimeric | Microporous | Metallic | Carbon | Ceramic
Temperature range | < 200 °C | 200 – 600 °C | 300 – 600 °C | 500 – 900 °C | 600 – 900 °C
aH2/N2 | low | 5 – 139 | > 1000 | 4 – 20 | > 100
Stability issues | Swelling, mechanical strenght | Stability in H2O | Phase Transition | Brittle, Oxidization | Stability in CO2
Poisoning issues | HCl, SOx |  | H2S, HCl, CO | Strong adsorbing vapours, organics | H2S
Material | Polymers | Silica, Alumina, Zirconia, Titania, Zeolite | Palladium, Palladium Alloy, etc. | Carbon | Proton Conductivity ceramics (mainly SrCeO3-d, BaCeO3-d)
Membranes for H2 separation
aH2/N2 = permeanceH2/permeanceN2

## Slide 8
ITM-CNR
Institute on Membrane Technology
Why inorganic membranes for H2 separation?
S. Yun, S. Ted Oyama, Correlations in palladium membranes for hydrogen separation: A review, J. Membrane Sci., 375 (2011) 28–45
Most attractive region

## Slide 9
ITM-CNR
Institute on Membrane Technology
Hydrogen permeability through different metals
Palladium
Basile et al., Synthesis, characterization and applications of palladium membranes, Eds. R. Malada, M. Menendez, Elsevier, Ch. 8 (2007).
Dense metal membranes:
Group 10 (Ni, Pd, Pt), Group 5 (V, Ta, Nb)
able to dissociate and dissolve H2.
Pd membranes show a very high H2 solubility in a wide range of T
Ta, Nb, V

## Slide 10
ITM-CNR
Institute on Membrane Technology
V, Ta and Nb are prone to a severe H2 embrittlement
DBTC (ductile-to-brittle transition hydrogen concentration) occurs for the V group metal as a function of CH2.
DBTCpure Nb: H/Nb = 0.25 - DBTCpure V : H/V = 0.22
The resistance to H2 embrittlement of Nb and V, during H2 permeation, can be improved by keeping CH2 below their critical value.
Matsumoto et al., In situ quantitative evaluation of hydrogen embrittlement in group 5 metal used for hydrogen separation and purification, ch. 12 in Advances in hydrogen production, storage and distribution, Woodhead Publishing, A. Basile & A. Iulianelli (Eds.), 2014.

## Slide 11
ITM-CNR
Institute on Membrane Technology
Ductile-to-brittle transition hydrogen concentration

## Slide 12
Palladium Membranes for H2 separation
Dense metal membranes
Dense ceramic membranes (mixed conduction)
Microporous membranes
Dense Pd-based membranes having full hydrogen perm-selectivity follows the Richardson equation:
where d is the membrane thickness, Peo, Ea, R and T are the pre-exponential factor, the apparent activation energy, the universal gas constant, and the absolute temperature, respectively.
Steps of solution/diffusion mechanism:
dissociation of molecular hydrogen at the gas/metal interface,
adsorption of the atomic hydrogen on membrane surface;
dissolution of atomic hydrogen into palladium matrix;
diffusion of atomic hydrogen toward the opposite side;
re-combination of atomic hydrogen to form hydrogen molecules at the gas/metal interface;
desorption of hydrogen molecules.

## Slide 13
ITM-CNR
Institute on Membrane Technology
Solution to embrittlement phenomenon for Pd membranes: Pd-alloy membranes
Pd-Ag thickness = 50 μm.
Membrane preparation = cold-rolling and welding techinque.
Membrane lenght (active surface) = 15 cm

## Slide 14
T, plumen
Hydrogen permeated flow (shell side) for CO2/H2 and N2/H2 feed mixture (lumen side) at T = 250 °C and plumen = 3.5 bar; shell is at 1 bar
T = 250 °C
T = 350 °C
Effect of CO adsorption on the Pd-Ag surface
DJH2
Basile et al., International Journal of Hydrogen Energy 32 (2007) 1837 – 1845
JH2 vs H2 concentration in the feed for CO/H2 and N2/H2 feed mixture (lumen side) at T = 250 and 350 °C and plumen = 3.5 bar; shell is at 1 bar
Pd-Ag dense unsupported membranes

## Slide 15
Ti-Ni-Pd dense unsupported membrane
A. Basile, F. Gallucci, A. Iulianelli, G.F.Tereschenko, M.M. Ermilova, N.V. Orekhova, Ti-Ni-Pd dense membranes – The effect of the gas mixtures on the hydrogen permeation, Journal of Membrane Science, 310 (2008) 44-50.

## Slide 16
Feed
Membrane
Retentate
Sweep-gas
Permeate
Catalyst
Pd-based Membrane Reactor Technology
Consider the following general reversible reaction:
A + B = C + D
If only the product C (for example HYDROGEN) is permeable through the membrane, the conversion becomes higher as the equilibrium is displaced towards the products side.
A + B = C + H2
Conventional Reactors
Membrane Reactors
Thermodyanamic equilibrium

## Slide 17
Pd-based Membrane Reactor Technology and Process Intensification
CH4 + H2O
Conventional Reformer
T = 800 -1000°C
H2, CO, CO2, not reacted CH4 and H2O
PrOx reactor
WGS stages
LT-WGS reactor
HT-WGS rector
PSA
Other
Low-temperature PEM fuel cells: CO content tollerated in the H2 supplied: < 10 ppm
CH4 + H2O
PEM fuel cell grade hydrogen
H2, CO, CO2, not reacted CH4 and H2O
Full H2 perm-selective Pd-based membrane reactor

## Slide 18
Unsupported dense Pd-based MRs
Ethanol steam reforming
Methanol steam reforming
Methane steam reforming
Methane Dry reforming
Oxidative ethanol steam reforming
Oxidative methanol steam reforming
Partial oxidation of ethanol
Glycerol steam reforming
Acetic acid steam reforming
Water gas shift
Cyclohexane dehydrogenation
Pd-based Membrane Reactor Technology: Highlights
Alimentazione
Retentato
Modulo del MR
Alimentazione
Anello di grafite
Permeato
Membrana
Supporti in acciaio inox alle estremità della membrane
Catalizzatore
Sfere di vetro
Termocoppia
Gas di lavaggio
10% - 12%
T = 300 °C
~ 20%
T = 360 °C
MR
FBR
Pd-Ag dense unsupported membrane, Thickness = 50 μm
Fe-Cr catalyst
WATER GAS SHIFT
REACTION

## Slide 19
A. Iulianelli, A. Basile, Hydrogen production from ethanol via inorganic membrane reactors technology: a review, Catalysis Science & Technology, 1 (2011) 366-379.
ETHANOL STEAM REFORMING
REACTION
Catalysts distribution for ESR reaction
Conventional Reactors
Membrane Reactors
Our work
Ethanol conversion [%]

## Slide 20
ITM-CNR
Institute on Membrane Technology
Pd-based membranes: potentiality at industrial scale
$
$
$
$
$
$
$
$
$
$
$
$
€
$
€
€
€
€
€
€
€
€
€
€
Pd-content
H2 permeance
Dense self-supporting Pd-membranes with thickness > 100/150 mm

## Slide 22
ITM-CNR
Institute on Membrane Technology
Dense self-supported Pd-based
Thickness = 50 μm [not commercial, by ENEA Laboratory (Frascati, Itay)]
Thickness = 150 μm [commercial, Johonson & Matthey]
Methane steam reforming
Ethanol steam reforming
Methanol steam reforming
Acetic acid steam reforming
Glycerol steam reforming
Water Gas Shift
Dense self-supported Ti-Ni-Pd
Thickness = 40 μm [not commercial, by Topchiev Institute (Moscow, Russia)]
Cyclohexane dehydrogenatation
Composite Pd-layer supported on porous stainless steel
Pd layer= 10 μm [not commercial, by RSE SpA (Milan, Itay) and University of Genova (Genova, Italy)]
Ethanol/Bio-ethanol steam reforming
Water Gas Shift
Carbon membranes
Pd layer= 5-8 μm [not commercial, by Najing Tech. University Laboratory (Najing, China)]
Methanol steam reforming
Bio-ethanol steam reforming
Bio-gas steam reforming
Composite Pd-layer supported on a-Al2O3
Palladium content decrease
Composite Pd-Cu
supported on a-Al2O3
Pd layer= 20 μm [not commercial, by CNR-ITM & Advanced Catalyst Srl (Rende/Pisa, Italy)]
Bio-gas steam reforming
Not commercial and not Pd-based, by University RoviraiVirgili (Tarragona, Spain)
Methanol steam reforming
From dense self-supported to thin Pd-based supported membranes or not Pd-based membranes for H2 production
Graphene membranes
By University of Valencia (Spain)]

## Slide 23: H2 separation by a Porous Stainless Steel supported Pd-based membrane
A bare support (PSS);
B oxidized support;
C g-alumina layer; D activated layer;
E Pd-layer 10 mm thick
He permeance at room temperature
Ideal selectivity [α (H2/N2)] = H2 permeance/N2 permeance
α (H2/N2) > 10000 (T = 400 °C)
S. Liguori, A. Iulianelli, F. Dalena, P. Pinacci, F. Drago, M. Broglia, Y. Huang, A. Basile, Performance and long-term stability of Pd/PSS and Pd/Al2O3 for hydrogen separation, Membranes, 4 (2014) 143-162.

## Slide 24
α (H2/CO2) > 4000 (T = 400 °C)
α (H2/CH4) > 9000 (T = 400 °C)
S. Liguori, A. Iulianelli, F. Dalena, P. Pinacci, F. Drago, M. Broglia, Y. Huang, A. Basile, Membranes, 4 (2014) 143-162.

## Slide 25: H2 separation by a Al2O3 supported Pd-based membrane
Pd - layer = 5/6 μm, Support: a-Al2O3
SEM image of the cross section of the composite Pd/Al2O3 membrane (a); morphology of the Pd-surface (b).
a)
b)
DOE Target
aH2/N2 = 1.0·104
Membrane failure

## Slide 26
Composite Pd/Al2O3 Membrane Reactor applied to bio-sources reforming reaction to produce H2: Highlights
H2 permeate purity vs space velocity (GHSV) during Bio-ethanol steam reforming at 400 °C and 2.0 bar of reaction pressure.
CO-free
S. Yun, S. Ted Oyama / Journal of Membrane Science 375 (2011) 28–45

## Slide 27
Chart: GHSV [h-1]
| 1900 | 2900 | 4800
2 bar | 58 | 57 | 53
1.5 bar | 50 | 48 | 45
2 bar | 70 | 60 | 50
1.5 bar | 65 | 53 | 38
Composite Pd/Al2O3 Membrane Reactor applied to bio-sources reforming reaction to produce H2: Highlights
T = 400 °C
Before exp. tests
After exp. tests
Critical issues
A. Iulianelli, V. Palma, G. Bagnato, C. Ruocco, Y. Huang, G. Vitulli, E. Macchia, N.T. Veziroğlu, A. Basile, From industrial bioethanol to high grade hydrogen generation: steam reforming reaction promoted by a novel Co-Pt catalyst in a H2-full perm-selective Pd-based membrane reactor, submitted to Journal of Power Sources.

## Slide 28
Composite Pd-Au/Al2O3 Membranes applied to H2 separation and to methane steam reforming in membrane reactor: Highlights
He permeance at room temperature

## Slide 29
T = 420 °C
MR
TR
Chart: Time (h)
| 0 | 0.25 | 0.5 | 0.75 | 1 | 1.25 | 1.5 | 1.75 | 2 | 2.25
Flow of Hydrogen out | 6.6556e-05 | 3.8971e-05 | 1.7482e-05 | 8.9484e-06 | 4.36e-05 | 0.0002675 | 0.00074687 | 0.001313 | 0.0017538 | 0.0020194
Flow of Hydrogen in | 0.0029908 | 0.0029908 | 0.0029908 | 0.0029908 | 0.0029908 | 0.0029908 | 0.0029908 | 0.0029908 | 0.0029908 | 0.0029908
Coke formation
Methane steam reforming
Before exp. tests
After exp. tests
A. Iulianelli, M. Alavi, G. Bagnato, S. Liguori, J. Wilcox, M.R. Rahimpour, R. Eslamlouyan, B. Anzelmo, A. Basile, Supported Pd-Au membrane reactor for hydrogen production: membrane preparation, characterization and testing, Molecules, 21 (2016) 581-594

## Slide 30
No Palladium-based inorganic membranes in H2 separation:
carbon membranes
Transversal photomicrography of the polymer films deposited on the ceramic support at different polymer concentrations (A untreated ceramic;
B 3wt%, C 13, and D 20wt%).
K. Briceño, D. Montané, R. Garcia-Valls, A. Iulianelli, A. Basile, Fabrication variables affecting the structure and properties of supported carbon molecular sieve membranes for hydrogen separation, Journal of Membrane Science, 415-416 (2012) 288-297.
Adsorption–desorption isotherms for supported carbon membranes at different pyrolysis temperatures.

## Slide 31
Carbon membranes applied in MR: methanol steam reforming
K. Briceño, A. Iulianelli, D. Montané, R. Garcia-Valls, A. Basile, Carbon molecular sieve membranes supported on non-modified ceramic tubes for hydrogen separation in membrane reactors, International Journal of Hydrogen Energy, 37 (2012) 13536-13544.
Ceramic support
Carbon layer (10-12 mm)
Methanol steam reforming
Methanol steam reforming
Critical issue: low H2 purity

## Slide 32
Future trends: MOC (Membrane on catalyst)
Configuration of the conventional MRF module and MOC module:
A: Conventional MRF module, B: MOC module.

## Slide 33
Pall Corporation
Hopkins & Zhao, NETL CO2 Capture Technology Meeting Pittsburgh / July 9 – 12, 2012
Conclusions
Composite Pd-based membranes: a reality
Power & Energy Inc. (USA)
H2 purity
from 97% to 99,9999999%
Up to 160 Nm3/h
of nominal flow capacity
www.powerandenergy.com

## Slide 34
Conclusions
Composite Pd-based membranes: a reality
Composite membranes solutions
HySep modules & ECN
H2 purity: from 99,5% to 99,995%
Palladium layer: from 3 to 9 mm
H2 purity ≥ 99,99%
NORAM Engineering & Constructors Ltd. (USA)
Palladium layer: < 20 mm

## Slide 35
AKNOWLEDGEMENTS
Separation Techniques Organization
Jessie Koch

## Slide 36
ITM-CNR
Institute on Membrane Technology
THANK YOU
FOR YOUR ATTENTION

## Slide 38
Permeation of hydrogen through composite Pd-based membranes
S. Yun, S. Ted Oyama / Journal of Membrane Science 375 (2011) 28–45

## Slide 39
ITM-CNR
Institute on Membrane Technology
A = Intermediate region; B = High H2 ideal selectivity and permeance; C = Low H2 ideal selectivity and permeance;
S. Yun, S. Ted Oyama / Journal of Membrane Science 375 (2011) 28–45

## Slide 40
ITM-CNR
Institute on Membrane Technology
Equations for hydrogen permeation through Pd-based membranes
[mol/m2s] Fick law: flux of hydrogen by diffusion through dense membranes
Diffusion coefficient
[mol/m2s] Fick law: flux of hydrogen by diffusion through dense membranes
Concentration gradient
Thickness of metal layer
Henry law: in case of surface reaction or mass transport is rate controlling step
Henry law substituted in Fick law
Permeance
Partial pressure of hydrogen in retentate (high) and permeate (low) sides
Sieverts law constant or solubility

## Slide 41
ITM-CNR
Institute on Membrane Technology
Equations for hydrogen permeation through Pd-based membranes
Concentration in Sieverts law substituted in Fick law
Knudsen law proportional to DpH2 = pH2,h – pH2,l
Membrane porosity
Pore diameter
Tortuosity
Molecular weight of diffusing gas
Viscous flow or Hagen-Pouiselle equation
Overal hydrogen permeating flux as a combination of bulk permeance through palladium and Knudsen and Hagen-Pouiselle mechanisms