## Slide 1: About OMICS Group
OMICS Group International is an amalgamation of Open Access publications and worldwide international science conferences and events. Established in the year 2007 with the sole aim of making the information on Sciences and technology ‘Open Access’, OMICS Group publishes 400 online open access scholarly journals in all aspects of Science, Engineering, Management and Technology journals. OMICS Group has been instrumental in taking the knowledge on Science & technology to the doorsteps of ordinary men and women. Research Scholars, Students, Libraries, Educational Institutions, Research centers and the industry are main stakeholders that benefitted greatly from this knowledge dissemination. OMICS Group also organizes 300 International conferences annually across the globe, where knowledge transfer takes place through debates, round table discussions, poster presentations, workshops, symposia and exhibitions.

## Slide 2: About OMICS Group Conferences
OMICS Group International is a pioneer and leading science event organizer, which publishes around 400 open access journals and conducts over 300 Medical, Clinical, Engineering, Life Sciences, Pharma scientific conferences all over the globe annually with the support of more than 1000 scientific associations and 30,000 editorial board members and 3.5 million followers to its credit.
OMICS Group has organized 500 conferences, workshops and national symposiums across the major cities including San Francisco, Las Vegas, San Antonio, Omaha, Orlando, Raleigh, Santa Clara, Chicago, Philadelphia, Baltimore, United Kingdom, Valencia, Dubai, Beijing, Hyderabad, Bengaluru and Mumbai.

## Slide 3
2015 September 01
Ahmet Serdar Önal
Beyçelik Gestamp Die and Automotive Parts Production Industry Company, Bursa, Türkiye
&
Necmettin Kaya
Mechanical Engineering Department / Uludağ University, Bursa, Türkiye
Crash behavior of telescopic crash box with aluminum foam

## Slide 4
1- Beyçelik Gestamp Introduction
2- Introduction
3- Finite Element Model
4- Results
5- References
6- Questions& Remarks
Presentation Headlines

## Slide 5
History
AUTOMOTIVE PLANT
60.000 m2
TOOLING PLANT &
R&D CENTER
10.000 m2
HOT STAMPING & G1 PLANTS
10.000 m2
ASSEMBLY PLANT
&
STEEL CENTER
22.500 m2
GEBZE CHASSIS PLANT
16.000 m2

## Slide 6
Customers & References

## Slide 7
Products
V36X – New Ford Transit
B460 – Ford Torneo Courier
V 408 – Ford Connect
BMW- F54
VOLVO- V526
X98 - Renault Clio IV(Cross-Car Beam)
TOFAŞ- B-SEDAN 356
M156 – Maserati Quattroporte
SKIN PANELS
CHASSIS GROUP
CRASH GROUP
REAR AXLE
ENGINE CROSS
MEMBER
INNER PANELS
FRONT RAIL
FRONT BUMPER
CROSS CAR BEAM
SPRING HANGER
CROSS MEMBER
SLIDING DOOR STEP
FRONT FLOOR CROSS MEMBER
SIDE RAIL CENTER
PILLARS
RINFORZA MONTANTE CENTRALE

## Slide 8
2. Introduction
Fig.1 . Frontal Impact
Thin-walled tubular structures behind the bumpers of vehicles protect passengers and the structure during the impact.

## Slide 9
2. Introduction
The bumper deforms first, then the following component deforms until the all energy is absorbed.
Fig. 2 Division of crash force transmission

## Slide 10
2. Introduction
Thin-walled structures absorb most of the crash energy with a progressive folding deformation.
Fig. 3 Under Body Crash Force Transmission

## Slide 11
2. Introduction
Crash Box is a the part which is usually advanced of the rails that should collapse at relatively low force to absorb energy in a controlled way [1].
Fig.4 . Shock Absorbers ( Crash Boxes)

## Slide 12
2. Introduction
In this study, aluminum foam effect of the crashworthiness behavior analyzed on the telescopic crash box geometry.
The geometric models were modeled with CATIA.
The post processing of the FEA models were prepared Hyper Mesh.
The crash simulations were performed with LS-DYNA.

## Slide 13
3. Finite Element Model
Fig.5 . Impact model and true stress-strain diagram of material
The behavior of the crash box has been studied by simulating the impact of a rigid barrier.

## Slide 14
3. Finite Element Model
Parameter | Abbreviation | Value | Unit
Rigid Barrier Velocity | v | 15600 | mm/s
Rigid Barrier Mass | m | 0,36 | t
Dynamic Friction Coefficient | FD | 0,1 | 
Static Friction Coefficient | FS | 0,1 | 
Table 1. Rigid Barrier Properties

## Slide 15
3. Finite Element Model
Parameter | Abbreviation | Value | Unit
Density | ρ | 7.85x10-9 | g/m3
Yield Stress | σak | 390 | MPa
Young’s Modulus | E | 210000 | MPa
Poisson’s Ratio | Nu | 0.3 | 
Thickness | t | 1.5 | mm
Table 2. DP600 Properties

## Slide 16
3. Finite Element Model
Parameter | Abbreviation | Value | Unit
Density | ρ | 1.11x10-9 | g/m3
Young’s Modulus | E | 1100 | MPa
Poisson’s Ratio | Nu | 0.0 | 
Yield Stress | SIGP | 0.777 | 
Table 3. Al-Foam Properties

## Slide 17
3. Finite Element Model
Fig.5. Undeformed, deformation characteristics and section view for empty telescopic crash box (deformed time=10 ms)

## Slide 18
3. Finite Element Model
Fig.5. Undeformed, deformation characteristics and section view for aluminum foam filled crash box (deformed time=10 ms)

## Slide 19
4. Results
Fig.11. Comparison of Kinetic Energy for with and without aluminum foam

## Slide 20
In order to maximize the absorbed energy, new telescopic box geometry with aluminum foam-filled is analyzed.
It is revealed that aluminum foam filled crash box energy absorption capability is % 47 higher than the empty one.
Profile | Total Absorbed Energy | Unit
Empty Crash Box | 8,81 | kJ
Aluminum Foam Filled Crash Box | 13,57 | kJ
4. Results
Table 4. Total Absorbed Energies

## Slide 21
Fig.10. Comparison of Reaction Force for with and without aluminum foam
4. Results

## Slide 22
The initial reaction force of the aluminum foam filled telescopic crash box profile %34 higher than the empty telescopic crash box profile.
4. Results
Profile | Initial Reaction Force | Unit
Empty Crash Box | 183 | kN
Aluminum Foam Filled Crash Box | 245 | kN
Table 4. Initial Reaction Forces

## Slide 23
Numerical simulation’s show that in terms of achieving maximum energy absorption, telescopic crash geometry and filling the box with aluminum foam can be preferable to thickening the box wall.
4. Results

## Slide 24
7. References
OptiBody,2007. Guidelines on optimal architectures for crashworthiness and compability improvement. WP3 report, Fp7 26622.
Optimisation of Collector Form and Response, http://www.engineering.lancs.ac.uk/lureg/group_research/wave_energy_research/Collector_Shape_Design.php, Access Date: 24.04.2015.
Kaya, N. and Öztürk F., Multi-objective crashworthiness design optimisation of thin-walled tubes, International Journal of Vehicle Design, Vol. 52, Nos. 1/2/3/4, 2010, pp.54-63.
Shen, Z., Qiao, X., Chen, H.,2012. BIW Safety Performance Research Based on Vehicle Frontal Crash, Proceedings of the FISITA 2012 World Automotive Congress, Beijing, China.

## Slide 25
Thanks for your attention …
Steel is not Cold for Us!!!
8. Questions & Remarks