## Slide 1: Characterisation of spent sulfite liquor and its valorisation using Aspen Plus® simulation software
Alberto Coz1, Carlos Arce1, Ana I Portilla1, Cristina Rueda1, Gema Ruiz1, Juan M. Romero-García2, Eulogio Castro2
1Green Engineering and Resources research group www.geruc.es, University of Cantabria, 39005, Spain
2Department of Chemical, Environmental and Materials Engineering, Universidad de Jaén, 23071, Spain
World Bioenergy Congress and Expo, Rome, June 13-14, 2016
conferenceseries.com

## Slide 2
Contents:
Introduction
Objective
Methods
Results
Conclusions
World Bioenergy Congress and Expo, Rome, June 13-14, 2016
conferenceseries.com

## Slide 3
Biorefinery
Biomass
Oil
Fuels
Refinery
Biorefinery
Products
Biofuels
Other (bio) products
Biorefinery
Energetic crops
Lignocellulosic waste
Biomass
Pre-treatment
Fermentation
Product purification
Detoxification
Final
products
World Bioenergy Congress and Expo, Rome, June 13-14, 2016
conferenceseries.com
Notes: 3

## Slide 4
TRADITIONAL PULP AND PAPER MILL
BIOREFINERY PULP AND PAPER MILL
Wood
Fuel
Cellulose
Spent liquor (waste material)
Pulp
Wood
Fuel
Cellulose
Liquor
Pulp
Biorefinery
Biofuels
Power
Bioproducts
Woody
biomass
Pulping process
Fermentation
Purification
Detoxification
Products
Biorefinery in pulp and paper mills
World Bioenergy Congress and Expo, Rome, June 13-14, 2016
conferenceseries.com

## Slide 5
Woody
biomass
Pulping process
Fermentation
Purification
Detoxification
Biorefinery in pulp and paper mills
World Bioenergy Congress and Expo, Rome, June 13-14, 2016
conferenceseries.com
Products
Pulping | Feedstock | Cooking Conditions | Yields (%) | Grade | Pulp properties
Refiner mechanical, RMP(Mechanical) | Softwood | No cooking ramp, chemicals or pretreatment is needed | 85-95 | corrugated paper | -
Thermomechanical, TMP(Mechanical) | Softwood | Heating ramp 1-10 min to 110-140 ºC; no chemicals or pretreatment is used | 93-95 | corrugated paper | -
Organosolv (Chemical) | Softwood and hardwood | 40-60 % ethylenglycol at 180-200 ºC for 30 to 90 min | 31-40 | paper | kappa: 25.5-27.5; α-cellulose: 21.2-33.7 %
Kraft (Chemical) | Softwood and hardwood | White liquor containing NaOH and Na2S; pre-heating ramp: 85 min up to 80 ºC; cooking temperature 165-170 ºC; dwell time: 95-180 min; 4:1 liquor-to-wood ratio | 40-47 | paper | brightness 28.9 %; kappa 26.8 1000-1100 mL/g
Prehydrolysis kraft (Chemical) | Softwood and hardwood | Cooking with steam prehydrolysis: prehydrolysis at 150-170 ºC, 45-90 min; pH after hydrolysis 3.3-3.7; Total time: 300-350 min | 35-39 | dissolving | brightness 26.2-44.4 %; kappa 20.7-7.8; 1024-1211 mL/g
Acid sulphite (Chemical) | Softwood and hardwood | pH: 1.2-1.5, 80 % free SO2-20 % bound SO2, bases of Ca, Mg, Na or NH3 can be used; pre-heated liquor: 70-80 ºC; dwell temperature 130ºC-145 ºC; pressure: 5,5-7 bar; 7 hours; liquor-to-wood ratio 4:1 | 35 -51 | dissolving | brightness 48.4-57.4 %; kappa: 5-7; 680-760 mL/g; alpha-cellulose > 88%

## Slide 6
Woody
biomass
Pulping process
Fermentation
Purification
Detoxification
Products
Biorefinery in pulp and paper mills
World Bioenergy Congress and Expo, Rome, June 13-14, 2016
conferenceseries.com
Hemicellulose
Furfural
5-Hydroxymethylfurfural
Acids
Phenolics
Lignosulphonates
Lignin
Hydroxymethylfurfural
Cellulose
Tanins, Terpenes
Resins
Heavy metals
Others
Physico-chemical: Liquid-liquid extraction
Adsorption (activated carbon, ion exchange resin…)
Membrane operations.
Thermal: Evaporation
Biological: Enzymatic processes

## Slide 7
Woody
biomass
Pulping process
Fermentation
Purification
Detoxification
Products
Biorefinery in pulp and paper mills
World Bioenergy Congress and Expo, Rome, June 13-14, 2016
conferenceseries.com
Influence of the sugar compound (C6 → C5)
Metabolism paths
Products:
- Biofuels: ethanol, butanol
- Hydrogen
- Xylitol
- etc.
C6H12O6 → 2 C2H5OH + 2 CO2
Use of microorganisms as bacteria, fungi to produce useful products

## Slide 8
Woody
biomass
Pulping process
Fermentation
Purification
Detoxification
Products
Biorefinery in pulp and paper mills
World Bioenergy Congress and Expo, Rome, June 13-14, 2016
conferenceseries.com
Equilibrium Separations: distillation, liquid-liquid extraction, supercritical fluid extraction.
Affinity-Based Separations: adsorption, ion exchange, simulated moving bed technologies.
Membrane Based Separations: microfiltration, ultrafiltration and diafiltration, nanofiltration, membrane pervaporation, and membrane distillation.
Solid-liquid Separations: conventional filtration and solid-liquid extraction.
Hybrid/Integrated Reaction-Separation Systems: membrane bioreactors, extractive fermentation, reactive distillation, reactive absorption.
Product(s)

## Slide 9
Woody
biomass
Pulping process
Fermentation
Purification
Detoxification
Products
Biorefinery in pulp and paper mills
World Bioenergy Congress and Expo, Rome, June 13-14, 2016
conferenceseries.com
Mathematical modelling (simulation of the process)
Initial composition of the streams
Thermodynamic characteristics
Mathematical equations per unit operation
Input parameters from experimental
Reactions involved
Unit operations
Simulation of the entire process
Software: Aspen Plus®

## Slide 10
Contents:
Introduction
Objective
Methods
Results
Conclusions
World Bioenergy Congress and Expo, Rome, June 13-14, 2016
conferenceseries.com

## Slide 11
Objectives
World Bioenergy Congress and Expo, Rome, June 13-14, 2016
conferenceseries.com
Characterisation of a spent sulphite liquor
Bibliographical analysis to conclude with the best alternatives of valorisation
Simulate the best alternatives by Aspen Plus®
TRADITIONAL SULPHITE PULP MILL
BIOREFINERY
Wood
Fuel
Cellulose
Spent liquor (waste material)
Dissolving Pulp
Wood
Fuel
Cellulose
Liquor
Dissolving Pulp
Biorefinery
Alternatives

## Slide 12
Contents:
Introduction
Objective
Methods
Results
Conclusions
World Bioenergy Congress and Expo, Rome, June 13-14, 2016
conferenceseries.com

## Slide 13
Methods: characterisation
World Bioenergy Congress and Expo, Rome, June 13-14, 2016
conferenceseries.com
Chemical parameters | Technique
Lignosulphonates | UV-VIS
Phenolics (OH) | UV-VIS
Individual Sugar | HPLC
Other components and inhibitors | HPLC
Metals and other elements | ICP-MS
Physical properties | Norm
pH | SM 423
Density and viscosity | ASTM-D-1298 UNE-EN ISO 3104
Dry matter | SM 209C
Suspended solids | SM 209C
Ash | Tappi 211 and 423

## Slide 14
Methods: simulation
World Bioenergy Congress and Expo, Rome, June 13-14, 2016
conferenceseries.com
Aspen Plus is the market-leading chemical process optimisation software used by the bulk, fine, specialty, & biochemical industries, as well as the polymers industry for the design, operation, and optimisation of safe, profitable manufacturing facilities
Wood components defined by National Renewable Energy Laboratory (NREL) database
Other components defined by Aspen Plus® data bank.
Component ID | Type | Component name | Alias
GLUCOSE | Conventional | DEXTROSE | C6H12O6
XYLOSE | Conventional | XYLOSE | C5H10O5-D2
ARABINOS | Conventional | ARABINOSE | C5H10O5-D1
MANNOSE | Conventional | MANNOSE | C6H12O6-N5
GALACTOS | Conventional | D-GALACTOSE | C6H12O6-N2
FURFURAL | Conventional | FURFURAL | C5H4O2
HMF | Conventional | 5-HYDROXYMETHYLFURFURAL | C6H6O3-N5
NITROGEN | Conventional | NITROGEN | N2
OXYGEN | Conventional | OXYGEN | O2
CO2 | Conventional | CARBON-DIOXIDE | CO2
AMMONIA | Conventional | AMMONIA | H3N
WATER | Conventional | WATER | H2O
HAC | Conventional | ACETIC-ACID | C2H4O2-1
BIOMASS | Solid |  | 
METHANE | Conventional | METHANE | CH4
BIOPHB | Solid |  | 
PHB | Solid |  | 
ETHANOL | Conventional | ETHANOL | C2H6O-2
XYLITOL | Conventional |  | 
H2SO4 | Conventional | SULPHURIC-ACID | H2SO4

## Slide 15
Methods: simulation
World Bioenergy Congress and Expo, Rome, June 13-14, 2016
conferenceseries.com
Aspen Plus is the market-leading chemical process optimisation software used by the bulk, fine, specialty, & biochemical industries, as well as the polymers industry for the design, operation, and optimisation of safe, profitable manufacturing facilities
Simulations developed in Aspen Plus using laboratory scale data
Aspen module | Real module | Description
Flash2 | Flash, evaporator or other single-stage separator | Vapor-liquid or vapor-liquid-liquid equilibrium calculation
Heater | Heater, cooler, valves, pumps | Determines the thermal and phase condition of a mixture with one or more inlet streams
Mixer | Mixer | Combines material streams (or heat streams or work streams) into one stream
Rstoic | Reactor | Can model reaction occurring simultaneously or sequentially and perform product selectivity and heat of reaction calculations
Ryield | Reactor | Can model reactions by specifying reaction yields and the stoichiometry is either unknown or not important
Ssplit | Divider | Combines material streams and divides the resulting stream into two or more streams
Swasher | Solids washer | Recovers dissolved components from an entrained liquid of a solid stream
Wood components defined by National Renewable Energy Laboratory (NREL) database
Other components defined by Aspen Plus® data bank.

## Slide 16
Contents:
Introduction
Objective
Methods
Results
Conclusions
World Bioenergy Congress and Expo, Rome, June 13-14, 2016
conferenceseries.com

## Slide 17
Results: characterisation
Fresh liquor
Unbleached pulp
Spent liquor
DIGESTERS
Spent sulphite liquor
STORAGE TANKS
WASHING
3020-VG
3040-VG
Dissolving pulp
BLEACHING
DRYING
WASHING
BLEACHING
BLEACHING
Wood chips
World Bioenergy Congress and Expo, Rome, June 13-14, 2016
conferenceseries.com

## Slide 18
World Bioenergy Congress and Expo, Rome, June 13-14, 2016
conferenceseries.com
Physical properties | Value
pH | 1.81 ± 0.01
Density | 1067 g/L
Viscosity | 1.87 ± 0.02 cP
Dry matter | 15.10 ± 0.69
Ash 500ºC Ash 900ºC | 1.85 ± 0.07 % 1.12 ± 0.06 %
Results: characterisation
Inhibitors from lignin | Value
Lignosulphonates | 52.80 ± 1.01 d.m. %
Phenolics (OH) | 0.18 ± 0.02 d.m. %
Sugars | Value
Cellobiose | 10.86 g/L
Glucose | 6.37 g/L
Arabinose | 0.97 g/L
Xylose | 27.14 g/L
Mannose | 0.95 g/L
Galactose | 1.18 g/L
Total sugar content | 47.47 g/L
Inhibitors from cellulose and hemicellulose | Value
Acetic acid | 10.19 g/L
Formic acid | 1.26 g/L
Levulinic acid | 0.06 g/L
Methanol | 0.17 g/L
Ethanol | 0.05 g/L
Furfural | 0.55 g/L
HMF | 0.01 g/L

## Slide 19
World Bioenergy Congress and Expo, Rome, June 13-14, 2016
conferenceseries.com
Physical properties | Value
pH | 1.81 ± 0.01
Density | 1067 g/L
Viscosity | 1.87 ± 0.02 cP
Dry matter | 15.10 ± 0.69
Ash 500ºC Ash 900ºC | 1.85 ± 0.07 % 1.12 ± 0.06 %
Results: characterisation
Inhibitors from lignin | Value
Lignosulphonates | 52.80 ± 1.01 d.m. %
Phenolics (OH) | 0.18 ± 0.02 d.m. %
Sugars | Value
Cellobiose | 10.86 g/L
Glucose | 6.37 g/L
Arabinose | 0.97 g/L
Xylose | 27.14 g/L
Mannose | 0.95 g/L
Galactose | 1.18 g/L
Total sugar content | 47.47 g/L
Inhibitors from cellulose and hemicellulose | Value
Acetic acid | 10.19 g/L
Formic acid | 1.26 g/L
Levulinic acid | 0.06 g/L
Methanol | 0.17 g/L
Ethanol | 0.05 g/L
Furfural | 0.55 g/L
HMF | 0.01 g/L
6.3 %
29.5 %

## Slide 20
World Bioenergy Congress and Expo, Rome, June 13-14, 2016
conferenceseries.com
Element | Value
Na | 189 mg/L
Mg | 5290 mg/L
Al | 4.19 mg/L
Si | 6.2 mg/L
K | 355 mg/L
Ca | 504 mg/L
Mn | 48.6 mg/L
Fe | 26.8 mg/L
Ba | 0.175 mg/L
Sr | 3.35 mg/L
Results: characterisation
Element | Value
Cr | 111 μg/L
Co | 56.2 μg/L
Ni | 485 μg/L
Cu | 75.4 μg/L
Zn | 2720 μg/L
Pb | 16.4 μg/L
As | 40.4 μg/L
Mo | 9.6 μg/L
V | 38.3 μg/L
Sb | 3.93 μg/L
Se | 13 μg/L

## Slide 21
Product | Process | Application | References
Lignosulphonates | Using lignosulphonates directly | Auxiliary substance / additive | Chakrabarty et al. (2009), Restolho et al., (2009), Ringena et al. (2005)
Ethanol | Xylose/glucose/arabinose fermentation | Alternative fuel | Xavier et al. (2010), Panagiotopoulos et al. (2009), Martín et al. (2002), Sanchez and Cardona (2008), Keating et al. (2006)
PHBs | Glucose/xylose/arabinose fermentation | Synthetic polymers | Fernandes (2010); Schreiner (2009), Mumtaz et al. (2010), Vlysidis et al. (2013)
Xylitol | Xylose catalytic hidrogenation Xylose fermentation | Sugar substitute for diabetics | Nair and Zhao (2010); Fouad (2010), Saha (2003), Lai and Bura (2012)
Furfural | Dehydration of 5C sugars | Raw material in other chemical processes | Zeitsch (2000), Mamman et al. (2008)
Spent sulfite liquor
Unbleached pulp
̴ 52% Lignosulphonates
̴ 30% Sugars
World Bioenergy Congress and Expo, Rome, June 13-14, 2016
conferenceseries.com
Results: biorefinery alternatives

## Slide 22
Wood
Fresh liquor
Pulp
Spent liquor
3020-VG
3040-VG
Dissolving pulp
DRYING
WASHING
STORAGE TanKs
Lignosulphonates
EvaporaTORS
Others
WASHING
BLEACHING
DigesteRs
Detoxification/purification
CONVERSION
Ethanol
PHBs
Furfural
Xylitol
SEPARATION
Sugar
Existing process
New implementation
BLEACHING
BLEACHING
World Bioenergy Congress and Expo, Rome, June 13-14, 2016
conferenceseries.com

## Slide 23
Woody
biomass
Pulping process
Fermentation
Purification
Detoxification
Ethanol
Xylitol
Furfural
PHBs
World Bioenergy Congress and Expo, Rome, June 13-14, 2016
conferenceseries.com
Results: biorefinery alternatives
Physico-chemical: Liquid-liquid extraction
Adsorption (activated carbon, ion exchange resin)
Membrane operations.
Thermal: Evaporation
Biological: Enzymatic processes
Detoxification
Anionic resins with or without overliming in the case of ethanol, xylitol and furfural
With no detoxification step in the case of PHBs

## Slide 24
Aspen tech®: bioethanol
Woody
biomass
Pulping process
Fermentation
Purification
Detoxification
Ethanol
Xylitol
Furfural
PHBs
World Bioenergy Congress and Expo, Rome, June 13-14, 2016
conferenceseries.com
Results: biorefinery alternatives

## Slide 25
Aspen tech®: PHBs
Woody
biomass
Pulping process
Fermentation
Purification
Detoxification
Ethanol
Xylitol
Furfural
PHBs
World Bioenergy Congress and Expo, Rome, June 13-14, 2016
conferenceseries.com
Results: biorefinery alternatives

## Slide 26
Aspen tech®: xylitol
Woody
biomass
Pulping process
Fermentation
Purification
Detoxification
Ethanol
Xylitol
Furfural
PHBs
World Bioenergy Congress and Expo, Rome, June 13-14, 2016
conferenceseries.com
Results: biorefinery alternatives

## Slide 27
Aspen tech®: furfural
Woody
biomass
Pulping process
Conversion
Purification
Detoxification
Ethanol
Xylitol
Furfural
PHBs
World Bioenergy Congress and Expo, Rome, June 13-14, 2016
conferenceseries.com
Results: biorefinery alternatives

## Slide 28
World Bioenergy Congress and Expo, Rome, June 13-14, 2016
conferenceseries.com
Results: biorefinery alternatives
With detoxification techniques  Anionic Resins and Overliming
Chart: Spent sulphite liquor (ton/h)
| 10 | 20 | 50 | 90
Ethanol | 0.0848 | 0.1696 | 0.424 | 0.6383
Xylitol | 0.0091 | 0.0915 | 0.4575 | 0.7319 | 0.9149
Furfural | 0.0106 | 0.1059 | 0.5293 | 0.847 | 1.0587

## Slide 29
World Bioenergy Congress and Expo, Rome, June 13-14, 2016
conferenceseries.com
Results: biorefinery alternatives
Without detoxification techniques
Chart: Spent sulphite liquor (ton/h)
| 0.5 | 2 | 10 | 50 | 80
PHBs | 0.064 | 0.074 | 0.128 | 0.396 | 0.598

## Slide 30
Contents:
Introduction
Objective
Methods
Results
Conclusions
World Bioenergy Congress and Expo, Rome, June 13-14, 2016
conferenceseries.com

## Slide 31
World Bioenergy Congress and Expo, Rome, June 13-14, 2016
conferenceseries.com
Different detoxification methods were assessed in order to recover the maximum quantity of sugars for further biorefinery processes
- The best results were obtained using overliming and anionic resins since the highest quantity of sugars as well as the minor inhibitors are recovered. However, overliming does not remove lignosulphonates properly.
Three different processes have been evaluated in order to transform the sugars into value added products: furfural, xylitol and ethanol.
- PHBs and Xylitol are recommended as future alternatives of biorefinery
Characterisation and valorisation options of a waste material from sulphite pulping was carried out.
- Due to the composition, lignosulphonates (about 52%) and xylitol, ethanol, furfural and PHBs from sugars (about 30%) were selected.
Conclusions

## Slide 32
Thank you for your attention
Alberto Coz
University of Cantabria
coza@unican.es
Financial support for this research by KBBE-2012-6-311935 research project.
www.brigit-project.eu
World Bioenergy Congress and Expo, Rome, June 13-14, 2016
conferenceseries.com
Notes: 32