## Slide 1: Silica-Based Matrixes for Drug Delivery: Ready for a Prime Time?
Dr. Alex Nivorozhkin
Neo-Advent Technologies LLC, USA

## Slide 2: Traditional Uses of Amorphous Silica in Pharma
Non-Porous | Particle Size | Applications | Function
Spherical | 5-50 microns | Tablets | Flow, Anticaking
Fumed (Branched) | 0.1-1 microns | Gels, Semisolids | Viscosity Modifier
Porous | Particle Size | Applications | Function
Spherical | 5-50 nm | Tablets | Filler, Oil/Wax Absorbing
Silicagel | 5-50 microns | Dessication | Moisture Absorbing
Three Different Physical Attributes:
-Shape/Size/ Porosity

## Slide 3: Fumed Silica – Viscosity Modifier

## Slide 4
Key Pathways to Producing the Silica
Silicagel, Precipitated Silica
Na2Si3O7 + H2SO4 → 3 SiO2 + Na2SO4 + H2O
(different pH ranges, the product dehydrated )
Sol-Gel process
Si(OEt)4→ SiO2 (basic or acid hydrolysis)
Mesoporous Silica (MSN, Pore Size 2-50 nm)
Si(OEt)4→ SiO2 in the presence of templating surfactant

## Slide 5: Toxicology of Silica
Plenty in nature (structural material), but not in humans
When used orally up to 5 g/kg is safe
SNP are more toxic
  Toxicity depends on size, charge, shape
  Role of increased solubility with decreased size?
  Lack of good in vitro-in vivo correlations

## Slide 6: Solubility of Silica
Amorphous
pH-dependent, increase at pH>9
Equilibrium solubility of Nonporous silica -70 ppm vs. Porous -120 ppm
Si(OH)4 is excreted with urine
at 1.8 mg/day
Crystalline Forms
Soluble thru conversion to Si(OH)4
Insoluble at ambient conditions
1 ppm at 400 oC
Very stable

## Slide 7: Mesoporous Silica Nanomaterials (MSN)
Key Properties of MSN
Ordered pore structure (2-50 nm)
Huge pore surface/volume
(1 cm3/g, 1000 m2/g)
Commercial Availability
MCM-41 (Aldrich $563/25 g)
Preparation of MSN
Liquid Crystalline Templating
(“Mobil Process”, 1992)
Variations in surfactant, inorganic framework, conditions

## Slide 8: SNP Surface Reactivity
Covalent Attachment Options
Negative Zeta-potential for unmodified SNP
Protonated amino groups after modification with 3-aminopropyl triethoxysilane
Drug-SNP Conjugates
Convenient general chemistry
Can it match potential for Polymer-Drug conjugates?
Can it be produced economically: concentration limits, washout steps, density of conjugation?

## Slide 9: Surface Functionalization
Co-condensation (one-pot)
Versatile post-process method
Possible pore clogging
Grafting Method
More homogeneous Distribution
Maybe difficult to fit into the prep

## Slide 10: Drug Delivery Modalities

## Slide 11: MSN-based Drug Delivery Vehicle
Challenges
Hydrophilic surface (-Si-OH), low loading of hydrophobic drugs (many cancer, CNS leads) ca. 1%
Hydrophobic surface modification results in sluggish and incomplete release
Filling the pores with surfactant improves loading and release
Pore-loading with Capping

## Slide 12: MSN as Multifunctional Nanoplatform
Functionalization Domains:
Silica framework
Mesopores
Outermost surface
of nanoparticles
Combination approach

## Slide 13: MSN Nanomotor for DNA Capture
M. Vallet-Regi, Small, 2012

## Slide 14: What the Future Holds?
Potential
Possibly low toxic
May be cheap
Versatile and compatible with various chemistries
Could be commercially as successful as liposomes?
New Development Products
Poorly soluble potent drugs (complement to non-MSN)
Imaging
Targeted delivery
Delivery of biologics (little explored)
Stimuli-triggered delivery
Challenges
Toxicity, particularly long-term
Manufacturing
Low drug loads
“Smart” approaches bring add-on issues, may be all of the above
Driving Forces
Solid industrial base
Advances in silica applications other than pharma, i.e. catalysis, ink, polymers
Need for new drug delivery technologies

## Slide 15: Thank You
Alex Nivorozhkin, Ph.D.
Founder, COO
Neo-Advent Technologies LLC, 410 Great Road, Littleton, MA 1-508-970-4858
www.neo-adventtec.com
Co-Chair
Formulation Drug Delivery
Committee, Massachusetts Biotechnology Council, Boston
Acknowledgements
Mr. Nelson Landrau
Dr. Ken Avery
Unilever, Port Sunlight, UK
Dr. Craig Jones
Dr. James Merrington
Dr. David Mealing