## Slide 1
Low cost fabrication of organic semiconductor monolayer via Organic Solid-Solid Wetting Deposition (OSWD): physico-chemical basics, controllability, process capability
11.08.2015
Alexander Eberle

## Slide 2: Outline
Solid-solid wetting
Organic solid-solid wetting deposition
The role of the dispersing agent
Possible prospective applications of OSWD

## Slide 3: Question
„What is solid-solid-wetting?“

## Slide 4: Solid-solid wetting
 | Active phase |  |  |  |  |  |  | 
Substrate | CrOx | MnOx | VOx | WOx | NbOx | TaOx | MoOx | ZrOx
Anatas | X | X | X | X | X | X | X | X
Al2O3 | X | X | X |  | X | X |  | X
SiO2 |  |  |  |  | X | X |  | 
Published 1985 (J. Haber) / 1988 (H. Knözinger)
Assembly of monolayers after heating up > 450 °C
No surface- or gas-phase-diffusion, no chemical reactions
Slope in the surface free energy, like a waterdrop wetting a surface
F. Bertinchamps, C. Grégoire, E. M. Gaigneaux: „Systematic investigation of supported transition metal oxide based formulations for the catalytic oxidative elimination of (chloro)-aromatics; Applied Catalysis B: Environmental 2006

## Slide 5: Advancement
Organic solid-solid wetting deposition
F. Trixler, T. Markert, M. Lackinger, F. Jamitzky, W.M. Heckl: „Supramolecular self-assembly initiated by solid-solid wetting“; Chemistry – a European Journal 2007, 13, 7785-7790

## Slide 6: γ-Quinacridone
SEM picture of γQAC Nanocrystals
3D structure of γQAC nanocrystals
Nanocrystals built up by hydrogen-bonds
γ Quinacridone

## Slide 7: OSWD
STM-picture:
8CB & γ-Quinacridone
2D-Model: γQAC on HOPG
γQAC: STM & DFT

## Slide 8: Advantages of OSWD
Ambient conditions
Organic semiconductors
No need for solubility
Domain growth, size & structure can be directed & engineered

## Slide 9: Question
„Does the dispersing agent affect the coverage and structure of the QAC arrays?“

## Slide 10: Class 1: Good OSWD
Propylene carbonate + γQAC
Water + γQAC + KOH (pH 8)

## Slide 11: Class 2: Medium OSWD
Ethylbenzene + γQAC
Water + γQAC

## Slide 12: Class 3: No OSWD
Dimethyl sulfoxide+ γQAC
Dodecane + γQAC

## Slide 13: Summary
The dispersing agent directs the monolayer properties
The chemical structure of the dispersing agent does hardly affect the OSWD
Neither do the physical properties viscosity, vapor pressure, surface tension, permittivity

## Slide 14: Question
„What parameter directs the surface coverage rate?“

## Slide 15
The monolayer coverage fits to the zeta potential (z33)

## Slide 16: Question
„How might solid-solid wetting work under ambient conditions?“

## Slide 17: Functional principle of the dispersing agent
Due to the solvation in the dispersing agent the nanocrystals gain a zeta potential
The zetapotential changes the surface free energy, hence the interfacial tension
If adhesion > cohesion, then the molecule mobility enables self-assembly
dispersion  physisorption  monolayer

## Slide 18: Question
„What might be possible prospective applications of OSWD?“

## Slide 19: Outlook band gap engineering
Graphene / PTCDI
Left: Positions to each other
Right: band gap structure
H. Medina, Y.-C. Lin, D. Obergfell, P.-W. Chiu: „Tuning of charge densities in graphene by molecule doping“; Advanced Functional Materials 2011
Band gap depends on chemical- and domain structure of the semiconductor  engineering possible

## Slide 20: Outlook Van der Waals heterostructures
A. K. Geim, I. V. Grigorieva: „Van der waals heterostructures”; Nature 2013
Assembly of Van der Waals heterostructures imaginable

## Slide 21: Double structures
Water + Disodium phosphate – γQAC
Propylene carbonate – γQAC
Double structures can already be assembled

## Slide 22: Take home message
OSWD offers the possibility for cheap a large-scale production of directable and engineerable monomolecular semiconductor layers with an huge spectrum of possible organic semiconductors, substrates and application possibilities

## Slide 23: Acknowledgement
Frank Trixler
Michaela Wenner
Volker Diete-Wendl
Klaus Macknapp
Martina Zeiler (PTS)
Veronika Schömig (TUM)

## Slide 24: Directed domain growth voltage pulse
Aceton – γQAC
Aceton – γQAC
pulse 4,96 V

## Slide 25: Nanomanipulation
CD - structures
Manipulated structures in PTCDA domain
Possible way to build up nano-circuits

## Slide 26: Directed domain growth Electric field
H2O + NaCl + γQAC
1 Scans, change in scan direction, another 2 scans

## Slide 27: Directed domain growth Mechanical pressure
8CB – γQAC
before comminute
8CB – γQAC
after comminute

## Slide 28: Directed growth Locally induced co-adsorption
QAC
PTCDA
Two domains of different pigments at the same time

## Slide 29: Directed domain growth dispersing agent
Additional
8CB
Olic acid
homogeneous Flavanthrone domains
8CB
Flavanthrone in double series structure

## Slide 30: Directed domain growth Mechanical pressure
γQAC without liquid phase
After comminute

## Slide 31: Richtungsänderung der Domänen
Molekül-Ketten-Stabilität vs. Auslenkung mittels STM-Spitze
Die Bindungsenergie der Molekülkette ist richtungsabhängig

## Slide 32
Pure γQAC, heated up to 240 °C on graphit substrate

## Slide 33: OSWD: Applicability
OSWD: So far observed with 14 pigments and 18 different dispersing agents on 4 substrates
Pigments | Dispersing agents | Substrates
γ-Quinacridone (γQAC) | 6CB (4´-Hexyl-4-biphenylcarbonitril) | Graphite
β-Quinacridone | 7CB (4´-Heptyl-4-biphenyl-carbonitril) | Graphene
Dimethyl-Quinacridone | 8CB (4´-N-Octylbiphenyl-4-carbonitril) | Carbon Nanotubes
Dichloro-Quinacridone | Oelic acid | MoS2
Quinacridone-Chinon | Vitamin K1 | 
Alizarin-Komplex | Alkyd resin | 
Acridone | Ethyl acetate | 
Perinone | Diethylene glycol | 
Flavanthrone | 2-Propanol | 
Indanthrone | Acetone | 
Me-PTCDI | Glycerol | 
PTCDA | Propylene carbonate | 
Phthalocyanine Pentacene | Water Ethylbenzene Propane-1,2-diol Anisole Dimethyl sulfoxide 3-Methyl-1-Butanol | 
During my Ph.D.

## Slide 34
The Zeta potential is related to a distribution

## Slide 35
Unterschied Z50 – Z33

## Slide 38: Force field calculation
Theory proof:
Acridone / QAC / PTCDA: adhesion > cohesion
Indigotin: no OSWD
Dreiding force field

## Slide 39: Liquid p. d. vs. solid-solid w.
8CB – Phthalocyanin
Monolayer
liquid phase deposition
8CB – γQAC
Domains
solid-solid wetting

## Slide 44: Directed growth Dispersing agents
10 µm
8 CB
Vitamin K1
Oelic acid
Different dispersing agents offer different manufacturing techniques
E.g.: dip-pen (OSWD confirmed via STM)