## Slide 1: About OMICS Group
OMICS Group International is an amalgamation of Open Access publications and worldwide international science conferences and events. Established in the year 2007 with the sole aim of making the information on Sciences and technology ‘Open Access’, OMICS Group publishes 400 online open access scholarly journals in all aspects of Science, Engineering, Management and Technology journals. OMICS Group has been instrumental in taking the knowledge on Science & technology to the doorsteps of ordinary men and women. Research Scholars, Students, Libraries, Educational Institutions, Research centers and the industry are main stakeholders that benefitted greatly from this knowledge dissemination. OMICS Group also organizes 300 International conferences annually across the globe, where knowledge transfer takes place through debates, round table discussions, poster presentations, workshops, symposia and exhibitions.

## Slide 2: About OMICS Group Conferences
OMICS Group International is a pioneer and leading science event organizer, which publishes around 400 open access journals and conducts over 300 Medical, Clinical, Engineering, Life Sciences, Phrama scientific conferences all over the globe annually with the support of more than 1000 scientific associations and 30,000 editorial board members and 3.5 million followers to its credit.
OMICS Group has organized 500 conferences, workshops and national symposiums across the major cities including San Francisco, Las Vegas, San Antonio, Omaha, Orlando, Raleigh, Santa Clara, Chicago, Philadelphia, Baltimore, United Kingdom, Valencia, Dubai, Beijing, Hyderabad, Bengaluru and Mumbai.

## Slide 3: Atomically-resolved imaging of surfaces of complex oxide thin films grown by laser-MBE
Alexander Tselev
Oak Ridge National Laboratory,
Oak Ridge, TN, USA

## Slide 4: What complex oxides offer
Superconductivity
Colossal magnetoresistance
Ferromagnetism (spintronics)
Ferroelectricity
Multiferroism
Metal-insulator transitions
Tunability by strain
Memristive bahavior
Can be integrated with existing Si-based technologies
Use in electrochemical energy storage and conversion systems
Notes: Introduction. Symmetry breaking at interfaces between dissimilar materials is at the origin of many unique properties associated with complex oxides. With decreasing thickness, properties of ultrathin films are more and more determined by both surface and interface with the substrate. Functionality of many complex oxide materials even in bulk (e.g., those used in electrochemical systems) strongly depends on properties of the surface. Therefore, understanding and control of properties and interfaces is a key challenge in the complex oxide material science and physics.
SrRuO3 is a complex oxide, metallic itinerant ferromagnet. It possesses a number of important physical properties, some of which are not fully understood, one example being thickness-dependent metal-to-insulator transition. On the other hand, SrRuO3 is widely used as a bottom electrode material in devices based on perovskite-related oxides, such as ferroelectric non-volatile random access memory arrays. With demand for shrinking device size and, consequently, reduced ferroelectric film thickness, more nanoscale and atomic-level information is needed about SrRuO3 surface properties to control interface of SrRuO3 with layers on top of it and to correctly understand its influence on properties of devices and structures.
Thus far, there are no published successful attempts to image surface of SrRuO3 with atomic resolution, except one recent work (J. Shin, et al., ACS Nano, 4, 4190 (2010)). Here, we report in situ STM imaging of PLD-grown SrRuO3 thin films. The film growth conditions are nearly identical to those used for growth of bottom electrodes. Depending on slightly varying preparation conditions, we observe different structures on the surfaces of as-grown SrRuO3 films.

## Slide 5: Perovskite structure
ABO3
SrTiO3
BO2
AO

## Slide 6: Epitaxial film growth
BO2
B-terminated single-crystalline substrate
Atomic force microscopy image
LaMnO3
SrTiO3
substrate
Growth at:
elevated substrate temperatures
650-850 °C &
in oxygen atmosphere 1-300 mTorr

## Slide 7: Pulsed Laser Deposition
The schematic is from: M. Opel,
J. Phys. D 45, 033001 (2012)
Adv. Mat. cover Dec 2012, connected to a paper from an ORNL group
Reflective High-Energy Electron diffraction

## Slide 8: Scanning tunneling microscopy
STM tip
A
+
-
last atom
e-
Atomic resolution is generally very difficult to achieve on PLD-grown films

## Slide 9: NanoTransport system at CNMS
RHEED gun
growth
chamber
SPM
chamber
Growth
chamber
Excimer laser
transfer
chamber
analysis
chamber
http://www.cnms.ornl.gov
STM
AFM
in
UHV

## Slide 10: SrRuO3
Widely used as a metal electrode

## Slide 11: Samples
Chart: 
| sample #3 | sample #2 | sample #1
Series 1 | 12 | 8.25 | 12
Series 2 | 22.5 | 22.5 | 0
Series 3 | 0 | 0 | 0
9nm / 23u.c.
7.5nm / 15 u.c.
9nm / 23u.c.
15 min. anneal
15 min. anneal
T = 690 °C
T = 650 °C
PO2 = 100 mTorr
PLD
Undoped SrTiO3 (100) substrates / TiO2 termination
In-situ RHEED
Transfer to the STM chamber right after film growth

## Slide 12: Film growth
Growth modes:
690 °C – step-flow
650°C – step-flow/island-formation
RMS Roughness = 55 pm
RHEED
Substrate selection:
RMS roughness < 70 pm
AMF topography
1 μm  1 μm

## Slide 13: Film surface: larger scale
690 °C, no anneal
ex-situ AFM (topography)
in-situ STM
3 μm  3 μm

## Slide 14: Competing surface patterns
zigzag
rectangular
rectangular
690 °C,
no ann.

## Slide 15: Zigzag and rectangular patterns
690 °C, ann.
650 °C, ann.

## Slide 16: Zigzag and rectangular patterns
rectangular
zigzag

## Slide 17: In-situ UPS
#2:
rectangular
#1:
zigzag
O 2p
Ru 4d

## Slide 18: Surface spin-glass behavior
Isosurfaces of magnetization densities
Randomly oriented local spins from Oad p-orbitals
Isosurfaces of magnetization densities

## Slide 19: La5/8Ca3/8MnO3
Classical Colossal magnetoresistance material

## Slide 20: Evolution of surface morphology
Here are 103 periods of RHEED oscillations.
16 u.c.
25 u.c.
250 u.c.

## Slide 21: 16 u.c. on SrTiO3
Up to 7 u.c. layers can be seen.
Two terminations: ordered and disordered.
(√2 x √2)R45° reconstruction
Vt = -1.8 V, It = 40-90 pA, T = 297 K

## Slide 22: 25 u.c. on SrTiO3
Appear after anneals in oxygen (at 400 °C for 30 min.) as well as after fast cooling (150 °C/min.) to room temperature.
No significant change after anneals in vacuum at 450 ° C for 30 min.

## Slide 23: 250 u.c. on SrTiO3
Up to 3 u.c. layers can be seen.
One termination: disordered.
Nearly perfects layer-by-layer growth.
X-ray: film is coherently strained to STO.

## Slide 24: Interpretation of the growth evolution
K. Bromann et al., PRL 75, 677 (1995)
Dependence of the barrier for interlayer adatom transport (Ehrlich-Schwoebel barrier) on strain.
Tensile strain increases the barrier.
Ag-on-Pt (111) as an example
½ of oxygen atoms is visible on A-termination

## Slide 25: 25 u.c. on B-terminated NbGaO3 – single termination
NbGaO3 (110)
-0.13%
25 u.c.
One, disordered, termination

## Slide 26: Acknowledgement
Funding:
Division of Materials Sciences and Engineering, Office of Basic Energy Sciences, U.S. DOE
Division of Scientific User Facilities, U.S. DOE.
Sergei Kalinin
Art Baddorf
Zhen Gai
Mike Biegalski
Rama Vasudevan
P. Ganesh
Lian Qiao
Wolter Siemons

## Slide 27: Let Us Meet Again
We welcome you all to our future conferences of OMICS Group International
Please Visit: http://materialsscience.conferenceseries.com/
Contact us at
materialsscience.conference@omicsgroup.us
materialsscience@omicsgroup.com