## Slide 1: Ionic liquid based artificial cellulase type catalysts for cellulosic ethanol process
Ananda S. Amarasekara*, Onome S. Owereh, Preethi Shanbhag, Bernard Wiredu
Prairie View A&M University,
Texas, USA

## Slide 2: 1st and 2nd generation ethanol
1st generation – ethanol from starch/sugars
US – 13.9 BGY-1, 64% of world production (corn ethanol) Brazil – 5.6 BGY-1, 25% of world production (Sugar cane ethanol) (2015)
2nd generation – cellulosic ethanol from non-food
biomass
About 20 ~ 20 MGY-1 plants in US + EU, few in
operation, mostly under construction (2015-16)
_______________________________________________________________
BioEnergy 2016
June 13-14, 2016 Rome

## Slide 3: Ionic liquids & biomass processing
___________________________________________________________________
R.D. Rogers et al.
J. Am. Chem. Soc. 2002, 124, 4974
Z.K. Zhao et al.
Adv. Synth. Catal. 2007, 349, 1847
BioEnergy 2016
June 13-14, 2016 Rome

## Slide 4: Brönsted acidic ionic liquids
________________________________________________________________
BioEnergy 2016
June 13-14, 2016 Rome

## Slide 5: Cellulose dissolution in acidic ionic liquids
Neutral Ionic Liquid
80 °C, 3 h.
10% Cellulose ( DP ~ 450)
Acidic Ionic Liquid
23 °C, 2 min.
20% Cellulose ( DP ~ 450)
__________________________________________________________________
BioEnergy 2016
June 13-14, 2016 Rome

## Slide 6: Cellulose dissolution and hydrolysis in acidic ionic liquids
Dissolution of cellulose
Hydrolysis of cellulose
t = 0 s t = 60 s t = 150 s
Microscope images of rapid dissolution of cellulose in acidic
Ionic liquid, at room temperature and atmospheric pressure
Neat, 70 OC, 90 min. 62% TRS.
14% Glucose
A.S. Amarasekara et al. Ind. Eng. Chem. Res. 2009, 48, 10153
BioEnergy 2016
June 13-14, 2016 Rome

## Slide 7: Switch grass saccharification in acidic ionic liquids
Neat, 70 OC, 120 min. 58% TRS
15% Glucose
A.S. Amarasekara et al. BioEnerg. Res.
2013, 6, 719
_____________________________________________________
Temp. ( °C) /time (min.)
before after Yield (%)
Entry IL/switchgrass adding H2O adding H2O TRS glucose
_____________________________________________________
1 1a/PV1 70/60 70/60 56 10
2 1a/PV2 70/60 70/60 48 13
3 1a/PV3 70/60 70/60 47 11
4 1b/PV1 70/60 70/60 50 10
5 1b/PV2 70/60 70/60 45 14
6 1b/PV3 70/60 70/60 58 15
7 1b/PV3 70/60 70/30 46 6
1b/PV3 70/60 70/120 36 5
1b/PV3 70/60 70/240 32 5
_____________________________________________________
PV-1 = pre-boot stage,
PV-2 = anthesis or flowering,
PV-3 = post-frost after senescence
BioEnergy 2016
June 13-14, 2016 Rome

## Slide 8: Acidic ionic liquids as homogeneous catalysts in water
Hydrolysis of cellulose
BAIL, 170 OC, 3 h. 33 % TRS
H2SO4, 170 OC, 3 h. 21 % TRS
[H+] = 0.032 M
A.S. Amarasekara et al. Ind. Eng. Chem. Res. 2011, 50, 12276
Chart: TRS % vs Temperature
| 140 | 150 | 160 | 170 | 180 | 190
H2SO4 | 17.4 | 20.5 | 21.5 | 22 | 22.1 | 22.2
BAIL | 22.6 | 28.4 | 32.2 | 32.6 | 30.3 | 17.4
High pressure reactor
140-190 0C
0.36 -1.25 MPa
BioEnergy 2016
June 13-14, 2016 Rome

## Slide 9: Structure activity relationships (SAR) TRS % yield vs Temperature ______________________________________________________
cellulose (DP ~ 450) in 0.032 M [H+]
A.S. Amarasekara et al. Sustain. Energ. 2014, 2(3), 102
Chart: Temperature (0C)
| 150 | 160 | 170 | 180
1a | 15.863 | 31.365 | 25.396 | 18.667
1b | 14.997 | 34.356 | 28.248 | 21.731
2 | 9.285 | 20.026 | 19.35 | 13.768
3 | 12.884 | 30.459 | 24.635 | 20.217
4 | 7.881 | 18.067 | 17.56 | 14.725
5 | 13.902 | 29.587 | 24.452 | 18.095
6 | 11.908 | 28.304 | 20.436 | 15.781
7 | 11.124 | 24.673 | 21.815 | 16.235
BioEnergy 2016
June 13-14, 2016 Rome

## Slide 10: Structure activity relationships (SAR) Glucose % yield vs Temperature
cellulose (DP ~ 450) in 0.032 M [H+]
__________________________________________________________________
A.S. Amarasekara et al. Sustain. Energ. 2014, 2(3), 102
Chart: Temperature (0C)
| 150 | 160 | 170 | 180
1a | 6.549 | 10.193 | 20.759 | 17.729
1b | 5.505 | 11.372 | 18.641 | 16.741
2 | 2.535 | 6.779 | 11.903 | 7.272
3 | 4.588 | 9.406 | 17.233 | 15.319
4 | 0.983 | 4.474 | 13.113 | 9.025
5 | 4.347 | 8.542 | 17.174 | 14.983
6 | 3.197 | 6.968 | 16.283 | 11.022
7 | 3.235 | 7.577 | 11.55 | 8.992
BioEnergy 2016
June 13-14, 2016 Rome

## Slide 11: Silica immobilized Brönsted acidic ionic liquid catalyst and hydrolysis of cellulose in water
Solid acid catalysts
190 OC, 3 h. 50% TRS
23% Glucose
A.S. Amarasekara et al. Cat. Commun. 2014, 48, 41
Chart: Temperature °C
| 140 | 150 | 160 | 170 | 180 | 190 | 200
AIL-SiO2 | 7.573 | 16.5 | 24.475 | 34.214 | 42.941 | 48.056 | 47.433
PrSO3H-SiO2 | 0.798 | 3.937 | 9.7113 | 13.595 | 18.574 | 19.995 | 18.546
SO3H-SiO2 | 0.34844 | 0.3934 | 1.0285 | 1.2139 | 6.716 | 13.207 | 9.582
Chart: Temperature °C
| 140 | 150 | 160 | 170 | 180 | 190 | 200
AIL-SiO2 | 0.2662 | 1.2088 | 4.9054 | 9.1936 | 15.135 | 21.9004 | 23.53
PrSO3H-SiO2 | 0.02 | 0.276 | 0.969 | 4.758 | 8.699 | 11.015 | 9.5145
SO3H-SiO2 | 0.0338 | 0.03025 | 0.07139 | 0.09801 | 0.12826 | 0.99645 | 3.133
BioEnergy 2016
June 13-14, 2016 Rome

## Slide 12: Acidic ionic liquid catalyzed hydrolysis of cellulose in water with metal ions as co-catalysts
160-170 OC, 3 h.
Mn2+ 92% TRS
(without metal ions 28% TRS)
Cellulose DP ~ 450
H2O, BAIL [H+] = 0.032 M
Mn+ = 20 mol% of glucose equv.
A.S. Amarasekara et al. Cat. Commun. 2015, 70, 82
Chart: Metal ion
| none | Cr | Mn | Fe | Co | Ni | Cu | Zn | La
150 C | 18.1602 | 2.022 | 78.356 | 20.311 | 30.552 | 13.566 | 23.066 | 17.727 | 13.243
160 C | 28.044 | 1.836 | 91.77 | 33.269 | 46.17 | 20.48 | 27.93 | 26.98 | 21.071
170 C | 28.71 | 3.184 | 91.96 | 60.093 | 49.187 | 22.2908 | 26.942 | 28.926 | 24.399
BioEnergy 2016
June 13-14, 2016 Rome
O
O
o

## Slide 13: Acidic ionic liquid catalyzed hydrolysis of corn stover in water with metal ions as co-catalysts
160 OC, 3 h.
Mn2+ 90% TRS
(without metal ions 54% TRS)
H2O, BAIL [H+] = 0.032 M
Mn+ = 20 mol% of glu + Xyl equv.
A.S. Amarasekara et al. Bioresource Technol. 2015, 189, 405
Chart: Metal ion
| none | Cr | Mn | Fe | Co | Ni | Cu | Zn | La
140 C | 42.9 | 18.3 | 68 | 60 | 61.1 | 31.9 | 51.2 | 46.3 | 46.4
150 C | 52.3 | 14.2 | 72.9 | 59.5 | 62 | 33.9 | 58.1 | 52.7 | 53.4
160 C | 54.4 | 2.8 | 90.2 | 71.6 | 74.5 | 43.2 | 51.1 | 49.8 | 47.1
170 C | 53.5 | 1.1 | 87.9 | 82.8 | 75.2 | 44.4 | 48.1 | 51.1 | 43.4
BioEnergy 2016
June 13-14, 2016 Rome
o
o
o
o

## Slide 14: Acidic ionic liquid catalyzed hydrolysis of cellulose at 37 oC, 1 atm.
37 OC, 1 atm., 4 d.
78% TRS
19 % Glucose
Cellulose DP ~ 450
30% (w/w) BAIL in ZnCl2·1.74H2O
10% (w/w) cellulose in solvent-catalyst medium
Chart: Metal ion
| none | Cr | Mn | Fe | Co | Ni | Cu | Zn | La
150 C | 18.1602 | 2.022 | 78.356 | 20.311 | 30.552 | 13.566 | 23.066 | 17.727 | 13.243
160 C | 28.044 | 1.836 | 91.77 | 33.269 | 46.17 | 20.48 | 27.93 | 26.98 | 21.071
170 C | 28.71 | 3.184 | 91.96 | 60.093 | 49.187 | 22.2908 | 26.942 | 28.926 | 24.399
BioEnergy 2016
June 13-14, 2016 Rome

## Slide 15: Summary – cellulose hydrolysis __________________________________________________________________________________________________________________
neat BAIL, 70 0C, 90 min. 62% TRS
0.032M aq. BAIL, 170 0C, 3h. 33% TRS
Silica-BAIL, 190 0C, 3h. 50% TRS
0.032M aq. BAIL + MnCl2, 160 0C, 3h. 92% TRS
30% (w/w) BAIL in ZnCl2.1.74H2O, 37 0C, 4d. 78% TRS
BioEnergy 2016
June 13-14, 2016 Rome
15

## Slide 16: Acknowledgements
Dr. Bernard Wiredu Preethi Shanbharg Dominique Wells
Dr. Hua-Jun Fan Julie Dominguez Moriam Animashaun
Dre'Langala Edwards Muhammad Hasan Onome Owereh
Timila Singh Eve Larkin Uyen Ha
Brian Ezeh Ashfaqur Razzaq Alexandria Martin
Paul Bonham
BioEnergy 2016
June 13-14, 2016 Rome