## Slide 1: Symbiosis of Chemistry and Biology: BASF`s Biodegradable and Renewable Polymers
Andreas Künkel, Vice President
Biopolymers Research BASF SE
Biopolymers and Bioplastics
San Francisco, USA, August 2015

## Slide 2: Agenda
Introduction
Biobased monomers and polymers
BASF biodegradable and biobased polymers & applications
Biodegradability: value and developments
Sustainability
Conclusion

## Slide 3: Definition of renewable and biodegradable
Renewable refers to the origin of the carbon atoms in the polymers
Biodegradation by microorganisms is a matter of polymer structure, not of carbon origin
Non-biodegradable
Biodegradable
Renewable raw materials
ecoflex®
ecovio®
(partly biobased)
PLA
PE
Bio-PE
PHA

## Slide 4: Agenda
Introduction
Biobased monomers and polymers
BASF biodegradable and biobased polymers & applications
Biodegradability: value and developments
Sustainability
Conclusion

## Slide 5: Biobased building blocks (monomers) and polymers from renewable resources (selected)
Succinic acid, Butanediol
Lactic acid  Lactide
Polybutylene succinat (PBS)
1,3-Propanediol
Polyhydroxyalkanoates (PHA)
Polylactic acid
Polytrimethylene terephthalate (PTT)
Ethanol  Ethylene
Biobased Monomers
Polymers
Feedstock
Glucose
Yellow = Biobased monomer
Red = Biobased (non-biodegradable)
Blue = Biodegradable and biobased polymers
Polyethylene (PE)
Cellulose
Fatty acids from plant oils
Dicarboxylic acids (e.g. azelaic acid)
Starch
Furandicarboxylic acid
Polyethylene furanoate (PEF)
Polyester

## Slide 6
Lab scale
Pilot scale
Production scale
3-HP as precursor for bio-acrylic acid
1,4-Butanediol
Adipic acid
New dicarboxylic acids, OH-Acids, Oils
Succinic acid
n-Butanol / Isobutanol
1,3-Propanediol
1,5-Pentamethylenediamin
2006: renewable building blocks are in lab scale and only few companies are active

## Slide 7
Lab scale
Pilot scale
Estimated capacity in 2015
50 kt
20 kt
only Isobutanol at < 20 kt
< 2 kt
 60-80 kt
60 kt
2014: renewable building blocks enter world scale production with new alliances
3-HP as precursor for bio-acrylic acid
1,4-Butanediol
Adipic acid
New dicarboxylic acids, OH-Acids, Oils
Succinic acid
n-Butanol / Isobutanol
1,3-Propanediol
1,5-Pentamethylenediamin

## Slide 8: Succinic acid fermentation technology
Status: pilot phase
+
Basfia
succiniciproducens
CO2 & C-Source
Succinate
CO2
Notes: Growing & aging world population
The United Nation estimates an increase of the world population over 9 billion in 2050, 40% more than today. The majority of this growth is expected in developing and emerging countries. Moreover, the portion of people over 60 should double to about 22%; the majority in the developed countries. In 2005 the number was only 10%.
How can we produce and distribute enough food for this growing population?
How can we assure good living conditions for the aging world

## Slide 9: Agenda
Introduction
Biobased monomers and polymers
BASF biodegradable and biobased polymers & applications
Biodegradability: value and developments
Sustainability
Conclusion

## Slide 10: ecoflex® as modular system
Terephthalic acid
Adipic acid
Succinic acid
1,4-Butanediol
Melt polycondensation
PBAT
(ecoflex®)
X
X
Y
Y
X
X
+
+
PBST
X
X
ecoflex® is a random aliphatic-aromatic copolyester
Access to biobased ecoflex® variants possible (e.g. by replacing adipic acid with biobased succinic acid)
Each monomer change influences melting point, tensile strength, crystallization speed & biodegradation behavior
Change of monomer and monomers composition results in new properties

## Slide 11: Limits of classical melt polycondensation for biodegradable polyesters
Compounds needed for broader property range
ecovio® is the trade name for BASF’s ecoflex® – PLA compounds
ecoflex
Poly lactic acid (PLA)
PS
PP
HDPE
LDPE
Polybutylen- succinate (PBS)
Elongation @ break (%)
E-Modulus （MPa）
PBT
Accessible property region for
biodegradable polyesters made by classical melt polycondensation
Polyhydroxybutyrate (PHB)
non-biodegradable Polymers
biodegradable Polyester
ecovio®

## Slide 12: BASF as solution provider for biodegradable packaging
ecovio® F Mulch
ecovio® F Film
ecovio® F Film
ecovio® FS Shrink Film
ecovio® FS Paper
ecovio® IS
Film Applications
Packaging Solutions
Source: B + K

## Slide 13: Coffee: past and present
1908
2006

## Slide 14: ecovio®, biodegradable coffee capsules
Coffee consumption in Germany: citizen/day
Compostable
Plastic waste
Used coffee capsule contain 70 wt-% of water
Missing
property
High variety of hot drinks easily prepareable via capsules
To use coffee grounds as composting material, degradable capsules
are required

## Slide 15: ecovio® as complete packaging solution

## Slide 16: Agenda
Introduction
Biobased monomers and polymers
BASF biodegradable and biobased polymers & applications
Biodegradability: value and developments
Sustainability
Conclusion

## Slide 17: General mechanism of polymer biodegradation
water soluble
polymer fragments
Microorganisms
biodegradable plastic
(e.g. ecoflex®)
extracellular
enzyme
CO2
H2O
CH4
Surface erosion
Microorganisms excrete
extracellular enzymes (e.g. Hydrolases)
Enzymes attach to surface and cleave polymer chains
Short chain intermediates and monomers
are dissolved into the medium
Intermediates are metabolized by microorganisms to CO2, CH4, water and biomass
UV/vis irradiation
moisture
oxygen
other abiotic factors
adapted from R.J. Müller

## Slide 18: Biodegradation in different environments
Controlled | Not controlled
Composting
aerobic
Anaerobic digestion
anaerobic
Biodegradation in soil
Waste water treatment
Marine water
mix

## Slide 19
Investigation of polymer biodegradation in environments relevant for applications
Dedicated research activities for water, soil, composting and anaerobic conditions
Field evaluation: assessing product performance under realistic conditions
Bringing together product performance and polymer biodegradability know-how
Knowledge of structure-properties relationship facilitates development of new tailor-made products
Holistic approach to understand and leverage biodegradability of polymers
Performance
Biodegradability

## Slide 20: From basic understanding to industrial scale
Basic understanding
Field evaluation
Anaerobic digestion field trial
Industrial composting field trial
Elucidating “interaction” between polymer and microflora
polymer blend
microorganisms
+
?
biodegradation?
Assessing product performance in field trials
Polymer characteristics
Microorganisms and enzymes
Abiotic factors
Understanding structure-property-relationship facilitates product development
Field trials needed for communication and to gain stakeholder acceptance

## Slide 21: Agenda
Introduction
Biobased monomers and polymers
BASF biodegradable and biobased polymers & applications
Biodegradability: value and developments
Sustainability
Conclusion

## Slide 22
Development and use of biobased and biodegradable polymers considers the complete lifecycle
Renewable raw materials & polymers
Processing
Applications
Biodegradability

## Slide 23: Sustainability contribution of biodegradable and highly biobased coffee capsules
ecovio® for coffee capsules can be industrially composted along with food waste. Recycling food wastes is more resource efficient than having it landfilled or incinerated.
Increased production of compost helps bring back phosphates and humus into agricultural soil. As result scarce resources are saved and soil erosion can be mitigated.
High content of Renewable raw materials enable reduced material carbon footprint allowing savings of greenhouse gas emissions.

## Slide 24: Agenda
Introduction
Biobased monomers and polymers
BASF biodegradable and biobased polymers & applications
Biodegradability: value and developments
Sustainability
Conclusion

## Slide 25: BASF concept for biodegradable and renewable polymers
GOAL: Performance of biodegradable plastics comparable to standard plastics
BASED on scientific evidence and basic understanding of biodegradability
WITH proven sustainability
FOR applications where biodegradability adds value to the solution
BY application of renewable resources only based on functionality (performance, LCA)
Performance made sustainable