## Slide 1
Optimization of conditions for obtaining hydrogels of PVA/SMTP and evaluation of the presence of crosslinks between chains
Profa. Dra. Andreia de Araújo Morandim-Giannetti
June, 2014

## Slide 2
Definition of biomaterials
The biomaterial can be defined as natural or synthetic biological compound used in contact with the intention to treat, augment or replace tissue, organs or body functions being formed mainly from metals, ceramic materials and polymer materials systems
Application:
Dermatology (prosthetic filling, release transdermal drug delivery system).
Ophthalmology (vitreous replacements, contact lenses, intraocular drug release) among others.
Okaya T., Suzuki A., Kikuchi K. Colloids and Surfaces A: Physiochemical and Engineering Aspects. V.153, p.123-125, 1999.
Swindle-Reilly K. E., Shah M., Hamilton P. D., Eskin T.A., Kaushal S., Ravi N. Investigative Ophthalmology & Visual Science, v.50, n.10, p.4840-4846, 2009.

## Slide 3
Definition of hydrogels
Crosslinked polymeric material which retains a significant fraction of water in its structure but without dissolving.
The crosslinking between chains can be obtained from:
covalent interactions
Physical interactions (eg, intermolecular interaction)

## Slide 4
Crosslinked hydrogels

## Slide 5
Choose the matrix
While obtaining possible hydrogels, it is possible to use various polymers alone or as blends as matrices. E.g.
polyvinyl alcohol
polyacrylamide
Chitosana
methylcellulose
starch
Methyl Methacrylate
polyvinylpyrrolidone
polysaccharides
hydroxyapatite
Chirila T.V., Hongb Y., Dalton P.D., Constable I.J., Refojo M.F. Progress in Polymer Science. V.23, p.475-508, 1998.
Okaya T., Suzuki A., Kikuchi K. Colloids and Surfaces A: Physiochemical and Engineering Aspects. V.153, p.123-125, 1999.
Swindle-Reilly K. E., Shah M., Hamilton P. D., Eskin T.A., Kaushal S., Ravi N. Investigative Ophthalmology & Visual Science, v.50, n.10, p.4840-4846, 2009.

## Slide 6
Selection of crosslinker agents
Regarding primers crosslinking, we can include:
ionizing radiation
1,5-hexadiene-3 ,4-diol
Ammonium persulfate
Ethylene diacrylate
glutaraldehyde
genipin
Trisodium trimetaphosphate

## Slide 8
Physical and chemical characterizations
Characterizations, include:
mechanical properties
rheological Testing
viscosity
density
infra red
Scanning electron microscopy
X-Ray Diffraction
thermal analysis
Refractive Index
Swell Grade
Fraction sol / gel

## Slide 9
Biological characterizations
Biological characterizations:
cytotoxicity
microbiological
“In vitro" tests
“In vivo“ tests

## Slide 10
PVA hydrogel with SMTP
Property | Unit
Weight | 4 g
Density | 1.0053-1.0089 g/cm
Water content | 98-99%
pH | 7.0-7.4
Viscosity | 4.0-4.2 mPa
Refractive Index | 1.3345-1.3348
100
mL
water
5 g de PVA
0.625
g SMTP
agitation
T = 80ºC
T = 2 h
hydrogel
Refractive Index
Density
Viscosity

## Slide 11
Experimental Design
coded variables |  |  | Non-coded variables |  | 
PVA | SMTP | pH | PVA | SMTP | pH
0 | + | 0 | 7.00 | 9.704 | 10.00
+1 | +1 | +1 | 10.00 | 8.000 | 12.00
+1 | -1 | -1 | 10.00 | 3.000 | 8.00
0 | 0 | 0 | 7.00 | 5.500 | 10.00
-1 | +1 | +1 | 4.00 | 8.000 | 12.00
0 | - | 0 | 7.00 | 1.296 | 10.00
- | 0 | 0 | 1.95 | 5.500 | 10.00
0 | 0 | + | 7.00 | 5.500 | 13.36
-1 | 1 | +1 | 4.00 | 3.000 | 12.00
+ | 0 | 0 | 12.05 | 5.500 | 10.00
0 | 0 | - | 7.00 | 5.500 | 6.64
0 | 0 | 0 | 7.00 | 5.500 | 10.00
+1 | +1 | -1 | 10.00 | 8.000 | 8.00
+1 | -1 | +1 | 10.00 | 3.000 | 12.00
-1 | +1 | -1 | 4.00 | 8.000 | 8.00
-1 | -1 | -1 | 4.00 | 3.000 | 8.00
coded variables |  |  | Non-coded variables |  | 
PVA | SMTP | pH | PVA | SMTP | pH
0 |  | 0 | 7.00 | 9.704 | 10.00
+1 | +1 | +1 | 10.00 | 8.000 | 12.00
+1 | -1 | -1 | 10.00 | 3.000 | 8.00
0 | 0 | 0 | 7.00 | 5.500 | 10.00
-1 | +1 | +1 | 4.00 | 8.000 | 12.00
0 |  | 0 | 7.00 | 1.296 | 10.00
 | 0 | 0 | 1.95 | 5.500 | 10.00
0 | 0 |  | 7.00 | 5.500 | 13.36
-1 | 1 | +1 | 4.00 | 3.000 | 12.00
 | 0 | 0 | 12.05 | 5.500 | 10.00
0 | 0 |  | 7.00 | 5.500 | 6.64
0 | 0 | 0 | 7.00 | 5.500 | 10.00
+1 | +1 | -1 | 10.00 | 8.000 | 8.00
+1 | -1 | +1 | 10.00 | 3.000 | 12.00
-1 | +1 | -1 | 4.00 | 8.000 | 8.00
-1 | -1 | -1 | 4.00 | 3.000 | 8.00

## Slide 12
Results and Discussion

## Slide 13
Parameters used during the analysis:
Final pH: Between 7.0 and 7.4 (optimum = 4.2)
Index of Refraction: <1.337
Dynamic viscosity (25 ° C): Between 4.0 and 4.2 (optimum = 4.1)
Density (25 º C): Between 1.0053 and 1.0089 (ideal = 1.0071)
Results and Discussion

## Slide 14
Results and Discussion

## Slide 15
Optimized input variables:
Initial pH: 9.328
Mass of polyvinyl alcohol per 100 ml water: 4.1383 g
Relationship SMTP / PVA: 1/7.4619
Optimized output variables
Final pH: 7.20
Refractive Index: 1.3407
Dynamic viscosity (25 ° C): 4.617 mPa
Density (25 º C): 1.0071 g / mL
Analysis of results

## Slide 16
Hydrogel without SMTP
Infrared spectra
Hydrogel with SMTP

## Slide 17
Analysis by atomic force microscopy

## Slide 18
Analysis by atomic force microscopy

## Slide 19
Analysis by atomic force microscopy
We observe a more compact material because of the presence of crosslinking between the PVA and the SMTP

## Slide 20
Biomaterial Properties
Changes in ownership of swelling due to lower availability of hydrogen bonds and larger space between the chains
24
Chart: hour
 | 120.3189 | 139.0322 | 137.8707 | 138.8824 | 131.2425 | 120.995 | 122.9104
 | 63.4801 | 74.7065 | 73.0834 | 81.261 | 75.3702 | 80.9426 | 81.3585
Degree of swelling of hydrogels with or without SMTP

## Slide 21
Conclusion
The biomaterial obtained had the necessary characteristics
Crosslinking between PVA and SMTP was checked due to the observed changes in the material
The SMTP was important to obtain the required specification

## Slide 22
Team
Andreia de Araújo Morandim Giannetti
Octaviano Magalhães Junior
Patrícia Alessandra Bersanetti
Paulo Schor
Regina Freitas Nogueira
Wallace Chamon Alves de Siqueira

## Slide 23
Acknowledgements

## Slide 24
Acknowledgements