## Slide 1
Recoverable and recyclable catalysts for sustainable chemical processes
Anna Chrobok
Silesian University of Technology, Poland

## Slide 2
reduce chemical waste,
improve the selectivity and
efficiency of synthetic processes
The design and synthesis of recoverable and recyclable catalysts
Ludwigshaven in Germany
What are the challenges for the sustainable chemical industry today?

## Slide 3
The need to implement green chemistry principles is a driving force towards the development of recoverable and recyclable catalysts.
What are the challenges for the sustainable chemical industry today?
CATALYST
Recyclability can either be achieved:
by bounding the catalyst to a solid phase,
by modification of solubility characteristics.
CATALYST e.g. acid or base is bounded to a solid phase
Filtration
Regeneration
Recycle
M. Benaglia, Recoverable and Recyclable Catalysts, 2009 John Wiley & Sons Ltd., 2009

## Slide 4
Green Chemistry
„Green chemistry is the design, development and implementation of chemical products and processes to reduce or eliminate the use and generation of substances hazardous to human health and the environment.“
(U.S. Environmental Protection Agency)
Notes: 12 Principles of Green Chemistry*
It is better to prevent waste than to treat or clean up
waste after it has been created.
1. Prevention -
Synthetic methods should be designed to maximize the
incorporation of all materials used in the process into
the final product.
2. Atom Economy -
Wherever practicable, synthetic methods should be
designed to use and generate substances that possess
little or no toxicity to human health and the environment.
3. Less Hazardous Chemical Synthesis -
Chemical products should be designed to effect their desired
function while minimizing their toxicity.
4. Designing Safer Chemicals -
The use of auxiliary substances (e.g., solvents, separation
agents, etc.) should be made unnecessary wherever possible and innocuous when used.
5. Safer Solvents and Auxilaries -
Energy requirements of chemical processes should be
recognized for their environmental and economic impacts and should be minimized. If possible,
synthetic methods should be conducted at ambient temperature and pressure.
6.Design for Energy Efficiency -
A raw material or feedstock should be renewable rather
than depleting whenever technically and economically practicable.
7. Use of Renewable Feedstocks -
Unnecessary derivatization (use of blocking groups, protection/
deprotection, temporary modification of physical/chemical processes) should be minimized or
avoided if possible, because such steps require additional reagents and can generate waste.
8. Reduce Derivatives -
Catalytic reagents(as selective as possible) are superior to stoichiometric
reagents.
9. Catalysis –
Chemical products should be designed so that at the end of their
function they break down into innocuous degradation products and do not persist in the
environment.
10. Design for Degradation -
Analytical methodologies need to be
further developed to allow for real-time, in-process monitoring and control prior to the formation of
hazardous substances.
11. Real-Time analysis for Pollution Prevention -
Substances and the form of a
substance used in a chemical process should be chosen to minimize the potential for chemical
accidents, including releases, explosions, and fires.
12. Inherently Safer Chemistry for Accident Prevention -
*- (Anastas, P. T.; Warner, J. C. Green Chemistry: Theory and Practice, Oxford University Press: New York, 1998, p.30)

## Slide 5
http://www.acs.org/content/acs/en/greenchemistry.html

## Slide 6
Product | tons p.a. | kg waste/ kg product
Oil refining | 106 - 108 | ca 0.1
Bulk Chemicals | 104 - 106 | < 1 - 5
Fine Chemicals | 102 - 104 | 5 - 50
Pharmaceuticals | 10 - 103 | 25 - 100+
Green Chemistry
R. A. Sheldon “Consider the Environmental Quotient”, ChemTech, 1994, 38.
E-factor (kg/kg)
E = kg waste/kg product
raw material
product
waste

## Slide 7
Case studies:
the recoverable and recyclable catalysts for chemical processes like:
esterification,
Diels-Alder reaction,
oxidation of alcohols and ketones.
IONIC LIQUIDS as homogeneous and heterogeneous catalysts
Recycling of ionic liquids prevents them from:
- ending up in the aquatic environment,
- release into the atmosphere (low volatility).
Ionic liquids from biomass.
Examples

## Slide 8
Ionic Liquids Basic Structures

## Slide 9
Ionic Liquids Properties

## Slide 10
Ionic liquids as catalyst and solvent
for esterification reaction
Modification of solubility characteristics

## Slide 11
H2SO4 + B → [HB][HSO4] χH2SO4 = 0.50
2H2SO4 + B → [HB][(HSO4)(H2SO4)] χH2SO4 = 0.67
3H2SO4 + B → [HB][(HSO4)(H2SO4)2] χH2SO4 = 0.75
Complex hydrogen-bonded anionic clusters
[(HSO4)(H2SO4)χ]-(χ = 0, 1, or 2)
K. Matuszek, A. Chrobok, F. Coleman, K. R. Seddon, M. Swadźba‑Kwaśny, Green Chem., 2014, 16 , 3463
m. p. < 100°C
RT ILs, Tg < 0°C

## Slide 12
Atoms of the hydrogensulfate anion are represented in blue,
Atoms of the sulfuric acid are in red.
K. Matuszek, A. Chrobok, F. Coleman, K. R. Seddon, M. Swadźba‑Kwaśny, Green Chem., 2014, 16 , 3463
Complex hydrogen-bonded anionic clusters
[(HSO4)(H2SO4)χ]-(χ = 0, 1, or 2)

## Slide 13
Catalyst acidity
Reactants ratio 1÷ 1,5 mol
Catalyst loading 1÷ 15 % mol
Catalyst recycle
Model esteryfication reaction
K. Matuszek, A. Chrobok, F. Coleman, K. R. Seddon, M. Swadźba‑Kwaśny, Green Chem., 2014, 16 , 3463

## Slide 14
Catalyst loading, %mol
Reactants ratio
BuOH : MeCOOH = 1:1; Temp. 30oC
Temp. 30oC
[Et3NH][(HSO4)(H2SO4)2]
Complex hydrogen-bonded anionic clusters

## Slide 15
BuOH : MeCOOH = 1:1.5; IL =12% mol; t= 2h; Temp. 30oC
[Et3NH][(HSO4)(H2SO4)2]
Recycling study

## Slide 16
Summary
Synthesis of a new family of protonic ionic liquids
Formation of hydrogen-bonded anionic clusters [(HSO4)(H2SO4) χ]- (χ= 1 or 2)
High acidity of new ionic liquids (AN up to 121)
New catalysts for esterification
Key parameters effecting the
reaction: miscibility of reagents,
catalyst acidity
Possibility to reuse catalyst
without the lost of activity

## Slide 17
Ionic liquids as catalyst and solvent
for Diels-Alder reaction
Designing of recyclable biocatalysts

## Slide 18
K. Erfurt, I. Wandzik, K. Walczak, K. Matuszek, A. Chrobok, Green Chem., 2014, 16, 3508
Ionic liquids from the biomass
Glucose-derived ionic liquids: exploring biodegradable, low-cost sources

## Slide 19
Diels-Alder reaction
K. Erfurt, I. Wandzik, K. Walczak, K. Matuszek, A. Chrobok, Green Chem., 2014, 16, 3508

## Slide 20
K. Erfurt, I. Wandzik, K. Walczak, K. Matuszek, A. Chrobok, Green Chem., 2014, 16, 3508
Diels-Alder reaction

## Slide 21
Ionic liquids as catalyst
for ketones oxidation
Bounding the catalyst to a solid phase

## Slide 22
A. Chrobok, S. Baj, W. Pudlo, A. Jarzębski, Appl. Catal. A: General, 2009, 366, 22
Immobilized Catalysts
Bounding ionic liquid to a solid phase
Scanning Electron Microscopy micrograph of bimodal structured silica

## Slide 23
3 recycles, 89-91% of catalyst recovery
A. Chrobok, S. Baj, W. Pudlo, A. Jarzębski, Appl. Catal. A: General, 2009, 366, 22
Immobilized Catalysts
Bounding the catalyst to a solid phase

## Slide 24
Ionic liquids as catalyst and solvent
for alcohols oxidation
Supported Ionic Liquid Phase SILP

## Slide 25
Supported Ionic Liquid Phase SILP
- materials science engineering with economic and environmental objectives
A. Chrobok, S. Baj, W. Pudlo, A. Jarzębski, Appl. Cat. A: General, 2010, 389, 179

## Slide 26
Scanning Electron Microscopy
micrograph of the ionogel
A_CuCl2/[bmim]OSO3Ocsup
Supported Ionic Liquid Phase SILP
A. Chrobok, S. Baj, W. Pudlo, A. Jarzębski, Appl. Cat. A: General, 2010, 389, 179

## Slide 27
Supported Ionic Liquid Phase SILP
A. Chrobok, S. Baj, W. Pudlo, A. Jarzębski, Appl. Cat. A: General, 2010, 389, 179
reaction conditions: alcohol (1 mmol), TEMPO (0.1 mmol), 0.025 mmol of CuCl2 included in A_CuCl2/[bmim]OSO3Ocsup, dibutyl ether as solvent, oxygen at atmospheric pressure, 65 oC

## Slide 28
Reusability of the A_CuCl2/[bmim]OSO3Ocsup and B_CuCl2/[bmim]OSO3Ocsup catalysts
reaction conditions: benzyl alcohol (5 mmol), TEMPO (0.5 mmol), 0.35g of catalyst containing 0.075 mmol of CuCl2, oxygen at atmospheric pressure, 65 oC; isolated yields after 7 h with 98% conversion of benzyl alcohol

## Slide 29
Summary
The development of recyclable catalysts
represents a big challenge.
It is interdisciplinary field,
where pure chemistry is connected to
material science, or engineering and where even business and economy-related issues play an important role in:
determining the planning, the design and the realization of a project in the area.
It is a field where many technologies and opportunities are offered to successfully realize an easy recoverable and, what is more important, reusable catalytic system.

## Slide 30
Acknowledgment
Karolina Matuszek
Agnieszka Drożdż
Magdalena Sitko
Karol Erfurt
Professor Andrzej Jarzębski
Dr Katarzyna Szymańska
HARMONY Grant no. UMO-55 2012/06/M/ST8/00030
Financing:
Professor Kenneth Seddon
Dr Małgorzata Śwadźba
Dr Fergal Coleman