## Slide 1: Effect of BMP-2 peptide conjugated TiO2 nanoparticle on osteogenic expression through biomimetic Zein PDA nanofibrous scaffold
Babitha Sekar
CSIR - Central Leather Research Institute Chennai ,Tamil Nadu, India

## Slide 2: Introduction
Bone
Heal & remodel without leaving a scar
Composite material of polymer ceramic matrix
Current treatment methods
Autologous bone graft , Allograft
Alternative – Metals & Ceramics
Tissue engineering
Cells, ECM, Intercellular communication, Cell – Matrix interaction, Growth factors, 3D configuration
Well co-ordinated spatial & time dependent

## Slide 3
Biomimetic scaffold

## Slide 4
Electrospinning
Versatile
Low start up cost
Control over size & morphology
Ease of fiber functionalization
Ease of material combination
Variety of polymers

## Slide 5
Nanofiber
    Large specific surface area
    Support & Strength
    Encapsulation
    Structure - porosity, diameter
    (50-1000nm)

## Slide 6
Natural biodegradable polymer
  Favors cell attachment, Less immunogenic & Promotes chemotactic response, Weak mechanical property
  Zein – Amphiphilic, Tensile strength, Elastic property, Ectopic bone formation
  Polydopamine - Versatile, Secondary surface-mediated reaction
  Metal oxide nanoparticles - TiO2 NPs
  Chemically reactive
  Synergistic effect
  Growth factors
  BMPs- Signaling molecules
  Recruit MSCs, Differentiate, Proliferate & Promote collagen production

## Slide 7
ZeinPDA
TiO2BMP-2 peptide
Solution
Composite nanofiber
16 kV
0.4 mL/Hr
15 cm
Preparation of composite nanofibrous scaffold

## Slide 8
Composite polymeric
matrix

## Slide 9: In-vitro analysis
Release profile
Compatibility studies
  Cell viability
  Haemocompatibility
  Cell biomaterial interaction
Osteogenic potential
  Alkaline phosphatase activity
  Mineralization assay
  Immunofluorescent staining
  ELISA

## Slide 10
Results
X-ray photoelectron spectroscopy

## Slide 11
Raman Spectroscopy
a
b
a – Only TiO2 NPs, b – BMP-2 peptide conjugated TiO2 NPs

## Slide 12: Morphology & Surface Wettability
b
a
a1
b1
a, a1 – Zein nanofiber
b, b1 – BMP-2 peptide conjugate TiO2 NPs incorporated ZeinPDA nanofibrous Scaffold
Scale bar - 1μm

## Slide 13
HR-TEM & Fluorescence microscopic images
a – Only Zein nanofibers (Scale - 0.5 μm)
b – BMP-2 peptide conjugated TiO2 nanoparticles on ZeinP DA nanofiber (Scale - 50 nm)
c – FITC tagged BMP-2 peptide conjugated TiO2 nanoparticles (Scale - 10 μm)

## Slide 14
Release Profile

## Slide 15
Cell Viability – MTT assay
** p value < 0.022

## Slide 16
Alkaline phosphatase activity
* p value less than 0.05
*
*
*

## Slide 17
Mineralization content assay – ARS
a – TCP, b – Zein NF, c – ZeinPDA NF, d – ZeinPDATi NF, e – ZeinPDATiBMP-2 NF

## Slide 18
Cell – Biomaterial Interaction
Control
Zein NF
ZeinPDA NF
ZeinPDATi NF
ZeinPATiBMP-2 NF
Scale bar - 1μm

## Slide 19
Immunofluorescent staining of Osteogenic markers
a,d – Osteocalcin; b,e – BMP-2; c,f - Osteopontin

## Slide 20
Protein Expression Analysis - ELISA
* P value less than 0.05

## Slide 21: Conclusion
Better biocompatibility, Increased mineralization content and enhanced expression of osteogenic markers
Act as an effective matrix for bone tissue engineering

## Slide 22: Future perspectives
Evaluate the performance of nanofibrous scaffold in-vivo
Ethical committee approval

## Slide 23: Thank you