## Slide 1
▪ Photonics / 2016 - Berlin ▪
Institute of Physics - Rennes / IPR CNRS 6251 - France
Orator : Bruno BÊCHE, Pr.
Institute of
Physics - Rennes
Rennes
400 000 inhabitants
60 000 students in formation
Notes: Mr Chairman, Ladies and Gentlemen,
On behalf of my colleagues and myself, I would like to thank you for your kind invitation.
It's my purpose in this brief talk to illustrate the various aspects of an integrated optical on SU-8 (fluorinated or not) polymer for designing of waveguides, S-bends, Y-junctions, and MZI.

## Slide 2
Soft Matter for Integrated Photonics and Resonances: various hybrid approaches and adaptive technologies
NanoRennes - clean room IETR-CNRS
Optical characterizations
 Collaboration IPR CNRS, IETR CNRS, STLO INRA

## Slide 3
Artist’s view of the phenomenon
▪ At the origin, discover in acoustic (Lord Rayleigh theory in 1910-1914)
St Paul Cathedral - London – United Kingdom
Gol Gumbaz – Bijapur - India
Compression of the air - acoustic
▪ Type of waves which can propagate along the concave surface (grazing reflection) + ‘tuning’ if cycle ! Notion of resonance.
The resonant waves or Whispering Gallery Modes (WGM)

## Slide 4
▪ Applications in QED (discrete modes coupling electromagnetic modes and atomic)  Rabi oscillation and intricated states ; on physical cavities and Laser (spontaneous recombination / stimulate), in optical telecommunications ((de)-multiplexing in wavelength or filters), in sensors (optical probe strongly localized and interactive measurements with shift of the resonance), and so on.
Factor of merit of an optical mode
▪ Optical micro-resonators (MRs) = seductive objects
- Control of electromagnetic fields in term of spatial localization (or strong confinement of the light into a restrict V-space volume)
- Quantification of the optical modes (called WGM) and increase of their own life time t into such cavities (Q=w.t)
OpticalPerimeterMR = m. lMaxwell
 One century later, in nano-sciences and nano-technologies, such concepts are totally transposed to electromagnetic waves in integrated photonics.
 Notion of photonic’s orbital

## Slide 5
▪ I.1] Organic chemistry for sub-l photonics
Part I
▪ Choices and study of organic materials, many products and liquid photoresist exist for the realizations of integrated photonics elements [PMMA, PS233, SU8, NOA stick, Kapton, and DUV210…]
Various integrated structures and functions-principles, wave-guiding, interference, resonant…
« I. Organic commercial Chemistry for polymer MRs : an example with Deep UV»

## Slide 6
▪ Usual lithography: insolation
at λ = 365 nm
▪ Limit of resolution < 1 µm
Lampe Hg
365 nm
DUV
248nm
▪ Deep UV lithography (DUV):
▪ Insolation at λ = 248 nm
                 Organic material (ex): UV 210 (positive photoresist)
▪ High resolution: 200 nm
▪ Judicious optical properties
n=1.565 + lower optical losses (3 dB.cm-1 at λ = 980nm)
 Possibility to develop sub-l patterns for nanotechnology and photonics
sub-l nano-hole
Width of waveguide 300nm
▪ Photolithography: limited by diffraction

## Slide 7
▪ The UV210 organic material
▪ Ellipsometric measurement & dispersion curves of UV210 (extinction k <10-3)
 Indices enough high for core waveguide applications on lower cladding
 Insolation dose increases  saturation of the value of index + diminution of film thickness, density increases (Gladstone empiric law)
at l=980 nm
Refraction index n
Refraction index n
Thickness variation (%)

## Slide 8
Families of resonant probes :
Stadium, disk
Dimensions of cavities:
Radius R = 25 µm et 50 µm
Gap g: 200 nm à 500 nm
Guides : width 5 µm
Injection
Détection
Détection
▪ Conception of quartz/chrome mask
▪ Realization of optical MRs families in UV210 with sub-l gap

## Slide 10
 Roughness surface : 2 nm
▪ SEM - AFM - Raman Analyses
Pedestal ring
(gap=500 nm)
Racetrack (gap=500 nm)
Serial /cascade of MRs (gap=500 nm)
g
2R
h
@1002cm-1
AFM
Raman imaging

## Slide 11
▪ Optical characterizations, experiences

## Slide 12
Structures | Disk |  | Stadium | 
Parameter R | 25µm | 50µm | 25µm | 50µm
FSR theo. (nm) | 2.92 | 1.46 | 1.78 | 0.89
FSRexp. (nm) | 2.70 | 1.45 | 1.95 | /
Quality factorQ | 700 | 950 | 700 | 
Δλ, FSR
Δλ, FSR
▪ Spectral transmissions - FSR (Dl)
Disk cavity : R = 25 µm Stadium cavity
Spectral principle resonance :
Wavelength (nm)
Wavelength (nm)

## Slide 13
0.5
1.0
1.5
2.0
2.5
0.2
0.4
0.6
0.8
1.0
FFT
FSR (nm)
Quality factor Q >3000 at lIR
Fourier

## Slide 14
▪ II.1] Fluorinated organic by plasma process : optical losses decrease
Part II
« II. Plasmas processes for organic MRs »

## Slide 15
▪ Elaborations of plasmas processes - fabrication
Optical, fluidic circuits
(100) Si substrate
(100) Si substrate
Thermal oxidation PECVD
Spin-Coating, PECVD, Plasmas (O2, Ar, CF4)
Mask / Lithography (D)UV / Development / Baking + Plasmas treatments : Etching and functionalization
SiO2
(100) Si substrate
SOG, NOA, PS233
(100) Si substrate
SU-8 (or PMMA)
Biphenol A ether glycidyl (SU8)
Molecular/radicals reaction
Surface reaction
ion/molecules
reactions
diffusion
Products
exit
Precursors entrance
Electrode
ˉ
ˉ
Optical emission
recombination
[lower pressure]
Electrode
+
+
+
[13.56 MHz]
Reactor
NOA, SOG, PS233

## Slide 16
Analysis of the SU-8 reference polymer and the fluorinated SU8 polymer
▪ Plasma treatments with CF4 for optical losses decrease into organic waveguides
SiO2
Si substrate
Rib guide
SU8
4 µm

## Slide 17
Plasma CF4 :
t=30s, PRF=50W, D=30sccm
Plasma CF4 + 10% H2 :
t=110s, PRF=20W, D=30sccm
 Fluorinated XPS peaks = C-H substitution ; successful C-FX functionalization
Optical propagation losses : decrease of 50 to 70 %
Avoid ‘RIE’ during plasma

## Slide 18
▪ Schematic diagram of elementary 2.5D MR (disk or ring))
li
l1, l2, … li … ln
x1
x2
x3
R
Wa
Wr
Upper view
l1, l2, ... li-1 li+1, ... ln
hr
ha
d
x1
x2
x3
Cut
▪ Problems and conceptions :
 Polymers no always compatible to shape 2,5D structures (good adherence of each layer, and ability to develop successively each pattern).
 Idea : Development et use of lithographic process combined to plasma [SOG/PS233/SU8, plasmas O2 and Ar].
▪ II.2] Plasmas to shape 2,5D MRs

## Slide 19
Reference liquid | gT-(totale) | gd-(LW) | g nd(+) | g nd(-)
Water | 72.8 | 21.8 | 25.5 | 25.5
Glycerol | 63.3 | 34.0 | 3.92 | 57.4
Diiodomethane | 50.8 | 50.8 | 0.0 | 0.0
(Unity: mJ.m-2)
▪ Plasma treatment (O2 and Ar) and principle of measurements (q, g)
▪ Surface energy measurement (superficial tensions, J.m-2) :
measurement
- Dispersive contribution gd-(LW) (London Van der Waals forces)
- Non-dispersive contribution (or polar) gnd (Keesom interactions, Debye forces, H / H2O atomic attraction, Acid-Base interactions]
gT-(total)
2d Newton law or PFD (F=gL)
 Young eq. at three interfaces
Van Oss Model (or Acid-Base)
liquid
gSL
SOG or PS233
vapor
Contact point (S-L-V)
q
R
H
gSV gS
gLV gL

## Slide 20
▪ Results:
[gS/O2]
[qwater]
q=117° (hydrophobe surface )
30s<tO2<60s
30s<tAr<180s
maximum

## Slide 21
[WSU8/PS233]
[WSU8/SOG]
 The overall determination of the gS of each solids (materials) fixe the adhesion work at the interface between the core waveguide SU8 and the cladding PS233 or SOG
[gS/Ar]
plateau

## Slide 22
▪ 2,5D Micro-resonators on organic materials
TE00 whispering gallery mono-mode (at l=670 nm)

## Slide 23
Part III
« III. Soft matter in complex fluid and biomolecular interface for MRs»

## Slide 24
Tension-meter
Movable barrier
Tank
Pinch (‘dipper’)
Sample
▪ III.1] Biomolecular lipid gap or Langmuir film
Lipids
4 nm
water
air
solid
liquid
Expended liquid
Collapse threshold
gas
Superficial tension (nN/m)
Average molecular surface(Å2/molécule)
Hydrophilic
Hydrophobic

## Slide 25
▪ III.2] Design of organic 3D MRs with micro-fluidics coupled to thin-film processes for photonics applications
Pharmacology and medicines

## Slide 26
▪ Technology and concepts of micro-fluidic: realization of 3D MRs
▪Micro-channels realization by thin layer processes (SU8, PDMS, glass and plasma cleaner).
▪ Generation of mono-disperses droplets ( T-flow focusing junction)
-‘T’-structure +restriction area : NOA pinching.
-NOA = dispersed phase (Qdp, µL/h)
-Silicon oil = continuous phase (Qcp, a few 100 µL/h)
 30µm<Rspheres<200µm.
Qd
Dp
Dd

## Slide 27
▪ Simple model in two times t, the rate Qp,d fixe the sizes of droplets:
(tdroplet-formation = tblocking+tpinching , with V=Q.t, Q=v.S)
Geometry
Rates
mNOA=200mPa.s, gNOA=4.3mN/m

## Slide 28
▪ The viscosity (m) and the superficial tensions of fluids (g) act (more the previous geometry) on the dynamic of flow : mdp high  difficulty to pinch and shape the spheres & privileged jet ; mdp high  easy to pinch and form the spheres, Minimization E=g.S impose S of spheres! Sn-spheres/Sjet=3rjet/2rsphere with L=4n.(rsphere)3/3/rjet2.
▪ A few parameters that determinate the flow regimes…
 Competition between these effects give various flow regimes : capillary number =mp.vd/g 1
g=4.3mN/m
The shape of the droplet is link to the factor of form (constituted by Bond number=c/b2=function(g) + profile imaging)
 g measurements
Laplace-Young eq. (local profile)
 This value of capillary number allows the existence of these two types of régimes on the ‘T’

## Slide 29
▪ Film ‘The formation of 3D MRs droplets’ (500 images/second)

## Slide 30
▪ Two kinds of dynamic flow regimes on the T-‘flow-focusing ’
▪ Dripping regime tpinching<tjet-formation (pinching enough fast).
▪ Jetting regime tjet-formation<tpinching, dynamic capillary instability called Rayleigh-Plateau  The energy minimization leads to the formation of droplets after the jet.
▪ Resonance in 3D organic MRs
▪ Use of Raman plate-form (l=785nm) to highlight the optical resonances (Stokes peak)
50 µm
wire
Excitation localization
End spot  Equatorial
trajectory
FSRaverage (Dl)= 0.86 nm & 0.88 nm (here Dsphere= 143 µm).
FSR
FSR
Wavelength (nm)
Wavelength (nm)

## Slide 31
▪ Coupling and excitation of whispering gallery modes
DIC Nomarski imaging

## Slide 32
r1
a
Intern caustic function (n,l quantic numbers)
dl=1.9nm and Q=450

## Slide 33
Q=l0/dl
▪ AFM analysis and statistic de moments for the origin of the Q-quality factor
hRMS quadric average distance of roughness
LC coherence length (topology sense and surface statistics !)
experimentaly
AFM & statistic mathematic
Origin of the value on Q-factor
85-90% by diffusion losses

## Slide 34
Part IV
« IV. The sensors on resonant probes (MRs)…towards the life science »

## Slide 35
▪ IV.1] Resonant probe of light for glucose detection
S 280 pm/(mg/ml)
Limit 0,04 mg/ml
DC Dn= 10-5
(Typically concentration in sugar into cells are weak  [0-5 mg/ml])

## Slide 36
▪ IV.2] Resonant probes of light to detect and follow the phase-transition in temperature : biology application, lipids (MSM)
Water
Liposome
a)
b)
Polar head
Apolar queue
Tm
T (°C)
Gel phase
Liquid Phase

## Slide 37
λ4
λ3
λ2
λ1
Serial spectral
&
statistic
 phase-transition (gel=>liquid) of MSM-lipids at Tm [31-32]°C

## Slide 38
For global references:
 See web site IPR http://www.ipr.univ-rennes1.fr/
Artist view of the phenomenon…
▪ IPR-CNRS :
V. Vié, P, Panizza, F. Artzner, A. St James, and me.
▪ Our ex-PhD et post-doct:
D. Pluchon, R. Castro-Beltran, D. Duval, M. Specht, Q. Li
▪ IETR-CNRS :
H, Lhermite.
▪ STLO-INRA :
D. Dupont.
+ LAUM-CNRS : E. Gaviot
…towards the reality