## Slide 1: Separation of cerium from other rare Earth elements by solvente extraction
Carlos Antônio de Morais
Thiago Silveira Formiga
Valencia, Spain
September 26-28, 2016
NUCLEAR TECHNOLOGY DEVELOPMENT CENTER
NATIONAL COMMISSION FOR NUCLEAR ENERGY
Belo Horizonte, Brazil
2nd International Conference and Expo on Separation Techniques

## Slide 2: THE PAPER
This work presents an investigation of solvent extraction parameters in order to obtain high purity cerium from a liquor containing a mixture of rare earths elements, as an alternative to cerium oxidation and selective RE dissolution. The sample used was a sulfuric liquor obtained from the leaching of monazite, rich in light rare earth elements (La, Ce, Pr, Nd). The experiments were carried out in hydrochloric, nitric and sulphuric media.

## Slide 3: Introduction
The RE are a group of 17 elements composed of the lanthanides, scandium and yttrium

## Slide 4: Introduction
The rare earth elements have extreme importance to advanced technology industry (electronic components, permanent magnets, nuclear medicine, automobile industry, wind turbines, among others).

## Slide 5: Introduction
The rare earth elements have very similar physical and chemical properties and therefore occur together in different proportions in their mineral sources. Obtaining the individual rare earth elements in industrial scale is very complex and only dominated by a few countries.
This behavior is responsible for the high prices of these elements (difficulties in detection, analysis and commercial extraction).

## Slide 6: Introduction
Schematic diagram of the continuous SX circuit – mixer-settlers counter current system
Extraction
Scrubbing
Stripping
SOLVENT
Feed solution
Stripping solution
Stripped solution
Scrubbing solution
Raffinate
Regeneration

## Slide 7: Introduction
Solvent extraction Laboratory – CDTN, Brazil

## Slide 8: Introduction - Cerium
Generally the separation of cerium is accomplished by the oxidation of Ce (III) to Ce (IV) following by the selective dissolution of the trivalent REEs. By this technique, the other REEs are usually contaminated with cerium or cerium is contaminated with other rare earth elements, justifying the study of its separation by the solvent extraction technique.

## Slide 9: Methodology
The Sulphuric liquor was provided by the Nuclear Industries of Brazil S.A. - INB.
Nitric and hydrochloric media were also investigated.
The nitric and hydrochloric solutions were prepared from the sulphuric liquor by precipitation of the rare earths as oxalate, calcination and dissolution of the rare earth elements in nitric or hydrochloric acid.

## Slide 10: Methodology
PARAMETERS INVESTIGATED
  Extractants:
    Solvation extractants (TBP, Cyanex®923);
    Cationic extractants (D2EHPA, P507);
    Anionic extractants (Primene®J-MT, Alamine®336 and Aliquat®336);
  Aqueous phase:
    The medium (hydrochloric, nitric and sulphuric);
    Acidity;
  Aqueous/organic volumetric ratio;
  Presence and absence of oxidizing agent.
Notes: Solvatação: Substitui água de hidratação
Ácidos ou catiônicos: Liberam H+ e se ligam ao cátion do metal
Básicos ou aniônicos: Possuem região positiva e se ligam em complexos aniônicos dos metais

## Slide 11: Methodology
TBP - tri-n-butyl-phosphate
Cyanex®923 - trialkylphosphine oxide
D2EHPA - di-2-ethylhexyl phosphoric acid -
P507 - 2-ethylhexyl mono (2-ethylhexyl) ester phosphonic acid
Primene®JMT
T-Alkyl(C16-C22) primary amine
Alamine®336 -trioctyl/decyl amine
Aliquat®336
trialkyl-methyl-ammonium-chloride
Notes: Solvatação: Substitui água de hidratação
Ácidos ou catiônicos: Liberam H+ e se ligam ao cátion do metal
Básicos ou aniônicos: Possuem região positiva e se ligam em complexos aniônicos dos metais

## Slide 12: Methodology
Bench extraction experiments
Extractant
RE liquor
Agitation
(5 min)
Organic phase
Aqueous phase

## Slide 13: Samples
Sample | Content (g/L) |  |  |  |  |  |  | 
 | La | Ce | Nd | Pr | Sm | Gd | Dy | Y
Sulphuric liquor | 6.7 | 14.8 | 5.6 | 1.5 | 0.69 | 0.56 | 0.16 | 0.49
Hydrochloric liquor | 6.5 | 14.6 | 5.6 | 1.6 | 0.70 | 0.56 | 0.16 | 0.47
Nitric liquor | 6.5 | 14.5 | 5.7 | 1.5 | 0.71 | 0.56 | 0.16 | 0.50
  Chemical composition of the liquors

## Slide 14: Results - Sulphuric liquor
REE extraction – without oxidant addition
  It was observed no extraction of REE.
  High acidity of the liquor – about 1 mol/L H+.
  The pH adjustment was unfeasible due to formation a precipitate of double sulfate of rare earth and sodium or ammonium, depending on the basic reagents used (NaOH, NH4OH or Na2CO3).

## Slide 15: Results - Hydrochloric liquor
REE extraction – without oxidant addition
Extractant | pH | Extraction (%) |  |  |  | Separation factor |  | 
 |  | La | Ce | Pr | Nd | Ce/La | Pr/Ce | Nd/Pr
P507 | 0.5 | 0.7 | 1.8 | 6 | 7 | 3.5 | 3.2 | 1.2
P507 | 1.0 | 5.0 | 16 | 37 | 40 | 3.9 | 3.2 | 1.2
P507 | 2.0 | 13 | 37 | 66 | 70 | 4.1 | 3.2 | 1.2
D2EHPA | 0.5 | 17 | 38 | 61 | 64 | 3.1 | 2.7 | 1.1
D2EHPA | 1.0 | 36 | 64 | 80 | 82 | 3.2 | 2.3 | 1.1
D2EHPA | 1.5 | 65 | 86 | 93 | 94 | 3.3 | 2.2 | 1.1

## Slide 16: Results - Hydrochloric liquor – pH 0
REE extraction – with oxidant addition
Extractant | Oxidant | Extraction (%) |  |  |  | Separation factor |  | 
 |  | La | Ce | Pr | Nd | Ce/La | Pr/Ce | Nd/Pr
P507 | Na2S2O8 | 6 | 12 | 15 | 17 | 2.1 | 1.3 | 1.2
P507 | K2S2O8 | 7 | 13 | 16 | 18 | 2.0 | 1.3 | 1.2
D2EHPA | Na2S2O8 | 16 | 28 | 37 | 42 | 2.1 | 1.5 | 1.1
D2EHPA | K2S2O8 | 16 | 27 | 38 | 39 | 2.0 | 1.5 | 1.1
Potential: Initial: 550 mv
After oxidant addition: 980 mv
After extraction : 580 (mV)
Notes: Extratantes que demonstraram maior potencial na primeira etapa deste estudo

## Slide 17: Results - Nitric liquor
REE extraction – without oxidant addition – pH 1.0
Extractant | Extraction (%) |  |  |  | Separation factor |  | 
 | La | Ce | Pr | Nd | Ce/La | Ce/Pr | Nd/Pr
Cyanex® 923 | 98 | 100 | 99 | 99 | - | - | -
P507 | 7 | 76 | 34 | 36 | 44 | 6.2 | 1.1
D2EHPA | 54 | 95 | 91 | 89 | 17 | 2.6 | 1.1
Notes: TBP e básicos não apresentaram extração (<5%)
Extração seletiva de Ce, meio nítrico é mais oxidante, manteve o Ce que oxida na calcinação na forma +4
D2EHPA extrai mais, P507 mais seletivo

## Slide 18: Results - Nitric liquor
REE extraction – without oxidant addition at different pH without oxidant addition
Extractant | pH | Extraction (%) |  |  |  | Separation factor |  | 
 |  | La | Ce | Pr | Nd | Ce/La | Ce/Pr | Nd/Pr
P507 | 1,0 | 7 | 76 | 35 | 36 | 44 | 5.8 | 1.0
P507 | 2,0 | 26 | 89 | 80 | 80 | 24 | 2.2 | 1.0
D2EHPA | 0,5 | 25 | 88 | 69 | 69 | 22 | 3.4 | 1.0
D2EHPA | 1,0 | 54 | 93 | 88 | 89 | 16 | 2.6 | 1.0
D2EHPA | 1,5 | 86 | 99 | 98 | 98 | 20 | 2.2 | 1.0
Initial potential: 1460 mv
Notes: P507 – pH 1,0 melhor separação

## Slide 19: Results - Nitric liquor
REE extraction – with oxidant addition - high acidity liquor
Oxidant | Contact | Extraction (%) |  |  | 
 |  | La | Ce | Pr | Nd
None | 1st | <1 | 45 | <1 | <1
 | 2nd | <1 | 15 | <1 | <1
K2S2O8 | 1st | <1 | 45 | <1 | <1
 | 2nd | <1 | 16 | <1 | <1
AgNO3 | 1st | <1 | 44 | <1 | <1
 | 2nd | <1 | 19 | <1 | <1
K2S2O8 + AgNO3 | 1st | <1 | 95 | <1 | <1
 | 2nd | <1 | 5 | <1 | <1
Potential
Initial: 1460 mv
K2S2O8 + AgNO3 :1620 mv
Final: 1410 mV

## Slide 20: Conclusions
The experiments without the oxidation of cerium (III) to cerium (IV) indicated the difficulty in its separation from the other trivalent REE.
In nitric medium, cerium was preferentially extracted from the other rare earth elements. Using a mixture of potassium persulfate and silver nitrate as oxidizing and P507 as extractant, 99.9% recovery with 99.9% purity was achieved in two stages.

## Slide 21: Thank you for the attention