## Slide 1: Adsorption of simple molecules on metal oxides by ab initio calculations Application to the detection of gases
Caroline LAMBERT – MAURIAT
Vincent OISON, Laurent RAYMOND, Khalifa AGUIR, Roland HAYN
Thesis: Lama SAADI and Hela OUALI
6th International Conference and Exhibition on Materials Science and Engineering, September 12-14, 2016 Atlanta, USA

## Slide 2: Plan
Principle of gas sensor devices
Calculations method
Results
  WO3 surface: O3, NO2 and CO adsorption
  CuO and Cu2O surfaces: O3 adsorption
Conclusion & perspectives

## Slide 3: Principle of gas sensor devices
ab initio calculations to understand microscopic mechanisms for gas detection
Electrical resistivity variation as principle of sensor device
Si
Si
SiO2 + Si3N4
SiO2
Gas
Sensitive layer (MOx)
Pt-electrodes
50 nm
0.2 µm
1.7 µm
I (R) measurement

## Slide 4: Plan
Sensor devices: principle
Calculations method
Results
  WO3 surface: O3, NO2 and CO adsorption
  CuO and Cu2O surfaces: O3 adsorption
Conclusion & perspectives

## Slide 5: Principle
Bulk study by geometry optimization
  Cell parameters, bulk modulus,…
  Electronical properties: DOS (density of states)
              Surface building
                Choice of the orientation
                In the case of non-trivial orientation: new unit cell
                Creation of the supercell = cell calculation
              Adsorption study
                Molecule on surface into specific site
Surface
Vacuum
Slab
Surface

## Slide 6: siesta code
Self-consistent DFT method in the local density (LDA-LSD) and generalized gradient (GGA) approximations
Periodic Limit Conditions
Calculation in Reciprocal space
Brillouin zone sampling  -mesh grid
  Basis set
    Linear combination of numerical atomic orbitals (LCAO)
    Size: number of orbitals per atom
    Range: cutoff radii of orbitals
Ground-state energy E of the system (at T = 0 K) !
Siesta : Spanish Initiative for Electronic Simulations with Thousands of Atoms
a
b
c

## Slide 7: Plan
Sensor devices: principle
Calculations method
Results
  WO3 surface: O3, NO2 and CO adsorption
  CuO and Cu2O surfaces: O3 adsorption
Conclusion & perspectives

## Slide 8: Bulk WO3 (L. Saadi thesis)
a = 7.14 Å
b = 7.45 Å
c = 7.61 Å
Bulk primitive cell
Monoclinic group
32 atoms per cell (W8O24)
n-type semiconductor
Supercells: WnO3n (n = 64)
Cell parameters
 | a* = 2a (Å) | b* = 2b (Å) | c* = 4c (Å) | b (deg.)
LDA | 14.48 | 14.90 | 30.44 | 90.5
GGA | 14.96 | 15.32 | 31.40 | 90.4
Vacuum thickness 15 Å
-mesh grid:
Atomic electronic structure
W: [Xe]4f14 6s25d4 O: 1s2 2s22p4
Core electrons
norm-conserving pseudopotentials
Valence electrons
Wave functions localized on atomic nucleus

## Slide 9: Surface (001) of WO3
To conserve stoichiometry and electronic neutrality
reconstruction
Oxygen
Tungsten
Vacancy
Formation energy of surface (meV/Å2)
LDA | 41.3
GGA | 21.0
I.N. Yakovkin and al. Surface Science 610 (2007):
22 meV/Å2 by VASP (GGA) calculations on WO3 cubic phase
Formation enthalpy (eV)
 | O2-poor | O2-rich
LDA | -1.65 | +1.45
GGA | -1.36 | +1.28

## Slide 10: Surface (001) of WO3
Total electronic Density Of States (DOS)
Filling the bottom of conduction band n-doping

## Slide 11: O3 dissociation on WO3
∆H
Reaction:
 | LDA | GGA
∆H (eV) | - 2.54 | - 2.86
Exothermic
LDA/GGA agreement
Cancellation of oxygen vacancy
Increasing partial pressure of O3 decreases the number of oxygen vacancies
The conductance of WO3 sensitive layer is decreased

## Slide 12: Response to ozone
Conductance (Ω-1)
Time (min)
M. Bendahan et al. / Sensors and Actuators B 100 (2004) 320–324
Twork = 523 K

## Slide 13: NO2 dissociation
NO2 dissociation + NO adsorption
2) NO re-oxidation
 | ∆H |  | = + ∆H
LDA | - 0.47 | - 1.12 | - 1.59
GGA | - 0.50 | - 0.55 | - 1.05
 | ∆H |  | 
LDA | - 0.47 | - 1.12 | - 1.59
GGA | - 0.50 | - 0.55 | - 1.05
Wv
Transition state
Cancelling oxygen vacancy conductance decreasing

## Slide 14: Response to NO2
B. Fruhberger et al. / Sensors and Actuators B 76 (2001) 226-234

## Slide 15: CO oxidation
∆H
CO approaching
CO2 weakly interacting
CO oxidation on stoichiometric surface leads to oxygen vacancy formation
Reaction:
 | LDA | GGA
∆H (eV) | - 1.73 | - 1.52
Exothermic
LDA/GGA agreement
Generation of oxygen vacancy
The conductance of WO3 sensitive layer is increased

## Slide 16: Response to CO
M. Hübner et al. / Sensors and Actuators B 151 (2010) 103–106
As CO increasing, the resistance decreasing ( = conductance increasing)

## Slide 17: Plan
Sensor devices: principle
Calculations method
Results
  WO3 surface: O3, CO and NO2 adsorption
  CuO and Cu2O surfaces: O3 adsorption
Conclusion & perspectives

## Slide 18: Bulk CuO (H. Ouali thesis)
Bulk primitive cell
Monoclinic group
8 atoms per cell (Cu4O4)
Antiferromagnetic order on Cu
p-type semiconductor
 | a (Å) | b (Å) | c (Å) | Eg (eV) | µ (µB/Cu)
LDA+U | 3.403 | 4.660 | 5.098 | 1.37 | ± 0.62
GGA+U | 3.498 | 4.787 | 5.242 | 1.48 | ± 0.63
Exp. | 3.423 | 4.684 | 5.129 | 1.2 – 1.9 | ± 0.68
b = 80.46°

## Slide 19: Surface (111) of CuO
Primitive cell
Basis set transformation
96 atoms per supercell
Vacuum thickness 15 Å
-mesh grid:
Top view
Cu3 (3-coordinated Cu) named Cu1
Cu4 (4-coordinated Cu) named Cu2

## Slide 20: O3 dissociation on CuO
0 eV
– 1,03 eV
-0,81 eV
-1,27 eV
-1,15 eV
Reaction steps
GGA + U calculations

## Slide 21: Response to O3 / DOS
Time (s)
0 1,000 2,000 3,000 4,000 5,000 6,000
1,200
1,100
1,000
900
800
700
600
500
400
300
Resistance (Ω)
A. Bejaoui et al. / Sensors and Actuators B 190 (2014) 8—15
-2 -1 0 1
Twork = 523 K
EF in the valence band
p-doping increases
Diminution of the resistance

## Slide 22: Cu2O: Bulk and (111) surface (H. Ouali thesis)
Bulk primitive cell
C
6 atoms per cell (Cu4O2)
p-type semiconductor
 | a (Å) | Eg (eV)
LDA | 4.223 | 0.52
GGA | 4.353 | 0.27
Exp. | 4.270 | 2.0 – 2.7
(111) Surface -Top view
Basis set transformation
72 atoms per supercell
Vacuum thickness 15 Å
-mesh grid:

## Slide 23: Response to O3 /DOS
EF in the valence band
p-doping increases
Diminution of the resistance
Time (min)
Resistance (Ω)
Twork = 448 K
-2 -1 0 1 2
Density of electronic states

## Slide 24: Plan
Sensor devices: principle
Calculations method
Results
  WO3 surface: O3, NO2 and CO adsorption
  CuO and Cu2O surfaces: O3 adsorption
Conclusion & perspectives

## Slide 25: Conclusion & perspectives
Adsorption on (001) surface of WO3
  O3 & NO2
    molecule dissociation leads to vacancy cancelling
    conductivity decreases (by n-doping weakening)
  CO
    oxidation to CO2 leads to vacancy formation
    Conductivity increases (by n-doping enhancement)
O3 adsorption on (111) surface of CuO & Cu2O
    Non dissociative adsorption leads to p-doping enhancement
      Conductivity increases
    Desorption of O2 leaves adsorbed O and decreases p-doping
      Conductivity decreases when O3 flux is stopped
Perspectives
Expand this approach to others oxides (ZnO) and others molecules
Use adsorption energies as input for molecular dynamic simulation
Ab initio calculations allow to specify the mechanisms involved in the gas detection