## Slide 1
1National Research Council ‑ Institute for Membrane Technology (ITM–CNR) c/o The University of Calabria, cubo 17C, Via Pietro BUCCI, 87036 Rende (CS), Italy
2King Abdulaziz City for Science and Technology (KACST) (Saudi Arabia)
Catia Algieri1, Angelo Garofalo1, Laura Donato1, Enrico Drioli1, Alessandra Criscuoli1, Maria Concetta Carnevale1, Omar Alharbi2, Saad Aljlil2
MFI Zeolite Membranes for Water Desalination

## Slide 2
Seeding parameters studied:
Support pore size (70 and 200 nm)
Zeolite slurry concentrations (0.032; 0.07 and 0.1 wt.%)
The prepared membranes were characterized by means of:
Single gas permeation tests
Vacuum membrane distillation
IN THIS WORK
Tubular MFI (Silicalite) zeolite membranes were prepared by secondary growth method coupled with the cross-flow seeding procedure
MFI Zeolite | 
Silicalite | Hydrophobic (aluminum free)
ZSM5 | Hydrophilic

## Slide 3: Major current applications for zeolites in the form of powders or pellets
Aluminosilicate mineral
Stable at high temperatures (several hundred °C)
Well defined pore size (0.3-1.3 nm)
Over 176 different zeolites are known
Occur in nature as minerals and can also be prepared synthetically
Good adsorbents, ion-exchangers and catalysts
Zeolite is………….
Detergent powder
Zeolite beads (d= 4mm)
for drying of gas and
liquids
Zeolite A crystals act as
softeners (by ion-
exchange) in detergent
Zeolites can be used for catalytic cracking
Adsorbent
Catalyst

## Slide 4
Zeolite Membranes
Supported zeolite membranes
High selectivitiy
High thermal and chemical
stability
Applications
Separation membranes
Catalytic membranes
Chemical sensor
Thermoelectric devices
Zeolites
MFI, dpore=5.4× 5.6 Å
FAU, dpore= 7.4 Å
LTA, dpore= 4.0 Å

## Slide 5
Zeolite Membranes-Hurdles of a Commercialization
Reproducibility problems of the membrane synthesis
Inter-crystaline defects
Membrane cost (US $ 3000 per m2 installed membrane area !!!!!!!)
First large scale pervaporation unit designed by Mitsui Engineering and Shipbuilding (MES) in 2001
Bio ethanol de-hydration plant in UK

## Slide 6
* Kita et al., 6th ICIM Montpellier 2000
** Noack et al., Chemie Ingenieur Technik (73), 2001, 958-967
Commercial Membrane | aH2O/EtOH | aH2/CO2
NaA Mitsui * | 10.000 | 6.0
NaA Inocermic** | 10.000 | 5.6
Knudsen behavior for H2/CO2
Industrial produced membranes containing larger inter crystalline pores**
These pores are non selective in gas separation
In presence of water all pores - zeolite and inter crystalline- of hydrophilic NaA are filled with liquid water
Industrial NaA-membranes
Separation of water/ethanol by pervaporation

## Slide 7: Two Main Routes for the Preparation of Zeolite Membranes
Synthesis solution
Washing and
drying
Zeolite membrane
Growth
Seeding
Seeded Support
Growth
Support
Zeolite crystals
suspension
Sodium
hydroxide
Deionized
water
+
+
M . C. Lovallo and M. Tsapatsis AICHE J. 42 (1996) 3020.
Tetraethoxysilane
+
+
+
Optimization of nucleation and crystal growth
More reproducible than the in situ method
Tetrapropylammonium
hydroxide
One step method
Secondary growth method
Secondary growth

## Slide 8
Critical Step: SEEDING
More controllable seeding procedures described in literature involve the filtration of a zeolite water suspension through a porous support
Rubbing 1-2
Dip Coating 3-5
[1] K. Kusakabe, S. Morooka, Y. Kubo, JP10036114; [2] K. Kusakabe, T. Kuroda, S. Mooroka, J. Membr. Sci. 148 (1998) 13; [3] M.C. Lovallo, M. Tsapatsis, AICHE J. 42 (1996) 3020; [4] M.P. Bernal, G. Xomeritakis, M. Tsapatsis, Catal. Today 67 (1–3) (2001) 101; [5] S. Mintova, T. Bein, Adv. Mater. 13 (24) (2001) 1880; [5] M. Pera-Titus, J. Llorens, F. Cunill, R. Mallada, J. Santamarıa, Catal. Today 104 (2005) 281. [6] S. Nakao, I. Kumakiri, T. Yamaguchi, T. Ando, JP2001097715. [7] A. Huang, Y.S. Lin, W. Yang, J. Membr. Sci. 245 (2004) 41. [8] Y. Takata, T. Tsuru, T. Yoshioka, M. Asaeda, Micropor. Mesopor. Mater. 54 (2002) 257.
Secondary Growth

## Slide 9
Cross-flow filtration of a water suspension of zeolite seeds through a porous support
Support rotation along its longitudinal axis
Support tilting with respect to the horizontal plane
a-Al2O3 tubular supports (IKTS, Germany) |  |  | 
dpore [nm] | I.D. [mm] | O.D. [mm] | Leff[cm]
70 200 | 7 | 10 | 10
Patent: C. Algieri, P. Bernardo, G. Barbieri, E. Drioli, “Procedimento per la produzione di membrane zeolitiche su supporti porosi tubolari”, RM 0001388750, 2011.
C. Algieri, P. Bernardo, G. Barbieri, E. Drioli, , Micropor. Mesopor. Mater. 119 (2009) 129.
Novel Seeding Procedure for Preparing Tubular MFI Membranes

## Slide 10
Operating Conditions Used During the
Membrane Synthesis
Seeds | Synthesized Silicalite crystals (~ 500 nm)
Zeolite concentration | 0.032 wt. %; 0.07wt. % and 0.1 wt.%
pH suspension | 7.0
Tilting | 2°
Rotation | 0.05 rpm
Feed flow rate | 8 ml min-1
Temperature | 23 °C
Time | 36 minutes
Pore size (α-Al2O3 support) | 70 and 200 nm
Seeding procedure
Molar ratio | 4 SiO2: 0.9 NaOH : 0.9 TPAOH : 1000 H2O
Solution aging | 12 hours
Temperature | 175 °C
Time | 70 hours
Hydrothermal treatment [1]
[1] G. Xomeritakis, A. Gouzinis, S. Nair, T. Okubo, M. He, R. N. Overney, M. Tsapatsis, Chem. Eng. Sci. 54 (1999) 3521.

## Slide 11
The calcination heating profiles in static air was performed at very low heating rates to minimize the defects formation.
Membranes synthesis was carried out in presence of the organic template, therefore calcination of the membranes was required for removing the TPAOH [1].
MFI Membrane Preparation: Calcination Step
[1] E. R. Geus and H. van Bekkum, Zeolites 15 (1995) 333.
MFI Topology
During calcination defects are created into the zeolite layer considering the different thermal expansion coefficients of alumina and zeolite

## Slide 12
The prepared MFI membranes were characterized before and after calcination by single gas (N2 and CO2) permeation tests at room temperature, according to the pressure drop method [1] and by setting a trans-membrane pressure difference without a sweep gas.
Single Gas Permeation Tests
[1] T. Matsufuji, N. Nishiyama, K. Ueyama, M. Matsukata, Catal. Today 56 (2000) 199.
ΔP = 0.4 – 2.8 bar

## Slide 13
Gas Tests Before Calcination
Sample | Crystals size (nm) | Support pore size (nm) | Zeolite slurry concentration (wt.%) | ∏N2 (µmol m-2 sec-1 Pa-1)
ZM1 | 500 | 70 | 0.032 | Gas-Tight
ZM2 |  |  |  | 
ZM3 |  |  |  | 
ZM4 |  |  |  | 
ZM5 |  |  | 0.07 | 1.9×10-3
ZM6 |  |  | 0.1 | 7.5×10-3
ZM7 |  | 200 | 0.032 | 3.2×10-2
ZM8 |  |  | 0.07 | 8.3×10-2
ZM9 |  |  | 0.1 | 5.4×10-1
MFI membranes synthesized using larger support pore size (200 nm) were permeable indicating presence of defects
Secondary growth method coupled with the cross-flow seeding procedure, using support of 70 nm and zeolite slurry concentration of 0.032 wt.% is a potential route to synthetize MFI zeolite membranes almost defects free

## Slide 14
The solution infiltration is less pronounced for 70 nm supports [1]
More homogeneous
zeolite layer
Better permeation
properties
Low concentration of zeolite water slurry permits to obtain sufficient uniform layer avoiding the formation of crystal clusters on the support surface [2]
[1] J.D.F. Ramsay et al., FOAA6, 24-28 May 1998, Elsevier.
[2] A. Huang, Y. S. Lin, W. Yang, Synthesis and properties of A-type zeolite membranes by secondary growth method with vacuum seeding, J. Membr. Sci. 245 (2004) 41-51.
EDX analyses showed the presence of siliceous species in the support pores
due to the synthesis solution infiltration during the hydrothermal treatment

## Slide 15
Gas Tests After Calcination
Sample | Crystals size (nm) | Calcination program (°C) | ∏N2 (µmol m-2 sec-1 Pa-1) | ∏CO2 (µmol m-2 sec-1 Pa-1) | iSF CO2/N2
ZM1 | 500 | 480 | 1.7 | 3.8 | 2.2
ZM2 |  |  | 1.7 | 3.9 | 2.3
ZM3 |  |  | 1.2 | 3.1 | 2.6
ZM4 |  |  | 1.3 | 3.2 | 2.5
THESE MEMBRANES
Gas Separations
Desalination process

## Slide 16
Membrane Post-Treatments
New cross-flow filtration
Dip-coating with polydimethylsiloxane (PDMS, Dow Corning) [1]
Seeds | Synthesized silicalite crystals (500 and 200 nm)
Zeolite concentration | 0.032 wt. %
pH suspension | 7.0
Tilting | 0°
Rotation | 0.05 rpm
Temperature | 23 °C
Time | 5 hours
polydimethylsiloxane
A new cross-flow filtration through the calcined membranes of a zeolite suspension was carried out using crystals with two different size (500 nm and 200 nm)
[1] J. M. S. Henis and M. K. Tripodi, U. S. Patent 4,230,463 (1980).

## Slide 17
Sample | Post treatment | ∏N2 (µmol m-2 sec-1 Pa-1) | ∏CO2 (µmol m-2 sec-1 Pa-1) | iSFCO2/N2
ZM1 | Cross flow * | 1.1 | 3.4 | 3.1
ZM2 | Cross flow ** | 3.2x10-1 | 1.1 | 3.4
ZM3 | Dip coating *** | 2.6x10-5 | 1.7x10-4 | 6.5
ZM4 | Dip coating **** | 1.4x10-4 | 5.3x10-4 | 3.9
Gas Tests After Post-Treatments
* cross flow with crystals of ~ 500 nm
** cross flow with crystals of ~ 200 nm
*** dip coating repeated 4 times
**** dip coating repeated twice
MFI membranes cured with the cross-flow using crystals of about 500 nm exhibited a little improvement of the permeation properties
The cross-flow with smaller crystals (~200 nm) produced a significant decrease of the N2 and CO2 permeances with a little enhancement of the ideal separation factor. These results evidenced that not all defects were sealed
MFI membranes “coated” four times with the PDMS exhibited an improvement of the membrane quality (higher ideal separation factor and low permeances)
Two coating with the PDMS determined an increase of the gas permeances with a decrease of the ideal separation factor

## Slide 18
Vacuum Membrane Distillation (VMD)
The possibility to reject monovalent ions with MFI membranes (pore size about 5.5 Å) was investigated in Membrane Distillation Process
Feed side (heated water) in direct contact with the inner membrane surface
Permeate was vapor under reduced pressure condensed in a separate external device
Scheme of the VMD set-up
Ion | Hydrated Diameter Å
H2O | 5.6
Li+ | 7.6
Na+ | 7.2
K+ | 6.6
Mg2+ | 8.6
Ca2+ | 8.2
OH- | 6.0
Cl- | 6.6
NO3- | 6.8
Water flux vs. operating time (ZM2 membrane)
Feed | Feed flow rate (L h-1) | P vacuum (mbar) | T feed (°C)
Distilled water | 75 | 4.5 | 60
Operating conditions

## Slide 19
Sample | Post treatment | Feed | Time (h) | Permeation flux (Kg m-2 h-1) | Rejection (%)
ZM2 | Cross flow | 0.2 M NaCl solution | 5 | 7.6±0.4 | 98.8±0.1
 |  | 0.6 M NaCl solution | 5 | 7.0±0.2 | 98.6±0.1
 |  | 1.2 M NaCl solution | 5 | 5.2±0.2 | 98.4±0.2
Vacuum Membrane Distillation (VMD)
Feed | Feed flow rate (L h-1) | P vacuum (mbar) | T feed (°C)
0.2 M NaCl solution | 75 | 4.5 | 60
0.6 M NaCl solution | 75 | 4.5 | 60
1.2 M NaCl solution | 75 | 4.5 | 60
Operating conditions
Membrane cured with PDMS were not suitable for VMD because permeate fluxes were not appreciable

## Slide 20
Vacuum Membrane Distillation (VMD)
Feed | Feed flow rate (L h-1) | P vacuum (mbar) | T feed (°C)
Distilled water | 75 | 4.5 | 60
Operating conditions
Increasing the NaCl concentration in the feed increse the driving force of NaCl across the membrane [1]
[1] A. Garofalo , L. Donato , E. Drioli , A. Criscuoli , M.C. Carnevale, O. Alharbi , S.A. Aljlil , C. Algieri, Supported MFI zeolite membranes by cross flow filtration for water treatment, Separation and Purification Technology 137 (2014) 28–35.
Other four membranes prepared with the same characteristics of those gas-tight and without post-treatments are characterized in VMD

## Slide 21
Vacuum Membrane Distillation (VMD)
Water flux after salt treatment and washing procedure

## Slide 22
Membrane Type | Process | Feed (NaCl solution) | Permeation flux (Kg m-2 h-1) | Rejection (%) | References
Silicalite | RO | 0.1 M | 0.16 | 22 | [1]
Silicalite | RO | 0.1 M | 0.12 | 77 | [2]
ZSM-5 | RO | 0.1 M | 1.13 | 93 | [3]
Silicalite | RO | 0.01 M | 1.2×10-3 | 97 | [4]
Membrane Type | Process | Feed (NaCl solution) | Permeation flux (Kg m-2 h-1) | Rejection (%) | References
Silicalite | VMD | 0.2 M | 17.5±0.5 | 98.8±0.1 | This work
Silicalite | VMD | 0.6 M | 13.3±0.4 | 98.5±0.2 | This work
Silicalite | VMD | 1.2 M | 11.0±0.2 | 98.1±0.1 | This work
ZSM-5 | PV | 0.7 M | 0.7 | 99 | [5]
Silicalite | PV | 0.6 M | 3.0 | 98 | [6]
[1] L. Li, J. Dong, T. Nenoff, R. Lee, Desalination, 170 (3) (2004) 309–316. [2] L.X. Li, J.H. Dong, T.M. Nenoff, R. Lee,, J. Membr. Sci. 243 (2004) 401-404. [3] L. Li, N. Liu, B. McPherson, R. Lee,, Ind. Eng. Chem. Res.46 (2007) 1584-1589. [4] L. Li, N. Liu, B. McPherson, R. Lee, Desalination 228 (2008) 217-225. [5] M. C. Duke, J. O’Brien-Abraham, N. Milne, B. Zhu, J.Y.S. Lin, J. C. Diniz da Costa,, Sep. Purif. Technol. 68 (2009) 343-350. [6] M. Drobek, C. Yacou, J. Motuzas, A. Julbe, L. Ding, J. Da Costa, J. Membr. Sci. 415-416 (2012) 816-823.
Comparison with Literature Data

## Slide 23
Secondary growth method coupled with the cross flow seeding procedure was used to prepare uncalcined defect free supported MFI membranes.
Curing treatments are used to seal the defects into the zeolite layer due to the calcination
Membranes treated with the PDMS could be suitable for gas separation process. A further improvement could be obtained varying both PDMS solution concentration and number of coating
It was demonstrated the possibility to use MFI zeolite membranes in vacuum membrane distillation process.
Membrane performance exhibited good results in terms of fluxes and salt rejections (~ 98.5 %).
C O N C L U S I O N S

## Slide 24
Thanks for Your Attention
Gracias por su Atención
Kiitos Huomiota
感謝您的關注
Grazie per l’Attenzione
شكرا لكم على اهتمامكم
आपका ध्यान के लिए धन्यवाद
당신의주의를위한 감사합니다
Merci pour Votre Attention
The authors gratefully acknowledge the support of the King Abdulaziz City for Science and Technology (KACST) for funding the research Project 895/33 entitled “Preparation and Characterization of Zeolite Membranes for Water Treatment”.