## Slide 1
Ece Bayrak, Burak Ozcan, Cevat Erisken
10th World Congress and Expo on
Cell & Stem Cell Research
New York, NY
March 21, 2018
Human Bone Marrow Stem Cell Behavior on Biomimetic Nanofiber Composites for Tendon-Bone Interface Regeneration
Notes: I would first like to thank the conference organizers for allowing us to present our research here today and I’d also like to thank my co-authors for their contribution to this research

## Slide 2
Tendon-to-Bone Interface
Rotator cuff tears are the most common injuries of the shoulder
  Over 250,000 repairs anually in U.S. (Gulotta et al., 2009)
 | Tissue | Cells | Composition
1 | Tendon | Fibroblasts | Collagen type I,III
2 | Non-Mineralized Fibrocartilage | Ovoid Chondrocytes | Collagen type I, II Proteoglycans
3 | Mineralized Fibrocartilage | Hyperthropic Chondrocytes | Collagen type I, X
4 | Bone | Osteoblasts Osteocytes Ostoclasts | Collagen type I
Lu and Thomopoulos, 2013
Successful repair is difficult with failure rates between 20% and 94% (Vitale et al, 2007; Galatz et al., 2004)
Injuries to rotator cuff often take place at the insertion, where a fibrocartilaginous transition is present (Iannotti et al., 1994; Benjamin&Ralphs, 1998)
Notes: This study was motivated by the fact that rotator cuff tears are the most …..
One of the characteristics of interface tissue …..
Put the table (rotator cuff)……
Font size ……………

## Slide 3
Mechanical strength of tendon-bone interface is determined partly by mineral compositions (Thomopoulos et al. 2003)
  Tendon tissue possesses weaker mechanical properties as compared to bone
  Mechanical properties change gradually at the interface
Rotator Cuff Tendon Repair
A better understanding of cell-material interactions is needed for scar-free healing of rotator cuff tears!
  Rotator cuff tears do not heal completely due to their complex anatomy and extended range of motion of the shoulder joint (Frank et al., 1997)
Notes: Genin,thomopoulos tendon-bone interface ortak makale
Journal of biophysical properties (?)

## Slide 4
Study Objectives and Hypothesis
Hypothesis:
A graded PCL scaffold incorporated with bioactive agents (TGF-β3, CTGF and nHA) can regulate the stem cells in terms of differentiation to form native-like interface tissue
Objectives:
Fabricate PCL-based, align scaffolds containing
  nHA, where concentrations of nHA change gradually
  TGF-β3 and CTGF
Characterize these scaffolds
Perform release of TGF- β3 and CTGF from nanofiber scaffolds
Evaluate stem cell behavior on the scaffolds
PCL(Polycaprolactone), TGF-β3(Transforming Growth Factor-β3, CTGF(Connective Tissue Growth Factor), nHA(nanoHyrdoxyapatite)

## Slide 5
Rationale for ingredients
TGF-β3 was found to be upregulated during TB insertion development
CTGF was shown to be sufficient to differentiate mesenchymal stem cells into tendon specific cells
nHA is the major mineral component of bone tissue

## Slide 6
Materials and Methods
Solution Preparation
PCL
  20% PCL (1g/5mL,Sigma, Mw 80.000) solution was prepared by using DMF/DCM with the volume ratio of 3:2 (vortex, overnight)
  PCL/nHA
    20% nHA (0.2g/5mL, Sigma) first dissolved in little amount of DMF (1h sonication), then added to PCL solution (1h sonication, 1h vortex)
    PCL/BSA/TGF-β3
      10% BSA (Sigma) added to 20% PCL solution (1h vortex)
      40 µL TGF-β3 (RayBiotech, Inc.) added (1h vortex)
      PCL/BSA/CTGF
      10% BSA (Sigma) added to 20% PCL solution (1h vortex)
      40 µL CTGF (RayBiotech, Inc.) added (1 h vortex)

## Slide 7
Materials and Methods
PCL/nHA Graded
PCL/TGFβ3 and PCL/CTGF Uniform Scaffold Fabrication
  Scaffolds were fabricated by multijet electrospinning of prepared solutions. Aligned fibers were obtained by using a rotating drum as the collector.
Groups
20%PCL/nHA
20% PCL / 10% BSA / TGF-β3
20% PCL / 10% BSA / CTGF
PCL-only (mL/h) | PCL-nHA (mL/h) | Total Flow rate (mL/h)
1.00 | 0.00 | 1.00
0.86 | 0.14 | 1.00
0.72 | 0.28 | 1.00
0.58 | 0.42 | 1.00
0.44 | 0.56 | 1.00
0.30 | 0.7 | 1.00
0.16 | 0.84 | 1.00
0.00 | 1.00 | 1.00

## Slide 8
Materials and Methods
Scaffold Characterization
  Fiber Diameter (SEM and ImageJ, n=3)
  Pore size (SEM and ImageJ, n=3)
  Particle size (SEM and ImageJ n=3)
  Thermogravimetric Analyses (TGA, n=3)
  Mechanical properties at 5 mm/min (Instron, n=3)
  Release study (Raybiotech, n=3)
  EDS spectrum (SEM)
TGF-β3 and CTGF Release Study
  1x1 cm scaffolds were immersed in 1.5 mL PBS (n=3)
  PBS samples were collected in Days 3, 7, 14 and 28
  TGF-β3 and CTGF ELISA tests were performed (Thermo Scientific).

## Slide 9
Diameter distribution of nHA-rich side
Diameter distribution of PCL-rich side
PCL/nHA Scaffold: Diameter Distribution
nHA-rich side
Avg: 459±241 nm
PCL-rich side
Avg: 361±179 nm
*p<0.05

## Slide 10
PCL/nHA Scaffold: Pore Size Distribution
Pore size distribution of nHA-rich side
Pore size distribution of PCL-rich side
Pore size comparison of PCL and nHA-rich sides
nHA-rich side
Avg: 2.86±0.51 µm
PCL-rich side
Avg: 2.51±0.10 µm

## Slide 11
PCL/nHA Scaffold:
Thermogravimetric Analyses

## Slide 12
PCL/nHA Scaffold: Particle Diameter & EDS
Analyses
nHA particles are bigger than ≈ 100 nm
nHA particles are smaller than 800 nm

## Slide 13
PCL/nHA Scaffold: Mechanical Properties
Notes: Strain @ break uç verileri çıkar.

## Slide 14
PCL/TGF-β3 and PCL/CTGF Scaffolds:
Diameter Distribution
PCL/BSA/TGF-β3
Avg: 334±386 nm
PCL/BSA/CTGF
Avg: 211±233 nm

## Slide 15
PCL/TGF-β and PCL/CTGF Scaffolds:
Release Study
CTGF Cumulative Release
TGF-β3 Cumulative Release

## Slide 16
Graded Scaffolds
Graded Scaffolds and Cell Behavior

## Slide 17
Graded PCL/CTGF/TGFb3/nHA Scaffold

## Slide 18
Graded PCL/CTGF/TGFb3/nHA Scaffold
*
*
Group
SEM Image
Diameter distribution

## Slide 19
Graded PCL/CTGF/TGFb3/nHA Scaffold
hBMSC Behavior
Cell seeding: 20K cells/scaffold (Gift from GATA)
Medium: 1% FBS, 1% P/S, 1% NEAA, 0.1% AMP-B
Cell proliferation: EZQuant dsDNA Quantitation Kit
Total Collagen: Total Collagen Assay (Biovision, Alfagen)

## Slide 20
Graded PCL/CTGF/TGFb3/nHA Scaffold
Time Point (day)
hBMSC Proliferation

## Slide 21
Graded PCL/CTGF/TGFb3/nHA Scaffold
Time Point (day)
Collagen/cell (pg)

## Slide 22
Discussion: PCL/nHA Scaffold
Mean fiber diameters are comparable with native tissue
nHA-rich side
Avg: 459±21 nm
PCL-rich side
Avg: 361±9 nm

## Slide 23
Discussion: TGF-β3 and CTGF Release Study
According to Xu et. al., 2014, CTGF release is 8.7% on
Day 3 and 10.4% at the end of 1 month using PCL
In our study; 8.0% CTGF release on Day 3 and 26.8% at the end of 1 month period
According to Erisken et. al. 2008, TGF-β3 release is 9% at day 3 using PLGA.
In our study; a burst release withTGF- β3, 54.4% on the first three days and 81.4% relase at the end of one month

## Slide 24
Discussion: Graded scaffolds
No difference between scaffold groups in terms of cell proliferation
No effect of scaffold type on collagen production

## Slide 25
Conclusions & Future Directions
Future work:
Histology for location-dependent mineral deposition (Alizarin Red), GAG production (Alcian Blue) and Collagen production (Picrosirius red)
Scaffold incorporated with nHA:
Fiber diameter increased
Mechanical properties increased
No significant difference on pore size
Scaffold incorporated with growth factors:
No significant difference on diameter
Burst release of TGF-β3
Regular release pattern for CTGF
No effect on cell proliferation and collagen production

## Slide 26
Acknowledgement
Funding resources
  The Scientific and Technological Research Council of Turkey (Project # :115C001)
  TOBB University of Economics and Technology
THANK YOU!