## Slide 1
Multidimensional Mass Spectrometry Methods for Synthetic Polymer Analysis
Chrys Wesdemiotis
The University of Akron, Departments of Chemistry and Polymer Science, Akron, OH 44325
International Summit on
Current Trends in Mass Spectrometry
July 13-15, 2015 New Orleans, USA
Notes: 30 slides (including the title slide)

## Slide 2
Mass spectrometry (MS): chemical analysis
based on mass (m/z) measurement
analyte
molecular
ions
The m/z value of the molecular ions
reveals the composition of the analyte.
MS
ionization
gas-phase
Key step

## Slide 3
New ionization methods (MALDI, ESI, DESI, APCI) have enabled the MS analysis of a wide range of synthetic polymers and are now widely used to determine:
the compositional heterogeneity of new polymers
the identify of chain end groups
molecular weight distributions
functionality distributions
detection of minor products with exceptionally high sensitivity
Structural identification or confirmation - Insight on polymerization mechanisms - Assessment of commercial viability

## Slide 4
Challenges in mass-based analysis
Polymerizations may create complex mixtures that are impossible to characterize by 1-D MS due to discrimination effects (in ionization or detection).
Isobaric components and isomeric architectures cannot usually be distinguished by m/z measurement alone.
With ESI, overlapping charge distributions complicate
mass determination and, hence, composition assignments.
Such problems can be addressed by 2-D MS (tandem mass spectrometry, MS2), and/or by interfacing MS with a separation method either before (LC-MS) or after ionization (ion mobility mass spectrometry, IM-MS).

## Slide 5
Tandem (2-D) mass spectrometry
Characterization of individual end groups
Analysis of (co)polymer repeat units & sequences
Differentiation of polymer architectures (for example,
macrocycle vs. tadpole, or linear vs. branched)
C. Wesdemiotis, N. Solak, M.J. Polce, D.E. Dabney, K. Chaicharoen, B.C. Katzenmeyer,
Mass Spectrom. Rev. 30 (2010) 523-559

## Slide 6
Tandem (2-D) mass spectrometry of polymers
MS-1 stage
Reaction
MS-2 stage
One oligomer ion,
among those formed
by MALDI or ESI,
is selected
This ion is
induced to
fragment.
The fragments are
mass-analyzed to
give the MS2
spectrum.
The structure (sequence) of the oligomer is determined
based on the types of fragments observed.

## Slide 7
Tandem mass spectrometry of polymers
Characterization of individual end groups
Analysis of (co)polymer repeat units & sequences
Differentiation of polymer architectures (for example,
macrocycle vs. tadpole, or linear vs. branched)
C. Wesdemiotis, N. Solak, M.J. Polce, D.E. Dabney, K. Chaicharoen, B.C. Katzenmeyer,
Mass Spectrom. Rev. 30 (2010) 523-559

## Slide 8
1000
1500
2000
2500
3000
3500
4000
m/z
2070.5 (19-mer)
Polystyrene
-C5H9 and -C9H9
end groups
MALDI-MS
n=10
12
14
16
18
20
22
24
26
28
30
32
34
36
Ag+



## Slide 9
250
500
750
1000
1250
1500
1750
2000
m/z
280
314
384
419
488
*
*
*
*
*
*
*
*
*
*
*
*
*
*
*
*
*
b3•
z2•
b2•
J2•
K3
z1•
b1•
^
^
^
^
^
^
^
^
^
^
^
^
^
^
^
^
207
2270.5
*
^
m/z 2270.5 (19-mer)
MALDI-MS2
an terminal fragments containing the α end group
yn terminal fragments containing the ω end group
Ag+
Fragmentation pattern for linear PS chains: dominant low-mass fragments and less abundant medium- and high-mass fragments with individual end groups
(fragments revealing the individual α and ω chain ends)

## Slide 10
500
1000
1500
2000
m/z
111
223
319
202
z1●
b1●
b2●
Polystyrene
an
yn
terminal
fragments
linear structure
596
651
909
964
2375.5
2271
[21-mer + Li]+
K3
J2●
Chain-end functionalization or cationization do not change the fragmentation pattern.
*
^
*
*
*
*
*
*
*
*
*
*
*
*
*
*
*
^
^
^
^
^
^
^
^
^
^
^
^
^
^
^
^
*
MALDI-MS2
Li+

## Slide 11
500
1000
1500
m/z
b1+
1892.8
b1•
J2•
b2•
K3
a4
a5
a6
a7
a8
a6b
b5
b6
b7
b8
a9
b9
b4
a7b
a8b
K3μ
a9b
K2
bn series with the
in-chain substituent
[15-mer + Ag]+
An in-chain functional group leads to a unique fragmentation pattern and, thus, can be differentiated from a chain-end group.
MALDI-MS2
in-chain substituted structure
Polystyrene

## Slide 12
2658.5
192.6
2555.7
2451.6
2347.4
2243.3
2139.1
2033.8
1929.8
1811.6
1707.4
1603.4
1499.3
1395.2
1291.1
1187.0
1082.9
978.8
874.7
770.6
Polystyrene
500
1000
1500
2000
m/z
302
419
[23-mer + Ag]+
-104
-104
-104
-104
Cyclic architectures also yield a distinct fragmentation pattern, based on which they can be conclusively identified.
cyclic structure
n-1
C. Wesdemiotis, N. Solak, M.J. Polce, D.E. Dabney, K. Chaicharoen, B.C. Katzenmeyer, Mass Spectrom. Rev. 30 (2011) 523
A.M. Yol, D.E. Dabney, S.-F. Wang, B.A. Laurent, M.D. Foster, R.P. Quirk, S.M. Grayson, C. Wesdemiotis, J. Am. Soc. Mass Spectrom. 24 (2013) 74
MALDI-MS2

## Slide 13
500
1000
1500
2000
m/z
2658.5
chain-end substituted structure
macrocyclic structure
Differentiation of polymer architectures by MS2
250
500
750
1000
1250
1500
1750
2000
m/z
2270.5
n-1
Abundant low-mass fragments
Abundant high-mass fragments
A.M. Yol, D.E. Dabney, S.-F. Wang, B.A. Laurent, M.D. Foster, R.P. Quirk, S.M. Grayson, C. Wesdemiotis, J. Am. Soc. Mass Spectrom. 24 (2013) 74

## Slide 14
500
1000
1500
m/z
1892.8
in-chain substituted structure
Differentiation of polymer architectures by MS2
500
1000
1500
2000
m/z
2375.5
chain-end substituted structure
500
1000
1500
2000
m/z
2658.5
macrocyclic structure
Abundant low-mass fragments
Abundant high-mass fragments
Fragment distribution
in mid-mass range

## Slide 15
Chromatographic separation
(Most efficient for amphiphilic polymers)

## Slide 16
V. Scionti, B.C. Katzenmeyer, N. Solak Erdem, X. Li, C. Wesdemiotis, Eur. J. Mass Spectrom. 18 (2012) 113.
N. Solak Erdem, N. Alawani, C. Wesdemiotis, Anal. Chim. Acta 808 (2014) 83-93.
The most widely used HPLC method for synthetic polymers is gel permeation chromatography (GPC), which separates according to hydrodynamic volume (size).
Interactive LC (adsorption-mode LC), which separates based on chemical composition, functionality and mass, is less common in polymer analysis. Nevertheless, it is ideally suitable for the separation of oligomer mixtures with constituents of different polarities.
Online LC-MS of polymers

## Slide 17
PEO-glucam sesquistearate (nonionic surfactant)
R = (stearate) or H
navg ≈ 5; ~1.5 mol stearate per mol surfactant
PEO-glucam mono and multiple stearates
PEO + stearates
Generally a mixture of:
V. Scionti, B.C. Katzenmeyer, N. Solak Erdem, X. Li, C. Wesdemiotis, Eur. J. Mass Spectrom. 18 (2012) 113.
N. Solak Erdem, N. Alawani, C. Wesdemiotis, Anal. Chim. Acta 808 (2014) 83-93.

## Slide 18
PEO
aggregates
hydrophobicity
RP-UPLC
Solvent A: 2.55 mM NH4OAc in 97% H2O / 3% MeOH – Solvent B: MeOH – Flow rate 0.4 mL/min
A / B : 100:0 → 60:40 (0-2 min); 60:40 → 40:60 (2-3 min); 40:60 → 0:100 (3-7 min); 100% MeOH (>7 min)
1
PEO-glucam sesquistearate (nonionic surfactant)
0.41
0.00
2.75
5.50
8.25
11.00
2.74
6.48
6.66
7.83
9.66
Time [min]
PEO
PEO-glucam monostearate
PEO
monostearate
PEO-glucam distearate
PEO
distearate
PEO-glucam tristearate
Notes: 2.74 min = longer chains that cannot interact with each other strongly enough to form association products
HPLC: particle size 5 u, pressure 6000 psi (~400 bar)
UPLC: particle size 1.7 u, pressure up to 15000 psi (1034 bar)

## Slide 19
m/z
300
675
1050
1425






























✚
✚
✚
✚
✚
✚
✚
✚
✚
✚
✚
✚
✚
✚
✚
754.498
44 Da
1
Accurate m/z: [M + 2NH4]2+ of
(PEO)n-glucam monostearate
with n = 26
3+
2+
1+
LC-MS
6.48 min
1284.82
645.39
333.2
245.2
*311.3
100
600
1100
1600
m/z
787.544
LC-MS2
1 stearic
acid loss
[M + 2Li]2+
(n = 28)
1568.09
44
Da
PEO-glucam monostearate
1
LC-MS & LC-MS2 analysis of peak
-284

## Slide 20
200
400
600
800
1000
1200
1400
1600
1800
m/z
756.420
614.291
1790.116
1506.867
1222.553
898.549
245.2
333.2
*311.3
44
Da
2 x 284 Da
stearic acid
loss
PEO-glucam distearate
LC-MS2
-284
-284
2
LC-MS & LC-MS2 analysis of an oligomer in peak
[M + 2Li]2+
(n = 29)
Complete mixture separation & characterization based on polarity.

## Slide 21
Faster separation with ion mobility mass spectrometry (IM-MS)

## Slide 22
IM-MS using an
ESI-Q/ToF mass spectrometer
ion mobility region
trap
All ions coming from the ion source, or ions selected by Q can be gated to the IM cell, where they travel in an electric field against the flow of N2 gas. This causes separation based on charge and collision cross-section, a function of size (mass) and shape.
IM
transfer
LC
system

## Slide 23
Differentiating 2D and 3D supramolecular
architectures by ESI-IM-MS & gMS2
core ligand T6
rim ligand R3
[T61–Zn12–R36]
[R32–Zn12–R36]
ZnII
ZnII
(PF6‾ counterions)
J.-L. Wang, et al., J. Am. Chem. Soc. 133 (2011) 11450;
X. Lu et. al., J. Am. Chem. Soc. 136 (2014) 18149
2D
wheel
3D
wheel
core ligand R3

## Slide 24
3D spoked wheel
ESI-MS
ESI-IM-MS
Confirms molecular composition and mass (12985.7 Da)
Confirms isomeric purity (single architecture)
[R32–Zn12–R36]

## Slide 25
Architecture and stability
insight on 2D vs. 3D wheel
1603 Å2
[T61–Zn12–T36]
12726.4 Da
[R32–Zn12–R36]
12985.7 Da
2D
3D
1550 Å2
CCS
A lower CCS (collision cross-section) is found for the 3D wheel, despite its higher mass, corroborating its compact, more globular architecture). TEM cannot detect such relatively small differences.
Meanwhile, the lower disappearance Ecm for the 3D wheel indicates a lower thermal stability, consistent with the noncovalent binding in its core.
1.57 eV
1.35 eV
Ecm (11+)

## Slide 26
Top-down approaches for large, labile, or not directly ionizable materials via
ESI or ASAP coupled with IM-MS / MS2
ASAP = analysis of solids at atmospheric pressure
(mild thermal degradation in an atmospheric pressure chemical ionization source)

## Slide 27
Thermoplastic polyurethanes
diisocyanate
diol
chain
extender
+
hard segments (m)
soft segments (n)
polyol
(small diol)
(aromatic or aliphatic;
linear or cyclic)
(polyether diol;
polyester diol;
PDMS diol)
Notes: Elastollan (BASF)
Source T = 120 oC
Desolvation T = 250 oC (at 1200 l/h)
WH = 9.5 V
WV = 300 m/s

## Slide 28
ASAP-IM-MS of a polyurethane PU-1; elastollan
450 oC
a
b
c
d
500
1000
1500
m/z
10
5
drift time (ms)
Mild thermal degradation → APCI → IM separation (by CCS) → ToF mass analysis (m/z)

## Slide 29
ASAP-IM-MS of PU-1; high T (450 oC) products
120
220
320
420
520
m/z
132
106
180
194
208
224
314
322
430
536
564
592
556
268
250
412
484
340
1 hard + n soft segment units
MDI
72
Da
IM region
a
72-Da repeat unit and m/z values are consistent with poly(tetrahydrofuran), PTHF, as the soft segment and 1,4-butanediol, BDO, as the chain extender (structures confirmed by MS2).
soft segment
hard segment
(n = 1-3)
hard segment
MDI
BDO
72
Da
72
Da
MDI

## Slide 30
150
200
250
300
350
m/z
400
450
500
484.3
485.3
413.2
469.3
456.3
426.3
384.2
340.2
278.2
368.2
222.1
224.1
232.1
322.2
250.1
413.2
322.2
340.2
MDI
1 hard + 2 soft segment units
Verification of ASAP products from PU-1 by MS2

## Slide 31
ASAP-IM-MS of PU-1; high T (450 oC) products
IM region
b
675.5
772.5
680
720
760
800
840
m/z
709.6
872.6
860.6
879.7
*
*
*
844.6
#
#
#
%
%
%
$
$
$
739.6
811.7
723.6
795.7
867.8
793.7
865.8
*
1 hard + n (5-7) soft segment units
#
soft segment chains
$
%
soft segment chains
Series with a 72-Da repeat unit

## Slide 32
ASAP-IM-MS PU-1; high T (450 oC) products
IM region
c
592.6
636.5
600
800
m/z
Irganox 1098

## Slide 33
ASAP-IM-MS of PU-1; high T (450 oC) products
700
800
900
1000
1100
1200
m/z
656.5
680.3
700.4
723.6
739.6
772.5
793.6
795.7
811.7
844.6
865.7
867.7
916.6
1008.6
1064.7
1120.8
1176.8
56
Da
56
Da
56
Da
[M-tBu]+
one ester bond hydrolyzed
IM region
d
Irganox 1010

## Slide 34
Peptide (Protein) - Polymer Hybrid Materials
Hybrid materials usually consist of covalently linked peptides (or proteins) and synthetic polymers. Over the last decade, they have experienced increasing use in medicine and materials science, in a variety of consumer, industrial, and biomedical applications.
Challenges in their characterization:
Peptide-polymer conjugates are difficult to crystallize for X-ray analysis.
Such hybrids cannot often be chromatographically purified for definitive NMR analysis
Alternative solution: top-down MS, involving tandem MS (MS2) and ion mobility mass spectrometry (IM-MS).
A. Alalwiat, S.E. Grieshaber, B.A. Paik, X. Xia, C. Wesdemiotis, Analyst, submitted (July 2015)

## Slide 35
Elastin Mimetic Hybrid Copolymer
+
Flexible hydrophobic domains (V, G, and P rich) for coacervation
Hydrophilic domains (K and A rich) for crosslinking
Elastin: extracellular protein providing elasticity to soft tissues (lungs, skin, arteries, etc.)
+
click rxn.
VPGVG–VPGVG
“VG2”
(in hydrophobic elastin domains)
poly(acrylic acid)
PAA
(pH-responsive & functionalizable)
X. Jia et al., Soft Matter 9 (2013) 1589-99
Notes: PAA: forms pH-responsive micelles, vesicles, hydrogels, and copolymer micelle-crosslinked hydrogels.

## Slide 36
Hybrid material
[PAA‒VG2]m
+
PtBA
VG2
Cu(I)
DMF
TFA
[PtBA‒VG2]m
[PAA‒VG2]m

## Slide 37
[VG2+2Na]⁺²
1090.6
959.4
855.3
700.2
640.1
601.1
553.6
500
600
700
800
900
1000
m/z
1011.5
y6
y7
a₆
[VG2+ Na]+
658.1
739.2
757.2
798.3
814.3
[VG2+2Na]•⁺
1107.5
a₇
y8
c₁₀•+17
y6
y7
y8
c4
a₂
a7
a₆
1113.5
[VG2+Na+17]⁺
c₉•+17
c₈•+17
c₇•+17
c₆•+17
701.2
602.1
c₅•+17
c₄•+17
545.2
[VG₂+Na+17]•⁺²
954.4
z₁₀•*
c5
c6
c7
c8
c9
c10
z10
ESI-MS2 (ETD)
VG2 sequence confirmed by MS2
VG2
Notes: 400 ms reaction time

## Slide 38
Hybrid material / [PAA‒VG2]m
1000
2000
ESI-IM-MS
NH4OAc (pH = 6.64)
+ 1% MeOH
3000
m/z
2+
3+
IM-MS removes chemical noise and separates the desired amphiphilic hybrid both by charge state as well as from incompletely hydrolyzed hybrid and unreacted polymer to enable conclusive compositional characterization.
2
4
6
8
drift time (ms)
PAA–VG2
PAA (n+)
PAA–PtBA (n+)
PAA–PtBA–VG2 (n+)

## Slide 39
Hybrid material / [PAA‒VG2]m
780
790
800
810
820
830
m/z
783.043
807.074
831.076
807.07
831.08
855.04
759.04
783.07
735.03
711.04
687.03
663.01
879.09
903.10
927.12
951.14
650
700
750
800
850
900
950
1000
m/z
PAA14
PAA15
PAA16
3+
ESI-IM-MS
[M+3H]3+
ESI-IM-MS provides conclusive evidence for the formation of hybrid material with one constituent PAA–VG2 block, [PAA–VG2]1:
Multiple blocks?

## Slide 40
Hybrid material / [PAA‒VG2]m
2+
ESI-IM-MS
1030.06
994.03
958.02
922.00
895.97
1066.07
1102.07
1138.10
1210.14
1246.14
1282.14
1318.18
1354.21
1174.12
900
1000
1100
1200
1300
m/z
1030.06
1066.07
PAA10
PAA11
[M+2H]2+
1030
1040
1050
m/z
1060
1070
ESI-IM-MS provides conclusive evidence for the formation of hybrid material with one constituent PAA–VG2 block, [PAA–VG2]1:
Multiple blocks?

## Slide 41
Hybrid material / [PAA‒VG2]m
ESI-IM-MS
0.00
2.50
5.00
7.50
10.00
drift time (ms)
5.42
3.88
6.95
0.00
2.50
5.00
7.50
10.00
drift time (ms)
5.96
4.06
7.13
[PAA10‒VG2]1
[M+2H]2+
m/z 1030
m/z 1102
[PAA12‒VG2]1
[M+2H]2+
[PAA10‒VG2]2
[M+4H]4+
[PAA12‒VG2]2
[M+4H]4+
[PAA10+K]+
[PAA11+K]+
IM-MS on mass-selected ions confirms the formation of a multiblock hybrid copolymer.
& [PAA24+Na+K]2+
& [PAA26+Na+K]2+

## Slide 42
Hybrid material / [PAA‒VG2]m
Architecture?
intramolecular azide click rxn.
linear ?
cyclic ?

## Slide 43
Chart: 
| 926.05 | 1054.19 | 1118.25 | 1182.28 | 1310.3599999999999
calcd., linear architecture | 388 | 428 | 444 | 458 | 499
calcd., cyclic architecture | 367 | 396 | 411 | 430 | 464
measured | 365 | 396 | 417 | 438 | 468
Hybrid material / [PtBAn‒VG2]1
Architecture
ESI-IM-MS
Collision
cross-section
(Å2)
m/z
n =
With all chain lengths, the measured CCS matches the one calculated for the macrocyclic architecture, indicating that all possible 3+2 cycloadditions have taken place (only triazole and no azide / alkyne functionalities).
4
6
7
8
10
2+ ions
calcd., linear
calcd., cyclic
measured
Notes: TWV = 350 m/s; TWH = 8 V; calibration with polyalanine

## Slide 44
Hybrid material / [PtBAn‒VG2]1
Architecture
ESI-IM-MS
Collision
cross-section
(Å2)
m/z
In the 3+ charge state, the composition is [PAA3-PtBAn-VG2 + 3H]3+. The agreement between measured CCS and calculated CCS for the macrocyclic architecture is again excellent (within 4%), confirming that only triazole functionalities are present.
Chart: 
| 732.44 | 775.17 | 817.84 | 903.23
calcd., linear architecture | 431 | 449 | 465 | 501
calcd., cyclic architecture | 404 | 416 | 439 | 469
measured | 398 | 415 | 432 | 458
calcd., linear
calcd., cyclic
measured
3+ ions
n =
5
6
7
9
Notes: TWV = 350 m/s; TWH = 8 V; calibration with polyalanine

## Slide 45
Hybrid material / [PAAn‒VG2]1
Architecture
ESI-IM-MS
Collision cross-section (Å2)
m/z
The measured CCSs are smaller then those of the macrocyclic architectures. This is attributed to extensive H-bonding between the COOH pendants and the VG2 amide groups, leading to compact conformations that were missed in the simulations.
Chart: 
| 921.97 | 957.39 | 1029.93 | 1101.95 | 1174.07 | 1209.98 | 1246.45
calcd., linear architecture | 376 | 395 | 413 | 432 | 464 | 459 | 471
calcd., cyclic architecture | 352 | 366 | 389 | 390 | 416 | 426 | 436
measured | 336 | 342 | 363 | 381 | 391 | 395 | 413
Chart: 
| 687.02 | 734.95 | 783.02 | 806.97 | 831.03
calcd., linear architecture | 417 | 445 | 457 | 474 | 483
calcd., cyclic architecture | 386 | 408 | 413 | 430 | 437
measured | 363 | 369 | 379 | 384 | 397
calcd., linear
calcd., cyclic
measured
Collision cross-section (Å2)
m/z
2+ ions
3+ ions
n =
7
8
10
12
14
16
n =
10
12
14
15
16
15
Notes: TWV = 350 m/s; TWH = 8 V; calibration with polyalanine

## Slide 46
Multidimensional MS [interfaced separation & mass
analysis methodologies] in polymer and materials science
Information about polymer architecture and sequence from MS2 studies.
Interactive LC is particularly useful for the separation of mixtures whose components differ significantly in polarity. On the other hand, IM separation is most effective for the separation of differently shaped polymers and ideally suitable for the analysis of labile/reactive/ weakly bound polymers (e.g., hybrid materials & supramolecular polymers).
Slow thermal degradation interfaced with IM-MS leads to composition and structure insight on complex polymers that cannot be desorbed/ionized and are difficult to analyze otherwise.
Top-down MS with IM-MS and MS2 removes the need of high purity for structural characterization (as needed in XRD and NMR).
Collision cross-sections add a further dimension of structural differentiation & identification.
Significant improvement in the microstructure characterization of synthetic macromolecules.

## Slide 47
Acknowledgements
Dr. Nilufer Erdem (Tubitak, Turkey)
Dr. Bryan Katzenmeyer (Valspar)
Dr. Aleer M. Yol (FDA)
Dr. Nadrah Alawani (Aramco)
Dr. Xiaopeng Li (Texas State U)
Ahlam Alalwiat
Lydia Cool
Selim Gerislioglu
Quirk - Cheng - Newkome - Pugh - Foster - Puskas - Jana - Weiss research groups
NSF
OBR
The University of Akron
GoJo
Lubrizol
Goodyear
Omnova Solutions Foundation
Dr. Xinqiao Jia (U Delaware)
Dr. Sarah Grieshaber (U Delaware)
Bradford Paik (U Delaware)

## Slide 48
Evening - Nighttime
Dale Chilhuly’s “Rocks”
Morning - Daytime

## Slide 49
Akron (Summit County)
Ohio

## Slide 50
Cuyahoga Valley
National Park
Rubber Companies
founded in Akron