## Slide 1: Recent Progress of DUV-LED
1
Cyril Pernot
Crystal Growth Section, Hakusan Factory, Manager
cyril.pernot@nikkiso.co.jp,
Bld No14, Meijo University, 1-501, Shiogamaguchi Tenpaku
Nagoya 468-0073, Japan
Analytica-2015,
Thursday, September 3, 2015
Session: Applications of Analytical and Bio analytical Methods
Session Introduction

## Slide 2
Presentation Outline
Introduction
  UV LED market trend, UV LED advantages and applications
Performance of DUV-LED
  Fabrication of DUV-LED
  Layer Structure
  Characteristics
  Packages
Applications for DUV-LED
  Disinfection Applications
  Analytical Applications
    - Dialyse Dose Monitor
    - Chromatography
Conclusion

## Slide 3
UV-LED Market

## Slide 4
4
Advantage of UV LED Systems
UV-LED Systems Benefits:
Shock resistant semiconductor
customizable emission wavelength
Easy integration (design flexibility, simple driving circuits, low voltage operation)
Instant on/off => No warm-up/cool-down cycles, No shutter needed
Diode Life time in excess of 10,000 hours
No mercury-filled UV bulbs
No ozone production => No system exhaust
By the Minamata Convention on Mercury, regulation on mercury will be strict from 2020. LED has low environmental impact, and has the potential to replace mercury lamps.
Source of UV:
・Gas-discharge lamps (mercury, deuterium, xenon…)
・UV-LED
3,5x3,5mm-sq SMD
Notes: Thinking about LED itself + package & module

## Slide 5
UV-LED Applications Map
Disinfection
UVB
(280-315nm)
UVA
(315-400nm)
UVC
(100-280nm)

## Slide 6
From Blue to UV LED

## Slide 7
AlGaN-based UV LED
Band gap and emission wavelength

## Slide 8
Slicing/Polishing
Substrate
Epitaxial Growth
EpiWafer
Process
ProcessWafer
Dicing/Sorting
LED Chip
Flip-chip/Package
FEED BAC
DUV-LED
Bulk Crystal
Flow Chart for LED Fabrication
@ NIKKISO

## Slide 9
Standard DUV-LED Structure
Sapphire
AlN
nAlGaN
Active Region
pAlGaN
pGaN
electrodes
electrodes
X
X
X
Internal Efficiency > 70%
Light Extraction Efficiency < 10 %

## Slide 10
EQE and max Power
Evolution of EQE
Bare chip measurement under same condition for 280-290nm LED
WPE = 5.0 % @ 10mA
289nm bare chip (2013)
EQE Limit for LEE of 10 %
Improvement obtained thanks to:
- Better crystal quality
- Better device layer structure
But still need improvement for Light Extraction:
- Reflective electrodes
- Encapsulation

## Slide 11
DUV LED Products and Characteristics
flat window
w/ lens
TO-46
●Low Power Type（IF=20mA）
●High Power Type（IF=100mA or 350mA）

## Slide 12
Lifetime ・ Degradation
Temperature and driving current are affecting lifetime of the DUV-LED device
but origin and mechanism of degradation are still unclear
By growing high quality DUV-LED, life time over 10000 hours can be achieved.
Output power degradation for 285 nm DUV-LED driven at 350 mA with Ts of 40℃

## Slide 13
Package | Thermal Resistance | Maximum CW operating current for keeping power over 80%
CAN PKG | >20℃/W | 20 mA, Power > 1mW
SMD PKG (2013 Product) SMD PKG (2014 Product) | 18℃/W 15℃/W | 200mA, Power > 15mW 350mA, Power > 25mW
New PKG Under development) | < 10℃/W | >350mA , Power> 50mW
Package & thermal resistance
Tj(℃)=Ts(℃)+IF(A)×VF(V)×Rj-s（℃/W）,

## Slide 14
High Packing Density Lighting Module
8 modules of 112 x 3.5mm-packages each
Irradiance of 80 mW/cm2
at a working distance of 10 mm
over an area of 25 x 25 cm2.
(Water Cooling)

## Slide 15
Wavelength(nm)
Disinfection Effect
DNA (before Irradiate UV LIGHT)
DNA (after Irradiating UV LIGHT)
15
Disinfection by UV Light
Wavelength(nm)
Absorption Coefficient
Principle
DNA:DeoxyriboNucleic Acid
DNA can be destroyed and inactivated by UV light irradiation.
When living microorganisms such as bacteria are exposed to UV-C light between 250nm and 280nm (germicidal action spectra), their DNA can be destroyed and inactivated by UVC effectively; DNA cannot reproduce itself => Disinfection

## Slide 16
16
UV-LED Specifications
Wavelength : 265nm and 285nm
Forward Current : 60mA
Lighting Intensity :
265 nm : 1.33 [mW/cm2]
285 nm : 2.41 [mW/cm2]
Irradiation Distance ：10mm
Bacterial
1) Escherichia coli NBRC3972
265nm
Chart: Escherichia coli NBRC 3972
| 0 | 60 | 120 | 160 | 240 | 300 | 360
大腸菌（試験値_260nm） | 560000 | 9500 | 6100 | 1700 | 1200 | 1000 | 110
大腸菌（試験値_280nm） | 560000 | 13000 | 4200 | 2000 | 880 | 540 | 60
大腸菌（未照射_260nm） | 560000 | 680000
大腸菌（未照射_280nm） | 560000 | 480000
Reference
No Irradiation
285nm
265nm
Disinfection Test Result by UV-LED
2) Bacillus substills, NBRC3134
3) Staphylococcus aureus subsp.sureus, NBRC 12732
4) Salmonella enterica subsp.enterica, NBRC 3313
5) Vibrio parahaemolyticus, RIMD 2210100
6) Cladosporium cladosporioides, NBRC 6348
7) Aspergillus niger, NBRC 105649
285nm
After 360sec
After 420sec
Demonstration of effective Disinfection
using DUV LED for the following Bacteria ⇒

## Slide 17
Water Disinfection Prototype Module
Disinfection Performance of 99,9% (3Log)
E.Coli : 500mL/min B.substils : 100mL/min
Fig. 1 Pass disinfection performance
Application example of low flow rate water disinfection module
Product release in 2014
DUV-LED on substrate
Log Reduction Ratio

## Slide 18
18
DUV-LED for Sensing Application
Technology Type | Area | Usage
Photo-absorption Type | Medical | Dialysis Dose Monitor (DDM) Blood analysis device.
 | Food Manufacturing | Measurement of amount of enzyme reaction.
 | Water Quality Measurement | Measurements of hypochlorite, enzyme reaction and COD.
Compact
Original Light Strength
【L0】
Weakened Light after Absorption. 【L1】
Light Source
Light Detecting Element
Sample
Electric Signal
Light Absorption
a. Compact and light weight.
b. No need for optical filter.
c. Easy to control (Instant start ,
Pulse lighting)
d. Mercury free
e. Wavelength is adjustable.

## Slide 19
285nm
UV-LED for Sensing Application
What is DDM?
Dialysis Dose Monitor → DDM.
Measurement of uric acid concentration contained in dialysis waste fluid
Uric acid is measured by absorption spectroscopy with UV-LED as light source
Pump
Blood Pump
D.D.M.
Pump
Monitoring for Uric Acid
Dialyzer
Dialysis Waste Fluid
λ:285nm
19

## Slide 20
Chromatography setting
UV Light source:
2 fixed wavelength
280 nm LED
300 nm LED

## Slide 21
Chromatography process using UV-LED
Advantages of UV LED:
-More robust
-No need for spectrometer
-No need for shutter
-Small Footprint
-Light weight
-Instant On/Off
(lower power consumption)
-Low Voltage operation
(simple driving unit)
-Longer Life time

## Slide 22
DUV-LED has some clear advantage compared with traditional UV light source
Significant improvement in the DUV-LED performance recently: possible to address a large range of market
more development is needed not only in the LED-chip performance but also in package, module design (arrays, cooling and optics)
Nikkiso Started Production in a new factory dedicated to DUV LED
By controlling all the fabrication steps, from wafer epitaxy
to chip packaging, including quality control and
UV-module development, we target higher
device performance, higher production yield ,
allowing to decrease the Cost-per-Watt
Customized Modules designs are possible thanks
to Nikkiso know-how in optics, fluid dynamic
and thermal analysis
Conclusion

## Slide 23: Thank you for your attention !