## Slide 1: Utilization of microalgal-derived ash as a mineral reinforcement material in biocomposite formulation with poly(vinyl alcohol)
TRAN DANG THUAN, Ph.D
Advanced Biomass R&D Center, Republic of Korea
Biopolymers and Bioplastics, August 10-12, 2015 San Francisco, USA
Notes: Cover

## Slide 2: Contents
Introduction
Experimental
Characterization of materials
Properties of composite materials
Summary & conclusions
Notes: Contents

## Slide 3: I. Introduction
Best Microalgae strain
Lipid Extraction
Biodiesel Production
Cultivation
Harvest
Best Microalgae strain
Lipid Extraction
Biodiesel Production
Harvest
Cultivation
Lipid-extracted algal biomass (LEA)
(C, H, N, S, mineral element, etc.)
Chemical composition of LEA
Element | Average (%) | STDEV
N | 5.63 | 0.01
C | 42.81 | 0.33
H | 6.25 | 0.06
S | 3.94 | 0.15
Nannochloropsis salina
Carbon-rich
material for
gasification

## Slide 4: I. Introduction
Lipid-extracted algal biomass (LEA)
(C, H, N, S, mineral elements, etc.)
Gasification
Steam (CO, H2, etc.)
Tar, Soot, Sulfer compounds
Ash (SiO2, CaO, MgO, P2O5, SO3, etc.)
Hirano A, Hon-Nami K, Kunito S, Hada M, Ogushi Y. Catal Today 1998;45(1–4):399–404.
How to utilize it?
Potential filler for
composite fabrication

## Slide 5: II. Experimental
Simple Gasification
Lipid-extracted algal biomass (LEA)
(C, H, N, S, mineral elements, etc.)
Burning in a Furnance
(575 oC, 3 hrs)
Raw ASH (RASH)
Activation
Characterization
Composite Fabrication

## Slide 6: II. Experimental
Hydro-chemical Activation
RASH
NaOH 1N (10 g RASH/60 mL NaOH)
110 oC, 400 rpm, 1 hrs
Filter & Wash until pH 7.0
Dry (105 oC, 24 hrs)
PASH

## Slide 7: II. Experimental
PASH dispersed in H2O
pH adjusted with NaOH 1N to 10
Poly(diallyldimethylammonium chloride) (PDDA)

## Slide 8
1. Heating & stirring Solution
2. Casting
3. Ambient drying
Hot plate
Knife coating device
Composite films
II. Experimental
Storage
(ASTM E104-02)
Saturated K2CO3, 25 oC, RH = 43.2%
Mechanical properties
Thermal properties

## Slide 9: III. Characterization of RASH and PASH
RASH |  | PASH | 
Component | Proportion (wt%) | Component | Proportion (wt%)
B2O3 | 4.71 | C | 3.21
Na2O | 1.86 | Na2O | 2.39
MgO | 2.57 | MgO | 2.99
Al2O3 | 4.34 | Al2O3 | 4.96
SiO2 | 24.40 | SiO2 | 27.80
P2O5 | 13.20 | P2O5 | 17.10
SO3 | 23.30 | SO3 | 3.61
K2O | 2.13 | K2O | 0.96
CaO | 17.60 | CaO | 22.20
TiO2 | 0.51 | TiO2 | 0.60
MnO | 0.09 | MnO | 0.11
Fe2O3 | 4.45 | Fe2O3 | 4.64
ZnO | 0.53 | ZnO | 0.60
Others | 0.31 | Others | 8.83
Surface area (m2/g) | 4.8 | Surface area (m2/g) | 65.2
Chemical composition determined by XRF

## Slide 10: III. Characterization of RASH and PASH
Crystal composition determined by XRD

## Slide 11: III. Characterization of RASH and PASH
IR spectra of RASH and ASH determined by FT-IR
O-H stretching
Si4+ in silicate Ca8Si5O18
Si─O and Si─O─Al asymmetric stretching vibrations
C─O and/or C─H bonds in carbonates
formation of relative larger interparticle pores

## Slide 12
III. Characterization of RASH and PASH
FE-SEM micrographs of RASH and PASH
Platelet-like particles
with smooth surface
Particles with irregular
shape, rough, and craters
on its surface
RASH
PASH

## Slide 13
III. Characterization of RASH and PASH
Particle size distribution of RASH and PASH determined by DLS
Shifting of particle size distribution to left side

## Slide 14
IV. Mechanical properties
UTSs of neat PVA, PVA/PASH, and PVA/PASH/PDDA composites

## Slide 15
IV. Mechanical properties
EBs of neat PVA, PVA/PASH, and PVA/PASH/PDDA composites

## Slide 16
IV. Mechanical properties
YMs of neat PVA, PVA/PASH, and PVA/PASH/PDDA composites
~ 1.6 GPa

## Slide 17
IV. Thermal properties
DSC thermograms of PVA, PVA/PASH and PVA/PASH/PDDA
Tg
Tg
Tm
Tm

## Slide 18
IV. Thermal properties
Thermal properties of PVA, PVA/PASH and PVA/PASH/PDDA
Sample | Tc (oC) | Tm (oC) | ΔHm (J/g) | ΔHf (J/g) | Crystallinity (%)
PVA | 133.5 | 225.5 | 34 | 71.83 | 51.83
PVA95PASH5 | 134.4 | 226.7 | 36.41 | 49.94 | 37.93
PVA90PASH10 | 133.1 | 227.9 | 34.25 | 63.37 | 50.80
PVA85PASH15 | 130.5 | 225.6 | 28.83 | 50.56 | 42.92
PVA80PASH20 | 132.4 | 227.3 | 28.34 | 43.64 | 39.36
PVA75PASH25 | 135.7 | 229.8 | 32.15 | 38.60 | 37.13
PVA95PASH5PDDA | 127.7 | 227.1 | 30.67 | 52.12 | 39.58
PVA90PASH10PDDA | 128.6 | 227.3 | 28.51 | 47.63 | 38.18
PVA85PASH15PDDA | 131.8 | 228.3 | 28.76 | 53.20 | 45.49
PVA80PASH20PDDA | 127.9 | 227.9 | 24.75 | 51.55 | 46.49
PVA75PASH25PDDA | 127.0 | 228.6 | 24.64 | 49.14 | 47.27
Tm
Heat resistance improvement

## Slide 19
IV. XRD pattern analysis
Characteristics of semi-crystalline polymers

## Slide 20
IV. IR spectra analysis
Shifting to lower wave number, and higher intensity
O-H stretching
C=O and C─O stretching

## Slide 21
IV. Morphological analysis (SEM)
PVA95PASH5
PVA75PASH25
PVA95PASH5PDDA
PVA75PASH25PDDA
Full coverage
Partial full coverage
Abundance
interfacial voids
Very little voids
bridge-like connection
brittle failure, poor filler-matrix adhesion
better polymer-reinforcement adhesion

## Slide 22
V. Summaries & Conclusions
Hydrochemical activation made RASH become PASH with smaller size, rough and crater surface, and high surface area
Better dispersion and adhesion of PASH in PVA was observed in presence of polycations (PDDA)
Result in higher tensile strength of PVA/PASH/PDDA compared to PVA/PASH composites at every loading of the filler
The process of pretreatment of RASH, utilization of PASH by composite formulation with PVA and polycation is easy and efficient, which can be integrated in downstream processing of microalgae-based biorefinery
Value-added composites produced from microalgal ash can partially improve economical feasibility of microalgal industry

## Slide 23
Acknowledgements
This research was financially supported by the Advanced Biomass R&D Center (ABC) of Korea Grant funded by the Ministry of Science, ICT and Future Planning (ABC-2010-0029728).
Supervised supports from
  Prof. Ji-Won Yang (CBE, KAIST)
  Prof. Min S. Park (CBE, ABC, KAIST)
  Prof. Yong Keun Chang (CBE, ABC, KAIST)
Many helps from my student
  Hyun-Ro Lee (M.S., CBE, KAIST)

## Slide 24
Thank you for your attention!