## Slide 1
Dr Inderpreet Kaur Prof. Ashok Kumar
Supervisor Co-Supervisor
CSIO-CSIR, Chandigarh IGIB-CSIR, New Delhi
Towards a novel FRET immunosensor using biocompatible Graphene Quantum Dot for early diagnosis of Myocardial Infarction
Presented By:
Ms DEEPIKA BHATNAGAR
Deepika Bhatnagar, Ashok Kumar, Inderpreet Kaur

## Slide 2
Introduction
  Myocardial damages
  Current Global scenario
  Myocardial Infarction (MI)
  Cardiac Troponin I (cTnI)
Carbon forms in biomolecular detection
Graphene Quantum dots
Design of work
Results & Discussion
References
Contents

## Slide 3
Myocardial pertaining to the muscular tissue of the heart.
Any disease causing loss of muscular or nervous function of the heart.
Includes myocarditis, ischemia, degeneration.
Myocarditis
Ischemia
Muscle degeneration
Myocardial damages

## Slide 4
Current worldwide scenario

## Slide 5
Necrosis of the cells of an area of the heart muscle (myocardium) occurring as a result of oxygen deprivation, which in turn is caused by obstruction to the blood supply.
Blockage in coronary arteries due to an unstable buildup of cholesterol and Fat.
Symptoms;
  Chest Pain or discomfort
  Upper body pain in arms, neck & jaw
  Shortness of breath
  Nausea
  Lightheadedness or cold sweats
Myocardial infarction
(heart attack)

## Slide 6
Myocardial infarction (MI) types 1 and 2 according to the condition of the coronary arteries.
Factors responsible for MI
Notes: Differentiation between myocardial infarction (MI) types 1 and 2 according to the condition of the coronary arteries.

## Slide 7
CK (CPK)
CK-MB
Troponin-I/T
Myoglobin
LD (LDH)
ALT/AST
Others
TEST | ONSET (hours) | PEAK (hours) | DURATION
CK/CK-MB | 3-12 | 18-24 | 36-48 hours
Troponins | 3-12 | 18-24 | Up to 10 days
Myoglobin | 1-4 | 6-7 | 24 hours
LDH | 6-12 | 24-48 | 6-8 days
Biomarkers in MI

## Slide 8
Laboratory range:
Since troponin I levels are virtually undetectable in normal subjects, the cut-off value is <0.04 ngmL-1
Increases drastically to 0.7-1.4 ngmL-1 within 3-12 h
Troponin I

## Slide 9
Carbon based nanoplatforms are comparably more stable
Graphene
Carbon nanotubes
Carbon dots
Graphene quantum dots
Nanodiamonds
Carbon nanocones
Biocompatibility
Easy functionalization
Incredibly large surface area
Comparatively cost effective
Carbon forms in biomolecular detection

## Slide 10
A 0D, unique sp2 and sp3 hybridized carbon structure with size range of 3-20nm derived from 2D graphene
Characteristics derived from both graphene and Carbon Dots (CDs)
Strong Fluorescence
Excellent Biocompatibility (Non-toxic)
High surface area
Photostable emission
Possibility for bioconjugation
Graphene quantum dots
Under UV illumination

## Slide 11
Graphene Quantum Dots (GQDs)
(as Donor)
Graphene
(as Acceptor)
Graphene forms selected for FRET
Notes: http://www.nanowerk.com/spotlight/spotid=9857.php
http://www.rsc.org/chemistryworld/News/2005/September/19090501.asp

## Slide 12
Design of work
(a)
anti-cTnI
EDC
NHS
–C-OH
O
=
O
–C-O
=
NHS ester
anti-cTnI/afGQDs
conjugate
O=C–
H-N
_
COOH
H-O
O=C-R
C-H
H2N
H2N-C=O
NH2
N-H
H2N
O=C-NH2
Ammonia
GQDs
afGQDs
NH2
Scheme 1. (a) Bioconjugation of monoclonal anti-cTnI with afGQDs using EDC-NHS chemistry.

## Slide 13
(b)
Graphene
Antigen
Wavelength (nm)
PL Intensity
Wavelength (nm)
PL Intensity
Wavelength (nm)
PL Intensity
457 nm
360 nm
anti-cTnI/afGQDs
No FRET
anti-cTnI/afGQDs/Gr/cTnI
FRET
anti-cTnI/afGQDs/Gr
Graphene (Quencher)
cTnI antigen
anti-cTnI antibody
afGQDs (Fluorophore)
Excitation
Emission
(b) Schematic mechanism of immunosensing based on specific interaction of anti-cTnI/afGQDs with graphene.

## Slide 14
Results
Figure 1. FESEM images of (a) amine functionalized GQDs, (b) anti-cTnI/afGQDs conjugate, (c) anti-cTnI/afGQDs/Gr and (d) anti-cTnI/ afGQDs/Gr/cTnI.
Field emission scanning electron microscopy (FESEM)

## Slide 15
Zeta Potential & UV-Vis spectra
Figure 2. (a) Zeta-potential studies of the GQDs (control) and synthesized anti-cTnI/afGQD conjugate.
(b) Positive shift in the value of zeta potentials
(c) UV-Vis Spectra of GQDs, afGQDs, anti-cTnI and anti-cTnI/afGQD conjugate.

## Slide 16
Photoluminescence studies
Figure 3. Photoluminescence studies of (a) various precursors at the nano-platform, (b) The fluorescence quenching spectra of anti-cTnI/afGQDs with increasing concentrations of graphene 0, 1.0, 1.5, 2.0, 2.5, 3.0, 3.5, 4.0 µg mL-1 from top to bottom, (Inset) Fluorescence quenching efficiency at varying concentrations of graphene and (c) Immunosensing behaviour and (d) Specificity check against specific (cTnI) and non-specific antigen BSA and Avidin.

## Slide 17
FRET observations through Confocal microscopy
(a)
(b)
(f)
(g)
(c)
(d)
(e)
Figure 4. CLSM images at 405 nm excitation of (a) afGQDs as control, (b) anti-cTnI/afGQDs nanoprobe, (c) anti-cTnI/afGQDs/cTnI, (d) anti-cTnI/afGQDs/Gr and (f) anti-cTnI/afGQDs/Gr/cTnI. CLSM images without excitation of (e) anti-cTnI/afGQDs/Gr and (g) anti-cTnI/afGQDs/ Gr/cTnI. Scale bar 10 µm.

## Slide 18
S. No. | Samples | Confocal Photon Count (Mean S/N=3) | PL Intensity
1 | afGQDs | 118.34 | 35.1
2 | anti-cTnI/afGQDs | 160.03 | 37.7
3 | anti-cTnI/afGQDs/cTnI | 145.31 | 33.4
4 | anti-cTnI/afGQDs/Gr | 4.45 | 6.7
5 | anti-cTnI/afGQDs/Gr/cTnI | 11.72 | 20.5
TABLE I Comparative studies of photo count from confocal laser scanning microscopy (CLSM) and PL intensity at different fluorescent nanoplatforms
Validation of the sensor
Figure 5. (a) The fluorescence recovery spectra of anti-cTnI/afGQDs/Gr system with increasing concentrations of cTnI antigen 0, 0.001, 0.01, 0.1, 1.0, 10, 100, 1000 ng mL-1 from bottom to top. (b) The linear relationship between the PL intensity of anti-cTnI/afGQDs/Gr system with increasing log concentrations of cTnI from picomolar to nanomolar.

## Slide 19
GQDs based developed sensor have high sensitivity of 0.192 pg mL-1.
Specific for cTnI; no cross reactivity.
Rapid method of detection.
Early diagnosis in MI.
Conclusion

## Slide 20: References
1 T. Reichlin, W. Hochholzer, S. Bassetti, S. Steuer, C. Stelzig, S. Hartwiger, S. Biedert, N. Schaub, C. Buerge, M. Potocki, M. Noveanu, T. Breidthardt, R. Twerenbold, K. Winkler, R. Bingisser, and C. Mueller, New Engl. J. Med. 361, 858 (2009).
2 A. S. Jaffe, C. Ritter, V. Meltzer, H. Harter and H. Roberts, J. Lab Clin. Med. 104, 193 (1984).
3 K. W. Ma, D. C. Brown, B. W. Steele and H. L. Arthur, Arch. Intern. Med. 141, 164 (1981).
4 G. S. Bodor, S. Porter, S. Landt and Y. J. H. Ladenson, Clin. Chem. 38, 2203 (1992).
5 J. E. Adams, K. B. Schechtman, Y. Landt, J. H. Ladenson and A. S. Jaffe, Clin. Chem. 40, 1291 (1994).
6 P.A. Anderson, N. N. Malouf, A. E. Oakeley, E. D. Pagani and P. D. Allen, Circ. Res. 69, 1226 (1991).
7 V. S. Mahajan and P. Jarolim, Circulation 124, 2350 (2011).
8 K. Vichairuangthum, W. Leowattana, L. O. Ajyooth and S. Pokum, J Med. Assoc. Thai. 89, 714 (2006).
9 J. R. Tate, Clin. Chem. Lab. Med. 48, 1489 (2008).
10 S. Lee, D. Kwon, C. Yim and S. Jeon, Anal. Chem. 87, 5004 (2015).
11 Z. Xu, Y. Dong, J. Li and R. Yuan, Chem. Comm. 51, 14369 (2015).
12 P. Kar, A. Pandey, J. J. Greer and K. Shankar, Lab Chip 12, 821 (2012).
13 A. Periyakeruppan, R. P. Gandhiraman, M. Meyappan and J. E. Koehne, Anal. Chem. 85, 3858 (2013).
14 H. Guo, J. Zhang, P. Xiao, L. Nie, D. Yang and N. He, J. Nanosci. Nanotechnol. 5, 1240 (2005).
15 Rajesh, V.Sharma, N. K. Puri, R. K. Singh, A. M. Biradar and A. Mulchanadani, Appl. Phys. Lett. 103, 203703 (2013).
16 J. Peng, W. Gao, B. K. Gupta, Z. Liu, R. Romero-Aburto, L. Ge, L. Song, L. B. Alemany, X. Zhan, G. Gao, S. A. Vithayathil, B. A. Kaipparettu, A. A. Marti, T. Hayashi, J. J. Zhu and P. M. Ajayan, Nano Lett. 12, 844 (2012).
17 L. Tang L, R. Ji, X. Cao, J. Lin, H. Jiang, X. Li, K. S. Teng, C. M. Luk, S. Zeng, J. Hao and S. P. Lau, ACS Nano 6, 5102 (2012).
18 S. Kim, S. W. Hwang, M. K. Kim, D. Y. Shin, D. H. Shin, C. O.Kim, S. B. Yang, J. H. Park, E. Hwang, S. H. Choi, G. Ko, S, Sim, C. Sone, H. J. Choi, S. Bae and B. H. Hong, ACS Nano 6, 8203 (2012).

## Slide 21
19 S. Park and R. S. Ruoﬀ, Nat. Nanotechnol. 4, 217 (2009).
20 G. Eda and M. Chhowalla, Adv. Mater. 22, 2392 (2010).
21 K. P. Loh, Q. Bao, P. K. Ang and J. Yang, Mater. Chem. 20, 2277 (2010).
22 S. Zhu, J. Zhang, C. Qiao, S. Tang, Y. Li, W. Yuan, B. Li, L. Tian, F. Liu, R. Hu, H. Gao, H. Wei, H. Zhang, H. Sun and B. Yang, Chem. Comm. 47, 6858 (2011).
23 X. Li, S. Zhu, B. Xu, K. Ma, J. Zhang, B. Yang and W. Tian. Nanoscale 5, 7776 (2013).
24 Q. Lu, W. Wei, Z. Zhou, Z. Zhou, Y. Zhang and S. Liu, Analyst 139, 2404 (2014).
25S. N. Baker and G. A. Baker, Angew. Chem. Int. Ed. 49, 6726 (2010).
26 M. Li, W. Ni, B. Kan, X. Wan, L. Zhang, Q. Zhang, G. Long, Y. Zuo and Y. Chen, Phys. Chem. Chem. Phys. 15, 18973 (2013).
27 P. Gao, K. Ding, Y. Wang, K. Ruan, S. Diao, Q. Zhang, B. Sun and J. Jie, J. Phys. Chem. C 118, 5164 (2014).
28 I. A. Ogaidi, H. Gou, Z. P. Aguilar, S. Guo, A. K. Melconian, A. K. A. Al-kazaz, F. Meng and N. Wu, Chem. Comm. 50, 1344 (2014).
29 H. Zhao, Y. Chang, M. Liu, S. Ghao, H. Yu and X. Quan, Chem. Comm. 49, 234 (2013).
30 M. J. E. Fischer, Methods Mol. Biol. 627, 55 (2010).
31 S. Saini, H. Singh and B. Bagchi, J. Chem. Sci. 118, 23 (2006).
32 B. Zhang, A. W. Morales, R. Peterson, L. Tang and J. Y. Ye, Biosens. Bioelectron. 58, 107 (2014).
33 T. Kong, R. Su, B. Zhang, Q. Zhang and G. Cheng, Biosens. Bioelectron.34,267(2012).