## Slide 1
Derya Boyacı
İzmir Institute of Technology
Turkey
Development of
Whey Protein Based Edible Films with pH-controlled Release
for Active Packaging

## Slide 2: Food Safety and Packaging
Microorganisms
Chemicals
O2
Moisture
Light
Functional Properties of Packaging Materials
Better shelf-life
and quality

## Slide 3: Active and Antimicrobial Packaging
Inhibit pathogenic bacteria
Control spoilage
Use minimum amounts of
active compounds
Environment
Food
Packaging
A packaging system releases active/antimicrobial compounds on the food surface to delay microbial growth.
Extend shelf life
Safe and High quality foods

## Slide 4
Controlled Release Packaging (CRP) System
Innovative form of active packaging where antimicrobial and antioxidant compounds incorporated into a polymer and relase in a controlled manner.
Figure 1. CRP System
Food
Non-active barrier film
Active CRP film
Active agent

## Slide 5: Controlled Release
Direct addition of antimicrobials
Excessive use !
Neutralization !
Antimicrobial sprays or dips
Diffusion into center of food !
Controlled release antimicrobial packaging
Prevent too high / too low concentration of active substances at food surface
Prevent sensorial or toxicological problems ( use lower amounts of active agent)

## Slide 6
Release Rate
Growth Rate
SLOWER
FASTER
Microbial Spoilage!
Diffusion into Food !

## Slide 7: pH-Controlled Release in WPI films
pH-triggering mechanism for controlled release of lysozyme from WPI films
Can be triggered by adjusting the pH of food when antimicrobial activity is needed
Before cold storage
After freezing-thawing
Before transportation and market display

## Slide 8: Edible Films and Antimicrobials
Whey Protein Isolate
20% of milk proteins
pI ≈ 5.4
One of the most commonly
used biodegradable film material
Forms transparent brittle films
Good O2, CO2, lipid and aroma barrier properties
Lysozyme
Hydrolases
pI ≈ 9,2
Molecular weight ≈ 14.7 kDa
Found in tears, mucus, egg white
One of the most frequently used biopreservative
Antimicrobial activity mainly on gram-positive bacteria

## Slide 9: WPI films
Whey protein film (WPI)
WPI – Oleic acid blend film ( 9% oleic acid)
WPI – Beeswax composite film (30% beeswax)
: Free lysozyme
: Bound lysozyme
Negatively charged WPI
pH
Neutral pH
Below pI (pH 5.4)

## Slide 10: Potential Application
Activation of Lyz based antilisterial activity
Listeria monocytogenes - Smoked fish processing (Smoked salmon)
  MAP  lost after opening the pack
  Vacuum packaging has no absolute effect on L. Monocytogenes
  pH-triggered release system can be employed as a hurdle to reduce the risk, especially during the storage of remaining food after the first consumption.
Cold smoked salmon

## Slide 11: Produced WPI Films
Released LYS activity into buffer
Released LYS activity on smoked salmon
In-vitro antimicrobial activity of films
Antimicrobial activiy of the films coated on smoked salmon
Morphological properties
LYS
LYS +
Oleic acid (9%)
LYS +
Beeswax (30%)
Control

## Slide 12: LYS Activity of the Films
LYS release at different pHs

## Slide 13: LYS Activity of the Composite and Blend Films
pH 5.5
pH 5.0
pH 4.5
pH 4.0

## Slide 14: Film Morphology
Control WPI film
WPI + LYS
WPI + Oleic acid
WPI + bees wax

## Slide 15: Release on Smoked Salmon
OLE & BW

## Slide 16
Film composition |  |  |  | Average zone area (mm2) at 4ºC | 
LYZ (mg/cm2) | OLE (%)a | BW (%)a | Acidification (5% citric acid) | 24 h | 48 h
- | - | - | - | Partial zones | Partial zones
- | - | - | + | Partial zones | Partial zones
0.7 | - | - | - | 51.7 ± 8.5d | 63.5 ±13.9c
0.7 | - | - | + | 101.1 ± 15.3c | 84.6 ± 22.5b
0.7 | 9 | - | - | 121.5 ± 14.9b | 93.9 ± 17.4b
0.7 | 9 | - | + | 141.6 ± 26.6a | 124.3 ± 32.7a
0.7 | - | 30 | - | 54.5 ± 7.4d | 55.6 ± 11.04c
0.7 | - | 30 | + | 58.5 ± 21.2d | 88.11 ± 55.6c
Antimicrobial Activity against L. innocua

## Slide 17
L.innocua counts during storage at 4°C (log CFU/g)a |  |  |  | 
Day 0 | Day 1 | Day 3 | Day 5 | Day 7
Uncoated 4.98 ± 0.08a,A | 4.82 ± 0.10ab,B | 4.82 ± 0.10a,B | 4.80 ± 0.11a,B | 4.83 ± 0.13a,B
WPI/OLE (control)b 4.92 ± 0.10a,A | 4.72 ± 0.10bc,C | 4.73 ± 0.08b,C | 4.78 ± 0.09a,BC | 4.84 ± 0.11a,B
WPI/OLE+LYS 4.92 ± 0.08a,A | 4.68 ± 0.07c,B | 4.69 ± 0.15b,B | 4.74 ± 0.12a,B | 4.49 ± 0.12b,C
WPI/OLE (acidified) 4.97 ± 0.04a,A | 4.84 ± 0.11a,B | 4.77 ± 0.13ab,B | 4.80 ± 0.12a,B | 4.57 ± 0.09b,C
WPI/OLE+LYS (acidified) 4.97 ± 0.07a,A | 4.49 ± 0.13d,B | 4.45 ± 0.13c,BC | 4.27 ± 0.19b,BC | 4.24 ± 0.15c,C
Antimicrobial Activity against L. innocua

## Slide 18: Conclusion
LYS release mechanism based on acidification of the film was tested
The films were successfully applied on smoked salmon slices
Activation of edible films by consumer before consumption or after for the remaining part of the food is possible
To optimize the concentration of LYS and increase the efficieny of film activity, further food applications are needed.