## Slide 1: Influence of Impact Speed on Water Droplet Erosion (WDE) Performance of Ti-6Al-4V and Mechanism of Material Removal During the Incubation and Advanced Stages
4th International Conference and Exhibition on Materials Science & Engineering
Florida, Orlando, USA, September 14-16, 2015
A. K. Gujba, L. Hackel, D. Kevorkov* and M. Medraj

## Slide 2: INTRODUCTION
Gas turbine efficiency in power generation industry is paramount but its adversely affected by ambient temperature.
Fog cooling is employed in order to reduce the temperature by spraying small droplets.

## Slide 3: INTRODUCTION
Gas turbine efficiency in power generation industry is paramount but its adversely affected by ambient temperature.
Fog cooling is employed in order to reduce the temperature by spraying small droplets.
Alstom
General Electric

## Slide 4: WATER DROPLET EROSION
Kong et al. 2010
Water hammer
Shock waves
Side jetting
Deformation
Sub-surface cracks
Surface cracks
and asperities
Main Erosion Mechanisms
Hydraulic penetration
Deep cracks

## Slide 5: WATER DROPLET EROSION
Droplet properties
Velocity, size, flow rate
Material properties
Hardness, toughness, ultimate resilience
Other parameters
Kong et al. 2010
Impact angle,
surface roughness…
Factors Influencing Water Erosion

## Slide 6: WATER DROPLET EROSION TESTING
The state of the art rig for liquid impingement erosion testing
at Concordia University, Montreal, Canada.
Rig parameters
Impact speed (m/s) = 150-500
Droplet size (µm) = 200-600
Test impact angle (⁰) = 1-90
Flow rate (liter/min) = 0.02-0.30
http://users.encs.concordia.ca/~tmg/index.php?title=Main_Page

## Slide 7: MATERIAL
Ti-6Al-4V (ASTM B265, Grade 5) alloy, used for compressor blades in gas turbine, was investigated.
T-shaped coupons, as shown, were machined using a CNC
The microstructure of the Ti-6Al-4V alloy contains α and β phases.
Sample geometry
β-phase
α-phase
Top surface
Cross section

## Slide 8: WATER DROPLET EROSION TESTING
The test was done in accordance with ASTM G73 standard
for liquid impingement erosion testing.
Test parameters
Impact speed (m/s) = 150-350
Av. droplet size (µm) = 460
Test impact angle (⁰) = 90
Flow rate (liter/min) = 0.05
Nozzle-sample distance (mm) = 5
http://users.encs.concordia.ca/~tmg/index.php?title=Main_Page

## Slide 9: CHARACTERIZATION OF ERODED COUPONS
Weigh coupon at certain interval
Optical images
SEM Micrographs - Mechanisms
Only incubation period and maximum erosion rate will be presented in this work

## Slide 10: RESULTS – WDE CURVES
Chart: Number of Impingements x 105
| 0 | 2.88 | 5.76 | 8.64 | 11.52 | 14.4 | 20.16 | 25.92 | 37.44 | 54.72 | 83.52 | 141.12 | 198.72 | 256.32 | 313.92 | 371.52 | 457.92
As-M-200 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.0011 | 0.0023 | 0.0041 | 0.0067 | 0.0094
As-Machined | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.0003 | 0.0007 | 0.0025 | 0.0052 | 0.0083 | 0.0113
As-M 150 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Chart: Number of impingements x 105
| 0 | 0.72 | 1.44 | 2.16 | 4.32 | 7.2 | 11.52 | 17.28 | 23.04 | 31.68 | 40.32
AsM | 0 | 0 | 0 | 0 | 0.0011 | 0.0048 | 0.0107 | 0.0141 | 0.0182 | 0.0195 | 0.0211
 | 0 | 0 | 0 | 0 | 0.0008 | 0.0025 | 0.0044 | 0.0063 | 0.0095 | 0.0123 | 0.0158
 | 0 | 0 | 0 | 0 | 0.0017 | 0.0046 | 0.0079 | 0.0107 | 0.0161 | 0.0198
F. Heymann
Incubation period
350m/s
325m/s
300m/s

## Slide 11: ANALYSIS OF WDE CURVES
Chart: Impact speed (m/s)
| 200 | 250 | 300 | 325 | 350
Impact Pressure, MPa | 705 | 919 | 1148 | 1268 | 1392
Impingement to initiation | 16.32 | 0.72 | 0.288 | 0.2028 | 0.2016
Chart: Impact speed (m/s)
| 200 | 250 | 300 | 325 | 350
As-Machined | 1.54 | 68 | 96 | 172 | 412
F. Heymann
Incubation period
Maximum erosion rate

## Slide 12: WDE MECHANISM – INITIATION STAGE
A
B
Incubation stage
Advanced stage
0min 6mins
32mins 56mins

## Slide 13: WDE MECHANISM – INITIATION STAGE
A
B
Incubation stage
Advanced stage

## Slide 14: WDE MECHANISM – INITIATION STAGE
Network of microcracks
Potential sites for pit growth and crack propagation
Formation of asperities due to impact and side jetting

## Slide 15
WDE MECHANISM – ADVANCED STAGE
Deep tunnel due to hydraulic penetration
Material upheaval due to stress wave
Stress wave direction
Fatigue surface cracks
Sub-surface crack from beneath the crater

## Slide 16
WDE MECHANISM – ADVANCED STAGE
Sub-surface cracks
Sub-surface cracking
Micro jetting effect forming due to hydraulic penetration
Material folding (upheaving)
Crack propagation due to lateral flow
Coupon top surface

## Slide 17: Conclusions
Higher the impact speed accelerates the erosion initiation and increases erosion rates.
Main causes of the erosion damage at early stages are the high impact pressure and the lateral jetting.
Formation of microcracks, isolated pits and shallow depressions were typical features associated with the incubation stage.
The hydraulic penetration and stress waves are the main causes of erosion in advanced stages.
Deep cracks, sub-surface cracks, material folding and upheaving are main features observed at the advanced stage.