## Slide 1: About OMICS Group
OMICS Group International is an amalgamation of Open Access publications and worldwide international science conferences and events. Established in the year 2007 with the sole aim of making the information on Sciences and technology ‘Open Access’, OMICS Group publishes 400 online open access scholarly journals in all aspects of Science, Engineering, Management and Technology journals. OMICS Group has been instrumental in taking the knowledge on Science & technology to the doorsteps of ordinary men and women. Research Scholars, Students, Libraries, Educational Institutions, Research centers and the industry are main stakeholders that benefitted greatly from this knowledge dissemination. OMICS Group also organizes 300 International conferences annually across the globe, where knowledge transfer takes place through debates, round table discussions, poster presentations, workshops, symposia and exhibitions.

## Slide 2: About OMICS Group Conferences
OMICS Group International is a pioneer and leading science event organizer, which publishes around 400 open access journals and conducts over 300 Medical, Clinical, Engineering, Life Sciences, Pharma scientific conferences all over the globe annually with the support of more than 1000 scientific associations and 30,000 editorial board members and 3.5 million followers to its credit.
OMICS Group has organized 500 conferences, workshops and national symposiums across the major cities including San Francisco, Las Vegas, San Antonio, Omaha, Orlando, Raleigh, Santa Clara, Chicago, Philadelphia, Baltimore, United Kingdom, Valencia, Dubai, Beijing, Hyderabad, Bengaluru and Mumbai.

## Slide 3: Evaluation and Characterisation of Composite mesoporous Membrane for Lactic acid Esterification BY OKON, EDIDIONG PRIMUS Centre for Process Integration & Membrane Technology (CPIMT),School of Engineering SUPERVISOR
PROF. EDWARD GOBINA

## Slide 4
OUTLINE
Introduction
Ethyl lactate applications
Cation-exchange resin for ethyl lactate
Membrane phenomenon
Innovation
Carrier gas transport
Membrane characterisation
Methodology
Results
Conclusion and future work
2 of 24

## Slide 5
3 of 24
INTRODUCTION
Ethyl lactate (EL) plays a major role as a green solvent and also a replacement for most petrochemical solvents. The production of ethyl lactate suffer a major draw-back such as low conversion and purity, which results in the production to be economically and technically uncompetitive. The use of membranes and heterogeneous catalysts for the selective removal of water from the reaction products to shift the equilibrium towards the higher yield of product have attracted a lot of attention.
Fig. 1: Esterification process on a catalytic membrane

## Slide 6
SOURCE OF ETHYL LACTATE
Ethyl lactate from renewable sources such as those from biomass feedstock. It is a biodegradable solvent with an excellent properties to be applied a green solvent in various applications including pharmaceutical, ink and coatings, food additives and organic synthesis.
4 of 24
Fig. 3: Synthesis of Ethyl lactate
Fig 2: Ethyl lactate life cycle

## Slide 7
Application of Ethyl lactate by industries
5 of 24
Fig 4: Schematic diagram of Ethyl lactate application by industries

## Slide 8
Solid Catalysts for Ethyl lactate Synthesis
Cation-exchange resin
Heterogeneous catalysts
-Amberlyst 36
-Amberlyst 16
-Amberlyst 15
-Dowex 50W8x
6 of 24
Fig. 6: Pictorial diagram of the different catalysts
Fig. 5: types of heterogeneous catalysts

## Slide 9
Membrane Phenomenon
Membrane is a selective or physical barrier that reduces or prevent the mass transfer in a certain material. In the past decade membrane have been regarded as a separation agent. Membranes may be classified as organic or inorganic membranes . The different types of inorganic membrane include:
7 of 24
Inorganic membrane
Porous membrane e.g metal, glass
Mesoporous = 2-50nm
Microporous = < 2nm
Macroporous = > 50nm
Composite membrane e.g metal-metal, glass-metal and ceramic metal
Dense membrane e.g metallic, solid-electrode
Fig. 7: Types of inorganic membranes
Notes: Porous composite and dense membrane

## Slide 10
ADVANTAGES OF AN ENHANCED MEMBRANE
High thermal stability
Mechanical strength
Chemical stability
They allow heterogeneous catalyst
to be deposited easily on the surface.
Increase in yield of product.
Cost effective
Long service life
8 of 24
Fig. 8: Pictorial diagram of a porous membrane
Ceramic porous core
Reactor housing
Seal
Notes: Inorganic membrane possess a lot of advantages

## Slide 11
To characterise resin and ceramic membrane pore size distribution using scanning electron microscopy.
Transport properties of the inorganic composite ceramic membrane with carrier gases use for ethyl lactate separation.
To determine the surface area and pore diameter of a mesoporous membrane using liquid nitrogen adsorption.
To carry out batch process esterification of lactic acid and ethanol and analysed the product using gas chromatograph-mass spectrometer.
Compare the BET surface area and BJH pore diameter results of the 1st and 2nd dip-coated membranes.
9 of 24
INNOVATION

## Slide 12
10 of 24
The four carrier gases used for the experiment include: Helium (He), Argon (Ar), Carbon dioxide (CO2) and Nitrogen (N2).
Fig. 10: Permeation test set-up
Fig. 9: Membrane dip-coating
METHODOLOGY
Membrane dip-coating and Carrier Gas Permeation test
Fig. 11: Air drying of the membrane
Notes: The four carrier gas use for the experiment include: Helium, Argon, Carbon dioxide, Nitrogen

## Slide 13
Transport Mechanism in inorganic ceramic membrane
11 of 24
Fig. 12: Transport mechanism in ceramic membrane
Fig. 13: Gas connection system

## Slide 14
Batch Process Esterification Process
Fig. 14: Batch process set-up
Fig. 15: Auto sample GC-MS instrument
Batch process esterification process and GC-MS instrument for the analysis of esterification product
12 of 24

## Slide 15
13 of 24
METHODOLOGY
Schematic diagram of ceramic membrane dip-coating technique for liquid nitrogen
Fig. 17: Before modification
Fig. 18: After modification
The sample was found to be expand after the modification process
Fig. 16: membrane fragment dip-coating
Notes: Schematic diagram of ceramic membrane preparation

## Slide 16
14 of 24
LIQUID NITROGEN ADSORPTION
Fig. 20: Analytical weighing balance
Fig. 19: Liquid nitrogen adsorption
Sample + cell
Weighing balance
Sample Preparation before the degassing process
Notes: LIQUID NITROGEN ADSORPTION OF MESOPOROUS

## Slide 17
PROPERTIES FOR NITROGEN ADSORPTION MEASEUREMET
Size and Shape
Surface area
Pore size
Pore volume
Porosity
Density
Different properties of membrane that could be measured with Gas Adsorption
Fig. 21: Typical vacuum apparatus
The degassing temperature was set at 65 oC for 2 hrs prior to the sample analysis. The liquid nitrogen temperature was 77 K.
15 of 24

## Slide 18
Nitrogen Adsorption Results for the silica membranes at 77 K
BET Curves for 1st and 2nd dip-coated membrane
Fig.22: Classification of adsorption isotherm
Fig. 22a: BET curve for 1st dip-coated membrane
Fig. 23b: BET curve for 2nd dip-coated membrane
16 of 24

## Slide 19
Fig. 24a: BJH curve for 1st dip-coated membrane
Fig 24b: BJH curve for 2nd dip-coated membrane
Sample | BET Surface area(m2/g) | BJH Pore diameter(nm) | Pore Volume (cc/g)
1st dipping | 0.253 | 4.184 | 0.006
2nd dipping | 1.497 | 4.180 | 0.004
The BET surface area of the dip-coated silica membrane showed a type IV isotherm characteristic of mesoporous structure with hysteresis. The BJH curves of the silica membrane was in accordance with mesoporous classification
Nitrogen Adsorption Results for the silica membranes at 77 K
17 of 24
BJH Curves for 1st and 2nd dip-coated membrane
Table 1: BET and BJH of the membranes

## Slide 20
Catalysts | Retention time (min) | Peak Area ()
Amberlyst 15 | 1.521 | 149055537.3
 | 4.169 | 1761909.18
 | 7.738 | 4826559.45
 | 9.218 | 113978453.4
Amberlyst 16 | 1.503 | 119782347.8
 | 4.143 | 9286786.17
 | 8.731 | 283366480.1
 | 10.502 | 23075482.13
Amberlyst 36 | 1.527 | 138638054.1
 | 3.628 | 98634990
 | 7.975 | 97944520.42
 | 8.726 | 121332143.6
 | 10.490 | 14091694.59
Dowex 50W8x | 1.523 | 142522149.5
 | 3.627 | 78276693.15
GC-MS Results
Fig. 26: NIST spectra for ethyl lactate
18 of 24
Fig. 25: Ion chromatogram of the esterification product
Table 2: Retention time and peak area of catalysts.

## Slide 21
SEM/EDXA Results
19 of 24
SEM/EDXA surface image of the membrane
The membrane showed a defect-free surface with no evidence of crack on the surface of the silica membrane
Ti
Ti
Zr
Zr
Si
Br
O
Ti
Fig. 27: EDXA spectra of the membrane
Fig 28: SEM/EDXA instrument

## Slide 22
The gas flow rate exhibited an increase with gauge pressure indicating Knudsen flow mechanism. The order of the gas kinetic diameter from the highest is given as: N2 > Ar > CO2 > He.
The gas permeance relationship with viscosity was in agreement with the viscous flow mechanism.
PERMEATION TEST RESULTS
20 of 24
Chart: feed perssure (bar)
| 0.1 | 0.2 | 0.30000000000000021 | 0.4 | 0.5 | 0.60000000000000042 | 0.7000000000000004 | 0.8 | 0.9 | 1
CO2 | 0.782 | 1.215 | 1.685 | 1.942 | 2.548 | 2.757 | 3.22 | 3.371 | 3.524 | 3.93
Ar | 0.908 | 2.094 | 2.257 | 2.738 | 3.423 | 3.928 | 4.443 | 4.872 | 5.32 | 6.003
N2 | 0.485 | 0.775 | 0.965 | 1.191 | 1.442 | 1.634 | 1.827 | 1.995 | 2.245 | 2.435
He | 0.51 | 1.12 | 1.35 | 1.73 | 2.05 | 2.98 | 3.02 | 3.25 | 3.42 | 3.79
Relationship between gas flow rate and gauge pressure
Fig. 29: Flow rate relation with pressure
Fig. 30: Permeance relation with viscosity
Notes: RESULTS

## Slide 23
CONCLUSION
21 of 24
The evaluation and characterization of composite mesoporous membrane for lactic acid Esterification was successfully carried out using different methods including nitrogen adsorption, FTIR, GC-MS and SEM/EDXA.
Helium gas with the higher permeation rate was used as one of the carrier gas for the analysis of esterification product.
The SEM surface image of the membrane showed a defect-free surface.
The NIST mass spectra of the esterification reaction product exhibited the structure of ethyl lactate on the spectra.
The BET surface area of the composite membrane showed a type IV isotherm with hysteresis indicating a mesopourous layer.
The BJH curve for the composite membrane was in accordance with the mesoporous classification
Notes: CONCLUSION

## Slide 24
To carry out permeation for the 3rd dip-coated membrane at different temperatures in contrast to the 4th dipping for further analysis of carrier gas with membrane.
To compare the specific surface area and pore diameter of the ceramic membrane with subsequence coating using Liquid nitrogen adsorption.
To carry out ethyl lactate production with flat sheet cellulose acetate membrane at different temperatures.
Quantify the esterification reaction product and correlate the experimental data.
FURTHER WORK
Further work will be carried out to investigate the following:
22 of 24
Notes: Further work will be carried out to investigate the effect of the dip-coating on the inorganic ceramic membrane at different temperature in the course of the research.

## Slide 25
23 of 24
Thanks for your Attention
Question?

## Slide 26: REFERENCES
Mandake MB, Anekar SV, Walke SM. Kinetics study of catalysed and Uncatalyzed Esterification Reaction of acetic acid with methanol. American International Journal of Research in Science, Technology, Engineering & Mathematics. 2013; 3(1):114-121.
Zhang Y, Ma L, Yang J. Kinetics of esterification of lactic acid with ethanol catalyzed by cation-exchange resins. Reactive and Functional Polymers. 2004; 61(1):101-114.
Peters TA, Alzate, JF, Marius AG and Keurentjes TF. Development of a catalytic membrane reactor for integration of reaction and separation in condensation reactions. 2004; 82 (2) 220-228
24 of 24