## Slide 1: PRODUCTION OF INFRA-STRUCTURE READY BIOFULES FROM OLIVE MILL WASTEWATER SLUDGE
Foster Agblevor, H. Abdellaoui, S. Beis, D. Djebbi, K. Halouani*
USTAR Bioenergy Center, Biological Engineering, Utah State University, Logan UT USA
*Sfax University, Sfax, Tunisia

## Slide 2: Contents
Introduction
Objectives
Experimental
Results
Discussion
Conclusions

## Slide 3: Three-Phases decanter

## Slide 4: Serious Environmental Impact of olive mill waste water
Evaporation ponds

## Slide 5: Évaluation des aspects techniques et financiers actuels en matière de gestion des margines en Tunisie
PHOTO
Storage pond

## Slide 6
Chart: 
| Moisture | Hexanes soluble fraction | 95vol%Ethanol soluble fraction | Water soluble fraction | Ash
 | 7.8 | 41.16 | 19.81 | 13.38 | 15.2
Characteristics of OMWS

## Slide 7: Red mud from polutant to Catalyst

## Slide 8
Sample iD | Mineral Constituents
Fresh Red mud | Gibbsite Hematite Calcite Magnetite Perovskite Quartz Goethite Anatase 3NaAISi04.Na2C03
Regenerated Red mud | Hematite Calcite Magnetite Perovskite Quartz Anatase 3NaAISi04.Na2C03
Table 1. Summary of X-Ray Diffraction Results

## Slide 9: Pyrolysis conditions
Feedstock---OMWS
Pyrolysis medium --- Sand or red mud
Pyrolysis temperature 400-500 C
Residence time---- 2-3 s
Feed rate 1 kg/h

## Slide 11
Green diesel fuel; HHV = 43 MJ/kg

## Slide 12
Biochar

## Slide 13
Pyrolysis medium | Sand |  |  | Red mud |  | 
Pyrolysis temp (oC) | 400 | 450 | 500 | 400 | 450 | 500
Organic liquid (%) | 33.1±0.5 | 37.47±1.4 | 30.4±1.9 | 34.6±2.6 | 29.8±1.4 | 29.5±0.4
Pyrolytic water (%) | 8.8±1.9 | 7.93±1.8 | 8.8±0.1 | 11.3±1.8 | 17.6±1.5 | 11.8±0.9
Total liquid (%) | 42.3±2 | 45.4±0.4 | 39.4±1.8 | 45.9±4.4 | 47.4±0.1 | 42.3±1.3
Char/coke (%) | 31.7±2.3 | 25.7±0.3 | 24.4±0.2 | 29.1±1.8 | 22.7±0.2 | 20.4±0.4
Gas (%) | 26.0±3.7 | 29.3±1.0 | 36.2±1.6 | 24.3±2.6 | 30.0±0.04 | 37.3±1.7
Pyrolysis products yields for red mud and silica sand media

## Slide 14
Pyrolysis medium | Silica sand |  |  | Red mud |  | 
Pyrolysis temp (oC) | 400 | 450 | 500 | 400 | 450 | 500
pH | 6.5 | 6.25 | 6.4 | 7.1 | 7.3 | 7.4
Dynamic viscosity (cP) | 42.9 | 42.9 | 28.0 | 9.2 | 5.4 | 4.6
Density (g/cm3) |  | 0.92 | 0.92 | 0.91 | 0.91 | 0.90
HHV (MJ/kg) |  | 37.5 | 38.8 | 39.5 | 40.4 | 41.3
Pyrolysis liquid characteristics

## Slide 15
No. | Retention time (min) | Percentage (%) | Chemical name
1 2 3 4 5 6 7 8 9 10 11 12 13 14 | 14.149 16.379 16.450 18.916 19.624 19.849 20.746 20.793 20.934 21.477 21.583 21.808 22.351 22.469 | 1.29 1.60 1.27 1.98 7.28 2.75 1.88 3.33 4.62 28.54 9.72 5.85 2.22 2.39 | Pentadecane 8-Heptadecene 1-Heptadecene Heptadecane Hexadecanoic acid Hexadecanoic acid, ethyl ester Unknown Unknown 9-Octadecenoic acid (Z), methyl ester Oleic acid Ethyl oleate Unknown Unknown Unknown
Major peaks of bio-oil (>1%) without catalyst identified by GC-MS

## Slide 16
Red mud 450 C
Sand 450 C

## Slide 17
Pyrolysis media | Silica sand |  |  | Red mud |  | 
Pyrolysis temp (oC) | 400 | 450 | 500 | 400 | 450 | 500
H2 | 0.45±0.03 | 0.8±0.1 | 1.1±0.1 | 2.15±0.03 | 3.8±0.3 | 3.88±0.1
CO | 4.7±0.1 | 6.3±0.4 | 6.0±0.6 | 5.9±0.2 | 7.3±0.01 | 10.9±0.9
CO2 | 81.1±2.6 | 76.6±1.4 | 74.6±0.7 | 78.5±0.1 | 72.5±0.9 | 65.2±1.5
CH4 | 1.5±0.4 | 2.1±0.2 | 2.6±0.2 | 1.6±0.2 | 2.6±0.1 | 3.8±0.04
C2-C5 | 10.5±1.9 | 11.5±1.5 | 13.3±0.8 | 10.0±1.1 | 10.8±0.9 | 13.6±0.9
Other hydrocarbons | 1.9±0.5 | 2.8±0.2 | 2.5±0.5 | 1.9±0.3 | 2.9±0.6 | 2.6±0.5
CO/CO2 (mass/mass) | 0.06 | 0.08±0.01 | 0.09 | 0.08±0.00 | 0.10±0.00 | 0.17±0.02
Table 5. Composition of pyrolysis gases generated from sand and red mud OMWS pyrolysis at various temperatures (mass%).

## Slide 18: Hydrotreating of red mud pyrolysis oil
High pressure batch reactor
400 C
37 bar initial hydrogen pressure
15 wt% catalyst
Reaction time 30 min.

## Slide 19
Hydrogenated OMWS pyrolysis oil

## Slide 20
 | Red mud pyrolysis oil | Hydrotreated oil
C (wt%) | 77.70 | 85.55
H (wt%) | 10.07 | 13.15
N (wt%) | 2.33 | 0.55
O (wt%) | 9.88 | 0.79
HHV (MJ/kg) | 40.58 | 45.07
Density (g/cm3) | 0.92 | 0.79
Oil properties

## Slide 21
Olive oil Industry
Bauxite Industry
OMWS
Red mud
Catalytic Pyrolysis
in Fluidized Bed Reactor
Gas
H2, CO, CH4, CO2
Green
Diesel
Fuel
Char
Fertiliser

## Slide 22: Conclusions
Straight pyrolysis of OMWS produces mostly long chain fatty acidic products and hydrocarbons
Red mud catalytic pyrolysis of OMWS produces mostly hydrocarbons, ketones, and alcohols
Hydrotreatment of the red mud catalytic pyrolysis oils produces C11 to C24 hydrocarbons with HHV 46 MJ/kg

## Slide 23: Thank you
Questions?