## Slide 1
2016
© CIC energiGUNE. 2015 All rights reserved
Exploring the limitations of garnet ceramic electrolytes for all-solid-state batteries
2nd International Conference and Expo on
Ceramics & Composite Materials
Berlin, July 26th, 2016
Frederic Aguesse
W. Manalastas, L. Buannic, J-M. Lopez del Amo, G. Singh, A. Llordés, J. Kilner
Notes: PORTADA

## Slide 2: Where are we
Vitoria Gasteiz, capital of Alava province in the Basque country
Initial research circa Sept 2011, Dec 2015 71 researchers

## Slide 3
Li+
Li+
Li+
Li+
Li+
Li+
Li+
Li+
Li+
Li+
Li+
Li+
Discharge
Charge
Positive electrode
Negative electrode
Liquid electrolyte
Current collector
Current collector
Cu
Al
e-
e-
e-
e-
e-
e-
Current Li-ion Battery
Negative electrode:
- High capacity
- Low voltage
- Stability
Positive electrode:
- High energy density
- Long cycling life
- Cost effective
Electrolyte:
- High ionic conductivity
- Low electronic conductivity
- Large electrochemical window

## Slide 4
Motivation
Why use ceramic electrolyte in batteries
Organic liquid electrolytes cause serious safety issues and instability of Li-ion batteries
All-solid-state batteries using non-flammable inorganic solid electrolytes
Main goals:
High safety
High reliability
High energy density
Finegan, D.P., M. Scheel, J.B. Robinson, B. Tjaden, I. Hunt, T.J. Mason, J. Millichamp, M. Di Michiel, G.J. Offer, G. Hinds, D.J.L. Brett, and P.R. Shearing, In-operando high-speed tomography of lithium-ion batteries during thermal runaway. Nat Commun, 2015. 6.
Positive electrode
Negative electrode
Ceramic electrolyte
e-
e-
Li+
Li+
Li+
Li+
Li+
Li+
Li+
Li+
Li+
Li+
Li+
Li+
Current collector
Current collector
Discharge
Charge
Notes: High energy density
(with higher voltage cathodes)

## Slide 5
Kamaya N et al. (2011) Nature Materials 10, 682–686
Li-ion electrolyte : State of the art
doped Li7La3Zr2O12
(Li,La)TiO3

## Slide 6
La rich layer
La poor layer
La rich layer
Ceramic Electrolytes: Li0.34La0.55TiO3
Formed from the cubic perovskite but heavily modified
Ba2+Ti4+O3
La3+2/3TiO3
Li3xLa2/3-xTiO3
A
BO3
ABO3
(1/3 of A-site vacant)
La O Li Ti
Tetragonal distortion of the cubic perovskite which forms into a layered structure

## Slide 7
  Influence of sintering atmospheres
  Li0.34La0.55TiO3
Sintering of the sample in different atmospheres:
    Air
    Synthetic air (mixture of N2, CO2, O2, etc. but no H2O)
    Pure O2 (protected with a humidity trap)
Increase of the GB conductivity by almost a decade
Similar bulk conductivity values
F. Aguesse, J-M. Lopez del Amo, V. Roddatis, A. Aguadero, J. Kilner

## Slide 8
Influence of the moisture level
on the Li-ion mobility : Solid State NMR
H+/Li+ exchange when exposed to air
  In perovskite : formation of Li2CO3
0
-10
10
δ (7Li) (ppm)
Li0.34La0.55TiO3
Air processing
Dry oxygen processing
Li0.34La0.55TiO3
  Li2CO3 at GB
Reduction of Li+ transport numbers
Blocking Li+ migration path

## Slide 9
  Effect on the microstructure
GBs
GBs
Li2CO3
Air sintering
Oxygen sintering
Secondary phase
Direct grain to grain contact

## Slide 10
Limitations of perovskite LLTO electrolyte
Low total ionic conductivity (10-4 S/cm)
Reduction of Ti+3/+4 at low voltage
  Mixed conductivity
Needs of a better candidate !!

## Slide 11
Courtesy of Travis Thompson-PlugVolt Webinar-April 20th 2016
Garnets : attractive properties

## Slide 12
Structural organisation of garnet
for high Li-ion mobility
LaO8 contiguous scaffold
ZrO6 incontiguous scaffold
Garnets
Complex crystal structure
C3A3B2O12
where
CO4 - tetrahedral cages
AO8 - dodecahedral cages
BO6 - octahedral cages
Adams S and Rao P (2012) J. Mater. Chem. 22, 1426
Awaka J et al. (2011) Chemistry Letters. 40 (1), 60-62
Lithium network formed
from face-shared polyhedra
Isolated lithium cages
Notes: Stuffed Garnets (Ia-3d space group)
Complex crystal structure
C3A3B2O12
where
CO4 - tetrahedral cages
AO8 - dodecahedral cages
BO6 - octahedral cages
Relieve structural strain to prevent Tg distortion
Modulate Li occupancy/vacancy distribution
Act as sintering aid
No aliovalent cationic state (voltage stability)

## Slide 13
Processing : Influence of the moisture level
Presence of H+ when processed in air for both garnet and perovskite
Close to 1:1 in ratio + two spin reservoirs are separated in space
Low protonation of the sample when prepared in dry atmosphere (e.g.: dry O2)
-10
0
10
δ (1H) (ppm)
-10
0
10
δ (1H) (ppm)
H+
LiOH*
46%
54%
LOW HUMIDITY LEVEL
Air processing
Dry oxygen processing
* Y. Hu et al., Nature Materials 12, 1130-1136 (2013)
Li6.55Ga0.15La3Zr2O12
Much attention should be paid to moisture level during synthesis and storage

## Slide 14
sLi+ : 2 orders of magnitude higher when processed in O2
20 µm
500 µm
@ RT σGARNET = 1.5 mS.cm-1
σPEROVSKITE = 0.07 mS.cm-1
σe-= 10-6 mS.cm-1
Conductivity
Improvement of the densification when sintering in dry O2 to densities higher than 92 %
Densification
Garnet processed in dry O2
Garnet processed in air
Li0.34La0.55TiO3
Li6.55Ga0.15La3Zr2O12
Air
Dry
O2

## Slide 15
Percolation study of
lithium pathway availability
“Effects of Gallium Doping in Garnet-Type Li7La3Zr2O12 Solid Electrolytes” R. Jalem, M. Rushton, W. Manalastas, Jr., M. Nakayama, T. Kasuga, J.A. Kilner and R. W. Grimes, Chem. Mat. A, 2015
Conductivity vs substituent x in Li7-3x□2xGaxLa3Zr2O12 predicted from MD runs
Chart: 
| 0 | 0.1 | 0.15 | 0.2 | 0.3 | 0.45
 | 1.15e-06 | 0.000121 | 0.0013 | 0.0009 | 7e-05 | 6.41e-05
Ionic conductivity : on the track with the literature
Best experimental value

## Slide 16
Li metal
Ga:LLZO
Interfacial
LiFePO4
catholyte
on Al
Implementation of ceramic electrolyte in a full cell battery
Cathode: Commercial LiFePO4 for flat plateau at 3.45 V
Interfacial catholyte: LP30 for good Li+ transfer at the interface
Ceramic electrolyte: garnet Ga:LLZO
Anode: Metallic lithium for high gravimetric capacity
charge
dishcarge
Li+

## Slide 17
Good capacity retention with increase polarization at discharge
Li metal
Li+
Increased interfacial resistance at discharge
Notes: Very good capacity retention for more than 10 cycles
Inconsistent Coulombic efficiency
 Side reactions, degradation of electrolyte (?)

## Slide 18
Limit of the system: instability at charge
Intermitent degradation at charge
Improvement when cycling at higher temperature

## Slide 19
200 mm
-350
-150
0
150
350
δ (7Li) (ppm)
Dendritic Li
6 mm
180
260
340
Bulk Li
Mobile Li-ion
δ (7Li) (ppm)
40 µm
Li-rich regions
500 µm
Post-test analysis

## Slide 20
Conclusion
  Dry condition processing is a preriquisite to achieve high density, purity and conductivity of garnet and perovskite Li-ion conductors
  Solid State NMR is a unique tool to ensure the absence of undesired H+ and to analyse the Li-ion mobility
  LiFePO4 cathode active material can retain good cycleability with a garnet electrolyte BUT suffers from dendrite formation leading to cracks

## Slide 21
Thank you for your attention !