## Slide 1
New Chemical Approaches to Complete Solvent Removal:
Their Applications in Preparation of Non-porous and Porous PLGA Microspheres
Hongkee Sah
College of Pharmacy, Ewha Womans University
Aug. 22, 2016

## Slide 2
Presentation Contents
Introduction to PLGA microspheres
Issues on contemporary microencapsulation technologies
Innovative approach to make non-porous PLGA microspheres
New paradigm in preparation of porous PLGA microspheres

## Slide 3
Biodegradable Polymer: Poly-lactide-co-glycolide
Source: AAPS J. 2010 Mar; 12(1): 27–32

## Slide 4
Injectable Long-acting Microspheres

## Slide 6
Diabetes Technol Ther. 2011 Nov; 13(11): 1145–1154
10 g BID
0.8 mg QW
2 mg QW
minimally effective level to
reduce fasting plasma glucose

## Slide 7
Sculptra® Aesthetic (injectable poly-L-lactic acid)
Unlike hyaluronic acid (HA) fillers, Sculptra Aesthetic helps stimulate your skin’s own natural collagen production to help restore its inner structure and increase facial volume that has been lost to aging.

## Slide 8
Presentation Contents
Introduction to PLGA microspheres
Issues on contemporary microencapsulation technologies
Innovative approach to make non-porous PLGA microspheres
New paradigm in preparation of porous PLGA microspheres

## Slide 9
Microencapsulation Technology Platforms
Phase separation
Solvent evaporation
Solvent extraction
(Cryogenic) Spray-drying
Spray-drying
Supercritical fluid-based method

## Slide 10
Brand | Company | API | US Patent | Process technology | Remarks
Decapeptyl SR Neo Decapeptyl Trelstar, Pamorelin LA | Debiopharm | Triptorelin pamoate | 5,192,741 | Hot-melt extrusion technology | Phase separation (W/O1/O2 emulsion) is also reported
Sandostatin LAR | Novartis Alkermes | Octreotide acetate | 5,992,682 | (O1+O2)/W emulsion solvent extraction | O1 = MeCl2 (methylene chloride) O2 = drug + methanol
Lupron Depot | Abbvie Endocrine Inc Takeda | Leuprolide acetate | 6,036,976 | W1/O/W2 emulsion solvent evaporation | MeCl2, in-water drying by blowing air to the surface of the emulsion
Risperdal Consta | J&J Alkermes | Risperidone | 6,803,055 | O/W emulsion solvent extraction | O = ethyl acetate + BA
Arestin | Orpharma | Minocylcine HCl | 5,500,228 | S/O1/O2 emulsion (phase separation) | S= milled drug particles O1 = MeCl2 O2 = silicone oil
Bydureon | Astrazeneca Amylin Alkermes | Exendin-4 | 7,456,254 | W/O1/O2 emulsion (phase separation) | O1 = MeCl2 O2 = silicone oil Hardening by heptane/ethanol mixture
Examples of Injectable PLGA Microsphere Products

## Slide 11
aqueous drug solution
organic phase
(PLGA, solvent )
W1/O emulsion
continuous phase (W2 or O2)
Various Emulsion-templated Microencapsulation Processes
W1/O/O2
W1/O/W2
organic phase
(PLGA, drug, solvent)
continuous phase (W or O)
O/W
S/O/W
O/O
S/O/O
solvent removal
emulsification
emulsification
microspheres

## Slide 12
Air
Water
Polymeric MeCl2 droplets
MeCl2 dissolved in water
Microspheres
Typical Emulsion-Based Microencapsulation
Excellent solvation power on PLGA polymers
It has a negligible water solubility (1.32 %)
It easily evaporates to air (39.8 °C)
Toxic halogenated ICH class 2 solvent presenting safety/toxicity issues
Inhalation hazard and a confirmed human carcinogen
One of 200 hazardous pollutants

## Slide 13
Solvent Extraction Techniques (Ethyl Acetate)
Organic solvent droplets
Organic solvent molecules dissolved in H2O
Addition of
Excessive H2O
Quenching
  
  
  
  
emulsion droplets microspheres

## Slide 14
Continuous Microsphere Process
(US Patents 5,945,126 & 6,361,798 )
Continuous phase
Dispersed phase
In-line mixer (L4R/L4RT,
Silverson Machines Inc.)
Solvent extraction
tank

## Slide 15
Limitations of Aqueous Quenching Solvent
The volume of an aqueous quenching solution
Disposal problems and cost
The size of tank/reactor
Ethyl acetate is not a perfect sovent

## Slide 16
Physical/Engineering approaches (solvent evaporation/extraction)
stirring time, temperature, reduced pressure
solvent composition of a dispersed phase
an excessive amount of a quenching liquid
adding semi-polar solvents into a continuous phase
blowing compressed air to the liquid surface of an emulsion
cryogenic solvent extraction
treating embryonic microspheres with heptane/ethanol mixture
hallow fiber filtration coupled with fluidization
II. New paradigms based on chemical approaches
our lab technology platforms
Solvent Removal Techniques

## Slide 17
Presentation Contents
Introduction to PLGA microspheres
Issues on contemporary microencapsulation technologies
Innovative approach to make non-porous PLGA microspheres
New paradigm in preparation of porous PLGA microspheres

## Slide 18
Dispersed phase
Aqueous phase
Dispersed phase
Aqueous phase
(A)
(B)
New Concept of Solvent Removal (I)
equilibrium
Continual solvent diffusion and elimination

## Slide 19
Organic solvent (4 mL)
Aqueous phase (40 mL)
GC analysis
NaOH solution
or
Nothing added
Experimental Design Used to Prove Our Concept

## Slide 20
GC Monitoring of Ethyl acetate/Aqueous Phase System
75 min
60 min
45 min
35 min
25 min
15 min
3 min
uV(x100,000)
0.0
min
75 min
60 min
45 min
35 min
25 min
15 min
3 min
uV(x100,000)
min
0.0
Blank
NaOH 5 mL
Ethyl acetate
Ethyl acetate
Ethanaol
IS

## Slide 21
Ethyl Formate/Aqueous Phase System
5 min
10 min
15 min
45 min
60 min
30 min
1.0
0.0
2.0
3.0
4.0
5.0
6.0
7.0
8.0
9.0
10.0
min
5.0
1.0
2.0
3.0
4.0
6.0
7.0
8.0
9.0
10.0
uV(x10,000)
0.0
1.0
0.0
2.0
3.0
4.0
5.0
6.0
7.0
8.0
9.0
10.0
min
5.0
1.0
2.0
3.0
4.0
6.0
7.0
8.0
9.0
10.0
uV(x10,000)
0.0
5 min
10 min
15 min
45 min
30 min
Blank
NaOH 6 mL
IS
IS
EtOH
EtOH
EF
EF

## Slide 22
Methyl propionate
IPF (IS)
Methyl propionate
Methanol
IPF (IS)
(A) methyl propionate/aqueous phase
(B) methyl propionate/{aqueous phase + NaOH}
GC Chromatograms of Solvent/Water Composites

## Slide 23
2-min 10-min 15-min
Conversion of O/W Emulsion into Single Aqueous Solution
Saponification (Base-Catalyzed Hydrolysis of Ethyl Acetate)

## Slide 24
Typical Non-porous Microsphere Morphology
PLGA/organic solvent droplet
microsphere hardening
non-porous microspheres
Solvent diffusion
Solvent removal
-Estradiol
Mestranol
Ethynyl estradiol

## Slide 26
Presentation Contents
Introduction to PLGA microspheres
Issues on contemporary microencapsulation technologies
Innovative approach to make non-porous PLGA microspheres
New paradigm in preparation of porous PLGA microspheres

## Slide 27
long-acting release
depot
porous scaffolds for
tissue engineering
pulmonary drug
delivery system
Applications of Porous PLGA Microspheres (III)

## Slide 28
Water phase (porogens)
organic phase (PLGA in MeCl2)
W1/O emulsion
aqueous phase (W2)
W1/O/W2 emulsion
pores
PLGA
aqueous solution with porogens
(BSA, NaCl)
leaching of porogens
solvent removal
PLGA
organic solvent
Preparation of Porous Microspheres by W1/O/W2 Emulsion Method Using Various Types of Porogens

## Slide 29
What Are Limitations in Research of
Porous PLGA Microspheres Reported in Literature?

## Slide 30
chemical triggers
Rx
leaching
PLGA/organic solvent droplet phase separation spongelike microspheres
PLGA-rich domains
PLGA-free reaction products
New Paradigm for Preparation of Spongy Microspheres
Make microsphere hardening and porosity generation synchronous in operation~!

## Slide 31
Mechanisms of Solvent Removal and Porosity Induction
An emulsion droplet consisting of PLGA and isopropyl formate
Reaction of the solvent with ammonia to yield water-soluble products
Their leaching to the aqueous continuous phase

## Slide 32
control
0 min 10 min 20 min 30 min
ammonia
Organic Solvent (4 ml) Containing Sudan Emulsified in
Aqueous Continuous Phase (30 ml)

## Slide 34
(a) Without ammonia, emulsion droplets coalesce together to form films
(b) Treatment with ammonia leads to quick microsphere solidification
LM Photographs of Emulsions Sampled at 15-min Stirring

## Slide 35
Morphology of Spongy Microspheres

## Slide 36
Typical Porous PLGA Microspheres Reported in Literature

## Slide 37
Morphology of Our Spongy PLGA Microspheres

## Slide 38
Control of Porosity Levels of Our Spongy PLGA Microspheres

## Slide 40
water phase (biomacromolecules)
organic phase (PLGA in MeCl2)
W1/O emulsion
aqueous phase (W2)
W1/O/W2 emulsion
solvent removal
hardening reactor
ㅜㅁ
normal protein
structure
organic
solvent
solid-liquid
interface
heat
shear
cavitation
liquid-liquid
interface
PLGA-protein
interaction
aggregation
(covalent &
noncovalent)
chemical reaction
(e.g., deamination,
acylation)
loss of activity
denaturation
immune response
Microencapsulation of Biomacromolecules via W1/O/W2 Technique

## Slide 41
An aqueous solution with biomacromolecules
Porous PLGA microspheres
Spontaneous pore-closing
Non-porous, self-closed PLGA microspheres
Loading Biomacromolecules into Pre-formed Porous Microspheres

## Slide 42
0 0.5 hr 1.0 hr 1.5 hr 2.0 hr 4.0 hr
Self-closing of Pores in PLGA Microspheres

## Slide 44
Incubation time (hr)
0 1 2
Loading of FITCDextran into Microspheres
(Pore-closing Process)
CLSM
Fluorometer

## Slide 45
Loading of Lysozyme into Spongelike Microspheres

## Slide 47
Non-halogenated solvents of 66 esters listed on the Joint FAO/WHO Expert Committee on Food Additives
Listed in the US FDA Everything Added to Food in the United States (EAFUS) database
Development of simple O/W emulsion-based microencapsulation technology platforms to manufacture non-porous and porous PLGA microspheres
new paradigm
originality
no porogens
excels W1/O/W2
practicability
scalability
spongy porosity
pore inter-connectivity
What Are Good Points of Our Technology Platforms?