## Slide 1: About Omics Group
OMICS Group International through its Open Access Initiative is committed to make genuine and reliable contributions to the scientific community. OMICS Group hosts over 400 leading-edge peer reviewed Open Access Journals and organize over 300 International Conferences annually all over the world. OMICS Publishing Group journals have over 3 million readers and the fame and success of the same can be attributed to the strong editorial board which contains over 30000 eminent personalities that ensure a rapid, quality and quick review process.

## Slide 2: About Omics Group conferences
OMICS Group signed an agreement with more than 1000 International Societies to make healthcare information Open Access. OMICS Group Conferences make the perfect platform for global networking as it brings together renowned speakers and scientists across the globe to a most exciting and memorable scientific event filled with much enlightening interactive sessions, world class exhibitions and poster presentations
Omics group has organised 500 conferences, workshops and national symposium across the major cities including SanFrancisco,Omaha,Orlado,Rayleigh,SantaClara,Chicago,Philadelphia,Unitedkingdom,Baltimore,SanAntanio,Dubai,Hyderabad,Bangaluru and Mumbai.

## Slide 3: HIGH-EFFICIENCY INTERBAND CASCADE LASERS
Charles D. Merritt, William W. Bewley, Chul Soo Kim, Chadwick L. Canedy, Joshua Abell, Igor Vurgaftman, & Jerry R. Meyer
Naval Research Lab, Washington DC 20375 [MWIR_lasers@nrl.navy.mil]
Mijin Kim
Sotera Defense Solutions, Crofton MD 21114
2nd International Conference on Lasers, Optics, and Photonics
Philadelphia, PA, Sept. 8, 2014

## Slide 4
3 DISTINCT WAYS TO PROVIDE CARRIERS FOR POPULATION INVERSION
n
n
n
n
(2) Quantum Cascade Laser
n
n
p
n
p
(3) Interband Cascade Laser
n
p
p
n
(1) Conventional
Diode Laser
Hybrid of conventional diode (Interband active transitions) & QCL (Cascaded stages)

## Slide 5
1st Proposed: R. Q. Yang (1994) Design Improvements: NRL (1996)
1st Experimental Demo: U. Houston & Sandia (1997)
Further Development: ARL, Maxion, JPL, U. Oklahoma, U. Würzburg, Nanoplus, U. St. Andrews
RT cw operation: NRL (2008)
THE INTERBAND CASCADE LASER

## Slide 6
REBALANCING EFFECT ON THRESHOLD
Dramatic threshold reduction compared to all previous ICLs
[Vurgaftman et al., Nature Com. 2, 585 (2011); U.S. Patent Application 13/422,309 (2012); International Patent Application PCT/US12/29396 (2012)]
Major performance breakthrough with “carrier rebalancing”, via heavy n-doping of electron injectors, to roughly equalize electron & hole populations in active region

## Slide 7
ICL SPECTRAL RANGE & LOW DRIVE POWER
Power density thresholds 30x lower than record QCL results
CW operation to T = 48 °C @ l = 5.7 mm
[Vurgaftman et al., Nature Com. 2, 585 (2011)]
Threshold power density: Pth = Vth x jth
T = 25 °C: Input for lasing < 30 mW Best QCL result:  700 mW
Critical for battery-operated, hand-held, solar-powered, etc.

## Slide 8
DFB ICLs
Poutcw = 18 mW @ T = 46 ºC
Threshold drive power < 400 mW @ 36 °C
Lifetime testing: > 10,000 hrs. cw operation @ 40 °C with negligible degradation
[von Edlinger et al., PTL 26, 480 (2014)]
Grown, processed, & tested @ NRL: Grating etched into deposited Ge [Kim et al., APL 101, 061104 (2012)]
Grown @ NRL; Processed & tested @ JPL:
2nd-order side grating yields single mode
Poutcw = 27 mW @ T = 40 ºC, 1 mW @ 80 ºC Threshold drive power = 280 mW @ 40 ºC
Single-mode tuning with temp: 21.5 nm with current: 10 nm
[Forouhar, et al., to be published]

## Slide 9
118°C
EPI-DOWN MOUNTING: HIGHER Tmaxcw
With NRL carrier rebalancing
[Bewley et al., Opt. Expr. 20, 20894 (2012); U.S. Provisional Patent Application 61611800 (2012)]

## Slide 10
Wider ridge (25.1 mm): 305 mW (M2 = 2.2); WPE = 6.6% @ Pmax
Pmaxcw > 200 mW @ T = 25 ºC (M2 = 1.6)
CORRUGATED-SIDEWALL ICLs
[Bewley et al., Opt. Expr. 20, 20894 (2012)]
Ridge
Lateral Mode Profiles
1
3
2

## Slide 11
Tapered ridge with no straight section
TAPERED ICLs
Pmaxcw (25 ºC) = 403 mW (M2 = 2.3), WPE = 7.0% @ Pmax
[Bewley et al., APL 103, 111111 (2013)]

## Slide 12
As of October 2012:
Try varying other parameters in rich ICL design space, e.g.:
  Thicker n-GaSb separate confinement layers (SCLs), for lower mode overlap with active & clad, hence reduced loss
  More active stages (e.g., 7 vs. 5), for higher slope efficiency & gain
TO FURTHER ENHANCE POWER & BRIGHTNESS: INCREASE EFFICIENCY
Active QWs
Substrate
Bottom Clad
Top Clad
Top Contact
SCL
SCL

## Slide 13
Thick SCLs increase efficiency at 300 K, but fail to provide enough gain at high T
FIRST 5 STAGES WITH THICKER SCLs

## Slide 14
7 STAGES
[Bewley et al., Opt. Expr. 22, 7702 (2014)]
Thick SCLs increase advantage at 300 K, while retaining sufficient gain at high T Even better news: Slope7/Slope5 > 7/5 indicates lower loss!

## Slide 15
Result is significantly higher EDQE:
EXTERNAL DIFFERENTIAL QUANTUM EFFICIENCY
7-stage ICLs with thick SCLs (Gen3B) exhibit higher EDQE & lower loss at all l

## Slide 16
CW POWER & FAR FIELD PROFILE
Pmaxcw = 384 mW in high-quality beam (M2 = 2.6)
WPE = 12.4%

## Slide 17
WIDER RIDGE (w = 32 mm)
[Bewley et al., Opt. Expr. 22, 7702 (2014)]
Pmaxcw up to 592 mW (WPE = 10.1%, M2 = 3.7) @ 25 C; 696 mW (11.7%) @ 15 C

## Slide 18
LATEST RESULTS: 10 STAGES (l = 3.45 mm)
Also: Pmaxcw = 464 mW (WPE = 11%, M2 = 1.9) @ 25 C

## Slide 19
RECORD ICL WALLPLUG EFFICIENCIES
CW WPEs for 4 devices from 2 wafers (7-Stage & 10-Stage): ≈18%
With much shorter 1 mm cavity:

## Slide 20
SUMMARY: CW POWER & BRIGHTNESS
Year | Stages | l | ai | Ridge | Mount | Lcav | width | Pmax25C | WPE(Pmax) | M2 | Brightness
 |  | (mm) | (cm-1) |  |  | (mm) | (mm) | (mW) | (%) |  | (Pmax/M2)
2008 | 5 | 3.75 | 12.2 | Straight | Epi-Up | 3 | 9 | 10 | 0.7 | ≈ 2 | 5
2009 | 5 | 3.67 | 6.6 | " | " | 3 | 10 | 59 | 3.1 | ≈ 2 | 30
2011 | 5 | 3.57 | 6.9 | " | " | 3 | 11 | 158 | 9.9 | 3 | 53
2012 | 5 | 3.66 | 4.5 | Straight | Epi-Down | 4 | 11 | 198 | 7.1 | 1.8 | 110
 |  |  |  | Corrug. | " | " | 25 | 305 | 6.5 | 2.2 | 139
2013 | 5 | 3.72 | 5.2 | Tapered | " | 4 | 5 - 63 | 403 | 7.0 | 2.3 | 175
2014 | 7 | 3.45 | 3.0 | Corrug. | " | 3 | 28 | 522 | 10.3 | 3.1 | 168
 | 10 | 3.45 | 3.4 | Corrug. | " | 4.5 | 18 | 464 | 11.2 | 1.9 | 245
 | 7 | 3.11 | 3.3 | Corrug. | " | 4.5 | 18 | 326 | 6.9 | 1.3 | 243

## Slide 21
QCLs much more widely studied & matured, provide very high cw output powers
ICLs provide much lower power dissipation, possibility for vertical emission, & minimal beam steering – also less mature, so more room for improvement
l = 3-4 mm: ICLs generally preferred
  QCLs now produce Pmaxcw > 1 W @ RT, but higher threshold, lower efficiency, & questionable yield thus far
l = 4-6 mm: QCL sweet spot for high power (Up to 5 W cw demonstrated)
  But ICL still preferred in applications requiring low power from ultra-compact battery-operated package (e.g. laser spectroscopy)
l = 2.5-15 mm LEDs: Only ICLs suitable for top emission
l = 6-150 mm Lasers: QCLs preferred (so far, high loss in ICLs)
QCLs & ICLs can complement each other throughout mid-IR
QCL vs. ICL

## Slide 22: Let Us Meet Again
We welcome all to our future group conferences of Omics group international
Please visit:
www.omicsgroup.com
www.Conferenceseries.com
http://optics.conferenceseries.com/