## Slide 1: Development of Innovative Tool Using Taguchi-methods for the Near Future Ikuo Tanabea aNagaoka University of Technology, 1603-1 Kamitomioka, Nagaoka, Niigata, 940-2188 Japan * Corresponding author. Tel:+0081-258-47-9727; fax:+0081-258-47-9770 E-mail address: tanabe@mech.nagaokaut.ac.jp.

## Slide 2: Background for research
Plan for development
Experiments・Investigation
Failure・
Mistake
Successful
Large cost・ Long time
Notes: 何度も失敗し，トライアルを繰り返す中でどんどん良い値が出てきて成功につながる．というのが一般的に行われている．
成功に至らないこともある．

## Slide 3: Background for research
The software for innovative tool using Taguchi-methods is developed and evaluated. Because developments with short-term and lower cost are strongly required for shorten products life cycle.
Short time・Easy
Speedy・Cheapness
Notes: 品質工学を利用して，対象となる機能を最高水準にするための制御因子の組合せを，きわめて短時間・容易に探索し，迅速・安価に工業製品の開発を行うことが可能なソフトウエアの開発を目的としています．

## Slide 4
Taguchi methods
Many parameters
Compression of
the parameter by
orthoganal table
Trial for influence
of noise by CAE
or experiment
Decision of
optimum parameter
with high robustness
SN ratio (db) = 10 log (μ 2 ／σ2 )
Sensitivity (db) = 10 log μ 2
More large
Many parameters
Compression of
the parameters by
orthoganal table
Trial with influence
of noise by CAE
Decision of
optimum parameter
with high robustness
New methods
Calculation of Properties, Standard
deviation, Total cost, Working time and
Non-defective unit rate for all parameter
Decision of the optimum combination of
Parameters for Properties（Accuracy),Standard
Deviation(Robustness), Total cost, Working time
and Their plural items
Next explanation is this
Notes: ☆ Next explanation is this.

## Slide 5
Cumulative distribution function and Order condition and cost table
Tolerance (ηtol )
Frequency
-ση
+ση
Desired property
Average：μ
σ : Standard
deviation
Non-defective unit rate
G = f (ηtol,μ ,σ)
Tolerance ( Spring back) 0.01
Order entry (unit) 1000
Delivery (hour) 24
Mat. M (yen/unit) 260
Magnesium Mat.O (yen/unit) 180
Sheet Mat.Ob(yen/unit) 180
Teflon (yen/unit) 50
Lubricant Lub. D (yen/unit) 0.00531
Lub. C (yen/unit) 0.304
Disposal cost (yen/unit) 2.16
Charge rate (yen/unit) 2000
Cost
Ordering
Condition
Non-defective unit rate G ＝ f ( ηtol，μ，σ ）
When ηtol :the tolerance , μ:Average，σ :Standard deviation
Number N of all products N ＝ Nord ／ G
When Nord : order entry
Working time for the product Tｍ ＝ Σ(from 1 to final machine number) TV
When TV ：the working time for the machine tool V
Total working time Tall ＝ N Tｍ
When Ｎ ：Numberof all products
Total cost Call ＝ [ Cmat＋Cwas＋Cdis(1－G ) ＋Cm-pri N ]＋TallCｍ
When Cmat: unit cost of material, Cwas :unit cost of consumption
article, Cdis, :waste cost for inferior goods, Cm-pri :amortize cost of the used machine tools, Cｍ :labor cost for one hour
Notes: ☆ This graph is a distribution for a property of a product.
☆ When the distribution is defined by the normal distribution, Cumulative distribution
functions for all combinations using all parameters are calculated using results of the
Taguchi methods. This is an example.
☆ This is order condition & cost table. When the tolerance was decided, Non-defective
unit rate decide.
☆ Then when the order entry was decided, Number of products, Cost, Time
can calculate by these equations

## Slide 6
Experimental set-up for evaluation , Spring back and Simulation model for the CAE
Orthogonal table
Control and noise factors
Levels 1 2 3 4 5 6
Tension MPa 10 50 90 130 170 210
Levels 1 2 3
Levels 1 2
Speed mm/min 150 300 500
Temperature ℃ 150 200 250
Lubricant Teflon Lub. C Lub.D
Material Mat. M Mat. O Mat.Ob
Die radius mm 6 8 10
Clearance mm 5 10 15
Holding force % －10 ＋10
Temperature % －5 ＋5
Mat. M % －1.5 ＋1.5
Mat. O % －3 ＋3
Material
Noise factors Control factors
Mat. Ob % －10 ＋10
New method with five divisions was used for normal distribution of noise factors
Z
Heater
Load cell
Punch
Die
Test piece
r 100 mm
r 8 mm
Blank holding force
10 mm
Blank holder
Experimental set-up
Punch radius rin
r’in
0 ← Spring back → 1
Spring back=│r’in－rin│/ r’in
Spring back
Punch
Die
Test piece
Y
X
Blank holder
CAE model
Notes: ☆ The example is the spring back
☆ Warm press forming consists of Die, Punch, Blank holder and Blank.
☆ Products are here. The product back a little after the forming, that is spring back. Blow 2 are good,
however upper 3 are not good.
☆ This CAE model was used for the trial. Commercial CAE used was Pam-stamp.
☆ These are control factors; Holding force, Punch speed, Temperature, Lubricant,
Material, Die radius and Clearance. Number of all combinations is 4374. Very big.
☆ Noise factors are here. Holding force, Temperature and Property of material are
distribute. Influences of noise factors were inputted by the bar graph with 5 divide
☆ 4374 combinations are compressed to 18 combinations by orthogonal table.
☆ Then the trials with influence of noise were performed by the CAE model

## Slide 7
Results of evaluation for this system
Result Condition
Accuracy
ηave
Priority item
Speed
Temperature
Spring back
Best result
Total Total Non-defective
cost time uinte rate
Call Tall G
Tension 5 5 5 5
2 2 3 2
2 2 2 2
Lubricant 1 3 1 1
Material 2 2 2 2
Die radius 3 3 3 3
Clearance 1 1 3 3
0.0039 0.0091 0.0071 0.0042
No-defective 100 87 93 100
unit rate %
Number of 1000 1152 1073 1000
forming unit
Total time h 7.8 9.0 5.0 7.8
Total cost 24.6 22.6 25.7 24.6
×1000 yen
Best Worst
Spring back 0.09 0.45
Std. deviation 0.007 0.100
SN ratio db 22.18 13.03
Sensitivity db －20.92 －6.94
a: Tension 6 2
b: Punch speed 1 2
c: Temp. of die 3 3
d: Lubricant 2 1
e: Test piece 1 1
f: Die radius 2 2
g: Clearance 2 2
Machining conditions for
confirmation experiment
Conditions
Predicted
results
Comparison results between
prediction and experiment
Best condition Worst condition Gain
SN ratio Prediction 22.18 13.03 9.15
db Experiment 22.06 12.98 9.08
Sensitivity Prediction －20.92 －6.94 －13.98
db Experiment －20.92 －9.12 －11.80
Notes: ☆ This is results. For example, This is the optimum condition for accuracy, the spring back is 0.0039.
This is the highest accuracy. And this is the optimum condition for working
time, the time is 5.0 hours. This is the most first time. .
☆ This is results of calculation before the performance. Therefore I experiment for
evaluation regarding best and worst condition. Experimental results are similar to
calculated results. Therefore this system can calculate the optimum condition
before the performance.

## Slide 8: Flow of my software
1st Trial
2nd Trial
The effective figures for SN ratio and Sensitivity
Using Taguchi-methods
・ The effective figures were rewritten
for the physical image regarding the
influences of the control factors.
・ An operator can intutively understand
and judge the influences of the
control factors.
Estimation of optimum condion for 2nd trial
Next explanation is this
Notes: 要因効果図をもっと物理的に大小関係がしっかり分かるような図に書き換えて，ソフトウエアの操作者に直感的・視覚的な判断を委ね，その判断結果で最適値を探るソフトウエア

## Slide 9
Value of control factor
Level 1
Level 2
Level 3
↑
↑
↑
Result of 1st trial
Recommended levels for 2nd trial
●
●
●
●
Level 1’
Level 3’
Level 2’
Average of function (Desired property)
Estimation for inside
Value of control factor
Level 1
Level 2
Level 3
↑
↑
↑
Result of 1st trial
Average of function (Desired property)
●
●
●
Level 1’
Level 3’
Level 2’
Recommended levels for 2nd trial
●
Estimation for outside
●
●
●
●
●
●
Explanation for my software
Notes: 指数・線形・対数・多項式・累乗
カーブフィットにより，物理的な影響力がよりイメージしやすくなる．

## Slide 10
F2
Valve II
2800 mm
Blender for air
Intake
Drain
Flow meter
Vessel of strong alkali water (545×385×310mm)
Distance D
Flow meter
Water pump
(Max. 2.1 MPa)
Hose (Innerφ8.5 mm)
1300 mm × Innerφ14 mm
Valve I
Compressor
(Max. 1.27 MPa)
1500 mm
Micro bubble device
F1
Terminal of air
Measuring device for heat transfer coefficient
Evaluation using a cooling system
Notes: 強制冷却能力を向上させるための条件探索の実験で本ソフトウエアの総合評価を行った．

## Slide 11
P
D
L
Q
Control factors |  |  |  |  | Noise factor
Name of factors | Length of hose L [mm] | Air pressure P [MPa] | Quantity of flow for strong alkaline water Q [L/min] | Distance from outlet of nozzle D [mm] | Number of experiments: 9
Level 1 | 500 | 0.05 | 0.5 | 10 | 
Level 2 | 1000 | 0.2 | 3.0 | 200 | 
Level 3 | 5000 | 0.4 | 6.0 | 400 | 
Sensor
L
D
P
Q
Experimental parameters for 1st trial
Notes: 制御因子は，空気混合器から吹き出し口までのホースの長さL [mm]，混合する空気の圧力P [MPa]，強アルカリ水の流量Q[l/min]，空気吹き出し口から熱伝達率測定器までの距離D[mm]の4因子．各機器・装置の仕様を考慮して，各3水準を設定した．L9直交表を使用．誤差因子は，9回の実験回数．
冷却効率を上げるためにマイクロバブルを常に8 .0[l/min]供給している．特性値は見かけ上の熱伝達率である．

## Slide 12
Chart: Length of hose L[mm]
| 500 | 1000 | 5000
長さ L[mm] | 4386.9734 | 3958.722 | 3402.0446
Chart: Air pressure P[MPa]
| 0.05 | 0.2 | 0.4
空気圧P[MPa] | 3522.6135 | 4737.0722 | 3540.6256
Chart: Quantity of flow for strong alkaline water Q[l/min]
| 0.5 | 3 | 6
水流量Q[L/min] | 3560.123 | 3367.0146 | 4928.8999
Chart: Distance from outlet of nozzle D[mm]
| 10 | 200 | 400
長さD[mm] | 3513.1768 | 4617.9051 | 3641.7908
Average of function
(Heat transfer coefficient)
Average of function
(Heat transfer coefficient)
Average of function
(Heat transfer coefficient)
Average of function
(Heat transfer coefficient)
L
Q
P
D
Experimental results for 2nd trial

## Slide 13
Chart: Length of hose L mm
| 70 | 250 | 500 | 1000 | 5000
10 | 5800 | 5400 | 5332 | 4817 | 4723
150 | 6172 | 5449 | 5123 | 5000 | 4800
200 | 8500 | 7305 | 7153 | 7224 | 6208
250 | 6362 | 5616 | 4908 | 4800 | 4600
400 | 5700 | 5400 | 5312 | 4625 | 4523
Optimum conditions
Chart: Air pressure P MPa
| 0.05 | 0.15000000000000024 | 0.2 | 0.25 | 0.4
0.5 | 4300 | 4600 | 5782 | 4400 | 4322
3 | 4067 | 4000 | 5469 | 4000 | 4088
4 | 4300 | 5127 | 5740 | 4820 | 4200
5 | 4800 | 5557 | 7016 | 5315 | 4600
6 | 5953 | 6253 | 8500 | 6050 | 5625
Optimum conditions
  At L=70 mm, D=200 mm constant
At P=0.2 MPa, Q=6 l/min constant
Final evaluation

## Slide 14
CONCLUSIONS
It is concluded from the result that;
The manufacture support system using Taguchi methods was made. This system could calculate the optimum condition for each target before the performance. This system was effective for the spring back.
(1)
Innovative tool using the Taguchi methods was useful for development with short-term and lower cost. This tool could quickly and exactly decide the optimum cooling condition. The cooling system with optimum condition using the innovative tool was very effective. And heat transfer coefficient of the proposed cooling system with optimum condition was 8490 W/m2K.
(2)
Notes: ☆ This is conclusions.
☆ (1) The manufacture support system using Taguchi method was made.
☆ (2) This system could calculate the optimum condition for each target before the performance.
☆ (3) This system was effective for the spring back.

## Slide 15
Thank you !
Happy man