## Slide 1
Computer modeling help in understanding molecular spectroscopic anomalies
Istvan Halasz
6th International Conference and Exhibition on
Analytical and Bioanalytical Techniques
Valencia, 2015

## Slide 2
Zeolites
Gels
Alkaline silicate
solutions
PQ is a major manufacturer of silica products
melting
crystallization
Glasses
gelling
Sand + alkaline salt
dissolution
Crystals
Nano, micro
particles
pores

## Slide 3
Al3+
Si4+
O2+
=
H+
Exchangeable cation
Zeolites: microporous (d < 2 nm) crystalline silicates; [SiO4] building blocks
Si4+ can be isomorphously substituted by Al3+ or other elements in lattice
Strong Brønsted acid!

## Slide 4
Modeling UV spectra of microporous titanium silicates
Quantum mechanical/molecular mechanical, QM/MM, approach
TDDFT spectrum calculations
TS-1 catalyst; MFI structure
Contains isomorphously inserted Ti4+
R CH CH2 + 3 H2O
TS-1
R CH2 CH3
+ 2 H2O2
O
O
NOH
+ NH3 + H2O2
TS-1
+ H2O
Ammoximation of cyclohexanone to the oxime
Commercialized:
Epoxidation of olefins

## Slide 5
206
270
211
200
250
300
350
Wavelength [nm]
0
1
2
3.0
Kubelka Munk units
FTUV Absorption of TS-1 samples
Higher
coordinated Ti4+
Isolated tetrahedral Ti4+
I. Halasz, M. Agarwal, E. Senderov, B. Marcus, Stud. Surf. Sci. Catal. 145 (2003) 435.
TS-1-A Well prepared; hydrophobic
TS-1-C Poorly prepared; hydrophilic
222
TS-1-B What is this?; hydrophilic
TS-1-B What is this?; hydrophilic

## Slide 6
Selective catalytic oxidation of n-Hexane by H2O2
I. Halasz, M. Agarwal, E. Senderov, B. Marcus, Catalysis Today 81 (2003) 227.

## Slide 7
I. Halasz, J-J. Liang, G. Fitzgerald, Catal. Lett. 141 (2011) 948.
Modeling UV spectra of microporous titanium silicates
QM/MM & TDDFT
Works well forTS-1!

## Slide 8
The UV of TS-1 with two broken Si-O-Ti bond defects
Ti4+
OH group
I. Halasz, J-J. Liang, G. Fitzgerald, Catal. Lett. 141 (2011) 948.
-Si-O
The Ti-(OH)2 unit turns away from the main channel
-Si-O

## Slide 9
I. Halasz, J-J. Liang, G. Fitzgerald, Catal. Lett. 141 (2011) 948.
Model of extralattice Ti(OH)4 confined in zeolite channel gives
perfect match with experimental UV spectra

## Slide 10
Uniform, submicroscopic micro-channels (d ~ 7.5 A) in a zeolite particle
Key catalyst component in Fluid Catalytic Cracking (FCC) and other technologies
Y zeolite

## Slide 11
Barrer, R. M.; Makki, M. B., Molecular Sieve Sorbents from Clinoptilolite, Can. J. Chem. 1964, 42, 1481
Acid leaching allows to change Si/Al ratio in zeolites.
Dissolved Al leaves hydroxyl nest behind.
Are stable
OH-nests real?

## Slide 12
No desorption beyond 250 C
No specific vibration for OH-nest
E. Senderov, I. Halasz, D. H. Olson Microporous Mesoporous Materials 2014, 186, 94-100

## Slide 13
FTIR confirms that molecular water desorbs up to ~250 oC

## Slide 14
OH-nest in primitive cell
Realistic model with OH nests
Na40Al40(OH)80Si132O304
I. Halasz, E. Senderov, D. H. Olson, J-J. Liang, J. Phys. Chem. C 2015, 119, 8619-8625

## Slide 15
Hydrated Na40Al40(OH)80Si132O304
Grand Canonical Monte Carlo computed
probability of H2O sorption
I. Halasz, E. Senderov, D. H. Olson, J-J. Liang, J. Phys. Chem. C 2015, 119, 8619-8625

## Slide 16
Experimental and computed FTIR spectra of dealuminated samples
Most intense (OH)4 nest bands not found in experimental spectra!

## Slide 17
Reactive Forcefield Molecular Dynamics calculation at 25 oC
Dehydration starts within < 20 ps at 25 oC!
(OH)4 nests can have only ephemeral existence even at room temperature
I. Halasz, E. Senderov, D. H. Olson, J-J. Liang, J. Phys. Chem. C 2015, 119, 8619-8625
Realistic siliceous Y zeolite model with (OH)4 nests

## Slide 18
Conclusion
Molecular modeling is a very useful tool
for interpreting spectroscopic results and
explaining material structures at the molecular level.

## Slide 19
Many thanks to people who helped
in the experimental and modeling work presented
Jian-Jie Liang, Biovia Inc., San Diego, CA, USA
George Fitzgerald, Biovia Inc., San Diego, CA, USA
Mukesh Agarwal, PQ Corporation, Conshohocken, PA, USA
Runbo Li, PQ Corporation, Conshohocken, PA, USA
Eric Senderov, PQ Corporation, Conshohocken, PA, USA (retired)
Davis Olson, Rutgers University, Piscataway, NJ, USA

## Slide 21
FTIR does not indicate new internal hydroxyls in dealuminated sample
The band near 3740 cm-1 is well known as isolated terminal Si-OH

## Slide 22
Static (OH)4-nest model in Y primitive cell
Model after dynamic excitement for 170 ps
Energy jumps with time during ReaxFF dynamic calculation;
50 oC, fs step intervals

## Slide 23
Modeling UV spectra of microporous titanium silicates
Quantum Mechanical/Molecular Mechanical, QM/MM, approach
Time Dependent Density Functional Theory, TDDFT, based spectrum calculations