## Slide 1
Development of anti-insect food packaging materials containing encapsulated essential oils
at a pilot plant scale
Jaejoon Han
Food Process Engineering Laboratory
Department of Food Bioscience and Technology
Korea University

## Slide 2
04
CONTENTS
01
- Insect-proof packaging
02
- For insect-proof packaging
03
INTRODUCTION
LAB SCALE
PILOT PLANT SCALE
HAN LAB
- lab introduction

## Slide 3
04
CONTENTS
01
- Insect-proof packaging
02
- For insect-proof packaging
03
INTRODUCTION
LAB SCALE
PILOT PLANT SCALE
HAN LAB
- lab introduction

## Slide 4
Introduction
▪ Increase of insect penetration risk into stored food products
< Analysis of foreign materials reported in food in 2015, Ministry of Food and Drug Safety, Korea (2016) >
Chart: 
| Insect | Mold | Metal | Plastic | Glass
 | 0.374 | 0.103 | 0.073 | 0.047 | 0.016
Foreign Materials reported in Foods
Plodia interpunctella larvae accounted for the majority of insect contamination
Indian meal moth larvae
Fly
Cockroach
Moth
- 4 -
Chart: 

## Slide 5
Introduction
▪ Indian meal moth (Plodia interpunctella)
< Analysis of foreign materials reported in food in 2015, Ministry of Food and Drug Safety, Korea (2016) >
Chart: 
| Insect | Mold | Metal | Plastic | Glass
 | 0.374 | 0.103 | 0.073 | 0.047 | 0.016
Foreign Materials reported in Foods
Plodia interpunctella larvae accounted for the majority of insect contamination
Indian meal moth larvae
Fly
Cockroach
Moth
- 4 -
One of the most troublesome pests in food industry in Korea during the last 10 years
“Penetrators”
- Penetrate and tear plastic films using sharp mandibles
Quantitative and qualitative losses in processed foods
- Repulsion of the products by consumers

## Slide 6
▪ Increasing needs of insect-proof food packaging system
Introduction
PESTICIDE
INSECT-PROOF PACKAGING
 Use of essential oil extracted from plants
 Non toxic to human and resistance to insect-invasion to food
BENEFIT
 Helps assure consumers of insect-free food and protects manufacturers against loss of goodwill arising from insect-infested packaging
▪ Various essential oils from plants can be applied
 Effective for preventing insects, but toxic to human
- 5 -
Citronella, Clove, Lemongrass, Lemon eucalyptus, Cedarwood, Rosemary, Tea tree, Eucalyptus, Cedar, Catnip, Lavender, Peppermint, Basil, Rose Geranium, Cinnamon, Thyme, Lemon, Orange, Pine, etc.

## Slide 7
Research objectives
1) To find the most effective anti-insect essential oil extracted from natural ingredients against insect penetration into food products
2) To micro-encapsulate the essential oils using various wall materials to demonstrate the controlled release mechanism
3) To verify the use of a pilot plant scale system on manufacture of insect-proof package and its applicability as a food packaging material
- 6 -

## Slide 8
CONTENTS
01
- Insect-proof packaging
02
- For insect-proof packaging
03
04
INTRODUCTION
LAB SCALE
PILOT PLANT SCALE
HAN LAB
- lab introduction

## Slide 9
Screening of the natural anti-insect agents – Essential Oils
Plant essential oils have been widely used for their antimicrobial, antioxidant and insecticidal effects
Natural active agents
Easily evaporate and spread into space (volatile)
Common name | Scientific name | Common name | Scientific name
Garlic | Allium sativum | Pine | Pinus rigida
Onion | Allium cepa | Mint | Mentha spp.
Oregano | Origanum vulgare | Tea tree | Melalueca alternifolia
Sage | Salvia officinalis | Clove | Syzygium aromaticum
Orange | Citrus sinensis | Rosemary | Rosematinus officinalis
Table 1. List of the essential oils from plants – more than 30 different essential oils
Essential oil
▪ Essential oils extracted from plants
- 8 -

## Slide 10
Screening of the natural anti-insect agents – Essential Oils
< Schematic diagram of the fumigant motality assay system >
Filterpaper with EO inside of the cap
0.5L Polyethylene jar
20 glass vials
Ventilation
Calico cloth
3rd instar larva
3 grains of brown rice
Indian meal moth
Plodia interpunctella
Fumigant toxicity assay system
* Fumigant mortality
▪ Screening of the Essential Oils (EOs) for anti-insect activity against Plodia interpunctella and Sitophilus oryzae was done by measuring the fumigant activity and repellent activity
▪ Fumigant motality assay
The number of dead larvae
Screening of Essential Oils
- 9 -
Rice weevil
Sitophilus oryzae

## Slide 11
Screening of the natural anti-insect agents – Essential Oils
Indian meal moth
Plodia interpunctella
▪ Acetylcholinesterase (AChE) inhibition assay:
Neurotransmitter inhibition activity of essential oils was measured by the modified colorimetric method using acetylcholinesterase as a substrate.
- 9 -
Rice weevil
Sitophilus oryzae
Enzyme source : 79 ㎕
+
Anti-insect agents 1 ㎕
+
4 mM 5,5′-dithio-bis(2-nitrobenzoic) acid (DTNB) : 10 ㎕
10 mM Acetylthiocholine iodide (ATChI) : 10 ㎕
+
Calculate the maximum velocity to measure O.D every 30 sec for 20 min in 405 nm with microplate spectrophotometer
homogenize
centrifuge
Supernatant: enzyme source
1 ml phosphate buffer
Thirty of
dead insects

## Slide 12
Screening of the natural anti-insect agents – Essential Oils
< Schematic diagram of the repellent assay system >
2% (v/v) EOs
Filter paper
A
B
C
Repellent
Larvae
Ventilation
Figure 3. Repellent activity of clove bud oil, rosemary oil, and orange oil after (a) 24 h and (b) 48 h against
Plodia interpunctella larvae. Values that do not share a common letter are significantly different (p ≤ 0.05)
CO : Clove bud oil
RO : Rosemary oil
ORO : Orange oil
24 h
48 h
▪ Repellent assay
Screening of repellent activity of EOs
Screening of repellent activity of EOs – Results
- 11 -

## Slide 13
Microencapsulation for controlled release of anti-insect agents
(1) Essential oils
(2) Wall materials
(3) Encapsulation
< β-Cyclodextrin >
< Halloysite nanotube >
▪ Encapsulation techniques for controlled release
GRAS (generally recognized as safe)
Displaying repellent activity
Highly volatile substance
Acting as a carrier
Protecting essential oils from burst release
(controlled release)
Improved stability of essential oil
Controlled release (sustained repellent activity)
Reduced intense odor
[ Examples of Wall materials ]
- 12 -

## Slide 14
Microencapsulation for controlled release of anti-insect agents
1) Microcapsule emulsion containing anti-insect agents
2) Microcapsule powder containing anti-insect agents
< Micrographs of emulsion form >
Wall materials : Gum arabic, maltodextrin, whey protein isolate, β-cyclodextrin, starch, polyvinyl alcohol (PVA)
< Micrographs of powder form >
▪ Microcapsule containing anti-insect agents
Spray dryer
- 13 -
Notes: impregnated

## Slide 15
Microencapsulation for controlled release of anti-insect agents
Halloysite suspension
Spray dryer
< Micrographs of nanotube form >
< Microcapsule powder >
▪ Microencapsulation of anti-insect agents using halloysite nanotube
1) Development of insect repellent-loaded halloysite nanotubes
2) Encapsulated anti-insect agent into HNTs
- 14 -
Notes: impregnated / SiO2 silica

## Slide 16
▪ Development of anti-insect sachet
β – Cyclodextrin
+ EOs
β - Cyclodextrin inclusion complex
Sachet
Anti-insect packaging system
▪ Development of anti-insect multi-layered film
▪ Anti-insect packaging system – Film
▪ Anti-insect packaging system – Sachet
(1)
(2)
- 15 -

## Slide 17
04
CONTENTS
01
- Insect-proof packaging
02
- For insect-proof packaging
03
INTRODUCTION
LAB SCALE
PILOT PLANT SCALE
HAN LAB
- lab introduction

## Slide 18
3. Application of a pilot-plant scale system
1) Twin screw extruder
: SiO2 impregnated with cinnamon oil and LDPE were used to produce master batch
by using a twin screw extruder
< Master batch of cinnamon oil >
Application of a pilot-plant scale system
LDPE
1. Melting
2. Mixing
3. Homogeneous discharge
4. Cooling
5. Pelletizing
SiO2 impregnated with cinnamon oil
▪ Twin screw extruder
[ Hot melt extrusion process ]
- 17 -

## Slide 19
Application of a pilot-plant scale system
▪ Manufacture of master batch
(1) Preparation of master batch manufacture
(2) Input of resin
(3) Mixture of natural insect-proof materials
(4) Extrusion process
(5) Freezing
(6) Cutting, drying, and packaging process
(7) Master batch
(cinnamon oil added)
Cooling

## Slide 20
Application of a pilot-plant scale system
▪ Application of master batch to manufacture food sheet and containers
[ Mixture of cinnamon oil and citric acid master batch ]
Cinnamon oil
master batch 15 %
Cinnamon oil
master batch 30 %
Citric acid
master batch 15 %
[ Extrusion process (cup) – temp 220 ]
(1) Input of blending material, hopper
(2) Purge and extrusion process
Cup

## Slide 21
[ Extrusion process (sheet) – temp 225 ]
Application of a pilot-plant scale system
(1) Input of blending material, hopper
(2) After pressing, sheet molding process
[ Extrusion process (tray) – temp 225 ]
(1) Input of sheet
(2) Molding process under high temperature and high pressure
(3) Cutting
Tray
Sheet

## Slide 22
were coated on PP and LDPE, respectively, and then dried to make insect-proof films
PP or
LDPE film
Essential oil such as Cinnamon oil, allyl disulfide, ally mercaptan, and clove bud oil
: (1) Cinnamon oil encapsulated with PVA
(2) Allyl disulfide and allyl mercaptan homogenized with rice flour
(3) Clove bud oil loaded into halloysite
Application of a pilot-plant scale system
< Process of gravure printed film >
< Developed insect-proof film and paper >
▪ Gravure printing method
[ Gravure printing process ]
- 18 -

## Slide 23
Application of a pilot-plant scale system
▪ Dry laminating & Extrusion lamination machine
: Insect-proof multilayer films, which composed of PP film coated with anti-insect material and LDPE, were produced by dry lamination and extrusion lamination machine
[ Process of insect-proof multilayer film manufacture ]
- 19 -
< Insect-proof multilayer film >

## Slide 24
Application of a pilot-plant scale system
< Penetration test trap >
▪ Penetration test of developed insect-proof films
[ Device for measuring the penetration activity of vermin ]
- 20 -

## Slide 25
Application of a pilot-plant scale system
Accumulated penetration rate (%)
Time (d)
1 2 3 4 5 6 7 8 9 10 11 12 13 14 15 16 17 18 19 20 21 22 23 24 25 26 27 28 29 30
Control : untreated film
AD 5%l : insect-proof film treated with allyl disulfide 5%
▪ Penetration test of developed insect-proof films
[ Result of penetration test of insect-proof multilayer film, 30µm thick]
50% reduction of insect-penetration was shown in multi-layer film but not in control film.
Insect-proof film containing 5 % allyl disulfide showed a high insect-proof ability and it has a potential use as an anti-insect material
- 21 -

## Slide 26
Application of a pilot-plant scale system
▪ Penetration test of developed insect-proof films
- 21 -
100%
48.8%
* Printed LDPE : Gravure-printed low-density polyethylene film
HNTs/CO film : Gravure printed film containing clove bud oil-loaded halloysite nanotubes
HNTs/CO/LBL film : Gravure-printed film containing clove bud oil-loaded halloysite nanotubes with polyethylenimine coating
In penetration tests, HNTs/CO/LBL film showed the anti-insect effect as compared to control.
The encapsulated essential oil was gradually and slowly released by the encapsulation process, causing delayed penetration by insects.
[ Result of penetration test of insect-proof multilayer film, 30µm thick]

## Slide 27
Encapsulated cinnamon oil
Application to real food packaging
[ Application of encapsulated cinnamon oil to corrugated paper box manufacture ]
▪ Encapsulated cinnamon oil for insect-proof adhesive
Anti-insect starch-based adhesive including cinnamon oil encapsulated with β–cyclodextrin
- 22 -
against Plodia interpunctella and Trogoderma granarium
(Khapra beetle)

## Slide 28
Chocolate
Cookie
Caramel
▶ Master batch including anti-insect material
Application to real food packaging
Tray
Cup
▶ Anti-insect films coated by gravure printing machine
▪ Master batch
▪ Gravure printed insect-proof films
[ Application of master batch ]
[ Application of printed insect-proof films ]
- 23 -
Brown rice

## Slide 29
Sensory evaluation
9. Like Extremely
8. Like Very Much
7. Like Moderately
6. Like Slightly
5. Neither Like nor Dislike
4. Dislike Slightly
3. Dislike Moderately
2. Dislike Very Much
1. Dislike Extremely
▪ Sensory evaluation and Acceptance test
Samples
50 Panelists
Chocolate
Color, flavor,
taste, texture
(most widely used scale for measuring food acceptability)
Cookies
Caramel
List
9-point-
hedonic scale
[ 9-point-hedonic scale ]
- 24 -

## Slide 30
Sensory evaluation
▪ Sensory evaluation and Acceptance test
< Table 2. Sensory evaluation of cookies with anti-insect films >
Cookie
Odor
Color
Texture
Taste
Odor of film
(Score)
Overall preference
(Score)
Cinnamon oil (CO) 0 % (control)
Micro-encapsulated CO emulsion 1 %
Cinnamon oil (CO) 2 %
Micro-encapsulated CO emulsion 2 %
< Table 3. Sensory evaluation of caramel candies with anti-insect films >
Caramel
Odor
Color
Texture
Taste
Odor of film
(Score)
Overall preference
(Score)
Cinnamon oil (CO) 0 % (control)
Micro-encapsulated CO emulsion 1 %
Cinnamon oil (CO) 2 %
Micro-encapsulated CO emulsion 2 %
Chocolate
Odor
Color
Texture
Taste
Odor of film
(Score)
Overall preference
(Score)
Cinnamon oil (CO) 0 % (control)
Micro-encapsulated CO emulsion 1 %
Cinnamon oil (CO) 2 %
Micro-encapsulated CO emulsion 2 %
< Table1. Sensory evaluation of chocolates with anti-insect films >
Sensory evaluation of Milk chocolate, cookies, and caramels
In chocolate and cookie, the flavor of films with cinnamon oil 5% was the strongest one in 4 experimental groups.
There was no big difference with a control group although the microencapsulated form of cinnamon oil was applied.
The application of insect-proof films to package real foods has no potential effect on organoleptic property
- 25 -
Number of people
Score
Number of people
Score
Number of people
Score
Number of people
Score
Number of people
Score
Number of people
Score
Number of people
Score
Number of people
Score
Number of people
Score
Number of people
Score
Number of people
Score
Number of people
Score
5
2
6
3
6
2
3
4
4
0
3
0
5
4
5
5
7
6
3
1
7
2
2
2
5
5
4
5
9
7
9
4
3
3
1
12
7
8
3
2
0
1
6
6
2
5
3
6.20
5
6
5.67
4.33
5
6.33
6
4.5
-
6.33
6.15
4.6
5.5
6.6
5
3.89
5.67
4.56
5
6
5.89
6.15
6.08
7.57
5.33
5.67
7
3.86
6
5
4
2.4
5
6.5
4.2
2.78
5.86
3.89
8
3
2.08
7.54
3.23
3.31
6.31
5.92
5.31
4.58
3.5
5
3
5
4.67
4.71
5.13
5.67
3
-
5
5
4
5
6.2
6.33
4.78
6
5.17
5.21
4.5
2.79
1.96
3

## Slide 31
Anti-insect Food Packaging Research
▪ Publications on SCI
< Journal of Stored Products Research, 2015 >
Development of anti-insect food packaging film containing a polyvinyl
alcohol and cinnamon oil emulsion at a pilot plant scale
< Journal of Food Science, 2013 >
< Journal of Food Science, 2013 >
< Journal of Food Science, 2014 >
< Journal of Food Science, 2016 >

## Slide 32
04
CONTENTS
01
- Insect-proof packaging
02
- For insect-proof packaging
03
INTRODUCTION
LAB SCALE
PILOT PLANT SCALE
HAN LAB
- lab introduction

## Slide 33
In Our Lab
Active packaging
Anti-microbial packaging
Anti-oxidant packaging
Anti-insect packaging
Oxygen scavenger
Smart packaging
Packaging study – Migration
Regulations on packaging safety
Biodegradable plastics
Edible coating
Eco-friendly film coating
1. Noble packaging materials
Apple peel by-products
Antioxidant activity
Film-forming ability
Turmeric
Gelatin
Turmeric-gelatin biodegradable film
Non-metallic
oxygen scavenger
Colorimetric pH indicator using natural pigments
Packaging materials
Foods
Mass transfer by concentration gradient
2. New packaging system & technology
3. Safety of packaging materials
▪ Emerging new technologies in food packaging
- 27 -

## Slide 34
http://hanlab.korea.ac.kr/
Food Process Engineering Lab at Korea university
Grazie mille