## Slide 1: PHA Copolymers from CH4
Biopolymers & Bioplastics 2015 (Aug 10, 2015)
Jaewook Myung

## Slide 2: Research backgrounds
Wastewater treatment
  Energy-efficient nitrogen removal
  Biological phosphorus removal
Polyhydroxyalkanoate (PHA)
  PHA recycling
  PHA production from biogas or natural gas

## Slide 3: Life Cycle of PHA Products
① Abiotic-biotic cycle
② Methane-PHA cycle
①
②

## Slide 4: Methane-PHA Cycle
K. H. Rostkowski, C. S. Criddle, M. D. Lepech, Cradle-to-gate life cycle assessment for a cradle-to-cradle cycle: biogas-to-bioplastic (and back). Env. Sci Technol. 46, 9822–9829 (2012).

## Slide 5: PHA Drawback: High Production Cost
Product | Manufacturer | Price ($/lb)
PLA | Natureworks (USA) | 0.85 – 3.00
P3HB | Metabolix (USA) | 2.00 – 2.75
PHBV | Tianan (China) | 2.40 – 2.75
Bio-PE | Braskem (Brazil) | 0.80 – 1.00
Product | Price ($/lb)
Polypropylene (PP) | ~ 0.60 (depending on oil price)
Bioplastics
Petroleum-based plastics

## Slide 6: One Solution
Methane
P3HB
Type II methanotrophs
Available as biogas and natural gas
Waste-driven feedstock
Low substrate cost
Carbon sequestration (CO2 to polymer)
Use of Inexpensive Substrate: Methane (CH4)

## Slide 7: Limitations of P3HB
Low thermal stability
Slow crystallization
Lack of flexibility
Narrow melt processing window
P3HB
PHBV copolymer overcomes these limitations

## Slide 8: PHBV
Poly(3-hydroxybutyrate-co-3-hydroxyvalerate)
http://www.bioplasticpieces.com/products.html
Duan, Wang. (2010) J. R. Soc. Interface, 7(5)
n
m

## Slide 9: Recall: how to produce PHBV?
Abiotic-biotic PHA recycling
PHBV copolymer was produced upon addition of odd-numbered VFAs

## Slide 10: Problem: C1 Metabolism
W.-C. Kao et al., Quantitative proteomic analysis of metabolic regulation by copper ions in Methylococcus capsulatus (Bath). J. Biol. Chem. 279, 51554–51560 (2004).
Many researchers clearly state that… obligate methanotrophs are limited to growing on C1 compounds.
Confirmed: No obligate methanotrophs were able to grow with VFAs

## Slide 11: P3HB Production by methanotrophs
methane
P3HB
Type II methanotrophs
methanol
or

## Slide 12: PHBV Production by methanotrophs
methane
PHBV
propionate
valerate
cosubstrates
methanol
Type II methanotrophs

## Slide 13: Pure culture & enrichment strategy
Methylocystis parvus OBBP
Methylosinus trichosporium OB3b
Methanotrophic enrichment
or
Methanotrophic pure culture
Inoculum from activated sludge

## Slide 14: CH4-Fed Microbial Enrichment

## Slide 15: Two Phases
1) Repeating cycle (balanced growth) – cell replication for 48 hours
2) PHA production step (nutrient-limiting condition) – PHA accumulation for 48 hours
PHA production
(75% of the cells for PHA harvest)
Repeating Cycle
(N > 300)

## Slide 16: PHA Accumulation
A
B
Before PHA production (t = 0h)
B
After PHA production (t = 24h)
A

## Slide 17: SSA-SEM
Serial Section Array-Scanning Electron Microscopy
Reichelt et al., (2012) PloS Pathog.

## Slide 18: SSA-SEM
Serial Section Array-Scanning Electron Microscopy
100 nm
section
reconstruction

## Slide 19: SSA-SEM

## Slide 20: SSA-SEM

## Slide 21: SSA-SEM
stack

## Slide 22: 3-D Reconstruction of PHA Granules
PHA 1
PHA 2
: 18.2%
: 16.0%
Volume fractions

## Slide 23: How do we know we got PHBV?
Gas chromatography (GC)
  - Monomer composition: 3HB and 3HV
Gel permeation chromatography (GPC)
  - Molecular weight distribution
  - Single peak: not a blend of P3HB and P3HV
Differential scanning calorimetry (DSC)
  - Peak melting temperature: typical range for PHBV
  - Single peak: not a blend of P3HB and P3HV

## Slide 24
Questions remain…
microbiologists
1. Is the produced polymer really a copolymer?
  - Need structural verification
2. Do methanotrophs really consume volatile fatty acids?
  - No transporters found in methanotrophs
  - Restricted to C1 metabolism
Solution: NMR & isotopic enrichment

## Slide 25: Hypothesis
Isotopic Enrichment + 13C NMR
methane
valerate
Type II methanotrophs
PHBV
methane
13C-valerate
Type II methanotrophs
13C-PHBV
(*)
(*) = 13C
(*)

## Slide 26: Result
13C NMR
PHBV from 13C-valerate
PHBV from 12C-valerate
(1)
(9)
(8)
(5)
(2)
(3)
(4)
(6)
(7)
(1)
(5)
(5)*
(1)
(5)
(5)*
(1) 3HB-3HB
(5) 3HV-3HV
(5)* 3HV-3HB
20-fold increase in (5) and (5)*
13C-enriched PHBV!

## Slide 27: NMR conclusion
Isotropic enrichment + 13C NMR
(1)
(5)
(5)*
Structural verification
  - PHBV copolymer
Methanotrophic incorporation of volatile fatty acids
  - Valerate is taken up by methanotrophs

## Slide 28: Methanotrophic PHBV Production
methane
P3HB
valerate
No polymer
methane (main substrate)
valerate (co-substrate)
Type II methanotrophs
Type II methanotrophs
Type II methanotrophs
PHBV

## Slide 29: Pure culture & enrichment strategy
Methylocystis parvus OBBP
Methylosinus trichosporium OB3b
Methanotrophic enrichment
or
Methanotrophic pure culture

## Slide 30: Stable microbial community
Methylocystis-dominated methanotrophic enrichment was stable in a long-term operation (> 300 days).

## Slide 31: Stable functional performance
Exponentially growing methanotrophic cells
Chart: PHA wt%
| cycle 12 | cycle 22 | cycle 40 | cycle 57 | cycle 75
Column3 | 49 | 53 | 55 | 52 | 57
Stable PHA production capacity

## Slide 32: PHA Production Phase
Growth Phase
PHA Production Phase

## Slide 33: “Customizable” PHBV Copolymer
Consistency of produced PHA polymer
Ability to tweak the polymer properties
Very critical requirements in polymer industry
Chart: Added valerate concentration (mg/L)
| 0 | 100 | 200 | 400 | 1000 | 2000
OBBP Avg | 0 | 24.5 | 31 | 36.9 | 38.7 | 40.2
3HB
3HV

## Slide 34: Summary
PHBV copolymer

## Slide 35: Thank you!
Acknowledgements
  Craig Criddle
    Wakuna Galega
    Nathan Strong
    Sung-Geun Woo
  Robert Waymouth
    James Flanagan
  Jizhong Zhou
    Joy Van Nostrand
    Tong Yuan
  Curtis Frank
  Sarah Billington
    Cecily Ryan
  Green Team
  Funding
    Samsung Scholarship
    Chevron