## Slide 1: Molybdenum nanoplates incorporated polycaprolactone nanofibers: A potential threat to skin cancer
Janani Indrakumar
Biological Materials Laboratory
CSIR-CLRI, India

## Slide 2
Uncontrolled division of abnormal cells
Stages :
Uncontrolled cell division
Hypoxia
Angiogenesis
Invasion
Metastasis
Cancer

## Slide 3
Basal cell carcinoma
Squamous cell carcinoma
Melanoma
Types of cancer
Non-Melanoma

## Slide 4: Need for this study
Excision is most practiced method
Chemotherapy and radiation are not targeted
After excision rate of relapse is high
Though mortality is not significant
Once metastasized five year survival rate is very low

## Slide 5: Nanoparticles
“Nano” word of the decade
Small size, easy penetration to the plasma membrane
Improves solubility, increases half life
Sustained and targeted delivery into the disease microenvironment
Types of nanoparticles: polymeric nanoparticles, drug nanoparticles, metal nanoparticles etc.,

## Slide 6: Metal oxide nanoparticles
Effective anticancer agents ( CeO2 , TiO2 )
Photo thermal therapy ( Au)
Imaging therapy ( Au , Fe )
Drug carriers

## Slide 7: Molybdenum
Essential trace element
Permissible level of molybdenum in circulation is
about 2 mg/day
Cofactor for various enzymes
Aldehyde oxidase , sulphide oxidase,
Nitrate reductase, xanthine dehydrogenase
Complexes have shown anti-diabetic activity

## Slide 8
MoO3
Cheap alternate
Safe metal oxide
Surface Plasmon resonance
Antibacterial activity

## Slide 9
Objectives
To synthesize and characterize metal oxide nanoparticles
To explore their potential targeted anticancer activity
To develop a carrier system for the nanoparticles targeting skin cancer cells

## Slide 10
Preparation of metal oxide nanoparticles
Metallic acid Precursor
Metal oxide NPs
H20
200ug
MoO3.2H2O MoO3
Calcination
500°C
2 h

## Slide 11
Characterization
X-ray Diffraction
X-Ray Photoelectron Spectroscopy
Orthorhombic plates
Elemental signature

## Slide 12
Hemolytic activity
Anti cancer activity
Compatibility Studies

## Slide 13
Synthesis 
Anticancer activity 
Characterization 

## Slide 14: Current treatment methods
Surgical excision
Chemotherapy
Radiation
Topical treatment

## Slide 15: Nanofibers
Greater loading
Easy transport
Minimal wastage
Sustained delivery
Targeted Release
Methods of preparing nanofibers : Self assembly, centrifugal spinning , Electrospinning
Polymers used : natural ( protein , carbohydrate ) , synthetic ( hydrophilic and hydrophobic )

## Slide 16
Metal oxide NPs
+
15% PCL
0.4ml/ hr
9 kV/ 16 kV
PCL Control Nanofibers
Sample PCL Nanofibers
Polymer
Preparation of Nanofibrous Scaffolds

## Slide 17
Encapsulation of Nanoplates in the nanofibrous scaffolds
FITC-MoO3 encapsulated PCL nanofibers
Raman spectroscopy
PCL , b. MoO3-PCL,
c. MoO3 Nanoplates

## Slide 18
Fourier Transform Infra Red
Spectroscopy
(FTIR )

## Slide 19
Compatibility studies
Anti cancer activity

## Slide 20
Control
PCL
MoO3-PCL
Samples | % Hemolysis
PCL NF | 1.19
MoO3-PCL NF | 1.48
Hemolytic Activity

## Slide 21
A431
HaCaT
AO/PI Staining
TCP
PCL
MoO3-PCL

## Slide 22
JC1 Staining
The mitochondrial membrane of the treated cells were damaged indicating the start of mitochondrial membrane mediated apoptosis
TCP
PCL
MoO3-PCL

## Slide 23
Conclusion
The nanoparticles were successfully prepared and characterized
The thus prepared nanoparticles were tested for their targeted anticancer activity against skin cancer cells
A nanofibrous scaffold system was successful in carrying the nanoparticle and delivering them in the area of interest

## Slide 24
Thank You