## Slide 1: Analysis of the transport of the individual gas mixture components in Polymers of Intrinsic Microporosity and PIM-based Mixed Matrix Membranes
John Jansen
Institute on Membrane Technology, ITM-CNR, Rende (CS), Italy.
September 26-28, 2016 - Valencia, Spain
1

## Slide 2: CNR Institute on Membrane Technology
Sunny Southern Italy
Preparative
Preparation and characterization inorganic, metal, polymeric and mixed matrix membranes
Membranes for fuel cells and hydrogen production
Catalytic membranes and membrane reactors
Processes
New membrane-based unit operations (crystallizers, emulsifiers, strippers, scrubbers, adsorbers, etc.)
Study and development of integrated membrane systems in industrial cycles in agro-food, tanning, textile fields, etc.
Membranes for agro-food and bio-medical applications
Membranes for gas and vapour separation
Membranes for nano-, ultra- and microfiltration
Fundamentals
Modeling and simulation of membrane structures
Study of basic transport phenomena
Mediterranean
Sea
23 Jan 2016
20 km from ITM
5 Mar 2016
45 km from ITM
Rende (CS)
ITM-CNR Headquarters

## Slide 3: Membranes for gas and vapour separation
Asymmetric membrane preparation
  Integrally skinned membranes
  Porous supports and thin film composites
Basic transport studies in dense membranes
  Traditional glassy and semi-crystalline polymers
  Block copolymers
  Amorphous glassy perfluoropolymers (High Free Volume)
  Polymers of intrinsic microporosity (High Free Volume)
  Ionic liquid-based membranes
Mixed matrix membranes
  MOFs, Zeolites, CNTs, graphene

## Slide 4: Introduction Experimental Results and discussion Conclusions

## Slide 5: Introduction : transport in membranes
Membrane
(selective barrier)
Feed mixture
e.g. CO2 /CH4
Retentate
Enriched in methane
CH4 > CO2
Permeate
Enriched in CO2
CO2 > CH4
Gas transport in dense membranes
(not 100% selective)

## Slide 6: Membrane as a black box(?)
Process engineering approach: correlation between input and output.
Knowledge about the membrane material not necessarily needed
Materials science approach: Look inside and know what happens at molecular level.
  How to improve the membrane performance
  Why things go wrong when they go wrong
  What to expect when used under different conditions
 For better membranes, further basic studies of the transport are needed…
?
Notes: In chemical engineering we tend to see membranes as a black box and we do not want to see what is inside the box.
What matters is only the correlation between what goes in and what comes out.
However, if you do not know what happens inside the box, you do not know:
How to improve the membrane performance
Why things go wrong when they go wrong
What to expect when used under different conditions

## Slide 7: Context of the work
Pure gas permeability data of novel membrane materials are common but mixed gas permeation data are relatively rare.
Individual diffusion data not common, diffusion data in mixtures are extremely rare or inexistent.
Aim: development of a technique that is able to analyse the diffusion coefficients of individual species in a gas mixture during permeation experiments.
Notes: Normally we express the performance of a membrane simply in terms of permeability and selectivity, but with the proper measurements we can obtain a lot more information.

## Slide 8: Non-stationary permeation
p1
p2
Permeation time
Feed
Permeate
Immediately after exposure of the membrane to the gas or to the vapour, an equilibrium concentration is reached at the interface of the membrane and the gas phase at the feed side.
Subsequently, the permeant starts diffusing into the membrane and if p1 >> p2 a linear concentration profile will be reached in the membrane after some time.
The speed with which the stationary state is reached depends on the diffusion coefficient.
Pressure (external)
Concentrazion (internal)
3 stages of permeation:
3) Stationary
2) Transient
1) Penetration
C1
C2
0
C1= S × p1
Mass transport vs. time:
[Crank J, Park GS, Diffusion in Polymers Academic Press, London, 1986]
Generally p1>>p2

## Slide 9: Permeation curve: expansion of series
Chart: 
Before TL | 0.00063328 | 0.00063328 | 0.00063328
After TL | 1.2421 | 1.8586 | 0.00063328
Time lag = | 0.00063328
Offset
(starting
pressure)
Baseline slope (leaks)
Stationary
Transient
Penetration

## Slide 10: Introduction Experimental Results and discussion Conclusions

## Slide 11: High Free Volume glassy polymers
The start:
P. Budd, N. McKeown et al.
Chem. Commun. 10, 2004, 230–231.
PIM-1
Highly contorted rigid structure
Poor chain packing, high free volume and high permeability (and solubility)
May strongly interact with the penetrants
Polymers of Intrinsic Microporosity

## Slide 12: Chain Rigidity and Chain Packing
Highly contorted stiff polymer chains
 Inefficient chain packing
 High free volume
 High permeability
PIM-EA-TB
M. Carta et al., Science 2013, 339, 303-307.

## Slide 13: PIM structural variations (1)
M. Guiver, Macromolecules 2009
PIM-1
Thioamide-PIM-1
Carboxy-PIM-1
Amine-PIM-1
PIM-Tetrazole
C. Mason, P. Budd et al., Macromolecules, 2011, 44, 6471-6479
M. Guiver, Nature Mater. 2011
P. Budd, N. McKeown et al.
Chem. Commun. 10, 2004, 230–231.
C. Mason, P. Budd et al., Macromolecules, 2014, 47, 1021-1029
Functional
groups

## Slide 14: PIM Structural variations (2)
PIM-EA-TB
PIM-SBI-TB
Contortion
site
Backbone
groups
SBF-PIM-1
IR-579a
PIM-1
Carta, McKeown, Jansen et al.,
Science, 339, 2013, 303-307.

## Slide 15: Free volume modelling
N2 probe
O2 probe
Positronium probe
Bulk / Slice model
Isolated FVE
Interconnected FVE
Sorption
&
Diffusion
Smaller molecules ‘see’ a larger and more interconnected free volume
 Diffusion selectivity (O2 vs. N2)
Affinity with the polymer allows a higher concentration
 Solubility selectivity (e.g. CO2 vs. N2)
Free volume model
E. Tocci et al., Macromolecules 2014, 47, 7900-7916.

## Slide 16: Permeation: 1) Fixed volume - variable pressure setup
Traditional time lag instrument based on dead end cell and gas pressure analysis

## Slide 17: Permeation setup – fixed V, variable p
Pressure increase measurement in fixed volume setup:
Pure gas permeation
Max. 8 gases
1 liquid (vapour)
Controlled temperature
Variable Pressure
< 1.3 bar
Sampling:
> 25 pts./second
Pneumatic valves:
short reaction times
Jansen et al., Polymer 48 (2007) 2619

## Slide 18: Pure gas setup - Instrumental time lag
PIM membrane IR-579a
Perforated aluminium foil
Small instrumental time lag (<0.1s) due to delay in reaction time of valves and pressure sensor.
 Constant for all gases and usually negligible, except perhaps for He and H2.
Chart: Time (s)
| 1E-3 | 0.16300000000000001 | 0.245 | 0.32700000000000001 | 0.40100000000000002 | 0.48299999999999998 | 0.56499999999999995 | 0.64800000000000002 | 0.72199999999999998 | 0.80400000000000005 | 0.88700000000000001 | 0.96899999999999997 | 1.0509999999999999 | 1.133 | 1.2150000000000001 | 1.2989999999999999 | 1.381 | 1.4630000000000001 | 1.5449999999999999 | 1.627 | 1.708 | 1.7909999999999999 | 1.873 | 1.956 | 2.0339999999999998 | 2.117 | 2.1989999999999998 | 2.282 | 2.363 | 2.4449999999999998 | 2.5339999999999998 | 2.6269999999999998 | 2.7090000000000001 | 2.7930000000000001 | 2.875 | 2.9580000000000002 | 3.0190000000000001 | 3.101 | 3.1840000000000002 | 3.2669999999999999
Hydrogen | 0.21878 | 0.54502 | 0.87059 | 1.1962 | 1.4915 | 1.82 | 2.1454 | 2.4774 | 2.7751 | 3.1009 | 3.4324 | 3.7618 | 4.0882 | 4.419 | 4.7437 | 5.0757 | 5.403 | 5.7314 | 6.0606 | 6.3841 | 6.7114 | 7.0481 | 7.3747 | 7.7045 | 8.0187 | 8.3416 | 8.6765 | 9.0011 | 9.3295 | 9.6514 | 10.0094 | 10.3739 | 10.7075 | 11.0395 | 11.37 | 11.6969 | 11.9393 | 12.2703 | 12.6044 | 12.929
Helium | 0.14999 | 0.37503 | 0.55675 | 0.78567 | 1.0099 | 1.2363 | 1.4627 | 1.6888 | 1.9164 | 2.1428 | 2.3666 | 2.5956 | 2.8219 | 3.0535 | 3.2809 | 3.5073 | 3.7349 | 3.9391 | 4.1663 | 4.3912 | 4.6208 | 4.8488 | 5.0805 | 5.3033 | 5.5309 | 5.7583 | 5.9866 | 6.2148 | 6.4427 | 6.6741 | 6.903 | 7.1265 | 7.3552 | 7.5858 | 7.8155 | 8.0429 | 8.2752 | 8.4979 | 8.7269 | 8.9583 | 9.191 | 9.4093 | 9.644 | 9.8681 | 10.0986 | 10.2965 | 10.5343 | 10.7568 | 10.9812 | 11.2073 | 11.4369 | 11.6645 | 11.9009 | 12.1247 | 12.3527 | 12.5812 | 12.8125 | 13.0416
Before TL | 0.040797 | 0.040797 | 0.040797
After TL | 0.42201 | 2.6896 | 0.040797
Time lag = | 0.040797
Chart: Time (s)
Before TL | 0.00063328 | 0.00063328 | 0.00063328
After TL | 1.2421 | 1.8586 | 0.00063328
Time lag = | 0.00063328

## Slide 19: Permeation: 2) Fixed pressure - variable volume setup
Mixed gas permeation instrument based on a cross-flow cell and gas composition analysis

## Slide 20: Mixed gas setup with cross-flow cell
Gas chromatography:
Slow, discontinuous analysis
Micro-GC faster, but less flexible
MFC
Ar
BPC
Traditional
gas analyser
(GC, GC-MS, Micro GC)
Retentate
Permeate
Sweep
MFC
N2
MFC
O2
MFC
CH4
MFC
CO2
Feed
Bubble Flow Meter
N2
O2
CH4
CO2
Ar
Bubble Flow Meter
Excess
Alternative
 In-line Mass spectrometric analysis

## Slide 21: Quadrupole MS residual gas analyzer
Quadrupole Mass Spectrometer for residual gas analysis
0.1 – 10 pt/s sampling time
Max. 200 AMU
Argon Sweeping gas (15-50 ml/min)
Mass flow controllers for Ar, N2, O2, CO2, CH4
Pressure controller 0-5 bar (1-6 bara)
Maximum 5 independent channels (alternatingly)
Membrane cell
Q-RGA
Channel selection
B. Flaconneche et al., Oil Gas Sci. Technol. 56 (2001) 245–259.
!

## Slide 22: System optimization : quick gas switch
TEST
Position 2
Retentate
MFC
Ar Purge
Purge
Test
MFC
Ar Purge
BPC
BPC
PURGE
Position 1
Independent
MS SV1
MS SV1
MS SV3
MS SV3
MS SV2
MS SV2
MFC
Ar
MFC
Ar
Retentate
Sweep
Sweep
6-Way valve
MFC
N2
MFC
O2
MFC
CH4
MFC
CO2
MFC
N2
MFC
O2
MFC
CH4
MFC
CO2
5
6
2
1
3
4
5
6
2
1
3
4
Feed
Feed
6-Way valve
Bubble FM
Bubble FM
Bubble FM
Bubble FM
Bubble FM
Bubble FM
Permeate
Permeate

## Slide 23: Effect of dead volumes in the system
TEST
Position 2
Test
MFC
Ar Purge
BPC
MS SV1
MS SV3
MFC
Ar
Retentate
Sweep
MFC
N2
MFC
O2
MFC
CH4
MFC
CO2
5
6
2
1
3
4
Feed
6-Way valve
Bubble FM
Bubble FM
Bubble FM
Permeate
MS SV2
MS SV2
Limitation: every part of the plant has dead volume causing delay in the gas analysis

## Slide 24: Introduction Experimental Results and discussion Conclusions

## Slide 25: Time lag analysis
Chart: Measurement time (h:mm)
CH4
O2
Sample IR-579a As cast
Feed gas on
5% CO2, 95% N2

## Slide 26: Time lag analysis (differential signal)
Chart: Measurement time (mm:ss)
CH4
O2
 | 0.00069444
Feed gas on
Sample IR-579a As cast
5% CO2, 95% N2
CO2
N2

## Slide 27: Integration of differential signal
Chart: Measurement time (mm:ss)
| 3.4722222222222222E-5 | 5.7870370370370366E-5 | 9.2592592592592588E-5 | 1.273148148148148E-4 | 1.9675925925925926E-4 | 2.7777777777777778E-4 | 3.4722222222222224E-4 | 4.1666666666666669E-4 | 4.9768518518518521E-4 | 5.6712962962962956E-4 | 6.3657407407407402E-4 | 7.175925925925927E-4 | 7.8703703703703705E-4 | 8.564814814814815E-4 | 9.3750000000000007E-4 | 1.0069444444444444E-3 | 1.0879629629629629E-3 | 1.1574074074074073E-3 | 1.2268518518518518E-3 | 1.3078703703703705E-3 | 1.3773148148148147E-3 | 1.4467592592592594E-3 | 1.5277777777777779E-3 | 1.5972222222222221E-3 | 1.6782407407407406E-3 | 1.7476851851851852E-3 | 1.8171296296296297E-3 | 1.8865740740740742E-3 | 1.9560185185185184E-3 | 2.0370370370370373E-3 | 2.1064814814814813E-3 | 2.1874999999999998E-3 | 2.2569444444444447E-3 | 2.3263888888888887E-3 | 2.4074074074074076E-3 | 2.4768518518518516E-3 | 2.5462962962962961E-3 | 2.627314814814815E-3 | 2.6967592592592594E-3 | 2.7662037037037034E-3 | 2.8472222222222219E-3 | 2.9166666666666668E-3 | 2.9976851851851848E-3 | 3.0671296296296297E-3 | 3.1365740740740742E-3 | 3.2175925925925926E-3 | 3.2870370370370367E-3 | 3.3564814814814811E-3 | 3.4375E-3 | 3.5069444444444445E-3 | 3.5879629629629629E-3 | 3.6574074074074074E-3 | 3.7268518518518514E-3 | 3.8078703703703707E-3 | 3.8773148148148143E-3 | 3.9467592592592592E-3 | 4.0277777777777777E-3 | 4.0972222222222226E-3 | 4.1782407407407402E-3 | 4.2476851851851851E-3 | 4.31712962962963E-3 | 4.3981481481481484E-3 | 4.4675925925925933E-3 | 4.5370370370370365E-3 | 4.6180555555555558E-3 | 4.6874999999999998E-3 | 4.7685185185185183E-3 | 4.8379629629629632E-3 | 4.9074074074074072E-3 | 4.9884259259259265E-3 | 5.0578703703703706E-3 | 5.1273148148148146E-3 | 5.208333333333333E-3 | 5.2777777777777771E-3 | 5.3587962962962964E-3 | 5.4282407407407404E-3 | 5.4976851851851853E-3 | 5.5787037037037038E-3 | 5.6481481481481478E-3 | 5.7291666666666671E-3 | 5.7986111111111112E-3 | 5.8680555555555543E-3 | 5.9490740740740745E-3 | 6.0185185185185177E-3 | 6.0879629629629643E-3 | 6.168981481481481E-3 | 6.238425925925925E-3 | 6.3194444444444444E-3 | 6.3888888888888884E-3 | 6.4583333333333333E-3 | 6.5393518518518517E-3 | 6.6087962962962966E-3 | 6.6782407407407415E-3 | 6.7592592592592591E-3 | 6.828703703703704E-3 | 6.9097222222222225E-3 | 6.9791666666666674E-3 | 7.0486111111111105E-3 | 7.1296296296296307E-3 | 7.1990740740740739E-3 | 7.2685185185185188E-3 | 7.3495370370370372E-3 | 7.4189814814814813E-3 | 7.5000000000000006E-3 | 7.5694444444444446E-3 | 7.6388888888888886E-3 | 7.719907407407408E-3 | 7.789351851851852E-3 | 7.858796296296296E-3 | 7.9398148148148145E-3 | 8.0092592592592594E-3 | 8.0902777777777778E-3 | 8.1597222222222227E-3 | 8.2291666666666659E-3 | 8.3101851851851861E-3 | 8.3796296296296292E-3 | 8.4606481481481494E-3 | 8.5300925925925926E-3 | 8.5995370370370357E-3 | 8.6805555555555559E-3 | 8.7499999999999991E-3 | 8.819444444444444E-3 | 8.9004629629629625E-3 | 8.9699074074074073E-3 | 9.0509259259259258E-3 | 9.1203703703703707E-3 | 9.1898148148148139E-3 | 9.2708333333333341E-3 | 9.3402777777777772E-3 | 9.4212962962962957E-3 | 9.4907407407407406E-3 | 9.5601851851851855E-3 | 9.6412037037037039E-3 | 9.7106481481481471E-3 | 9.780092592592592E-3 | 9.8611111111111104E-3 | 9.9305555555555553E-3 | 1.0011574074074074E-2 | 1.0081018518518519E-2 | 1.0150462962962964E-2 | 1.0231481481481482E-2 | 1.0300925925925927E-2 | 1.0381944444444444E-2 | 1.045138888888889E-2 | 1.0520833333333333E-2 | 1.0601851851851854E-2 | 1.0671296296296297E-2 | 1.074074074074074E-2 | 1.082175925925926E-2 | 1.0891203703703703E-2 | 1.0972222222222223E-2 | 1.1041666666666667E-2 | 1.1111111111111112E-2 | 1.119212962962963E-2 | 1.1261574074074071E-2 | 1.1331018518518518E-2 | 1.1412037037037038E-2 | 1.1481481481481483E-2 | 1.1562499999999998E-2 | 1.1631944444444445E-2 | 1.1701388888888891E-2 | 1.1782407407407406E-2 | 1.1851851851851851E-2 | 1.1921296296296298E-2 | 1.2002314814814815E-2 | 1.207175925925926E-2 | 1.2152777777777778E-2 | 1.2222222222222223E-2 | 1.2291666666666666E-2 | 1.2372685185185186E-2 | 1.2442129629629629E-2 | 1.252314814814815E-2 | 1.2592592592592593E-2 | 1.2662037037037039E-2 | 1.2743055555555556E-2 | 1.2812499999999999E-2 | 1.2881944444444446E-2 | 1.2962962962962963E-2 | 1.3032407407407407E-2 | 1.3113425925925926E-2 | 1.3182870370370371E-2 | 1.3252314814814814E-2 | 1.3333333333333334E-2 | 1.3402777777777777E-2 | 1.3483796296296298E-2 | 1.3553240740740741E-2 | 1.3622685185185184E-2 | 1.3703703703703704E-2 | 1.3773148148148147E-2 | 1.3842592592592594E-2 | 1.3923611111111111E-2 | 1.3993055555555555E-2 | 1.4074074074074074E-2 | 1.4143518518518519E-2 | 1.4212962962962962E-2 | 1.4293981481481482E-2 | 1.4363425925925925E-2 | 1.4432870370370372E-2 | 1.4513888888888889E-2 | 1.4583333333333332E-2 | 1.4664351851851852E-2 | 1.4733796296296295E-2 | 1.480324074074074E-2 | 1.4884259259259259E-2 | 1.4953703703703705E-2 | 1.503472222222222E-2 | 1.5104166666666667E-2 | 1.5173611111111112E-2 | 1.525462962962963E-2 | 1.5324074074074073E-2 | 1.539351851851852E-2 | 1.5474537037037038E-2 | 1.554398148148148E-2 | 1.5613425925925926E-2 | 1.5694444444444445E-2 | 1.5763888888888886E-2 | 1.5844907407407408E-2 | 1.5914351851851853E-2 | 1.5983796296296295E-2 | 1.6064814814814813E-2 | 1.6134259259259261E-2 | 1.621527777777778E-2 | 1.6284722222222221E-2 | 1.6354166666666666E-2 | 1.6435185185185188E-2 | 1.650462962962963E-2 | 1.6574074074074074E-2 | 1.6655092592592593E-2 | 1.6724537037037034E-2 | 1.6805555555555556E-2 | 1.6875000000000001E-2 | 1.6944444444444443E-2 | 1.7025462962962961E-2 | 1.7094907407407409E-2 | 1.7175925925925924E-2 | 1.7245370370370369E-2 | 1.7314814814814814E-2 | 1.7395833333333336E-2 | 1.7465277777777777E-2 | 1.7534722222222222E-2 | 1.7615740740740741E-2 | 1.7685185185185182E-2 | 1.7766203703703704E-2 | 1.7835648148148149E-2 | 1.7905092592592594E-2 | 1.7986111111111109E-2 | 1.8055555555555557E-2 | 1.8124999999999999E-2 | 1.8206018518518517E-2 | 1.8275462962962962E-2 | 1.8356481481481481E-2 | 1.8425925925925925E-2 | 1.849537037037037E-2 | 1.8576388888888889E-2 | 1.8645833333333334E-2 | 1.8715277777777779E-2 | 1.8796296296296297E-2 | 1.8865740740740742E-2 | 1.894675925925926E-2 | 1.9016203703703705E-2 | 1.9085648148148147E-2 | 1.9166666666666669E-2 | 1.923611111111111E-2 | 1.9305555555555555E-2 | 1.9386574074074073E-2 | 1.9456018518518518E-2 | 1.9537037037037037E-2 | 1.9606481481481482E-2 | 1.9675925925925927E-2 | 1.9756944444444445E-2 | 1.982638888888889E-2 | 1.9907407407407408E-2 | 1.9976851851851853E-2 | 2.0046296296296295E-2 | 2.0127314814814817E-2 | 2.0196759259259258E-2 | 2.0266203703703703E-2 | 2.0347222222222221E-2 | 2.0416666666666666E-2 | 2.0497685185185185E-2 | 2.056712962962963E-2 | 2.0636574074074075E-2 | 2.071759259259259E-2 | 2.0787037037037038E-2 | 2.0868055555555556E-2 | 2.0937499999999998E-2 | 2.1006944444444443E-2 | 2.1087962962962961E-2 | 2.1157407407407406E-2 | 2.1226851851851854E-2 | 2.1307870370370369E-2 | 2.1377314814814818E-2 | 2.1458333333333333E-2 | 2.1527777777777781E-2 | 2.1597222222222223E-2 | 2.1678240740740738E-2 | 2.1747685185185186E-2 | 2.1817129629629631E-2 | 2.1898148148148149E-2 | 2.1967592592592594E-2 | 2.2048611111111113E-2 | 2.2118055555555557E-2 | 2.2187499999999999E-2 | 2.2268518518518521E-2 | 2.2337962962962962E-2 | 2.2407407407407407E-2 | 2.2488425925925926E-2 | 2.255787037037037E-2 | 2.2638888888888889E-2 | 2.2708333333333334E-2 | 2.2777777777777775E-2 | 2.2858796296296294E-2 | 2.2928240740740739E-2 | 2.2997685185185187E-2 | 2.3078703703703702E-2 | 2.314814814814815E-2 | 2.3229166666666665E-2 | 2.3298611111111107E-2 | 2.3368055555555555E-2 | 2.344907407407407E-2 | 2.3518518518518518E-2 | 2.3587962962962963E-2 | 2.3668981481481485E-2 | 2.3738425925925923E-2 | 2.3819444444444445E-2 | 2.388888888888889E-2 | 2.3958333333333331E-2 | 2.4039351851851853E-2 | 2.4108796296296298E-2 | 2.417824074074074E-2 | 2.4259259259259258E-2 | 2.4328703703703703E-2 | 2.4409722222222222E-2 | 2.4479166666666666E-2 | 2.4548611111111115E-2 | 2.462962962962963E-2 | 2.4699074074074078E-2 | 2.476851851851852E-2 | 2.4849537037037035E-2 | 2.4918981481481483E-2 | 2.4999999999999998E-2 | 2.5069444444444446E-2 | 2.5138888888888891E-2 | 2.521990740740741E-2 | 2.5289351851851851E-2 | 2.5358796296296296E-2 | 2.5439814814814814E-2 | 2.5520833333333336E-2 | 2.5590277777777778E-2 | 2.5659722222222223E-2 | 2.5740740740740745E-2 | 2.5810185185185183E-2 | 2.5879629629629627E-2 | 2.5960648148148149E-2 | 2.6030092592592594E-2 | 2.6111111111111113E-2 | 2.6180555555555558E-2 | 2.6249999999999999E-2 | 2.6331018518518517E-2 | 2.6400462962962962E-2 | 2.6469907407407411E-2 | 2.6550925925925926E-2 | 2.6620370370370374E-2 | 2.6689814814814816E-2 | 2.6770833333333331E-2 | 2.6840277777777779E-2 | 2.6921296296296294E-2 | 2.6990740740740742E-2 | 2.7060185185185187E-2 | 2.7141203703703706E-2 | 2.7210648148148147E-2 | 2.7280092592592592E-2 | 2.736111111111111E-2 | 2.7430555555555555E-2 | 2.75E-2 | 2.7581018518518519E-2 | 2.7650462962962963E-2 | 2.7731481481481478E-2 | 2.7800925925925923E-2 | 2.7870370370370368E-2 | 2.7951388888888887E-2 | 2.8020833333333332E-2 | 2.809027777777778E-2 | 2.8171296296296302E-2 | 2.8240740740740736E-2 | 2.8321759259259258E-2 | 2.8391203703703707E-2 | 2.8460648148148148E-2 | 2.854166666666667E-2 | 2.8611111111111115E-2 | 2.8680555555555553E-2 | 2.8761574074074075E-2 | 2.883101851851852E-2 | 2.8912037037037038E-2 | 2.8981481481481483E-2 | 2.9050925925925928E-2 | 2.9131944444444446E-2 | 2.9201388888888888E-2 | 2.9282407407407406E-2 | 2.9351851851851851E-2 | 2.9421296296296296E-2 | 2.9502314814814815E-2 | 2.9571759259259259E-2 | 2.9641203703703701E-2 | 2.9722222222222219E-2 | 2.9791666666666664E-2 | 2.9861111111111113E-2 | 2.9942129629629628E-2 | 3.0011574074074076E-2 | 3.0081018518518521E-2 | 3.0162037037037032E-2 | 3.0231481481481481E-2 | 3.0312499999999996E-2 | 3.0381944444444444E-2 | 3.0451388888888889E-2 | 3.0532407407407411E-2 | 3.0601851851851852E-2 | 3.0671296296296294E-2 | 3.0752314814814816E-2 | 3.0821759259259257E-2 | 3.0902777777777779E-2 | 3.0972222222222224E-2 | 3.1041666666666665E-2 | 3.1122685185185187E-2 | 3.1192129629629629E-2 | 3.1273148148148147E-2 | 3.1342592592592596E-2 | 3.1412037037037037E-2 | 3.1493055555555559E-2 | 3.15625E-2 | 3.1631944444444442E-2 | 3.1712962962962964E-2 | 3.1782407407407405E-2 | 3.1863425925925927E-2 | 3.1932870370370368E-2 | 3.2002314814814817E-2 | 3.2083333333333332E-2 | 3.2152777777777773E-2 | 3.2222222222222222E-2 | 3.2303240740740737E-2 | 3.2372685185185185E-2 | 3.24537037037037E-2 | 3.2523148148148148E-2 | 3.259259259259259E-2 | 3.2673611111111105E-2 | 3.2743055555555553E-2 | 3.2812500000000001E-2 | 3.2893518518518523E-2 | 3.2962962962962965E-2 | 3.3043981481481487E-2 | 3.3113425925925928E-2 | 3.318287037037037E-2 | 3.3263888888888891E-2 | 3.3333333333333333E-2 | 3.3402777777777774E-2 | 3.3483796296296296E-2 | 3.3553240740740745E-2 | 3.363425925925926E-2 | 3.3703703703703701E-2 | 3.3773148148148149E-2 | 3.3854166666666664E-2 | 3.3923611111111113E-2 | 3.4004629629629628E-2 | 3.4074074074074076E-2 | 3.4143518518518517E-2 | 3.4224537037037032E-2 | 3.4293981481481481E-2 | 3.4363425925925929E-2 | 3.4444444444444444E-2 | 3.4513888888888893E-2 | 3.4594907407407408E-2 | 3.4664351851851849E-2 | 3.4733796296296297E-2 | 3.4814814814814812E-2 | 3.4884259259259261E-2 | 3.4953703703703702E-2 | 3.5034722222222224E-2 | 3.5104166666666665E-2 | 3.5173611111111107E-2 | 3.5254629629629629E-2 | 3.532407407407407E-2 | 3.5405092592592592E-2 | 3.5474537037037041E-2 | 3.5543981481481475E-2 | 3.5624999999999997E-2 | 3.5694444444444445E-2 | 3.577546296296296E-2 | 3.5844907407407409E-2 | 3.5914351851851857E-2 | 3.5995370370370372E-2 | 3.6064814814814813E-2 | 3.6134259259259262E-2 | 3.6215277777777777E-2 | 3.6284722222222225E-2 | 3.636574074074074E-2 | 3.6435185185185189E-2 | 3.650462962962963E-2 | 3.6585648148148145E-2 | 3.6655092592592593E-2 | 3.6724537037037035E-2 | 3.6805555555555557E-2 | 3.6874999999999998E-2 | 3.695601851851852E-2 | 3.7025462962962961E-2 | 3.7094907407407403E-2 | 3.7175925925925925E-2 | 3.7245370370370366E-2 | 3.7326388888888888E-2 | 3.7395833333333336E-2 | 3.7465277777777778E-2 | 3.75462962962963E-2 | 3.7615740740740741E-2 | 3.7685185185185183E-2 | 3.7766203703703705E-2 | 3.7835648148148153E-2 | 3.7916666666666668E-2 | 3.7986111111111116E-2 | 3.8055555555555558E-2 | 3.8136574074074073E-2 | 3.8206018518518521E-2 | 3.8287037037037036E-2 | 3.8356481481481484E-2 | 3.8425925925925926E-2 | 3.8506944444444448E-2 | 3.8576388888888889E-2
CH4
O2
 | 0.00069444
Feed gas on
Sample IR-579a As cast
5% CO2, 95% N2

## Slide 28: Time lag
Chart: Time (s)
 | 5.0613 | 12.5562
 | 0 | 0
 | 0 | 0
 | 0.57205 | 1.2608
Chart: Time (s)
 | 8.8377e-11 | 1.2379e-10
 | 0 | 0
 | 4.681e-11 | 9.8101e-11
 | 0 | 0
Sample IR-579a As cast
5% CO2, 95% N2
Q
CO2
Q
N2
Q
CO2
Q
CH4
52% CO2, 48% CH4
Clearly slower kinetics for CH4

## Slide 29: Steady state permeation
Chart: Total feed pressure (bar)
| 1.0343499999999999 | 1.9870000000000005 | 2.9870000000000005 | 3.9870187500000003 | 4.987000000000001 | 5.9869250000000003 | 4.9870450000000002 | 3.9869454545454546 | 2.9869550000000005 | 1.9870000000000005 | 0
CO2 | 3904.1545 | 3911.7604 | 3836.7887 | 3751.1199 | 3647.8731 | 3788.6117 | 3946.9855 | 3842.4505 | 3945.915 | 3980.4408
O2 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
N2 | 178.9608 | 181.4046 | 180.8241 | 178.6417 | 174.1012 | 175.5118 | 179.4791 | 184.2219 | 186.0003 | 187.7362
CH4 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
CO2/N2 | 21.8157 | 21.5637 | 21.2184 | 20.998 | 20.9526 | 21.5861 | 21.9913 | 20.8577 | 21.2146 | 21.2023
Pressure-independent
No hysteresis
5% CO2, 95% N2
Chart: Total feed pressure (bar)
| 1.0155706896551724 | 1.9890157894736842 | 2.9890074999999992 | 3.9889774999999998 | 4.9889625000000004 | 5.9890157894736857 | 4.9889850000000013 | 3.9889842105263158 | 2.9889849999999987 | 1.9890000000000001 | 1.0157842105263157
CO2 | 3494.0158 | 3348.9036 | 3244.6795 | 3166.8167 | 3107.6292 | 3040.6961 | 3142.8105 | 3267.0823 | 3391.4782 | 3487.0393 | 3633.2286
O2 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
N2 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
CH4 | 150.1297 | 153.6659 | 156.2223 | 159.2834 | 163.1295 | 166.0359 | 168.3665 | 170.5374 | 170.7699 | 169.7536 | 169.4658
CO2/CH4 | 23.2733 | 21.7934 | 20.7696 | 19.8817 | 19.0501 | 18.3135 | 18.6665 | 19.1576 | 19.8599 | 20.5418 | 21.4393
52% CO2, 48% CH4
Pressure-dependent
Slight hysteresis

## Slide 30: Correction for instrumental time lag
Assumption:
Every part of the setup has its characteristic reaction times and we must correct for this to ‘isolate’ the real time lag related to the transport in the membrane.

## Slide 31: Alternative: Time lag vs (Thickness)2
TEST
Position 2
Test
MFC
Ar Purge
BPC
MS SV1
MS SV3
MS SV2
MFC
Ar
Retentate
Sweep
MFC
N2
MFC
O2
MFC
CH4
MFC
CO2
5
6
2
1
3
4
Feed
6-Way valve
Bubble FM
Bubble FM
Bubble FM
Permeate
MS SV2
For the membrane:
For the whole system:
Can we describe our system with just one additional delay term?

## Slide 32: Instrumental time lag: Q vs (Thickness)2
Mixed gas setup
Comparison: Pure gas setup
Chart: Pebax2533 30cc/min Ar sweep
| 8281 | 24649 | 36864
CO2_30 | 30.155 | 51.6922 | 68.836
N2_30 | 32.3998 | 54.4315 | 67.6913
O2_30 | 27.4126 | 41.4274 | 50.0981
CO2
N2
O2
Chart: Pebax2533
| 8262.8100000000013 | 24711.839999999997 | 36979.29 | 50940.49
O2 | 7.4619 | 20.517 | 30.9186 | 46.8464
N2 | 11.0912 | 26.3207 | 40.5812 | 60.6392
CH4 | 14.9354 | 42.5473 | 63.8829 | 94.756
CO2 | 11.4586 | 33.0991 | 49.0521 | 74.0672
He | 0.91285 | 2.2104 | 2.7972 | 4.6636
H2 | 1.3702 | 3.754 | 5.4948 | 8.5145
Instrumental time lag, Q0

## Slide 33: Instrumental time lag: Q vs (Thickness)2
Chart: Time (s)
Mixed gas setup
Validation: Pinhole in Aluminium foil
Chart: Pebax2533 30cc/min Ar sweep
| 8281 | 24649 | 36864
CO2_30 | 30.155 | 51.6922 | 68.836
N2_30 | 32.3998 | 54.4315 | 67.6913
O2_30 | 27.4126 | 41.4274 | 50.0981
CO2
N2
O2
Instrumental time lag, Q0
Q0

## Slide 34
Gas Permeability of PIM-1/UiO-NH2 MMMs
Chart: Total feed pressure (bar)
| 1.0256500000000002 | 1.9979937499999998 | 2.9980081818181787 | 3.9979999999999993 | 4.9979999999999976 | 5.9979722222222236
CO2 | 9441.5287 | 10042.2591 | 10162.8989 | 10069.9669 | 9960.0249 | 9880.786
O2 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
N2 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
CH4 | 440.4285 | 484.602 | 522.082 | 539.6087 | 556.6399 | 577.1708
CO2 single gas | 8738.8933
CH4 single gas | 594.8695
CO2 decreasing pressure | 10119.7072 | 10434.3549 | 10733.9029 | 10908.5877 | 10758.5383
CH4decreasing pressure | 586.4714 | 587.2457 | 584.6566 | 574.92 | 521.0489
UiO-NH2 MOFs
Gas mixture : 52% CO2, 48% CH4
Mixed Matrix Membrane with Metal Organic Frameworks
Detailed quantitative diffusion analysis of pure gases and mixtures is in progress

## Slide 35: Introduction Experimental Results and discussion Conclusions

## Slide 36: Conclusions
Mass spectrometry allows quick in-line permeate gas analysis during membrane gas permeation experiments.
Short analysis times enable visualization of transient phenomena of the individual components in gas mixtures.
Accurate correction of the instrumental time lag is possible and is needed for determination of the effective diffusion coefficient.
The method is suitable to study time-dependent and anomalous phenomena such as coupling effect, dilation, aging etc..
Outlook
Further minimization of the dead volume to optimize the response times
Effect of pressure, gas composition; aging studies
Check of Helium sweeping gas to reduce interference

## Slide 37: Acknowledgements: Financial support
FP7 Project: M4CO2 - Energy efficient MOF-based Mixed Matrix Membranes for CO2 Capture.
Contract ENERGY-2013-1608490
CNR (Italy) / FCT (Portugal) bilateral collaboration program 2015-2016.
CNR (Italy) / CAS (Czech Republic) bilateral collaboration program 2016-2018.

## Slide 38: Acknowledgements
Universidad Nova de Lisboa, Lisbon, Por
  Joao Crespo
  Carla Brazinha
  Sofia Fraga
The University of Manchester
  Peter Budd
  Christopher R. Mason
  Alexandra F. Bushell
  Louise Maynard-Atem
  Bekir Satilmis
  Kane W.J. Heard
  …….
University of Edinburgh, UK
  Neil B. McKeown
  Mariolino Carta
  C. Grazia Bezzu
  Ian Rose
Others . . . . .
Institute on Membrane Technology, Rende, IT
  Paola Bernardo
  Elisa Esposito
  Alessio Fuoco
  Marcello Monteleone
  Elena Tocci
University of Chemistry and Technology Prague (former ICT), Prague, CZ
  Karel Friess
  Kryštof Pilnácek
  Marek Lanč
Institute of Chemical Process Fundamentals, Prague 6 - Suchdol, CZ
  Pavel Izák
  Zuzana Sedláková

## Slide 39: Acknowledgements : EC Erasmus+
Marek Lanč
UCT Prague
2016
Krystof Pilnáček
UCT Prague
2012
Thank you for your attention !
? ? ? Questions ? ? ?