## Slide 1: Extreme confinement and propagation regimes of tHz surface waves on planar metallic waveguides
J. Mangeney1, D. Gacemi3, R. Colombelli2 and A. Degiron2
1Laboratoire Pierre Aigrain, UMR 8551, Ecole Normale Supérieure, France
2Institut d’Electronique Fondamentale, UMR 86622, CNRS, Univ-Paris Sud, France
3 Laboratoire Matériaux et Phénomènes Quantiques, UMR 7162, CNRS, Université Paris, France

## Slide 2: Confinement of THz waves
Diffraction limit of THz waves ~150 µm
Integrated THz technology (high-speed electronic circuits,…)
Imaging and spectroscopy of small objects
Biological sensing
…
Plasmonic Concepts -> Sub-l confinement at optical frequencies
Plasmonic for confining THz waves (<l)
Can sub-l confinement be achieved at THz frequencies ?
Requirement of highly confined THz waves
Surface waves propagating at the interface between a dielectric and a conductor.
Microfluidic channel

## Slide 3: Dispersion relation
Optics
THz
Surface wave’s properties highly change from optics to THz
Surface waves at the interface of metal and dielectric :

## Slide 4: Dispersion relation
k
Re(w/c)
w=ck
Surface Plasmon Polariton
Zenneck waves
375 THz (l=450 nm)
1 THz (l=300 µm)
ddiel=0.18 µm < l
dair=63 mm >> l
Challenge : achieve sub-l confinement of the THz surface waves
Optical range
THz range

## Slide 5: Planar metallic waveguide
Yansheng Xu et al., MOTL. 43, 290, (2004).
Christopher Russell, et al., Lab Chip, to be published 2013
Treizebre, A, Int. J. Nanotechnol. 5, 784-795 (2008).
`
1/ Coupling between EM fields and the free electrons at the metal surface
2/ Interaction of the EM fields with the metal surface modified by the thin dielectric layer.
Physical mechanisms that bind the surface wave to the surface :
Akalin at al, IEEE VOL 54, N°6,2762 (2006).
Extremey simple geometry adapted for complex integrated
schemes with high functionalities
Single conductor deposited on thin dielectric layer

## Slide 6: Outline
    Study of planar metallic waveguides to achieve electric field confinement
  Planar metallic waveguides based on the coupling between EM fields and free electrons at the metal surface (Simulation)
  Planar metallic waveguides based on the interaction of the EM fields with a metal surface modified by the thin dielectric layer (Simulation)
  Planar metallic waveguides based on hybrid mode (Experiments)
    Study of the propagation regimes of planar metallic waveguides

## Slide 7: Single Au stripe
Au: metal with finite conductivity
Comsol MultiPhysics :
- Cross Section of the power
- Effective index of propagating modes
1 THz
1/ Coupling between EM fields and the free electrons at the metal surface
Single Au stripe embedded in a homogeneous medium
Existence of only one mode at 1 THz : radial field distribution

## Slide 8: tranverse size of metal stripe
h=120 µm, w=50 µm
h=50 µm, w=50 µm
h=25 µm, w=25 µm
h=10 µm, w=10 µm
h=5 µm, w=5 µm
h
w

## Slide 9: Influence of the stripe size
The mode evolves into a highly confined solution as the transverse dimensions of the metal waveguide tend to zero
Re(neff)  Field confinement 
Im(neff)  Field confinement 
Frequency : 1 THz

## Slide 10: A perfectly conducting stripe supported by a dielectric layer
Perfect electric
conductor
1 THz
2/ Interaction of the EM fields with the metal surface modified by the thin dielectric layer
Existence of only one mode at 1 THz : : radial field distribution

## Slide 11: Influence of the stripe size
Shrinking the transverse size of perfect conducting stripe increases the electric field confinement at THz frequencies
neff  -> Field confinement 
Frequency : 1 THz

## Slide 12: Transverse Size role
Frequency : 1 THz
w=30µm, h=10µm
2.2µm ~  /93
38µm ~  /5
A
B
w=2µm, h=20nm
2.2µm ~  /136
407µm>l
B
A
Frequency : 1 THz
D. Gacemi et al., Scientific Reports 3, 1369 (2013)
A :
B :
Extreme confinement (sub-l ) of the electric field at THz frequencies whatever the binding mechanisms

## Slide 13: Experimental study
Guided –wave time domain THz spectroscopy
3/ Hybrid Mode : a combination of both mechanisms
dielectric layer
metal stripe
1/ Coupling between EM fields and the free electrons at the metal surface
2/ Interaction of the EM fields with the metal surface modified by dielectric layer.

## Slide 14: Surface mode properties
L1/e=64.5 µm
Horizontal component of E
Vertical component of E
D. Gacemi et al. Optics Express 20, 8466 (2012)
Experimental determination of the mode confinement ~ l/10
w=10 µm , t=200 nm, quartz substrate 250 µm

## Slide 15: Propagation characteristics
Decay Length
at 0.5 THz, dL= 54 µm
Experimental determination of the mode confinement ~ l/10

## Slide 16: Influence of the stripe width
200 µm
30 µm
D. Gacemi et al. , Scientific Reports 3, 1369 (2013)
Reducing transverse size of a metallic structure provides a powerful tool for confinement of THz surface waves

## Slide 17: State of the art
A.J. Huber, Nano Lett. 8, 3766-3770 (2008)
J.A. Deibel, Proc. of IEEE 95 1624-1640 (2007)
l/3000
metal tip apexes
Seo M. A. et al., Nature Photon. 3, 152-156 (2009).
Sholaby M. et al, Appl. Phys. Lett. 99, 041110-041112 (2011).
l/25
metallic nanoslits
Astley, V., App. Phys. Lett. 95, 031104-031106 (2009).
Liu, J. Appl. Phys. Lett. 100, 031101-031103 (2012).
Zhan, Opt. Express 18 ,9643-9650 (2010).
Zhan, H., JOSA B, 28, 558-566 (2011).
l/250
parallel-plate waveguides
J. B. Pendry et al., Science 305, 847 (2004)
C. R. Williams et al., Nature Photonics 2 (2008)
~l
corrugated metal
All design strategies involved reduced dimensions of metal structures

## Slide 18: Dielectric layer properties
Low losses (< 0.4 mm-1) up to 0.8 THz
Performances of these single conductor waveguides are fully compatible with key THz applications
Dispersion coefficient of 0.28 ps/mm
200 µm
58 µm

## Slide 19: Distinct propagation regimes
e=0, the mode is bound to the metal stripe because of its finite conductivity
a variant of a Sommerfeld wave
e ->leff/4, the dielectric film provides additional confinement to the mode.
a Goubau mode
e>l eff /4, the mode looses its confinement to the point that it ceases to be bound beyond a certain cut-off condition.
  cut-off frequency
D. Gacemi et al. APL 191117 (2013)

## Slide 20: Conclusions
Size effects can be used as a simple formidable tool for high electric field confinement at THz frequencies (smaller than λ/100).
Au planar single conductor supported by thin layers of dielectric show remarkable performances
Further works :
  to generalize this result into a unified theory (universality).
  Develop Bends, Mach-Zender, Y-splitting

## Slide 21: `collaborations
Institut d’Electronique Fondamentale
P. Crozat
Institut d'Electronique de Microelectronique et de Nanotechnologie
T. Akalin, J-F. Lampin, C. Blary
Laboratoire Ondes et Matière d’Aquitaine
R. Yahiaoui
Funding support from:
EMRP Researcher Grant NEW07
Research Project ‘THz Security’

## Slide 22: Dispersion relation
Maximum GVD of 5.6x10-22 s2/m
Low Losses