## Slide 1: Thermochemical Recycling of Municipal Solid Waste
Juma Haydary
Department of Chemical and Biochemical Engineering
Institute of Chemical and Environmental Engineering
Faculty of Chemical and Food Technology
Slovak University of Technology in Bratislava, Slovakia

## Slide 2
Slovak University of Technology in Bratislava
Faculty of Chemical and Food Technology

## Slide 3: Institute of Chemical and Environmental Engineering
Reactor Engineering Reaserch Group
Experimental study and mathematical modeling of fuel thermal processes
Pyrolysis, gasification and combustion of solid fuels
Biomass, polymer waste, MSW, and coal thermal and catalytic processing for production energy and materials
National center for research and application of renewable energy sources

## Slide 4
Energy
Energy
Energy
Mechanical recycling loop
Thermochemical recycling loop

## Slide 5: Refuse-Derived Fuel (RDF)
MSW
RDF
Biodegradables
Metals
Inorganics
Hazardous wastes

## Slide 6: RDF composition
Component | Material | wi [kg/kg]
Paper | White paper, recycled paper | 0,6317
Foil | LDPE, HDPE | 0,1578
Plastics | Rigid plastics, polystyrene, polyurethane | 0,1910
Textile | Polyamide, polyester, cotton , wool | 0,0194

## Slide 7: Proximate and Elemental Composition of RDF
Com. | Mois. | VM* | FC* | ASH* | C | H | N | S | O**
Wt. % | 10 | 75.5 | 8.9 | 15.6 | 51.7 | 5.9 | 0.9 | 0.4 | 25.5
*moisture free basis
**calculated to 100%

## Slide 8: Behaviour of Thermal decomposition

## Slide 9
Behaviour of Thermal decomposition

## Slide 10: Heating value of RDF
Component | Heating value [kJ/kg]
Paper | 13410
Foil | 43860
Plastics | 33570
Textile | 19770
Mixed RDF | 20810

## Slide 11
Tar content measurement
Chart: Temperature (°C )
| 700 | 800 | 900 | 1000 | 1100
 | 81.5 | 71 | 61 | 36.5 | 30.5

## Slide 12: Gasification Model
Assumptions:
Steady state flow is considered inside the gasifier
No temperature and concentration gradient exist inside the reactor
The residence time is enough long to reach complete decomposition of RDF and unreacted part of RDF is only carbon.
Only the major species are considered in the product gases, i.e CO, CO2, H2, CH4 , H2O, NH3, H2S, N2 and Tar
Global material balance of RDF gasification
RDF
TAR
Reactions:
Equilibrium constant:
,

## Slide 13
Enthalpy balance:

## Slide 14: Results of modelling RDF gasification
Observed parameters:
Conversion of RDF
Reactor Temperature
Gas composition
Content of pollutants (NH3, H2S, TAR)
Variables:
Oxygen (air) to RDF mass ratio
Steam to RDF mass ratio

## Slide 15
Chart: m(air)/m(RDF)
| 0.5 | 0.625 | 0.75 | 0.875 | 1 | 1.125 | 1.25 | 1.375 | 1.5 | 1.625 | 1.75 | 1.875 | 2 | 2.125 | 2.25 | 2.375 | 2.5 | 2.625 | 2.75 | 2.875
Temperature | 658.0895 | 720.0279 | 764.1249 | 797.5419 | 823.9013 | 845.3545 | 863.2867 | 878.6256 | 892.0101 | 903.8912 | 914.5946 | 924.3615 | 933.3741 | 953.8536 | 1015.8853 | 1090.7196 | 1163.0856 | 1231.3832 | 1295.8308 | 1356.7483
Conversion | 33.4562 | 35.4848 | 38.1813 | 41.8586 | 46.3931 | 51.5768 | 57.2288 | 63.215 | 69.4408 | 75.8402 | 82.3668 | 88.987 | 95.6768 | 100 | 100 | 100 | 100 | 100 | 100 | 100
Chart: m(air)/m(RDF)
| 0.5 | 0.625 | 0.75 | 0.875 | 1 | 1.125 | 1.25 | 1.375 | 1.5 | 1.625 | 1.75 | 1.875 | 2 | 2.125 | 2.25 | 2.375 | 2.5 | 2.625 | 2.75 | 2.875
H2 | 0.11268 | 0.17149 | 0.2067 | 0.2244 | 0.23117 | 0.23161 | 0.2285 | 0.22349 | 0.21754 | 0.21118 | 0.20474 | 0.1984 | 0.19226 | 0.1879 | 0.17795 | 0.16218 | 0.14668 | 0.13222 | 0.11881 | 0.10639
CO | 0.0031696 | 0.011693 | 0.025508 | 0.042829 | 0.061794 | 0.081045 | 0.099769 | 0.11755 | 0.13421 | 0.14973 | 0.16412 | 0.17746 | 0.18983 | 0.19725 | 0.19525 | 0.19148 | 0.1869 | 0.18167 | 0.17582 | 0.16943
CH4 | 0.18838 | 0.12534 | 0.084569 | 0.058849 | 0.042385 | 0.031524 | 0.024113 | 0.018887 | 0.015092 | 0.012265 | 0.010111 | 0.0084377 | 0.0071158 | 0.0038081 | 0.00045538 | 4.3402e-05 | 5.5621e-06 | 9.3656e-07 | 1.9456e-07 | 4.7509e-08
CO2 | 0.19004 | 0.18751 | 0.18109 | 0.17249 | 0.16273 | 0.15258 | 0.14252 | 0.13281 | 0.12362 | 0.11498 | 0.10692 | 0.099418 | 0.092441 | 0.087003 | 0.084971 | 0.084408 | 0.08465 | 0.085559 | 0.087065 | 0.089104
N2 | 0.47299 | 0.47206 | 0.47089 | 0.47078 | 0.47178 | 0.47362 | 0.476 | 0.47869 | 0.48154 | 0.48446 | 0.4874 | 0.49033 | 0.49322 | 0.49895 | 0.51467 | 0.53399 | 0.55312 | 0.57144 | 0.58887 | 0.6054
Air Gasification

## Slide 16
Chart: m(air)/m(RDF)
| 0.5 | 0.625 | 0.75 | 0.875 | 1 | 1.125 | 1.25 | 1.375 | 1.5 | 1.625 | 1.75 | 1.875 | 2 | 2.125 | 2.25 | 2.375 | 2.5 | 2.625 | 2.75 | 2.875
Tar | 0.0899 | 0.080108 | 0.072097 | 0.065368 | 0.059661 | 0.054791 | 0.050605 | 0.046984 | 0.043827 | 0.041055 | 0.038605 | 0.036427 | 0.034477 | 0.032831 | 0.031511 | 0.030293 | 0.029166 | 0.02812 | 0.027146 | 0.026238
H2S | 0.0032426 | 0.0026146 | 0.0021878 | 0.0018834 | 0.0016571 | 0.0014825 | 0.0013436 | 0.0012302 | 0.0011359 | 0.0010559 | 0.0009873 | 0.00092767 | 0.00087535 | 0.00083372 | 0.00081203 | 0.00079789 | 0.00078487 | 0.00077196 | 0.00075898 | 0.00074563
NH3 | 0.00028912 | 0.00026338 | 0.00022452 | 0.00018829 | 0.00015826 | 0.0001342 | 0.000115 | 9.9572e-05 | 8.7027e-05 | 7.6704e-05 | 6.8107e-05 | 6.0871e-05 | 5.4717e-05 | 4.5765e-05 | 2.7802e-05 | 1.554e-05 | 9.1856e-06 | 5.7422e-06 | 3.7484e-06 | 2.5289e-06

## Slide 17
Chart: m(O2)/m(RDF)
| 6.25E-2 | 9.375E-2 | 0.125 | 0.15625 | 0.1875 | 0.21875 | 0.25 | 0.28125 | 0.3125 | 0.34375 | 0.375 | 0.40625 | 0.4375 | 0.46875 | 0.5 | 0.53125 | 0.5625 | 0.59375 | 0.625
Temperature | 443.6795 | 625.0198 | 724.9828 | 788.5584 | 833.597 | 867.7522 | 895.0666 | 917.8821 | 937.6391 | 955.2731 | 971.4281 | 986.5743 | 1026.4635 | 1180.1952 | 1357.9424 | 1530.6401 | 1697.5209 | 1858.1558 | 2011.7983
Conversion | 24.3502 | 32.3909 | 34.8657 | 37.8592 | 42.4207 | 48.2832 | 55.0444 | 62.406 | 70.174 | 78.2232 | 86.4711 | 94.8613 | 100 | 100 | 100 | 100 | 100 | 100 | 100
Gasification of RDF Using O2
Chart: m(O2)/m(RDF)
| 6.25E-2 | 9.375E-2 | 0.125 | 0.15625 | 0.1875 | 0.21875 | 0.25 | 0.28125 | 0.3125 | 0.34375 | 0.375 | 0.40625 | 0.4375 | 0.46875 | 0.5 | 0.53125 | 0.5625 | 0.59375 | 0.625
H2 | 0.0081544 | 0.13861 | 0.30397 | 0.39839 | 0.43931 | 0.45185 | 0.4505 | 0.44254 | 0.43155 | 0.41936 | 0.4069 | 0.39467 | 0.39188 | 0.37622 | 0.35151 | 0.32764 | 0.30448 | 0.28201 | 0.26052
CO | 2.5886e-06 | 0.0022238 | 0.019894 | 0.057044 | 0.10577 | 0.15828 | 0.21012 | 0.25926 | 0.30499 | 0.34723 | 0.38613 | 0.42198 | 0.44905 | 0.47323 | 0.49669 | 0.51574 | 0.53081 | 0.54231 | 0.55043
CH4 | 0.64581 | 0.45395 | 0.27978 | 0.1725 | 0.11181 | 0.076518 | 0.054819 | 0.040709 | 0.031082 | 0.024246 | 0.019229 | 0.015446 | 0.0056404 | 0.00010684 | 3.009e-06 | 1.9392e-07 | 2.1754e-08 | 3.5925e-09 | 7.8946e-10
CO2 | 0.27758 | 0.35012 | 0.3479 | 0.3278 | 0.30166 | 0.27396 | 0.2468 | 0.22112 | 0.19723 | 0.17518 | 0.1549 | 0.13626 | 0.12196 | 0.11696 | 0.11703 | 0.12106 | 0.12855 | 0.13905 | 0.15208
N2 | 0.028814 | 0.0189 | 0.014126 | 0.011223 | 0.0093567 | 0.0080794 | 0.007152 | 0.0064459 | 0.0058879 | 0.0054341 | 0.0050568 | 0.0047375 | 0.0045348 | 0.0046621 | 0.0048665 | 0.0050689 | 0.0052684 | 0.0054649 | 0.0056557

## Slide 18
Effect of RDF composition
Com. | Wt. %
Mois | 10
VM | 75.5
FC | 8.9
ASH | 15.6
C | 51.7
H | 5.9
N | 0.9
S | 0.4
O | 25.5
Chart: m(O2)/m(RDF)
| 6.25E-2 | 9.375E-2 | 0.125 | 0.15625 | 0.1875 | 0.21875 | 0.25 | 0.28125 | 0.3125 | 0.34375 | 0.375 | 0.40625 | 0.4375 | 0.46875 | 0.5 | 0.53125 | 0.5625 | 0.59375 | 0.625
Temperature | 443.6795 | 625.0198 | 724.9828 | 788.5584 | 833.597 | 867.7522 | 895.0666 | 917.8821 | 937.6391 | 955.2731 | 971.4281 | 986.5743 | 1026.4635 | 1180.1952 | 1357.9424 | 1530.6401 | 1697.5209 | 1858.1558 | 2011.7983
Conversion | 24.3502 | 32.3909 | 34.8657 | 37.8592 | 42.4207 | 48.2832 | 55.0444 | 62.406 | 70.174 | 78.2232 | 86.4711 | 94.8613 | 100 | 100 | 100 | 100 | 100 | 100 | 100
Com. | Wt. %
Mois | 1.2
VM | 80.22
FC | 5.23
ASH | 13.34
C | 51.66
H | 8.82
N | 0.66
S | 0.08
O | 25.42

## Slide 19: Effect of Steam in RDF Gasification
Chart: m(Steam)/m(RDF)
| 3.125E-2 | 6.25E-2 | 9.375E-2 | 0.125 | 0.15625 | 0.1875 | 0.21875 | 0.25 | 0.28125 | 0.3125 | 0.34375 | 0.375 | 0.40625 | 0.4375
H2 | 0.38348 | 0.39036 | 0.39688 | 0.40307 | 0.40894 | 0.41454 | 0.41986 | 0.42494 | 0.4298 | 0.43444 | 0.43887 | 0.44313 | 0.4472 | 0.45111
CO | 0.45497 | 0.43779 | 0.42161 | 0.40632 | 0.39185 | 0.37813 | 0.36509 | 0.35268 | 0.34085 | 0.32956 | 0.31877 | 0.30846 | 0.29859 | 0.28914
CO2 | 0.12752 | 0.13749 | 0.1469 | 0.15581 | 0.16425 | 0.17226 | 0.17987 | 0.18712 | 0.19404 | 0.20063 | 0.20693 | 0.21296 | 0.21873 | 0.22425
Chart: m(Steam)/m(RDF)
| 3.125E-2 | 6.25E-2 | 9.375E-2 | 0.125 | 0.15625 | 0.1875 | 0.21875 | 0.25 | 0.28125 | 0.3125 | 0.34375 | 0.375 | 0.40625 | 0.4375
Temperature | 1173.5687 | 1167.0322 | 1160.608 | 1154.3019 | 1148.1162 | 1142.052 | 1136.1086 | 1130.2841 | 1124.5781 | 1118.9865 | 1113.5072 | 1108.1371 | 1102.8731 | 1097.7121
Heating value | 9.8858 | 9.7431 | 9.6092 | 9.4831 | 9.3639 | 9.251 | 9.144 | 9.0422 | 8.9453 | 8.853 | 8.7649 | 8.6808 | 8.6003 | 8.5232

## Slide 20: Conclusion
For RDF studied in this work,100% of RDF conversion in gasification by air was reached at mair/mRDF=2,2. However, the gas heating value was 4,4 MJ/Nm3
Gasification of RDF using Oxygen enables production of a gas with heating value around 10 MJ/Nm3 at mO2/mRDF=0,45
Elemental Composition of RDF has a crutial effect on riquired mair/mRDF
Raw untreated gas tar content was 3.3 mass %; tar fraction content a solid phase insoluble in isopropanol
By increasing the msteam/mRDF the content of H2 and CO2 increased, However, the content of CO, reactor temperature and gas heating vale decreased

## Slide 21
Thank you for attention