## Slide 1: About OMICS Group
OMICS Group International is an amalgamation of Open Access publications and worldwide international science conferences and events. Established in the year 2007 with the sole aim of making the information on Sciences and technology ‘Open Access’, OMICS Group publishes 400 online open access scholarly journals in all aspects of Science, Engineering, Management and Technology journals. OMICS Group has been instrumental in taking the knowledge on Science & technology to the doorsteps of ordinary men and women. Research Scholars, Students, Libraries, Educational Institutions, Research centers and the industry are main stakeholders that benefitted greatly from this knowledge dissemination. OMICS Group also organizes 300 International conferences annually across the globe, where knowledge transfer takes place through debates, round table discussions, poster presentations, workshops, symposia and exhibitions.

## Slide 2: About OMICS Group Conferences
OMICS Group International is a pioneer and leading science event organizer, which publishes around 400 open access journals and conducts over 300 Medical, Clinical, Engineering, Life Sciences, Phrama scientific conferences all over the globe annually with the support of more than 1000 scientific associations and 30,000 editorial board members and 3.5 million followers to its credit.
OMICS Group has organized 500 conferences, workshops and national symposiums across the major cities including San Francisco, Las Vegas, San Antonio, Omaha, Orlando, Raleigh, Santa Clara, Chicago, Philadelphia, Baltimore, United Kingdom, Valencia, Dubai, Beijing, Hyderabad, Bengaluru and Mumbai.

## Slide 3: Dy-FREE HIGH STRENGTH, HIGH COERCIVITY Nd2Fe14 PERMANENT MAGNETS
K.A. Gschneidner, Jr.
The Ames Laboratory and Department of Materials Science and Engineering
Iowa State University, Ames, Iowa, 50011 USA
3rd International Conference and Exhibition on Materials and Engineering
San Antonio, Texas, USA
October 6, 2014
IOWA STATE UNIVERSITY
OF SCIENCE AND TECHNOLOGY
Research supported by the U.S. Department of Energy, Advanced Research Projects Agency-Energy ,
Rare Earth Alternatives in Critical Technologies for Energy (REACT)

## Slide 4: BASIC DEFINITIONS – I
B vs. H Curves

## Slide 5
B = 4pM + H
BHmax = -8.8 MGOe
BHmax = -5.1 MGOe
BHmax = -28.7 MGOe
Magnetic Field, H (kOe)
-14
-12
-10
-8
-6
-4
-2
0
M, B (kG)
0
2
4
6
8
10
12
14
Spindle Magnet (M)
Spindle Magnet (B)
CEA-1-55 (M)
CEA-1-55 (B)
Speaker Magnet (M)
Speaker Magnet (B)
Br, Hc, Hci, BHmax
BASIC DEFINITIONS – II
Br Remanence (kG)
Hc Coercivity (kOe) (line with data point)s
Hci Intrinsic Coercivity (kOe) (solid line)
BHmax Maximum Energy Product (MGOe) (largest area under curve)
Hc
Hci
Area under curve
Br

## Slide 6: NEODYMIUM-IRON-BORON PERMANENT MAGNETS Nd2Fe14B
Strongest permanent magnet
Fe – magnetic properties due to iron
Nd – locks the iron magnetic moments, keeps them from rotating
(coercivity)
Applications
electric motors (cars, wind turbines, elevators)
spindle magnet of computers
speakers (ear buds)
magnetic refrigerators
Role of Dy
added to Nd2Fe14B to further increase the coercivity (1 to 10%)
increases the high temperature useful limit

## Slide 7: DYSPROSIUM
USEFULLNESS
Magnet weighs less for the same strength compared to magnets
without Dy (automobiles – CART requirements)
Improves high temperature performance
DRAWBACKS
Supply of Dy in the world is limited
One of Dept. of Energy’s critical elements (most critical)
Expensive
DOE’s ARPA-E REACT PROGRAM
Rare Earth Alternatives in Critical Technology for energy
Get rid of Dy, or reduce the amount needed
Reduce Nd content, or replace it with new non-rare earth magnets

## Slide 8: WHY CERIUM
Most abundant rare earth
Ce needs to be removed to get at the other rare earth
elements in the separation process
50% excess Ce supply over demand
General Motors found that in La2Fe14B-Nd2Fe14B
pseudo binary system two phases formed after high
temperature anneal – will Ce do the same?
Ce is a mixed valent metal with a history of doing
unusual and strange things
The Ce valence is 3.4 in Ce2Fe14B

## Slide 9: FIRST SURPRISE IN (Nd1-xCex)2Fe14B SYSTEM
An anomaly in the c lattice parameter vs. Ce
concentration plot at ~20% Ce substitution
for Nd!
An increase in coercive field at ~20% Ce
concentration (Slide 8)!

## Slide 10: BHMAX, Br, Hc, HA AND MS OF (Nd1-xCex)2Fe14B RIBBONS
0.2
0.2

## Slide 11: SECOND SURPRISE IN (Nd1-xCex)2Fe14B SYSTEM
The drop-cast ingots of (Nd1-xCex)2Fe14B are two
phase alloys, with micron size Ce-rich grains in
Nd-rich matrix (Slide 10)!
The two-phase region extends from x ~0.15 to x ~0.4 (Slide 10).

## Slide 12: SEM IMAGES OF (Nd1-xCex)2Fe14B DROP CAST ALLOYS

## Slide 13: THIRD SURPRISE – THE EFFECT OF COBALT ADDITIONS
Cobalt was added to increase the
ordering temperature – which it does
But it squares up the BH loop (Slide 12)!
Wow!

## Slide 14: MAGNETIZATION VS. FIELD FOR (Nd0.8Ce0.2)2Fe14-yCoyB ALLOYS

## Slide 15: ADDITION OF TiC OR ZrC GRAIN REFINERS
Increased BHmax as expected (Slide 14)
ZrC is better than TiC

## Slide 16: MAGNETIZATION VERSUS FIELD OF (Nd0.8Ce0.2)~2Fe14B WITH AND WITHOUT ADDED TiC MELT SPUN RIBBONS
Shape of blue curve is just
what the magnet design
engineers want in the
second quadrant

## Slide 17: FOURTH SURPRISE – TEMPERATURE DEPENDENCE OF Hc
The temperature dependence of the coercivity
drops much slower than that of a sintered
Nd-Dy-Fe-B alloy (Slide 16)! Wow!
At ~500 K (~225°C) Hc is larger than that of a
sintered Nd-Dy-Fe-B alloy (Slide 16)!
Wow! Wow!
The temperature under the hood of an automobile
may reach 475 K (200°C) during a hot summer day.

## Slide 18: COERCIVITY AS A FUNCTION OF TEMPERATURE FOR (Nd0.8Ce0.2)2+zFe12Co2B RIBBONS WITH EXCESS RARE EARTH AND/OR TiC, ZrC AS A FUNCTION OF TEMPERATURE.
Note cross-over

## Slide 19: SYNERGISM BETWEEN MIXVALENT Ce AND Co
Cobalt addition:
Increases Tc as expected
Increases both Hc and BHmax Wow!
Smaller temperature dependence of Hc and BHmax;
These are better than sintered Nd-Dy-Fe-B magnet
above ~475 K (~200°C); i.e. magnetic properties
of co-doped Ce,Co better than sintered Dy
containing magnets
Ce and Co occupy adjoining crystallographic sites in
Nd2Fe14B structure (Slide 18)

## Slide 20
Nd2Fe14B STRUCTURE
Ce occupies Nd(4f) sites; and Co occupies Fe(4c) sites
Ref.: L. Ke, D. Kukusta, V. Antropov, Ames Laboratory Seminar, March 2014.

## Slide 21: PROCESSING COMMERCIAL (Nd0.8Ce0.2)2.4Fe12Co2B
Ce and Nd – commercial grade metals (~98 at.% pure)
Ferrous boron – commercial grade (~2 at.% non-
ferrous impurities)
MQ1(1) melt spun ribbons – isotropic grains
MQ2(2) hot pressed magnet (ingot) – isotropic
grains
MQ3(3) die upset magnet ingot – anisotropic

## Slide 22: B-H CURVES (Nd0.8Ce0.2)2.4Fe12Co2B
#1 – ribbons
#2 – hot pressed
#3 – die upset

## Slide 23
(Nd0.8Ce0.2)2.4Fe12Co2B: DIE UPSET
Bright-field TEM images

## Slide 24
(Nd0.8Ce0.2)2.4Fe12Co2B

## Slide 25: CONCLUSIONS
The co-doped Ce,Co Nd2Fe14B Permanent Magnets are:
Competitive with some Dy-doped sintered magnets, especially at T > 475 K (>200°C)
Larger Hc(Hci) and BHmax values using commercial
grade rare earths, and lower purity ferrous boron
Will help reduce the strain on Dy markets
Will relieve the demand for Nd
Will help utilize some of the Ce surplus
Mixed valent Ce still has some amazing tricks up her sleeve!

## Slide 26: ACKNOWLEDGEMENTS
The Ames Laboratory and Department of Materials Science and Engineering and Iowa State University, Ames, Iowa, 50011 USA
R.W. McCallum
M. Khan (Current address: Department of Physics, Miami University, Oxford, Ohio, USA)
A.K. Pathak
V.K. Pecharsky
L. Zhou
K. Sun
K.W. Dennis
M.J. Kramer
Molycorp Magnequench, Singapore
D. Brown
MEDA Engineering and Technical Services, Southfield, MI
C. Zhou
General Motors R&D Center, Warren, MI
F.E. Pinkerton
REFERENCE: “Dy-free, Reduced Nd, High Performance Nd2Fe14B-based Permanent Magnets,” Proceedings 23rd International Workshop on Rare Earth and Future Permanent Magnets and Their Applications (REPM 2014), G.C. Hadjipanayis, C.H. Chen, J.P. Liu, editors, pp. 403-406, Annapolis, Maryland, USA (August 17-21, 2014)

## Slide 27: Let Us Meet Again
We welcome you all to our future conferences of OMICS Group International
Please Visit: http://materialsscience.conferenceseries.com/
Contact us at
materialsscience.conference@omicsgroup.us
materialsscience@omicsgroup.com