## Slide 1
Mitglied der Helmholtz-Gemeinschaft

## Slide 2
The majority of the electric energy is generated by the use of fossil fuels resulting in the emission of large amounts CO2
The steady increase in the concentration of CO2 in the atmosphere contributes to global warming
Until the year 2035 the demand for electricity will increase by about 70 %
Motivation
CO2 Capture in the power plant is requiered
Use of membranes for energy-efficient gas separation
1) IEA World Energy Outlook 2012, OECD Publishing
2) IEA, CO2 Emissions From Fuel Combustion – Highlights 2013, pp. 158

## Slide 3
Introduction
  Separation mechanism
  Membrane design
  CO2-separation from flue gas
Results
  Laboratory tests
  Exposure tests
  Module test rig
Conclusions
Outlook
Acknowledgements
Outline

## Slide 4
of porous membranes
Separation mechanism

## Slide 5
Definition in: International Union of Pure and Applied Chemistry (IUPAC):
Macro porous: Pore Size > 50 nm
Meso porous: Pore Size 2 - 50 nm
Micro porous: Pore size < 2 nm
Effective gas separation with micro porous membranes needs microstructures with „free volume“ in the range of size of the gas molecules which have to be separated
He: 2.6 Å
H2: 2.89 Å
CO2: 3.3 Å
N2: 3.64 Å
also sorption properties are relevant for separation
e.g. amorphous SiO2-Structures
Separation mechanism

## Slide 6
Membrane design
mechanical stability
Gas separation
Reduction of pore size and surface roughness
Graded multilayer system
39 mm
Support: α-Al2O3
Vacuum-slip-cast
Layer thickness : ca. 2 mm
Pore size: 80-100 nm
Inter layer: γ-Al2O3 / 8YSZ Sol-Gel-dip coating
Layer thickness : 4-5 µm
Pore size : 4-7 nm
Functional layer: SiO2
Sol-Gel-dip coating
Layer thickness: < 100 nm
Pore size: ≈ 2 nm
200 nm
200 nm
400 nm
Cross-section
Top view
1 µm
α-Al2O3-support
γ-Al2O3-interlayer
SiO2-functional layer

## Slide 7
39 mm
Membrane design
Selective CO2-transport:
Enhanced CO2-affinity by post synthesis functionalization with amino-groups (-NH2)
Pore channel
Selective adsorption of CO2
CO2 -transport along a partial pressure gradient
R-NH2
CO2: 0,33 nm
N2: 0,36 nm
Reversible adsorption of CO2 forming carbamates and carbonates
Silica
reversible reaction
Diffusion von N2

## Slide 8
CO2-Separation from flue gas
Air
Furnace
Coal
Steam generation
Flue gas
Turbine and generator
N2, CO2, O2, H2O
SO2, NOX
dust
Flue gas cleaning
N2, CO2, O2, H2O
T < 100°C
P ≈ 1 bar
Flue gas
CO2
N2, (O2, H2O)
CO2-Separation
Flue gas
high CO2/N2-selectivity and high CO2-permeabitity
Stability in application environment
Membrane requirement
Main goals of the work
Development of a CO2/N2-selective silica-membrane
Systematic investigation of the aging behavior under application-oriented conditions
Membrane
Post-Combustion Capture

## Slide 9
Chart: Temperature [°C]
| 30 | 70 | 90 | 110 | 130 | 190
K1_848 | 7.758e-09 | 1.081e-08 | 8.3058e-09 | 1.0234e-08 | 8.9671e-09 | 1.0559e-08
K1_848 | 3.5741e-10 | 8.4545e-10 | 7.2646e-10 | 1.0089e-09 | 1.0637e-09 | 2.6083e-09
K1_849 | 9.5803e-09 | 1.313e-08 | 1.2645e-08 | 1.1957e-08 | 1.078e-08 | 9.6675e-09
K1_849 | 4.5636e-10 | 2.2012e-09 | 2.0697e-09 | 1.9895e-09 | 1.8038e-09 | 2.6486e-09
CO2
N2
Chart: Temperature [°C]
| 30 | 70 | 90 | 110 | 130 | 190
 | 79 | 68 | 67 | 63 | 59 | 41
 | 78 | 50 | 51 | 50 | 50 | 38
Mixed gas permeation
CO2 / N2 (15/85)
Amino functionalization of the pore surface
Liquid-phase modification
Single gas permeation
CO2
He
H2
N2
T = 110°C
Chart: kinetic diameter [Å]
| 2.6 | 2.89 | 3.3 | 3.6
nicht funktionalisiert | 5.8777e-07 | 7.8729e-07 | 1.6819e-07 | 2.2158e-07
K1_848 | 8.8527e-08 | 6.3013e-08 | 5.764e-09 | 2.962e-10
K1_849 | 1.2524e-07 | 9.8006e-08 | 1.1001e-08 | 3.6195e-09
Modifing solution:
0,064 M APTES* in 1-Propanol
Laboratory tests
*γ-Aminopropyltriethoxysilan
Chart: Sputtertime [min]
| 0 | 0.5 | 1 | 1.5 | 2 | 2.5 | 3 | 3.5 | 4 | 4.5 | 5 | 5.5 | 6 | 6.5 | 7 | 7.5 | 8 | 8.5 | 9 | 9.5 | 10 | 10.5 | 11 | 11.5 | 12 | 12.5 | 13 | 13.5 | 14 | 14.5 | 15 | 15.5 | 16 | 16.5 | 17
nicht modifiziert | 0.3159 | 0.2882 | 0.8883 | 0.5593 | 0.5862 | 0.1492 | 0.8035 | 0.5685 | 0.607 | 0 | 0.2401 | 0.337 | 0.2124 | 0.3778 | 0.4664 | 0.0682 | 0.6936 | 0.4507 | 0.3646 | 0.0693 | 0.1556 | 0.2819 | 0.0309 | 0.3597 | 0.1743 | 0.4024 | 0.2868 | 0.2937 | 0 | 0.2188 | 0.2625 | 0.2626 | 0.1394 | 0.2854 | 0.2982
K1_848 | 0.9675 | 1.5656 | 1.6036 | 1.6655 | 2.0643 | 1.7596 | 1.7442 | 2.0028 | 1.9329 | 1.9055 | 1.3004 | 2.2719 | 1.7643 | 1.5827 | 1.109 | 1.1163 | 1.0318 | 0.6972 | 0.7173 | 0.9595 | 1.0056 | 0.892 | 0.9178 | 0.9659 | 1.0064 | 1.0053 | 0.9453 | 0.5669 | 0.8795 | 0.6964 | 0.7933 | 0.5773 | 1.1115
K1_849 | 1.3118 | 1.4103 | 1.3305 | 1.5125 | 1.4992 | 1.8442 | 1.348 | 1.5612 | 0.8793 | 1.2893 | 1.0291 | 1.1349 | 1.5367 | 1.2161 | 1.077 | 1.0305 | 1.1582 | 0.8439 | 1.2608 | 0.7478 | 0.8732 | 0.9506 | 0.4522 | 0.5594 | 0.2947 | 0.571 | 0.7363 | 0.5942 | 0.5436 | 0.3574 | 0.9819 | 0.5876 | 0.7567 | 0.5954 | 0.537 | 0.7643 | 0.6134 | 0.5281
Nitrogen
not
funktionalized
K1_848
K1_849
Characterisation
XPS-sputter-profil
SiO2
γ-Al2O3
Silica-surface
Silica-surface

## Slide 10
Exposure tests
RWE lignite powerplant Niederaußem und EnBW hard coal power plant Karlsruhe
Investigation of aging behavior of membrane components in direct contact with flue gas
Exploring the conditions for membrane processes in the power plant
EnBW “Rheinhafen-Dampfkraftwerk” Block 7
Fuel: hard coal
Year: 1985
Electrical output: 550 MWel
RWE power plant Niederaußem Block K
Fuel: lignite
Year: 2003
Electrical output: 1000 MWel
Motivation
Power plants
Flue gas
bypass
REAplus
Flue gas
Membrane test rig
Karlsruhe
Niederaußem
Flue gas
Flue gas cleaning
Flue gas
Membrane test rig
Trace components [mg/Nm3]
Dust 5-20
SO2 50-200
NOX 20-200
Trace components [mg/Nm3]
Dust < 1
SO2 < 10 (> 1000*)
NOX 20-200
ϑ ≈ 60°C
rH ≈ 60 %
ϑ ≈ 70°C
rH ≈ 100 %
Air
Furnace
Coal
Steam generation
Turbine and generator
Main components [Vol.-%]
CO2 13-15
N2 78
O2 6-8
* Short peaks during efficiency tests of the desulphurization unit

## Slide 11
Exposure tests
Rauchgas
Rauchgasreinigung
Rauchgas
Membranprüfstand
Rauchgas
Nebenleitung
REAplus
Rauchgas
Membranprüfstand
Karlsruhe
Niederaußem
Motivation
Hauptanteile [Vol.-%]
CO2 13-15
N2 78
O2 6-8
Spurenanteile [mg/Nm3]
Staub 5-20
SO2 50-200
NOX 20-200
Spurenanteile [mg/Nm3]
Staub < 1
SO2 < 10
NOX 20-200
T ≈ 60°C
rH ≈ 60 %
T ≈ 70°C
rH ≈ 100 %
Membrane test rig
25 cm
RWE lignite powerplant Niederaußem und EnBW hard coal power plant Karlsruhe
Investigation of aging behavior of membrane components in direct contact with flue gas
Exploring the conditions for membrane processes in the power plant

## Slide 12
Power plant Niederaußem
Sample holder
1.4571
Power plant Karlsruhe
After 1100 h Exposition
Sample holder
1.4571
Polyactive on 316L
316L (1.4404)
316L (1.4404)
Polyactive on 316L
Little corrosion, distinct ash/dust covering
Severe corrosion, no identifiable ash/dust covering
(Colouring of Polymer-membrane due to corrosion of sample holder)
Exposure tests

## Slide 13
Karlsruhe
SO2 Ø200 mg/m3
K1_721
20 µm
Niederaußem experiment 2
Exposure tests
Niederaußem experiment 1
Top view
Cross section
K1_722
40 µm
K1_722
5 µm
(Exposure time ca. 100 h)
K1_721
5 µm
EDX: Al, O, S, Si, Na, K, Cl
XRD: Natronalunite NaXK1-XAl3(SO4)2(OH)6
10 µm
K1_587
K1_587
5 µm
EDX: Al, O, S, Si, Na, K, Cl
SO2 < 10 mg/m3
Begin: SO2 Ø374 mg/m3
End: SO2 < 10 mg/m3
no
functional layer
amino functionalized
SiO2-function layer
no
function layer

## Slide 14
no
functional layer
K1_764
40 µm
K1_750
40 µm
K1_412
50 µm
SO2 Ø200 mg/m3
SO2 < 10 mg/m3
Beginn: SO2 Ø374 mg/m3
Ende: SO2 < 10 mg/m3
K1_750
5 µm
K1_764
5 µm
K1_412
5 µm
SO2 Ø200 mg/m3
K1_721
20 µm
K1_722
40 µm
K1_722
5 µm
K1_721
5 µm
EDX: Al, O, S, Si, Na, K, Cl
XRD: Natroalunite NaXK1-XAl3(SO4)2(OH)6
10 µm
K1_587
K1_587
5 µm
EDX: Al, O, S, Si, Na, K, Cl
SO2 < 10 mg/m3
Begin: SO2 Ø374 mg/m3
End: SO2 < 10 mg/m3
K1_750
5 µm
K1_764
5 µm
K1_412
5 µm
Exposure tests
Karlsruhe
Niederaußem experiment 2
Niederaußem experiment 1
EDX: Al, O, S, Si, Na, K, Cl
K1_412
50 µm
K1_412
5 µm
EDX: Al, O, S, Si, Na, K, Cl
XRD: Natronalunite NaXK1-XAl3(SO4)2(OH)6
K1_562
2 µm
K1_562
20 µm
SO2 Ø247 mg/m3
Niederaußem experiment 3
+900 h
no
functional layer
amino functionalized
SiO2-functional layer
(Exposure time ca. 100 h)
Top view
Cross section

## Slide 15
no
functional layer
no
functional layer
amino functionalised
SiO2-functional layer
Helium-single gas permeation
Before exposure: 5,5 m3·m-2·h-1·bar-1
After exposure: 0,1 m3·m-2·h-1·bar-1
Niederaußem experiment 2
K1_761
2 µm
K1_761
20 µm
EDX: Zr, O, Y, Al, S, Na, K
Beginn: SO2 Ø374 mg/m3
Ende: SO2 < 10 mg/m3
Exposure tests
(Exposure time ca. 100 h)
Top view
Cross section

## Slide 16
Membrane module test rig
Feed
Retentate
Permeate
21
· · ·
· · ·
· · ·
· · ·
· · ·
· · ·
· · ·
· · ·
· · ·
· · ·
21
21
21
21
Modules
1 m2 12 m2
blower
Vaccuum pump
HZG Membrane module
(up to 70 m2 and 900 m2/m3)
Flue gas
Flue gas
pre-conditioning
https://www.enbw.com/blog/kunden/files/2014/09/130802_RDK_024.jpg
Operated by the Helmholtz-Zentrum Geesthacht (HZG) at the EnbW Rheinhafen-Dampfkraftwerk Karlsruhe

## Slide 17
Membrane area ≈ 3 cm2
ϑ ≈ 35°C
rH ≈ 50 %
CO2-concentration ≈ 14 %
Membrane module test rig
Proof of CO2-separation at application conditions
Transfer of the membrane concept to tubular supports
Assembly of a membrane module with ten tubular membranes resulting in 500 cm² membrane area!
36 h test run of the module with preconditioned flue gas at the Metpore II module test rig
(Rheinhafen-Dampfkraftwerk Karlsruhe)
Execution
First time proof of CO2 separation under application conditions!
CO2-concentration in the permeate
  Begin ≈ 60 %
  End ≈ 50 %
results
Membrane area ≈ 50 cm2

## Slide 18
Damage mechanisms in direct contact with flue gas
Conclusions
Exposure tests in direct contact with flue gas
Forming of a filter cake respectively a layer of fly ash and gypsum
Corrosion of γ-Al2O3 intermediate layer connected to a phase transition
Blocking of pores by condensing water and minerals in the inter layers
The operation of ceramic membranes in direct contact with flue gas is problematic.
Analogues to polymeric membranes a flue gas conditioning is required (dehumidification)

## Slide 19
First time proof of CO2 separation under application conditions
Amino-functionalized membranes: Promising for CO2/N2-Separation at high temperatures
Conclusions
CO2-concentration from 15 Vol.-% up to 67 Vol.-% at 90°C in the laboratory
CO2-enrichment from 14 Vol.-% up to 60 Vol.-% at 35°C
(pre-conditioned flue gas)

## Slide 20
Outlook
Single gas permeation after exposure |  | 
New membrane | Permeation [Nm³/(m² h bar)] | Selectivity [CO2/N2]
CO2 | (3,026) 2,967 | (56) 53
N2 | (0,054) 0,056 | 
Conditions (Feed) |  |  | 
Parameter |  | Components | 
Pressure difference [bar] | 1 | CO2 [Vol.-%] | 15
Temperature [°C] | 40 | O2 [Vol.-%] | 6
Volume flow [Nl/h] | 70 | SO2 [ppm] | 3
Humidity [ rH %] | 10 | NOx [ppm] | 100
 |  | N2 [Vol.-%] | Rest
Almost no loss of selectivity and permeability after 2250 h!
Development of ceramic membranes will continue in the follow-up project MemKoR
As a consequence of the results the setup of the test rig was changed
First experiment with a Polyactive™ membrane from our project partner HZG was successful

## Slide 21
Acknowledgements
Thank you for your kind attention!
METPORE II
Nano-structured ceramic and metal supported
membranes for gas separation
(FKZ: 03ET2016)
MemKoR
Membrane processes for separation of carbon dioxide from power plant flue gases
(FKZ: 03ET7064)