## Slide 1: Luminescent Periodic Microstructures for Medical Applications
Kenta Miura
Division of Electronics and Informatics,
Graduate School of Science and Technology,
Gunma University, JAPAN
Materials Science 2016
September 13, 2016
Atlanta, USA

## Slide 2: Background
1
Transmission
(Refraction)
Emission
GaN etc.
Total Reflection
Periodic
Structure
Interface
Diffraction
Integration of periodic structures and light-emitting diodes (LEDs) was reported as one solution for achieving high light-extraction efficiencies of LEDs.
It was reported that two-dimensional (2-D) periodic structures can effectively extract light emitted from active layers of LEDs according to diffraction laws.
K. Orita, et al., Jpn. J. Appl. Phys. 43 (2004) 5809.

## Slide 3: Improvement of light-extraction efficiency by periodic structure
H. Kitagawa et al., APEX. 1 (2008) 032004.
2
- A green-emitting GaInN 2-D periodic structure with air holes has been investigated.
- The photoluminescence (PL) intensity from the sample with the air holes was approximately three-times stronger than that of a sample without air holes.
- These air holes have been processed using electron-beam (EB) lithography and plasma etching.
Emission patterns of the samples
PL spectra of samples
SEM image of a 2-D periodic structure with air holes (bird’s-eye view)

## Slide 4: Si nanocrystals (Si-ncs) produced by using sputtering
R.K. Soni et al., J. Lum. 83-84 (1999) 187.
H. Seifarth et al., Thin Solid Films 330 (1998) 202.
3
Si-ncs exhibit a quasi-direct band gap as a result of the quantum-size effect.
 They can show visible photoluminescence (PL) depending on their size.
Average size of Si-nc
(calculated from T)
HRTEM image of Si-ncs embedded in SiO2
Size dependent PL spectra from Si-ncs embedded in SiO2

## Slide 5: Preparation of a Si:SiO2 co-sputtered thin film
An Si:SiO2 co-sputtered film was deposited on a fused SiO2 substrate by using radio-frequency (RF) magnetron sputtering method.
We used an SiO2 plate (65 mmf) on which four Si pellets (20 mmf) were placed as a co-sputtering target.
Sputtering conditions:
- Base pressure: 2.7 ×10-4 Pa
- Ar pressure: 1.3 Pa
- RF power: 200 W
- Unheated substrate
The film was annealed in ambient air for 20 min at 1000oC using an electric furnace.
4
SiO2 plate
(65 mmf)
Si tablet
(20 mmf)
Schematic of the co-sputtering target (top view)
O. Hanaizumi et al., Appl. Phys. Lett. 82 (2003) 538.
O. Hanaizumi et al., Jpn. J. Appl. Phys. 41 (2002) L1084.

## Slide 6: Measurement of photoluminescence (PL) spectra
Photoluminescence (PL) spectra were measured at room temperature.
A monochromator, a photomultiplier, and a lock-in amplifier were used.
The intensities of PL spectra were calibrated by using a white-light spectrum measured with an optical spectrum analyzer.
Experimental set-up
5
He-Cd laser (l=325 nm)
Chopper
Mirror
Filter
Lens
Sample
Filter
Lens
Monochro-
mator
Photomultiplier
Amplifier
Lock-in
amplifier
Recorder
Oscilloscope

## Slide 7: Measured PL spectrum of the Si:SiO2 co-sputtered film
6
◆ Red-light emission was observed from the Si:SiO2 co-sputtered film.
◆ The PL peak is located around a wavelength of 800 nm.
Red-light emission

## Slide 8: Design using wave vector and grating vector
7
Transmission (Refraction)
 Snell’s Law
k1
k1
k1
k2
k2
k2
k2//
(=k1//=k0//)
k1//
k1//
q1
q1
q2
q2
q1
q2
k1//
G
k1=2pn1/l
k1=2pn1/l
k0
k0
k0=2p/l
Si:SiO2
(n=n1)
Air
(n=1)
k0=2p/l
k0=2p/l
k1=2pn1/l
Total Reflection
Transmission (Diffraction)
 Diffraction Laws
k2// ≧ |G| = 2p / L ）
Lmin = 2p / k2// = 2p / k1// = l / (n1 sinq1) ~ 800 nm
@ l=800 nm, n1=1.75, q1 = 35o (total reflection angle)
k2// (=k1//)
G : Grating Vector
L : Period of Grating

## Slide 9: Fabrication Process of Periodic Structures
1. Spin coating of photoresist on the Si:SiO2 co-sputtered film.
2. Double photolithography using two-beam interference method.
3. After development, reactive ion etching of the surface of the film using the patterned resist as a mask.
Experimental setup of two-beam interference lithography
He-Cd laser
（l=325 nm）
Mirror
Half mirror
Beam expander
(X 40)
Shutter
Sample
Mirror
Mirror
2q
8

## Slide 10: Double-interference exposure
9
(1) A 1-D periodic pattern was formed by the first exposure.
 The periodicity of the 1-D pattern D is expressed as
D = l/(2sinq )
(l=325 nm, 2q is the angle between the two beams)
(2) A 2-D periodic pattern was formed by the second exposure
after rotating the sample.
 Rotation of the sample by 60o produces a hexagonal lattice.
 The lattice constant of the hexagonal lattice L is expressed as
L = 2D/31/2
D
(1)
1-D periodic pattern
(2)
2-D periodic pattern
L

## Slide 11: AFM images of the 2-D periodic structure
150 nm
◆ A 2-D periodic structure with a hexagonal lattice was obtained.
◆ Lattice constant L (measured) : ~810 nm (average)
◆ Depth of processed patterns： ~50 nm (average)
Top view
Bird’s-eye view
10

## Slide 12: Measured PL spectra
With Periodic Structure
Without Periodic Structure
11
◆ Si-based materials have biocompatibility.
◆ The emission wavelength of 800 nm penetrate a human body.
 Light-emitting devices for medical applications will be realized.