## Slide 1
Printed Nanomaterial-Based Flexible Device Sheets
Kuniharu Takei
Department of Physics and Electronics
Osaka Prefecture University, JAPAN
Nanotechnology 2015, August 12th, 2015

## Slide 2
Large-scale, flexible sensor network that can conformably cover any surfaces
Flexible sensor sheets for what?
Robotics
Environmental
Energy
Transportation
Health monitor
Human Interface

## Slide 3
Printing fabrication methods
Nature Mater., 9, 821-826, 2010.
ACS Nano, 4, 5855-5860, 2010.
Nanotech., 23, 045201, 2012.
Nanowire printing (Si, Ge, Ge/Si, InAs etc.)
Nature, 468, 286, 2010. APL, 99, 103507, 2011.
Nano Lett., 11, 5008, 2011. Nano Lett., 12, 2060, 2012.
APL, 102, 153513, 2013. JPC C, 117, 17845, 2013
2D film transfer (InAs, InGaSb etc.)
Nano Lett., 11, 5408, 2011. Nano Lett., 12, 1527, 2012.
Nature Mater., 12, 899, 2013. Nano Lett., 13, 5425, 2013.
Adv. Mater., in press, 2015
Nanotube printing
PNAS, 111, 1703, 2014. Adv. Funct. Mater, 24, 3299, 2014.
ACS Nano, 8, 3921, 2014. pss A, 11, 2631, 2014.
ACS Nano, 8, 12851, 2014. RSC Adv. 5, 30170, 2015.
Adv. Ele. Mater. in press, 2015
Screen printing

## Slide 4
Large-scale, flexible sensor network that can conformably cover any surfaces
Robotic applications
Robotics

## Slide 5
Artificial electronic whisker (e-whisker)
How can this robot distinguish whether it can go forward or not between obstacles like a cat.

## Slide 6
Animal whiskers detect:
Spatial distribution by touching an abstacle
Wind flow
Temperature
Object
Scan direction
Whisker of rat
Printable strain sensor array
Artificial electronic whisker
K. Takei et al., PNAS 2014, S. Harada et al., ACS Nano 2014.

## Slide 7
Printable strain sensor array
S. Harada et al. ACS Nano 2014.
Sensor material: Mixture of CNT and AgNP inks
Sensor material: Mixture of CNT and PEDOT:PSS inks

## Slide 8
Printable strain sensor array
Lflex=0.5mm-9mm
Thickness
(0.1-1.5 mm)
Lsensor=3-8 mm
Flexible substrate
Sensor materials
CNT-AgNP
or
PEDOT:PSS-CNT
1.5mm-3mm
A
S. Harada et al. ACS Nano 2014.

## Slide 9
Printable strain sensor
High strain sensitivity ~59 %/Pa
Sensitivity tunability
S. Harada et al. ACS Nano 2014.
Strain sensor : Mixture of CNT ink and Ag nanoparticle ink

## Slide 10
Printable temperature sensor array
Temperature sensitivity ~0.6 %/°C
High selectivity between strain and temperature
S. Harada et al. ACS Nano 2014.
Strain sensor : Mixture of CNT ink and Ag nanoparticle ink
Temp. sensor : Mixture of CNT ink and PEDOT:PSS

## Slide 11
Printable strain sensor array
S. Harada et al. ACS Nano 2014.

## Slide 12
#5
#4
#3
#6
#8
#7
#9
S. Harada et al. ACS Nano 2014.
Printable strain sensor array

## Slide 13
Multi-functional e-whisker (Temp & Strain)
S. Harada et al. ACS Nano,2014 2014.

## Slide 14
Three-axis force detections
Fully printed strain and temperature sensor arrays
S. Harada et al. ACS Nano 2014.
Strain sensor : Mixture of CNT ink and Ag nanoparticle ink
Temp. sensor : Mixture of CNT ink and PEDOT:PSS

## Slide 15
Three-axis force and temp. mappings
Defective pixel
S. Harada et al. ACS Nano 2014.

## Slide 16
What else do we need?
Signal processing circuits are required to integrate with the sensors on a flexible substrate

## Slide 17
Flexible CMOS circuits
W. Honda et al. Advanced Materials, 2015.

## Slide 18
Voltage gain ~50
Electrical characteristics
Voltage gain ~50
Power consumption at the steady state : < 7 nW/mm
W. Honda et al. Advanced Materials, 2015.
Field-effect mobility: CNT-TFT ~4 cm2/Vs, InGaZnO-TFT ~6 cm2/Vs

## Slide 19
W. Honda et al. Advanced Materials, 2015.
Electrical characteristics under bending
Almost no change is observed under bending up to 2.6 mm radius
Small Vth shift is most likely due to hysteresis of CNT-TFTs

## Slide 20
W. Honda et al. Advanced Materials, 2015.
Electrical characteristics under bending
High reliability against bending cycles up to 1000 times (<6mm radius)

## Slide 21
W. Honda et al. Advanced Materials, 2015.

## Slide 22
Good mechanical flexibility of CMOS
CMOS NAND
CMOS NOR
Bending radius ~2.6 mm
W. Honda et al. Submitted 2015.

## Slide 23
Painless needle
Temp. sensors
Drug delivery
Display
Circuits
Wireless coil
Heart race sensor
Toward future wearable electronics
takei@pe.osakafu-u.ac.jp

## Slide 24
Acknowledgements
Thank you for your attention!!
Contact: takei@pe.osakafu-u.ac.jp
Osaka Prefecture Univeristy
Prof. Seiji Akita
Prof. Takayuki Arie
Mr. Shingo Harada
Mr. Wataru Honda
Mr. Kenichiro Kanao
Mr. Yuki Yamamoto
Research fundings
Tateishi Science and Technology Foundation