## Slide 1: Low – temperature heat treatment (80 oC) effect on the electrochemically synthesized CuInTe2 thin films for energy harvesting applications
4th International Conference on Materials Science & Engineering
(Materials Science 2015)
held at
Florida, USA
14th – 16th Sept. 2015
By
Manorama Gahininath Lakhe
Under the Supervision of
Dr. Nandu B. Chaure
DEPARTMENT OF PHYSICS,
SAVITRIBAI PHULE PUNE UNIVERSITY , INDIA

## Slide 2
Introduction
http://revolution-green.com/new-4g-solar-power/

## Slide 3
Thin Film Technologies
Amorphous Silicon
Si:H
13.6 %
CIGS
(Concentrator)
23.3 %
CIGS
21.7 %
CdTe
21.5 %

## Slide 4: Importance of the CIT material
Direct bandgap semiconductor material.
The band gap varies from ~ 0.96 eV to 1.1 eV depending upon the processing.
Absorption coefficient = 105 cm-1 [1]
Highest reported efficiency for 6.92 % [2] by MBE technique.
References
M.R. Ananthan, S. Kasiviswanathan, Solar Energy Materials & Solar Cells 93 (2009) 188 – 192
Takahiro Mise and Tokio Nakada, Prog. Photovolt: Res. Appl. 2013; 21:754–759
R Diaz, M Cervera and F Rueda, Journal of Physics D: Applied Physics 45 (2012) 235101 – 235110
It has been showed that two single crystals with compositions close to CuIn2Te3.5, CuIn3Te5 and CuIn4Te6 polycrystal present a similar chalcopyrite structure with a different number of (2VCu + InCu) defect pairs [3].
Because of these defect pairs, the different number of structural vacant sites in the Cu sublattice permits an ion motion which make these compound new mixed ionic and electronic conductors MIEC .

## Slide 5
4. M. Lakhe, N. B. Chaure: Solar Energy Materials & Solar Cells 123 (2014) 122–129
Precursors used : CuSO4, In2(SO4)3 ,TeO2 & Complexing agent: Citric acid [4]
pH of CIT solution: 4.0 by H2SO4 or NaOH.
Stirring rate = 150 rpm & Bath/deposition temperature = 75 oC
Experimental setup

## Slide 6
Cyclic voltammogram recorded at 75 C in an aqueous bath at pH 4 containing precursor ratios Cu/In = 0.25 and Cu/Te = 0.35 on CdS coated FTO substrate. Scan rate was 2 mV/sec.
Cyclic voltammetry
Samples deposited on the small area
Backside interface
Samples deposited on the large area

## Slide 7
The XRD pattern of (a) and (c) as deposited and (b) and (d) heat treated at 80 oC and deposited at 0.7 V & – 0.8 V respectively
Raman Spectra of as - deposited (black line) and heat treated FTO/CdS/CIT films (red line) at 80 oC deposited at [A] - 0.7 V and [B] - 0.8 V respectively. Inset shows the Lorentzian fitting for as deposited films for both potentials.
Results of heat treated samples at 80 oC
X ray diffraction
Raman Spectroscopy
Mode | Std. Mode frequencies (cm-1) | Observed mode frequencies (cm-1) in present data |  |  | 
Literature data |  | -0.7 V |  | -0.8 V | 
 |  | As deposited | Soft annealed | As deposited | Soft annealed
E | 109 | silent | silent | 109 | silent
A1 | 123 | silent | 123 | silent | 123
E | 128 | 128 | silent | 126 | silent
B31 | 143 | silent | 142 | silent | 142
E | 159 | 150 | silent | 150 | silent
E5 and/ or B23 | 171 | 180 | silent | silent | silent
E and B2 | 267 | 261 | 267 | silent | 266
Phonon mode frequencies

## Slide 8
(b)
(112), d = 3.61 Ao
(204/220), d = 2.185 Ao
(a)
(112), d = 3.57 Ao
(204/220), d = 2.19 Ao
(d)
(112), d = 3.605 Ao
(204/220), d = 2.188 Ao
(c)
(112), d = 3.605 Ao
(204/220), d = 2.19 Ao
(A) HRTEM Images of the samples (a) as deposited and (b) heat treated sample, deposited at -0.7 V; (c) as deposited and (d) heat treated sample, deposited at – 0.8 V. The region defined by square in both the films (b) and (d) shows fringing pattern in the heat treated films.
(B) Diffraction pattern of CIT samples (a) as deposited, (b) heat treated; samples deposited at -0.7 V and (c) as deposited, (d) heat treated; samples deposited at -0.8 V
HR TEM results of as deposited and heat treated CIT thin films deposited on FTO/CdS
(d)
d = 0.360 nm
(b)
d = 0.186 nm
(a)
(c)

## Slide 9
Deposition Potential (Volts) | Substrate | Sample Condition | Elemental Composition in At. % |  |  | Cu/In ratio
 |  |  | Cu | In | Te | 
- 0.7 | FTO/CdS | As deposited | 19.57 | 23.05 | 57.38 | 0.85
 |  | Heat treated | 18.98 | 25.29 | 55.73 | 0.75
- 0.8 |  | As deposited | 17.81 | 29.56 | 52.62 | 0.60
 |  | Heat treated | 22.28 | 26.28 | 51.44 | 0.84
EDAX
(a)
(c)
As deposited
(d)
(b)
Heat treated
- 0.7 V
- 0.7 V
- 0.8 V
- 0.8 V
FESEM

## Slide 10
Plot of (αhν)2 Vs Eg (hν) for FTO/CdS/CIT films (a) & (b) shows the as deposited & heat treated film deposited at -0.7 V respectively and (c) & (d) shows as deposited and heat treated film deposited at -0.8 V respectively
Optical study
Optical band gap in eV |  | 
Deposition Potential (V) | As deposited | Heat treated
- 0.7 | 1.08 | 0.91
- 0.8 | 1.11 | 1.02

## Slide 11
I-V characteristics of a FTO/CdS/CIT/Au of (a) – as deposited (black line) and (b) heat treated at 80 0C for 60 hour (red line) CIT films deposited at [A] - 0.7 and [B] - 0.8 V. (Inset shows both as deposited and soft annealed I-V plots on different scale
Typical 1/Cs2 Vs Voltage (V) plots for as-deposited (black line with square symbols) and heat treated (red line with circles) films deposited at – 0.7 V and – 0.8 V
I-V characteristic of as deposited and heat treated CIT thin films deposited on FTO/CdS
Capacitance – Voltage plot of as deposited and heat treated CIT thin films deposited on FTO/CdS

## Slide 12
Carrier concentration Vs Voltage
Depletion width (W) as a function of voltage (V)
Carrier concentration – voltage (V) of as deposited and heat treated CIT thin films
Change in depletion width as a function of applied potential (V) of as deposited and heat treated CIT thin films

## Slide 13
Deposition Potential (V) | Sample condition | Bulk Concentration (cm-3) | Mobility (Cm2/Vs) | Conductivity (1/Ω cm) | Resistivity ( Ω cm) | Sheet Concentration (cm-2) | Average Hall Coefficient cm3/C
-0.7 | As - deposited | 7.55 x 1019 | 23.06 | 2.78 x 102 | 3.58 x 10-3 | 3.53 x 1016 | 8.27 x 10-2
 | Heat treated | 6.48 x 1019 | 29.44 | 3.05 x 102 | 3.27 x 10-3 | 3.04 x 1016 | 9.64 x 10-2
-0.8 | As - deposited | 8.36 x 1019 | 18.40 | 2.46 x 102 | 4.05 x 10-3 | 3.93 x 1016 | 7.46 x 10-2
 | Heat treated | 7.32 x 1019 | 24.13 | 2.83 x 102 | 3.53 x 10-3 | 3.44 x 1016 | 8.52 x 10-2
Hall probe measurement
model ECOPIA HMS-3000 having area 0.5 cm x 1.0 cm under the constant magnetic field 0.54 T and probe current 10 mA

## Slide 14
Development of CuInTe2 solar cells
Short circuit current density (Jsc) = 40.75 mA/cm2
Open circuit voltage (Voc) = 255 mV
Fill factor (FF) = 43 % and
Efficiency = 4. 01 %

## Slide 15
Capacitance – Voltage plot of FTO/CdS/CIT/Au structure after etching treatment

## Slide 16: Conclusion
In conclusion thick films can be deposited by electrodeposition technique on CdS deposited FTO substrate for superstrate configuration of the solar cell.
Even low temperature heat treatment gives good structural, optical, morphological and transport properties.
The superstrate solar cell structure FTO/CdS/CIT/Au obtained for higher pH 4; capacitance-voltage profile reveals increase in diffusion capacitance after successive annealing whereas the carrier concentration was found to be ~ 1 x 1019 cm-3.
The superstrate solar cell structure (FTO/CdS/CIT/Au) obtained for lower pH 4 exhibits the short circuit current density (Jsc), 40.75 mA/cm2; open circuit voltage (Voc), 255 mV; fill factor (FF), 43 % and power conversion efficiency (η), 4.01 % with power intensity 100 mW/cm2.
This lower temperature annealing i.e. 80 oC could be very much useful for flexible solar cells devices.