## Slide 1: MASS SPECTROMETRY AIMED AT SEQUENCE ANALYSIS OF NATURAL AND SYNTHETIC BIODEGRADABLE MACROMOLECULES
Marek M. Kowalczuk
School of Biology, Chemistry and Forensic Science
Faculty of Science and Engineering
University of Wolverhampton
Polish Academy of Sciences
Centre of Polymer and Carbon Materials

## Slide 2: OUTLINE
Introduction – natural and synthetic biodegradable macromolecules
Molecular level structure of natural PHA
MS for synthetic analogues of PHA
Conclusions
Mass Spectrometry Reviews, DOI: 10.1002/mas.21474

## Slide 3
D. Seebach, M. G. Fritz, International Journal of Biological Macromolecules, 25 (1999) 217-236
Biopolymers
Monomers | Oligomers | Polymers
3-HB (3-hydroxy-butyric acids) | cP(3-HB) (channel component) | sP(3-HB) (cf. storage)
Amino acids | Oligopeptides | Polypeptides (enzymes, silk)
Monosacharides | Oligosacharides | Polysacharides (cf. cellulose, starch)
Nucleotides | Oligonucleotides | Polynucleotides (cf. DNA, RNA)
Notes: Czy tak ma być zrobiona ta druga linijka?

## Slide 4
Production of PHA from renewable resources by fermentation
PHA production by genetically modified plants
In-vitro production of PHAs
History of PHA
Identification of sudanophilic inclusions
Identification of P(3HB)
Determination of the functions of P(3HB)
Determination of the properties of native P(3HB) granules
Identification of 3-hydroxyalkanoates other than 3HB
Production of PHA containing 3-, 4-, 5-hydroxyalkanoate units
Industrial production of P(3HB- co-3HV)
Cloning of the PHA biosynthesis genes
PHA production in recombinant bacteria
Observation of mobile P(3HB) in vivo by NMR
PHA production in transgenic plants
In vivo biosynthesis of PHA
Identification of pathways linking PHA biosynthesis to
central metabolic pathways
1st stage
2nd stage
3rdstage
4th stage
Protein engineering?
Price: 2GBP/kg

## Slide 5
Waste cooking oil
Work by a research team at the University of Wolverhampton, UK suggests that using waste cooking oil as a starting material for the production of bioplastic can reduce production costs significantly
Bioplastics!
Bacteria with PHA granules
Bacterial bioplastics from vegetable frying oil

## Slide 6
Recovery and purification of PHA
In outer cell membrane of Gram-negative strains:
Pyrogenic Endotoxins (Lipopolysaccharides)
Membrane coat:
Hydrophilic sourrounding
PHA:
Hydrophobic core part
Regulator Protein
Phospholipids
PHA Depolymerase
PHA Synthase (Polymerase)
Phasin (Structural Protein)
M. Koller, H. Niebelschütz, G. Braunegg, Engineering in Life Sciences,
13 (2013) 549–562

## Slide 7
Short-chain-length PHA
Medium-chain-length PHA
Thermoplasts (Tm 120-180°C)
High crystallinity (40-80%)
Density >1.2 g cm-3
Elongation at break 6-10%
Industrial production: +
Elastomeric, thermoplastic, duroplastics or fluidoplastic properties (Tm n.d.-80°C)
Low crystallinity (0-40%)
Density: ca. 1.05 g cm-3
Elongation at break: adjustable (>100%)
Bacterial synthesis of poly(3-hydroxyalkanoate)

## Slide 8
• Ion trapping ESI mass spectrometers can trap ions of a selected mass and analyze fragments derived from these precursors
Artist: Nils G. Stenqvist
• Multistage ESI MS (MSn) allows all relationships between precursor ions and products to be established
Polymer MS molecular level structure evaluation

## Slide 9
Angewandte Chemie International Edition, 53 (2014) 13010 -13019
„Indeed, modern chemical methods for sequence analysis allow reading and understanding the codes of life. Thus, sequencing methods currently play a major role in applications as diverse as genomics, gene therapy, biotechnology, and data storage. However, in terms of fundamental science, sequencing is not really a question of molecular biology but rather a more general topic in macromolecular chemistry. Broadly speaking, it can be defined as the analysis of comonomer sequences in copolymers”

## Slide 10
Macromolecules, 33 (2000) 5797-5802
Characterization of PHBV macroinitiator
ESI MS (‒)
PHBV

## Slide 11
Biomacromolecules, 7 (2006) 2210–2216
ESI MS(‒) spectra of partially depolymerized PHBV
Depolymerization
12.0 mol %
12.9 mol %
27.1 mol %

## Slide 12
Calculated agreement factors (AF) as a function of copolymer composition for PHBV oligomers of 12.0 mol % depolimerization
Sequential fragmentation spectrum (MS2)
HB6HV2 selected from 8-mer oligomer cluster of a 12.0 mol % PHBV
Biomacromolecules, 7 (2006) 2210–2216
ESI MS2 (‒)
[HB6HV2-H]−
715  **

## Slide 13
Characteristic collision voltage (CCV) versus the precursor ion masses of the studied singly lithium cationized polymers. The data points per polymer were linear fitted and grouped into four groups: polyethers (red), polymethacrylates (blue), polyesters (green), polysaccharides (orange)
K. Vékey et al., Analytical Chemistry, 82 (2010) 9350-9356
Discrimination of polymers by using their characteristic collision energy

## Slide 14
International Journal of Mass Spectrometry, 304 (2011) 15-24
ESI MS/MS(‒)
[PHBn-H]−
n = 2 dimer
n = 3 trimer
n = 4
tetramer
n = 5 pentamer
n = 6 hexamer
n = 4
tetramer
Mechanism of fragmentation active for PHB oligomers

## Slide 15
Rapid Communications in Mass Spectrometry, 17 (2003) 2260–2266
Bacterial poly(3-hydroxybutyrate- -co-3-hydroxyhexanoate)
NODAX TM
HB7HH2 selected from the 9-mer cluster of PHBH oligomers
ESI MS/MS (+)
[HB7HH2 +Na]+
853  **

## Slide 16
European Polymer Journal, 48 (2012) 621-631
PHA block copolymers
ESI MS(‒)
PHB 13-mer oligomers
PHBV 13-mer oligomers
PHO 8-mer oligomers

## Slide 17
M. Kawalec, G. Adamus, P. Kurcok, M. Kowalczuk,
I. Foltran, L. Focarete, M. Scandola,
Carboxylate induced degradation of poly(3-hydroxybutyrate)s, Biomacromolecules, 8 (2007) 1053-1058
E1cB degradation mechanism of PHB

## Slide 18
E1cB degradation mechanism of PHB
Mass spectrum of a-PHB sample after 4h of the isothermal treatment at 120C
a-PHB oligomer with crotonate end group
ESI MS2 (‒)
687  **
ESI MS (‒)

## Slide 19
Biomacromolecules, 14 (2013) 1181-1188
Reduction of PHA biopolyesters
LiBH4

## Slide 20
Reduction of PHBH with LiBH4
ESI MS/MS(+)
771  **
[HB6HH2+Na]+
ESI MS(+)

## Slide 21
Reduction of PHBH with LiBH4

## Slide 22
Transesterification reaction of P(3HB-co-4HB) by (4-chloro-2-methylphenoxy)acetic acid (MCPA) mediated by TSA∙H2O
Bioactive conjugates from natural PHA
ESI- MS2
[MCPA–(OHB)8+Na]+
911  **
New forms of pesticides containing carboxyl functionalities
R=CH3, x=3HB units
or
R=H, x=4HB units
PLoS One. 2015; 10(3): e0120149.

## Slide 23
ESI MS/MS(+)
[Tyrosol–(OHB)3+Na]+
419  **
New forms of pesticides containing hydroxyl functionalities
Synthesis of oligo(3HB)-tyrosol conjugates using the two-step method
-120
299
PLoS One. 2015; 10(3): e0120149.
Bioactive conjugates from natural PHA

## Slide 24
structure
properties
BIOCOP ®

## Slide 25
Michael Szwarc (June 9, 1909, Będzin, Poland – August 4, 2000, United States) was a British (University of Manchester) and American (State University of New York) polymer chemist who discovered and studied ionic living polymerization
Anionic living polymerization
Kyoto Prize in 1991
http://www.inamori-f.or.jp/laureates/k07_a_michael/prf_e.html
Living Polymers, Nature, 178 (1956) 1168–1169

## Slide 26
Activation of anionic species
Regioselectivity
Stereoselectivity
Propagation on carboxylate active centers
Z. Jedliński, M. Kowalczuk, W. Główkowski, J. Grobelny, M. Szwarc,
Macromolecules, 24 (1991) 349-352
Anionic ROP
anionic catalyst
supramolecular catalyst
activated by e.g.,
18-crown-6
no polymerization
PBL
BL

## Slide 27
John W. Kramer, Emil B. Lobkovsky, Geoffrey W. Coates
Organic Letters, 8 (2006) 3709-3712
Tomasz Bałakier, Wojciech Chaładaj , Janusz Jurczak, Grażyna Adamus, Marek Kowalczuk
Tetrahedron, 69 (2013) 4990-4993
Biodegradable polymers synthesis based on clean coal technologies and biomass

## Slide 28
Random Copolyester
Diblock Copolyester
Macromolecules, 42 (2009) 4547-4557
Copolyesters of β-butyrolactone with β-etoksymethyl-β-propiolactone

## Slide 29
m/z
m/z
900
950
1000
1050
1100
0
10
20
30
40
50
60
70
80
90
100
Relative Abundance
1075,8
1033,9
989,8
1077,9
947,8
1061,8
991,8
903,9
975,8
1017,7
1105,9
1035,9
931,7
949,8
973,8
1059,9
905,8
993,9
907,8
A
A
A
B
B
B
B
900
950
1000
1050
1100
0
10
20
30
40
50
60
70
80
90
100
Relative Abundance
1075,8
1033,9
989,8
1077,9
947,8
1061,8
991,8
903,9
975,8
1017,7
1105,9
1035,9
931,7
949,8
973,8
1059,9
905,8
993,9
907,8
A
A
A
A
A
A
A
A
A
A
A
B
B
B
B
B
B
B
B
B
Random Copolyester
Diblock Copolyester
Copolyesters of β-butyrolactone with β-etoksymethyl-β-propiolactone
ESI MS(+)
3-HB/EMPL
ESI MS(+)
3-HB/EMPL

## Slide 30
m/z
300
400
500
600
700
800
900
1000
0
10
20
30
40
50
60
70
80
90
100
Relative Abundance
973,2
887,2
715,2
801,2
1033,3
903,3
773,2
629,2
643,2
671,1
757,2
557,1
427,1
513,1
987,1
368,8
Diblock Copolyester
ES MS/MS(+)
[3-HB5/EMPL4+Na]+
1033  **
ESI MS/MS spectrum of 3-HB/EMPL

## Slide 31
ESI MS/MS spectrum of 3-HB/EMPL
Random Copolyester
ES MS/MS(+)
[3-HB5/EMPL4+Na]+
1033  **

## Slide 32
300
400
500
600
700
800
900
1000
m/z
0
10
20
30
40
50
60
70
80
90
100
Relative Abundance
973,2
887,2
715,2
801,2
1033,3
903,3
773,2
629,2
643,2
671,1
757,2
557,1
427,1
513,1
987,1
368,8
Mass Spectrometry Reviews, DOI: 10.1002/mas.21474
ESI MS/MS mass spectra of selected parent ions
300
400
500
600
700
800
900
1000
m/z
0
10
20
30
40
50
60
70
80
90
100
Relative Abundance
973,2
843,2
903,3
887,2
1033,2
817,2
687,2
801,2
541,1
497,1
455,2
947,3
861,2
773,2
713,2
300
400
500
600
700
800
900
1000
m/z
0
10
20
30
40
50
60
70
80
90
100
757,2
671,2
601,2
541,1
497,1
455,2
325,0
411,0
ES MS/MS(+)
[3-HB5/EMPL4+Na]+
1033  **
Diblock Copolyester
Random Copolyester
ES MS/MS(+)
[3-HB5/EMPL4+Na]+
1033  **

## Slide 33
Analytica Chimica Acta, Special Issue: Polymer Mass Spectrometry, 808 (2014) 104-114
Synthetic analogues of PHA
R1= | —CH3 |  | R = R1= | —CH3
 |  |  | or | 
R2= | —CH2OC4H9 |  | R = R2= | —CH2OC4H9
 | or |  |  | or
 | —CH2OPh |  |  | —CH2OPh
 | or |  |  | or
 | —CH2OBn |  |  | —CH2OBn

## Slide 34
Structure at the molecular level
ES MS/MS(+)
[HB8/BnOHB+Na]+
963  **
Analytica Chimica Acta, Special Issue: Polymer Mass Spectrometry, 808 (2014) 104-114
ES MS(+)

## Slide 35
CONCLUSIONS

## Slide 36: ESI MSn for natural and synthatic biodegradable macromolecules characterization at the molecular level
macromolecular topology
verification of chemical homogeneity and end group analysis
location of functional groups
structural analysis of copolymers including composition and sequence distribution of individual structural units

## Slide 37
The University of Wolverhampton has a long and cherished history dating back to Wolverhampton's Mechanics' Institute and College of Art in the mid-1800s

## Slide 38
Centre of Polymer and Carbon Materials
Polisch Academy of Sciences
PL 41-819 Zabrze, M. Curie-Skłodowskiej 34
PL 44-121 Gliwice, Sowińskiego 5

## Slide 39: RESEARCH SUPPORTED BY
NCN DEC-2012/07/B/ST5/00627

## Slide 40
THANK YOU
FOR YOUR KIND ATTENTION
Artist: Agnieszka Bieniek – Wydrzyńska, Rybotycze, 2012