## Slide 1: TRANSFORMATION OF STEARIC ACID IN HYDROCARBONS OVER Pd/ZSM-5 CATALYSTS
MARTA ARROYO
Rey Juan Carlos University, Móstoles, Madrid (Spain)
Group of Chemical and Environmental Engineering.

## Slide 2
INTRODUCTION
Energy
Petroleum accounts for more than 95% of the energy demand for the transport sector.
10% renewable sources 2020
VEGETABLE OILS
High energy density
Structural similarity to petroleum-based fuels
Direct use
Engine compatibility problems
Alkyl esteres
(Biodiesel)
C1-C14
Alkenes/alkanes
CRACKING:
TRANSESTERIFICATION:
C12-C18
n-Alkanes
DEOXYGENATION:
C1-C14
Alkenes/alkanes
CRACKING:
DEOYGENATION:
C12-C18
n-Alkanes

## Slide 3
INTRODUCTION
CRACKING REACTIONS
FCC catalysts (zeolites and mesopores aluminosilicates)
High temperatures 400-600ºC
Alkanes, alkenes are generated
DEOXYGENATION REACTIONS
DECARBOXYLATION
    R-COOH  R-H + CO2
DECARBONYLATION
R-COOH + H2 R-H+ CO+ H2O R-COOH  R’-H+ CO+H2O
HYDRODEOXYGENATION
    R-COOH+ 3H2  R-CH3+H2O
Alkenes, alkanes with the same carbons atoms or one less than the feed acid.
Noble metals are use like catalysts supported over zeolites, oxides and carbons

## Slide 4
INTRODUCTION
Zeolitic materials
Crystallinity
Uniform microporosity
Strong acidity
Shape selectivity
Diffusional and steric limitations
in reactions involving bulky substrates
- Secondary mesoporosity
- Improvement of the accessibility
Hierarchical zeolites
BIFUNCTIONAL CATALYST
Acid+metal sites
METAL
Reduction of the stearic limitations
Increase in the rate of intracrystalline difusion
Decrease in the deactivating effect of coke

## Slide 5
Water
Source of silica (TEOS)
Source of aluminium (AIP)
Structure-directing agent (TPAOH)
Ageing
Precrystallization
Silanization
48 h
Room
temperature
7 d
170 ºC
Pautogenous
6 h
90 ºC
Reflux
Patm
Silanization agent
8%
Centrifugation
Drying
Calcination
(550ºC 1.8º/min)
20 h
90 ºC
Reflux
Patm
Removal
of alcohol
EXPERIMENTAL PROCEDURE
Crystallization of protozeolitic silanized units method

## Slide 6
Incipient wetness technique
Solid support was outgassed in a rotavapor under vacuum
Sonication for 30’
Aqueous PdCl2 solution
(1 wt% in the final catalyst)
Rotation under vacuum for 5h
Drying
Calcination
(550ºC, 20ºC/min)
H2  30 ml/min
Tº = 450 ºC
2ºC/min
Catalyst activated by hydrogen reduction
EXPERIMENTAL PROCEDURE

## Slide 7
EXPERIMENTAL PROCEDURE
FEED: 10% Stearic acid/n-dodecane
Catalyst: Palladium based ones supported over commercial and hierarchical ZSM-5
Temperature: Variable range 275-325ºC
Atmosfere: 6 bar N2 or H2
Time reaction: 3 hours
Products : GASES + LIQUID
Gas chromatography

## Slide 8: Characterization:
X-ray diffraction
ICP-AES
Adsorption isotherms at 87 K
Ammonia temperature-programmed desorption
Transmission electron micrographs
EXPERIMENTAL PROCEDURE
Materials:
Pd/c-ZSM-5
Pd/h-ZSM-5  different Si/Al atomic ratio

## Slide 9
CHARCTERIZATION
OF MATERIALS
XRD
MFI patterns
PdO reflexion main  34º

## Slide 10
CHARCTERIZATION
OF THE CATALYST
TEXTURAL PROPERTIES
 | SBET (m2 g-1) | VTOTAL (cm3 g-1) | VMP a (cm3 g-1) | Si/Al b | Pd b (wt %) | TMAX c (ºC) | Acidity c (mmol NH3 g-1)
Pd/c-ZSM-5 (30) | 377 | 0.434 | 0.171 | 32 | 0.84 | 330 | 0.345
Pd/h-ZSM-5 (30) | 477 | 0.497 | 0.130 | 33 | 0.96 | 340 | 0.305
Pd/h-ZSM-5 (50) | 479 | 0.471 | 0.157 | 51 | 0.91 | 340 | 0.242
Pd/h-ZSM-5 (100) | 486 | 0.557 | 0.165 | 122 | 0.94 | 332 | 0.122
Pd/h-ZSM-5 (200) | 467 | 0.521 | 0.172 | 269 | 0.94 | 275 | 0.078
a. Volume of zeolitic micropores (0-7 Å); b. Determinated by ICP analysis; c. Determinated by TPD |  |  |  |  |  |  | 

## Slide 11
CHARCTERIZATION
OF MATERIALS
TEM IMAGES
200 nm
Pd/c-ZSM-5 (30)
200 nm
Pd/h-ZSM-5 (30)
200 nm
Pd/h-ZSM-5(50)
200 nm
Pd/h-ZSM-5(100)

## Slide 12
200 nm
Pd/h-ZSM-5(200)
Pd/h-ZSM-5(200)
CHARCTERIZATION
OF MATERIALS
Hierarchical zeolites palladium particle size between 13-17 nm
Pd/c-ZSM-5 (30)  Larger palladium particles due to the lower BET surface area and microporosity, 23 nm
TEM IMAGES

## Slide 13
TEMPERATURE INFLUENCE OVER Pd/c-ZSM-5 (30)
REACTION RESULTS
Conversion increase with the temperature
The selectivity to C5-C11 increase with higher temperatures
High selectivity to gases products at 275ºC
3 Horus, 6 N2 bar, Pd/c-ZSM-5 (30), amount 0,8 g
Bencene, toluene and xylene weren’t detected and oxygen was remove like CO2 mainly.

## Slide 14
HIERARCHICAL POROSITY INFLUENCE
REACTION RESULTS
3 hours, 6 N2 bar, Pd/ZSM-5 (30) amount 0,4 g
Catalyst | Conversion (%) | S.(%) C1-C4 | S.(%) C5-C11 | S.(%) C13-C18
Pd/c-ZSM-5 (30) | 33 | 29,9 | 53,9 | 16,2
Pd/h-ZSM-5 (30) | 67 | 15,1 | 70,6 | 14,3
Hierarchical material  higher stearic acid conversion and improved selectivity to C5-C11 compounds due to the higher accesibility to the acids sites and the better dispersion of the palladium particles.

## Slide 15
RATIO Si/Al INFLUENCE
REACTION RESULTS
Conversion decreases on increasing the Si/Al atomic ratio of the catalyst
Similar selectivities for Si/Al =30-100
Gases: 15-21wt %
Gasoline : 70-75%
Diesel: 8-15%
3 Horus, 6 N2 bar, Pd/h-ZSM-5, amount 0,4 g

## Slide 16: Transformation of stearic acid over Pd/ZSM-5 in presence of N2
High selectivity to C5-C11 products due to cracking reactions
Products derivated from descarboxylation and decarbonylation weren’t detected
H2 has been generally observed to promote the reaction

## Slide 17
ATMOSPHERE INFLUENCE
REACTION RESULTS
 | Nitrogen | Hydrogen
Conversion Stearic acid (%) | 47 | 89
S. (%) C1-C4 | 23,2 | 4,5
S. (%) C5-C11 | 68,5 | 69,2
S. (%) C17 | 0,0 | 18,0
S. (%) C18 | 0,0 | 4,3
S. (%) others C13-C18 | 8,3 | 3,4
3 Horus, 6 N2 bar, Pd/h-ZSM-5 (100), amount 0,4 g
Conversion incrases in presence of hydrogen  favours the contact between feed and metal sites.
Selectivity increases to descarboxylation/decarbonylation and HDO reactions
Selectivity cracking reactions is disminished

## Slide 18
CONCLUSIONS
CONCLUSIONS
The transformation of stearic acid in presence of inert atmosphere allow to obtain high conversion with high selectivity to hydrocarbons in the gasoline range
The presence of secondary porosity in the ZSM-5 materials improves the catalyst properties allowing better dispersion of the palladium particles and enhances catalytic activity.
The presence of hydrogen involve higher conversion and promove the desoxygenation reactions via descarboxylation/decarbonylation and hydrodeoxygenation

## Slide 19
CONCLUSIONS
THANK YOU FOR YOUR ATTENTION
Thank
D.P. Serrano
J.M. Escola