## Slide 1
Construction, Functionalization, and Organization of Dendrimer with Conjugated Backbones
Masatoshi Kozaki*, Shuichi Suzuki, Keiji Okada
Graduate School of Science, Osaka City University, Osaka 558-8585 Japan
E-mail: kozaki@sci.osaka-cu.ac.jp
4th International Conference on Nanotek & Expo
December 01-03, 2014, San Francisco, USA

## Slide 2
Top-down and Bottom-up Approach to Nano-scale Architectures
Moore’s Low
7.0 nm
11.0 nm
Top-down
Bottom-up

## Slide 3
Molecular Devices and Machines
Functional Units
Dendrimers
Step 1 Precise Arrangement of Functional Units
Step 2
Integration of Dendrimers
The Concept of the Stepwise Approach to Nano-scale Architectures

## Slide 4
1) A dendrimer has rigid conjugated backbones within the flexible dendritic structure.
2) The rigid backbone serves as a scaffold for the construction of a well-designed assembly as well as a mediator in both the electron and energy transfer processes
3) The rigid backbones are useful for the construction of well-organized nano-scale assembly of dendrimers.
Introduction of Dendrimers with Rigid Backbones

## Slide 5
Kozaki, M.; Okada, K. Org. Lett. 2004, 6, 485-488.
How to make the Dendrimer
(Convergent Approach)

## Slide 6
Synthesis of a Conjugated Chain with Branched Side Chains

## Slide 7
Functionalized Dendrons and Core units

## Slide 8
dendrimer-16 (C460H332N4O32Zn: 6486)
Preparation of Dendrimer with Light-Harvesting Ability

## Slide 9
Advantage of the Dendrimer with Conjugated Chains
(1) Jiang, D.-L.; Aida, T. J. Am. Chem. Soc. 1998, 120, 10895-10901.

## Slide 10
Figure 2. (a) Arrangement of pigment.protein complexes in the modeled bacterial PSU of Rb. sphaeroides. (b) Excitation transfer in the bacterial photosynthetic unit. LH-II contains two types of BChls, commonly referred to as B800 (dark blue) and B850 (green), which absorb at 800 nm and 850 nm, respectively. BChls in LH-I absorb at 875 nm and are labeled B875 (green). (Hu,X.; Damjanović, A.; Ritz, T.; Schulten, K. Proc. Natl. Acad. Sci. USA 1998, 95, 5935-5941.)
How to Make the Visible Light Harvester (Biomimetic Strategy)
B875
B800
B850
B800
B875
B850

## Slide 11
Uetomo, A.; Kozaki, M.; Suzuki, S.; Yamanaka, K.; Ito, O.; Okada, K. J. Am. Chem. Soc. 2011, 133, 13276-13279.
dendrimer-17 (C1016H1028N52O16Si4Zn13: 15186)
Strategic Arrangement of Porphyrins using the Dendritic Architecture

## Slide 12
Figure 3. Absorption spectra of dendrimer-17 (black), 18 (blue), 19 (green), and 20 (red) measured in THF. The inset shows expanded absorption spectra in the Q-band region.
strong absorptions throughout the visible region e > 56,000 M-1 cm-1

## Slide 13
Figure 4. Steady-state fluorescence spectra of (a) dendrimer-3 (red) and 11 (blue) (λex = 426 nm), (b) dendrimer-3 (red) and 12 (green) (λex = 453 nm), and (c) dendrimer-3 (λex = 498 nm) measured in THF. Fluorescence intensities are measured after normalizing the absorbance at excitation wavelength.
Excited on TP-Por
Excited on TE-Por
19
18
FEN = 91%
FEN = 94%
Excited on DE-Por

## Slide 14
Figure 9. Energy diagram and relaxation process from an excited states of TP-Por in dendrimer-17. * and ** denote the first and the second excited states, respectively.
TP-Por**
TP-Por* 2.07 eV
DE-Por* 1.91 eV
TE-Por* 1.77 eV
kd(TP-Por*) = 5.3 ×108 s-1
kEN2 = 5.0 ×109 s-1
45%
kd(TP-Por*) = 4.0 ×108 s-1
Effective Light Harvesting Antenna
51%
kEN1 = 5.7 ×109 s-1
kd(TP-Por*) = 6.7 ×108 s-1
kEN3 = 3.0 ×1010 s-1
Fast energy transfer through conjugated chains
0
dendrimer-17
96% total quantum efficiency
98% quantum efficiency

## Slide 15
Dendrimer with both Light-Harvesting and Charge-separating Properties
dendrimer-21
Notes: 次にUVですが、それぞれの化合物でポルフィリン部に特徴的なソーレー帯、Ｑバンドの吸収が観測され、その他に、短波長領域にポリベンジルエーテル鎖、共役鎖、アントラキノンの吸収が観測されました。ここで、アントラキノンを有するデンドリマーにおいてのみ吸収の広がりが見られました。これは、このデンドリマーにおいてポルフィリン核とアントラキノン間になんらかの相互作用があるためと推測しています。

## Slide 16
dendrimer-16
dendrimer-23
14
15
Figure 10. Fluorescence spectra of dendrimer-1 and -2, 14, and 15 in DMF.
Charge-Separating Properties of the Dendrimer

## Slide 17
Table 2. Charge-separation rate constants (kCS) from the the excited singlet state of ZnP to AQ.
Figure 11. Charge-separation rate constants (kCS) from the the excited singlet state of ZnP to AQ.
Compds. | kCS / s-1 a |  |  | 
 | 1,4-dioxane | THF | benzonitrile | DMF
 | 0.782 × 109 (35%) | 2.50 × 109 (63%) | 5.74 × 109 (88%) | 8.63 × 109 (92%)
 | 0.238 × 109 (65%) | 0.208 × 109 (37%) | 1.19 × 109 (12%) | 1.70 × 109 (8%)
14 | - | 0.284 × 109 | 1.55 × 109 | 2.08 × 109
15 | - | - | 0.486 × 109 | 0.691 × 109
a Fluorescence lifetimes of dendrimer-1 were used as a standard ((tf )ref ). |  |  |  | 
Chart: 
| 1,4-dioxane | THF | PhCN | DMF
1 | 0.782 | 2.5 | 5.74 | 8.63
1 | 0.238 | 0.208 | 1.19 | 1.7
3 | 0 | 0.284 | 1.55 | 2.08
4 | 0 | 0 | 0.486 | 0.691
Kozaki, M.; Akita, K.; Okada, K. Org. Lett. 2007, 9, 1509-1512. Kozaki, M.; Akita, K.; Okada, K.; Islam, D.-M. S.; Ito, O. Bull. Chem. Soc. Jpn. 2010, 83(10), 1223-1237.
kCS X 10-9/ s-1
Figure 12. (a) Fluorescence decays of dendrimer-1 and -2, 14, and 15 in DMF at around 610 nm-670 nm range.
dendrimer-1
dendrimer-2
15
14
dendrimer-1
dendrimer-1

## Slide 18
Charge-separating System
Light-harvesting Antenna
Org. Lett. 2007, 9, 1509-1512.
Bul. Chem. Soc. Jpn. 2010, 83, 1223-1237.
J. Am. Chem. Soc. 2011, 133, 13276-13279.
Precise arrangement of Dendrimers Creation of advanced functions that are not realized with low molecular weight materials
Establishment of the Synthetic Methodology for the Construction of a Nanoscale Array of Denderimers
Dendrimers with Conjugated Backbones

## Slide 19
A4-type Dendrimer
AB2-type Dendrimer
Methodology for the Construction of Nanoscale Architectures
Advantages of the Assembling Method
The well-defined arrangement of connecting sites and rigidity of conjugated backbones ensure the accurate formation of pre-designed architectures.
A well-designed and highly organized array of functional units can be prepared using the conjugated backbones as a scaffold. Moreover the interaction among these units is adjustable by structural modification of backbones.

## Slide 20
AB2-type Dendrimer with Necked Coupler
A4-type Dendrimer with
Buried Coupler
Dendrimers with Necked and Buried Couplers

## Slide 21
Pd2(dba)3•CHCl3 AsPh3THF/NEt3
40 oC, 72 h
52%
A4-type Dendrimer 11
AB2-type dendrimer 7
Assembly 12 (C876H750N4O32: 11,846)
Necked Coupler
11 nm
Buried Coupler
Integration of Dendrimers

## Slide 22
Assembly 16 (C1188H1070N4O56: 16,299)
17%
A4-type Dendrimer 15
AB2-type Dendrimer 7
13.5 nm
Synthesis of Porphyrin Dendrimers

## Slide 23
azide
ethynyl
triazole
Cu(I)
Iterative Convergent / Divergent Strategy
Simple procedure and clean conversion
+
Click Reaction (CuAAC reaction)
D1A
D1E
D2
D1
Azidation
Deprotection
Click Reaction
Iterative Convergent / Divergent Strategy

## Slide 24
Azidation
(NaN3, DMF)
Click Reaction
（CuI, i-Pr2NEt / THF)
94%
92%
Azidation
Deprotection
D2A
D2E
Deprotection
(K2CO3, 18-crown-6
MeOH / CH2Cl2)
Click Reaction
D4 (MW15,414)
D1A
D1E
D1 (MW 3,936)
D2 (MW 7,762)
76%
91%
Azidation
Deprotection
76%
Click Reaction
Iterative Convergent / Divergent Synthesis
59%

## Slide 25
94%
79%
Azidation
D4A
D4E
D8 (MW 30,718)
48 nm
93%
Click Reaction
Deprotection
D4 (MW15,414)
Iterative Convergent / Divergent Synthesis

## Slide 26
Conclusion
Dendrimers containing rigid conjugated backbones were prepared by a convergent method where the attachment of dendritic branches and the extension of phenylene-ethynylene units were alternatively manipulated on the structure of AB2 substituted diphenylacetylene in a combination with Suzuki-Miyaura and Sonogashira cross-coupling reactions.
These dendrimer structures were applied for the construction of several light-harvesting antennas and charge-separating systems. The conjugated network inside the dendritic structure was shown to play an important role as a mediator in both the photoinduced energy- and electron-transfer processes.
We present a novel methodology for the stepwise construction of shape-persistent assemblies using the dendrimers with conjugated backbones as the key modular building blocks. These examples demonstrate advantage of the dendrimer with conjugated backbones for the construction of nanoscale molecular devices such as artificial photosynthetic systems.
Acknowledgment
This work was partially supported by Grants (No.23350022 and 22350066) from JSPS. We thank for Otsuka Electronics for measurements of fluorescence quantum yields.

## Slide 27
Figure 5. Fluorescence decays of 6 (red), 4 (gray), 9 (blue), and 13 (green) at 610 with lex = 426 nm in THF.
Figure 6. Fluorescence decays of 6 (red), 7 (gray), and 14 (green) at 660 with lex = 454 nm in THF.
610 nm
(lex = 426 nm)
660 nm
(lex = 454 nm)

## Slide 28
Table 1. Photophysical data of 1, 4, 8, and 9 in THF.
compd | lex/nm | ldetect/nm | kEN/s-1 | energy-transfer step | calcd kEN / s-1 a
6 | 427 | 610 | 1.2 × 1010 | EN1+EN2 | -
9 | 427 | 610 | 5.7 × 109 | EN1 | 2.57 × 1010
13 | 427 | 610 | 5.0 × 109 | EN2 | 1.81 × 109
6 | 456 | 660 | 3.0 × 1010 | EN3 | 9.89 × 109
14 | 456 | 660 | 3.0 × 1010 | EN3 | 9.89 × 109
Figure 7. Energy diagram and relaxation process from an excited states of TP-Por in the antenna 1. * and ** denote the first and the second excited states, respectively
a Energy transfer rates were evaluated using the Förster equation.
710 nm
(lex = 427 nm)
Figure 8. Fluorescence decay curve at 710 nm of 6 excited at 427 nm in THF (dots). The red solid line was obtained by the simulation. The shape decay (blue) is lamp profile.

## Slide 29
Figure 1. UV-vis spectra of dendrimer-16 and Zn-TPP in THF. (upper right) Steady-state fluorescence spectra of dendrimer-16 in THF. (lower right) (a) 286 nm excitation (The intense peak at 572 nm is the scattering of excitation light). (b) 372 nm excitation (The weak peak at 415 nm is the scattering of excitation light). (c) 433 nm excitation.
dendrimer-16
Zn-TPP
scattering
scattering
Conjugated Chains
Branching Chains
Porphyrin
Highly efficient (~100%) intramolecular singlet energy transfer
Ff＝0.05
Ff＝0.05
Ff＝0.05
(a)
(b)
(c)
Kozaki, M.; Akita, K.; Okada, K. Org. Lett. 2007, 9, 1509-1512.
Light Harvesting Properties of the Dendrimer
Conjugated Chains
Branching Chains
Porphyrin
(Soret band)

## Slide 30
32 %
Major and Minor Products
17 %
C1188H1070N4O56 MW 16,299
C1030H934N4O50MW 14,172

## Slide 31
Synthesis of Dendrimers

## Slide 32
Synthesis of Porphyrin Dendrimers

## Slide 33
Synthesis of Porphyrin Dendrimers
A4-type Dendrimer with
Buried Coupler

## Slide 34
巨大分子の合成特有の問題点
（１）低分子量の化合物の反応では、マイナーな副反応や副生成物が主となる場合がある。
（２）低分子量の反応では容易に分離できる副生生物の分離が困難な場合が多い。
Problems in the Assembling Process of Dendrimers
・ Low Encounter-probability inhibits an intramolecular reaction. As the results, formation of the product from intramolecular side reaction was increased.
・ Separation and purification is problematic. Strong tendency of aggregation impede the GPC-separation.
C1188H1070N4O56 MW 16,299
C1030H934N4O50MW 14,172
Summary
Advantage of Dendrimers in the formation of a nano-scale architecture
・ Bonding between the ends of conjugated chain results in the formation of nano-scale architecture with well-defined shape and pai-conjugated network.

## Slide 35
Retention time / min
9.0 15.0 21.0 27.0
Figure 1. GPC chart of the mixture of assembly 16 and 17
100
75
50
25
%Int.
100
75
50
25
%Int.
10,000 12,000 14,000 16,000 20,000 22,000
10,000 12,000 14,000 16,000 20,000 22,000
m / z
m / z
Figure 2. MALDI-TOF MS spectrum of 16
Figure 3. MALDI-TOF MS spectrum of 17
16: MW 16299
14,170
16,299 M+
Separation by GPC
0
0
CHCl3 : CS2
1:0
9:1
1:1

## Slide 36
9.0 8.0 7.0 6.0 5.0
d / ppm
9.0 8.0 7.0 6.0 5.0
d / ppm
Figure 4. 1H NMR spectra of 16 (left) and 17 (right) in CDCl2CDCl2 at various temperature
16
17
130 oC
95 oC
60 oC
25 oC
130 oC
95 oC
60 oC
25 oC
VT NMR in CDCl2CDCl2

## Slide 37
Efficient intramolecular singlet energy transfer
Porphyrin (427 nm)
wavelength / nm
Scattering peak
Normalized Intensity
Branching Chains (299 nm)
Conjugated Chains (364 nm)
Ff＝0.11
Ff＝0.078
（72％）
Ff＝0.073
（67％）
Figure 9. UV-vis spectra of assembly-3 in THF. (left) Steady-state fluorescence spectra of asesembly-3 in THF. (right) (a) 286 nm excitation (The intense peak at 598 nm is the scattering of excitation light). (b) 372 nm excitation. (c) 433 nm excitation.
Normalized Intensity
Normalized Intensity
assembly-3
X 10
6
5
4
3
2
1
0

## Slide 38
D1
Synthesis of Dendrimers
Flexible linker

## Slide 39
Schanze, K. S. et al.
J. Phys. Chem. Lett. 2013, 4, 1410-1414.
Aggregated
Non aggregated
Figure 5. UV-vis spectra of D1, D2, D4, and D8 in CH2Cl2.
UV-vis Spectra (in CH2Cl2)
 | l max / nm
D1 | 407
D2 | 396, 423
D4 | 397, 426
D8 | 397, 427

## Slide 40
D1
2.72×106 M
5.43×107 M
2.72×107 M
5.36×106 M
1.07×106 M
5.36×107 M
Figure 6. UV-vis spectra of D2 in CHCl2CHCl2.
Figure 7. UV-vis spectra of D1 in CHCl2CHCl2.
Concentration Dependence (in CHCl2CHCl2)

## Slide 41
D1 at 90 oC
D2 at 90 oC
Temperature Dependence
(D2 in CHCl2CHCl2)
Figure 8. UV-vis spectra of D2 in CHCl2CHCl2.
Figure 9. UV-vis spectra of D1 and D2 in CHCl2CHCl2.

## Slide 42
Schanze, K. S. et al.
J. Phys. Chem. Lett. 2013, 4, 1410-1414.
lex = 395 nm (conjugated chains)
Figure 6. Fluorescence spectra of D1, D2, D4, and D8 in CHCl2CHCl2.
Fluorescence Spectra in CH2Cl2

## Slide 43
Higher Order Structure of Octamer
Folded form
Extended form
heating
cooling