## Slide 1
Effect of Passivation on Suppression or
Utilization of Atomic Migration Phenomena
in Metallic Thin-film Materials
M. Saka
Tohoku University
Sendai, Japan
Saka-01

## Slide 2
Human Body
Environment
SKIN
Saka-02
Fig. 1

## Slide 3
(b) EM with Passivation
Passivation
(Natural oxide film, Artificial)
(ib)
(iib)
(iiib)
Depletion
Accumulation
e-
e-
Back Flow
Metallic material
(ia)
Atoms
(iia)
Depletion of
Atoms Void
Electron Flow e-
Accumulation of
Atoms Hillock
(a) EM without Passivation
(No Back Flow)
Saka-03
Fig. 2

## Slide 4
. . . .
Via
Gate
First layer
Third layer
Second layer
Pad
Multi-level interconnections
H. Abé, K. Sasagawa & M. Saka, Int. J. Fracture, (2006)
Saka-04
Fig. 3

## Slide 5
■ Electromigration(EM) in Straight Thin-film Line
■ EM in Corner Part Composed of Dissimilar Metals
CONTENTS
(Atomic Migration in Metallic Thin-film Materials in Relation
with PASSIVATION)
without Passivation
with Passivation
without Passivation
with Passivation
Saka-05
■ Fabrication of Micro Materials Based on EM with
Passivation
■ Fabrication of Micro and Nano Materials Based on
Stress Migration(SM) with Passivation

## Slide 6
Saka-06
■EM in Straight Thin-film Line
(a)
(b)
(c)
x
(without Passivation)
Hillock
Hillock
Hillock
Void
Void
Void
e-
e-
e-
e-
e-
e-
M. Aoyama & M. Saka, Microsyst. Technol., (2015)
T : absolute temperature
Fig. 4

## Slide 7
■EM in Corner Part Composed of Dissimilar Metals
Fig. 6
Material 1
Material 2
b
b
j
r
r1
r2
j

Circumferential component of current density vector at  = /2
(3)
(4)
Area size of j concentration
Volume of accumulation and depletion of atoms at  = /2
M. Saka & X. Zhao, Int. J. Heat and Mass Transfer, (2012);
Y. Kimura, X. Zhao & M. Saka, Proc. APCF/SIF-2014, (2014)
(without Passivation)
Saka-09

## Slide 8
(with Passivation)
Fig. 7
Material 1
Material 2
b
b
j
r
r1
r2

Electrically insulated
2
j
1
M. Saka, Y. Kimura & X. Zhao, (2016)
Saka-10

## Slide 9
■Fabrication of Micro Materials Based on EM with
Passivation
Fig. 12
(a)
(b)
M. Saka, H. Tohmyoh, M. Muraoka, Y. Ju & K. Sasagawa, Mater. Sci. Forum, (2009)
Fig. 13
PASSIVATION
: m
Saka-17

## Slide 10
■Fabrication of Micro and Nano Materials Based on
SM with Passivation
Fig. 14
M. Saka ed., Metallic Micro and Nano Materials, (2011)
 : compressive hydrostatic stress
grad : driving force of SM
Saka-18
(from Google Web)

## Slide 11
M. Saka, H. Tohmyoh, M. Muraoka, Y. Ju & K. Sasagawa,
Mater. Sci. Forum, (2009)
Ta
Cu
Ta
Hole
Hillock
Hillock
Ta
Cu
Cu2O
Weak spot
Ta
Fig. 16
Fig. 15
SiO2
Si
Passivation(Artificial or
Oxide Film) on Surface
of Metallic Material
SiO2
Si
Cu NW
Ta
Cu
Ta
Hillock
SiO2
Si
Atoms are discharged
through Weak Spots
Hillock, Wire
Thermal-compressive hydrostatic
stress
Saka-19

## Slide 12
Y. Lu, Y. Li & M. Saka, Mater. Lett., (2016)
●Ag thin wires
(1～2m diameter, ～680m length)
[ Thick Brittle TiN (600nm) Passivation ]
●Ag micro-particles
[ Thin TiN (2nm) Passivation ]
Atomic discharge
Crack
N
M
Tensile (+)
Compressive (-)
Tensile (+)
Grain boundary
Ag atom
TiN (600 nm)
Ag (300 nm)
Ti (300 nm)
Cu foil (80 m)
Fig. 17
Saka-20

## Slide 13
CONCLUSIONS
Suppression or Utilization of Atomic Migration (EM, SM)
in Relation with PASSIVATION
This work was supported by JSPS KAKENHI Grant-in-Aid for Scientific Research (B) No.26289001.
Fig. 16
Fig. 13(a)
Saka-21