## Slide 1
Ming Xuan Gan, S. Techanithisawat, and Chee How Wong
Presenter: Ming Xuan Gan
Singapore Centre for 3D Printing, Nanyang Technological University.
SLM Solutions Singapore Pte Ltd, Singapore.
26th June 2017
Consistency of 3D Printing Spodumene Articles

## Slide 2: Outline
Introduction
  Additive manufacturing (AM)
  Selective laser melting (SLM)
SLM of spodumene
  Multilayer printing
  Properties characterisation
Summary

## Slide 3: Introduction
Additive Manufacturing (AM)
  3D printing
  Layer by layer process
  Fabrication of complex geometries
Additive manufacturing |  |  | 
Material format | Powder | Solid | Liquid
Material types | Metal/Polymer | Metal/Polymer | Polymer
Joining means | Laser or Electron beam/Binder jetting | Laser/Heating coil | UV* source, material jetting
Joining methodology | Melting or sintering/Solidifying | Melting/Fusing | Photo-curing
Chua, C.K., Leong, K.F., 3D PRINTING AND ADDITIVE MANUFACTURING: Principles and Applications (with Companion Media Pack) of Rapid Prototyping, World Scientific Publishing Co Inc2014.

## Slide 4: How does it work?

## Slide 5: Typical AM methods
Metals
Polymers

## Slide 6: Selective Laser Melting
Kruth, J.-P., et al., Binding mechanisms in selective laser sintering and selective laser melting. Rapid prototyping journal, 2005. 11(1): p. 26-36.
Yadroitsev, I., et al., Single track formation in selective laser melting of metal powders. Journal of Materials Processing Technology, 2010. 210(12): p. 1624-1631.
Energy density of laser beam:
Material’s optical properties:
Limited to metals

## Slide 7: Literature
Laser additive manufacturing of ceramics
Material | Relative sintered density (%) | Flexural strength (MPa) | References
Alumina | 90.5 | – | 8
Alumina | 98.0 | 476 | 9
Zirconia-stabilised alumina | – | 175 | 10
Glass-infiltrated Alumina | – | 415 | 11
Silicon carbide | 73.0 | 128 | 12
Table 2: Summary of direct ceramic stereolithography.
Table 1: Summary of indirect selective laser sintering of ceramics.
Material | Binders | Relative green density (%) | Relative sintered density (%) | References
Alumina | Polyamide | – | 92 | 4
Alumina | Polypropylene | 83 | 88 | 5
Alumina | Semi-crystalline PVA | 57 | 98 | 6
Yttrium stabilized tetragonal zirconia | Polypropylene | – | 85 | 6
Silicon carbide | Polymethylsilsesquioxan | 60 | 50 | 7

## Slide 8: Literature
Material |  | Flexural strength (MPa) | Micro-hardness (HV500) | References
Al2O3-ZrO2 |  | 538.1 | – | 13
Al2O3-ZrO2 |  | > 500 | – | 14
Yttria-stabilised ZrO2 |  | – | 1209 ± 262 | 15
Table 3: Selective laser melting of ceramics.
[4] Deckers, J., et al., Isostatic pressing assisted indirect selective laser sintering of alumina components. Rapid Prototyping Journal, 2012. 18(5): p. 409-419.
[5] Shahzad, K., et al., Additive manufacturing of alumina parts by indirect selective laser sintering and post processing. Journal of Materials Processing Technology, 2013. 213(9): p. 1484-1494.
[6] Tang, H.-H., M.-L. Chiu, and H.-C. Yen, Slurry-based selective laser sintering of polymer-coated ceramic powders to fabricate high strength alumina parts. Journal of the European Ceramic Society, 2011. 31(8): p. 1383-1388.
[7] Friedel, T., et al., Fabrication of polymer derived ceramic parts by selective laser curing. Journal of the European Ceramic Society, 2005. 25(2): p. 193-197.
[8] Hinczewski, C., S. Corbel, and T. Chartier, Ceramic suspensions suitable for stereolithography. Journal of the European Ceramic Society, 1998. 18(6): p. 583-590.
[9] Chen, S., et al., Effective fabrication method of 3D ceramic photonic crystals with diamond structure. Rapid Prototyping Journal, 2012. 18(1): p. 49-55.
[10] Hay, G., et al. Conductive lithographic film fabricated resistive strain gauges. in Sensors, 2003. Proceedings of IEEE. 2003. IEEE.
[11] Tasaki, S., S. Kirihara, and T. Sohmura, Visualization of mechanical properties in alumina dental crowns fabricated by using laser scanning stereolithography. 2010.
[12] Tian, X., et al., Reaction-bonded SiC derived from resin precursors by Stereolithography. Ceramics International, 2012. 38(1): p. 589-597.
[13] Wilkes, J., et al., Additive manufacturing of ZrO2-Al2O3 ceramic components by selective laser melting. Rapid Prototyping Journal, 2013. 19(1): p. 51-57.
[14] Hagedorn, Y.-C., et al., Net shaped high performance oxide ceramic parts by selective laser melting. Physics Procedia, 2010. 5: p. 587-594.
[15] Liu, Q., B. Song, and H. Liao, Microstructure study on selective laser melting yttria stabilized zirconia ceramic with near IR fiber laser.
Rapid Prototyping Journal, 2014. 20(5): p. 346-354.

## Slide 9: Issues in SLM of ceramics
  Low thermal expansion
  LAS glass-ceramic from spodumene mineral
  Reduce ΔT
  Support structures
  High temperature preheating
  Low α material
  Glass-ceramic
σ = EαΔT
Wilkes, J., et al., Additive manufacturing of ZrO2-Al2O3 ceramic components by selective laser melting. Rapid Prototyping Journal, 2013. 19(1): p. 51-57.

## Slide 10: Spodumene
Naturally occurring mineral – α phase
Lithium aluminum silicate – LiAl(Si2O6)
Oxides | wt%
Li2O | 7.1
Fe2O3 | 0.1
K2O | 0.25
Al2O3 | 25.4
SiO2 | 65.7
P2O5 | 0.13
Na2O | 0.23
LOI | 0.32

## Slide 11: Failure characteristics
Unsuccessful adhesion of first layer
Non-bonded adjacent tracks
Failure to continue printing after the first layer

## Slide 12: Single layer (2D)
(b)
M. X. Gan and C. H. Wong, "Selective Laser Melting of Spodumene: An Exploratory Study", paper presented at 2nd International Conference on Progress in Additive Manufacturing, 16 May-19 May, Singapore.(2016).
(a)
(c)
Energy density

## Slide 13: Multilayer (3D)
(a)
(b)
(c)
(d)
M. X. Gan & C. H. Wong, “Effect of hatch spacing on the density of selectively laser melted spoduemene,” 6th International Congress on Ceramics, Dresden, Germany, 21 August 2016 – 25 August 2016.

## Slide 14: Repeatability
Rows |  | Columns |  | 
 | 1 | 2 | 3 | 4
1 | -0.051 | -1.021 | 0.599 | 0.599
2 | -0.761 | -0.961 | 0.009 | 0.009
3 | 1.029 | 2.239 | -0.431 | -0.431
4 | 0.019 | -0.221 | 0.849 | 0.849
5 | -0.821 | -0.36 | 0.779 | 0.779
Table 4: Percentage difference with respect to an average of 59.231 %.

## Slide 15: Properties
Chart: Strain
Chart: Strain
Chart: Strain
M.X. Gan, S. Techanithisawat, and C.H. Wong (2017). In submission
― Sample 1
― Sample 2
― Sample 3
As-printed
650 °C
950 °C

## Slide 16: Properties
M.X. Gan & C.H. Wong (2017). Properties of selective laser melted spodumene glass-ceramic. Journal of the European Ceramic Society, 37: p. 4147-4154.

## Slide 17: Properties
×: β-spodumene
□: hexagonal LAS
○: unidentified
50 µm
100 µm
150 µm
As-printed
850 °C
950 °C
M.X. Gan & C.H. Wong (2017). Properties of selective laser melted spodumene glass-ceramic. Journal of the European Ceramic Society, 37: p. 4147-4154.

## Slide 18: Importance of support structures
Mertens, R., Clijsters, S., Kempen, K., & Kruth, J. P. (2014). Optimization of Scan Strategies in Selective Laser Melting of Aluminum Parts With Downfacing Areas. Journal of Manufacturing Science and Engineering,136(6), 061012.
Gan, M. X., & Wong, C. H. (2016). Practical support structures for selective laser melting. Journal of Materials Processing Technology, 238: p. 474-484.

## Slide 19: Minimal contact
M.X. Gan & C.H. Wong (2016). Practical support structures for selective laser melting. Journal of Materials Processing Technology, 238: p. 474-484.

## Slide 20: Summary
Current work
  Advantages of additive manufacturing
  Potentially useful for ceramics and glass-ceramics
  Properties of laser melted spodumene
    Laser AM of natural mineral
    Very encouraging
    Alumina + LAS
  Importance of support structures